## Slide 1: SRF Cavities with Wire-Laser Metal 3D Printing
iSAS First Annual Meeting, March 14th 2025

## Slide 2: Today we will cover
Wire-Laser Metal 3D Printing
Meltio Product Portfolio
Niobium Wire Tests
Geometry Tests
Future Developments

## Slide 3: Wire-Laser Metal 3D Printing
Safe and Reliable
Accessible
Cost Efficient
Integration Ready
Notes: Enter Meltio
focused on the laser wire process
Safe
cost effective
Integration Ready
Accessible (easy to use)
So, thats it right? Everything solved!

## Slide 4: The Benefits of a Wire-Laser Based Process
Meltio started as a powder and wire metal 3D printing technology provider, however, after 2 years in operation 99% of our customer base and R&D work is around improving the laser wire process due to its obvious benefits towards industrial adoption.
Better Microstructure
The laser process from Meltio delivers an extremely compact heat-affected zone which mitigates heat transfer to the layers below or to the vicinity of the melt pool.
Controlled Process
With Meltio’s LMD the wire enters the melt pool coaxially and melts at the point of contact with the substrate. With heat input independent from the material flow, Meltio can employ a sophisticated feedback system, which leads to a stable process.
Minimal Over Thickness
Thanks to the lower heat input and controlled wire-laser process the surface rivals powder based processes. Typically the required over thickness ranges from a maximum 1.5mm in wire-LMD to a few hundred micrometers.

## Slide 6: Meltio Product Portfolio
Meltio M450
3D Printer
For near net shape manufacturing.
Meltio Engine
CNC Integration kit
For hybrid manufacturing, repairs and feature addition.
Meltio Engine
Robot Integration kit
Versatile solution for complex parts and laser cladding.
Meltio
Robot Cell
Turn-key robotic Solution.
Meltio M600
Industrial 3D Printer
The ideal companion for your manufacturing operations.
Generation. I
Generation. II

## Slide 7: Generation I Deposition Head
Coaxial Wire Feed
Integrated Wire Feed/s
Distributed Infrared Laser System
Easy to Service
Hotwire Compatible
Integrated Process Control

## Slide 8: Generation II Deposition Head
No Fibers
No Calibration
Longer service intervals
New Sensors
Vision System
1000W 450 nm Lasers

## Slide 9: Niobium Wire Tests

## Slide 10: Niobium Wire Laser 3D Printing
Single wall and solid cube tests in Meltio M600.
Material Challenge | Technical Capability
Melting point 2,750 K | High Efficiency Blue Laser
Prone to Oxidation | Argon Atmosphere (O2 20ppm)
Weldable on Titanium | Multiple Wire Printing

## Slide 11: Niobium Wire Laser 3D Printing
Single wall and solid cube tests in Meltio M600.
1.0 mm wire
Successful 100mm cylinder - 2.0mm wall
Suboptimal cube

## Slide 12: Geometry Tests

## Slide 13: Single 1.3GHz Cavity in 316L
Printing with Meltio Engine CNC Integration, to combine Additive and Subtractive processes, to obtain optimal internal surface roughness.

## Slide 14: Single 1.3GHz Cavity in 316L
Printing with Meltio Engine CNC Integration, to combine Additive and Subtractive processes, to obtain optimal internal surface roughness.

## Slide 15: Future Developments

## Slide 16: Potential Areas of Investigation
Printing Nb an Cu with Meltio Engine Robot Cell
Increased power 1.4kW - 450nm
Possibility of Inert Chamber

## Slide 17: Thanks
www.meltio3d.com