## Slide 1: WP3: Nb3Sn on Cu films for 4.2K cavity operation First Annual Meeting @LNL, March 13, 2025
All information contained in this presentation and any accompanying documents is for iSAS project only, and must be treated as strictly confidential.
Any dissemination, distribution or other use of this information without the consent of its owner is prohibited.
Funded by the European Union. Views and opinions expressed are however those of the authors only and do not necessarily reflect those of the European Union or the European Commission. Neither the European Union nor the granting authority can be held responsible for them.

## Slide 2
WP3 Nb3Sn on Cu films for 4.2K cavity operation: MAIN GOAL
The objective is focused on the development of thin-film cavities and aims to transform conventional superconducting radio-frequency technology based on off-shelf bulk niobium operating at 2 K, into a Nb3Sn technology operating at 4.2 K using a highly functionalized material, where individual functions are addressed by different layers
Calculated AC power dissipation of Nb and Nb3Sn cavity cells at cryogenic temperatures at 1.3 GHz. A Nb3Sn cavity operated at 4.2 K outperforms a Nb cavity at 1.8 K - even when allowing for elevated residual resistance values. (courtesy of Sebastian Keckert from HZB).
Complementary to H2020 project I.FAST, iSAS WP3 is focused on minimizing trapped flux and increasing coating mechanical strength to allow cavity tunability

## Slide 3
WP3: Nb3Sn on Cu films for 4.2K cavity operation
Institutes participating: INFN, CEA, HZB, UKRI
Convener: Cristian Pira (INFN LNL)
Task 3.1: Coordination of R&D on SC cavities – M1-M48 (INFN, CEA, HZB, UKRI) – Cristian Pira This task aims to coordinate the different task activities and organize the periodic WP meetings.
Task 3.2: Flux Trapping – M1-M32 (INFN, CEA, HZB, UKRI) – Oleg Malyshev
This task aims to minimize flux trapping in Nb3Sn thin films studying and optimizing coating parameters and cooling procedure
Task 3.3: RF Tunability – M1-M32 (INFN, CEA, HZB, UKRI) – Oliver Kugeler
This task aims to study and improve mechanical properties of SC thin films to assess the impact of future cavity tuning during normal 4.2 K operation
Task 3.4: Adaptive Layers – M1-M40 (INFN, CEA, HZB, UKRI) – Thomas Proslier
This task aims at developing suitable adaptative layers synthesized by Atomic Layer Deposition (ALD) to reduce the detrimental effect of mechanical deformation on the superconducting properties of Nb3Sn
Task 3.5: Working Cavity – M1-M48 (INFN, CEA, HZB, UKRI) – Reza Valizadeh
This task encompasses the main outcome of WP3: to optimize the SC cavity coating procedure at 1.3 GHz using the experience and knowledge gained in Tasks 3.2-3.4. and demonstrate suitability for operation at 4.2 K.

## Slide 4
WP3 Nb3Sn on Cu films for 4.2K cavity operation: Task 3.1
Coordination (INFN, CEA, HZB, UKRI) – Cristian Pira
Status:
WP3 Meeting 01 - Task leaders Pre-Kick-Off remote meeting on 21/02/2024
https://agenda.infn.it/event/40107/
WP3 Meeting 02 - Kick-Off meeting in Paris (hybrid) on 16/04/2024 (in collaboration with I.FAST WP9) https://indico.cern.ch/event/1357302/sessions/528505/#20240416
WP3 Meeting 03 - Task Leaders remote meeting on 17/07/2024 (in collaboration with I.FAST WP9) https://indico.cern.ch/event/1437516/
WP3 Meeting 04 – Hybrid meeting in Berlin on 02-03/12/2024 (in collaboration with I.FAST WP9)
https://events.hifis.net/event/1875/
WP3 Meeting 05 – Annual meeting in LNL (hybrid) on 12/03/2025
https://indico.ijclab.in2p3.fr/event/11291/timetable/#20250312

## Slide 5
WP3 Nb3Sn on Cu films for 4.2K cavity operation: Task 3.2
Flux Trapping (INFN, CEA, HZB, UKRI) – Oleg Malyshev
Objectives
Explore new coating parameters for planar samples and small resonators to minimize flux trapping in SC A15 films.
Upgrade the STFC choke cavity and the HZB QPR to support detailed flux trapping analyses of coated superconducting films.
Characterize trapped flux, flux viscosity and the interaction with the RF field with SC A15 films in small resonators and samples with the upgraded systems.
Deliverable 3.2 Flux trapping Report on flux dynamics study in Nb3Sn on Cu samples - HZB - Report M30
Milestone 3.1 Modification of choke cavity for flux trapping study - Engineering report M12
Completed in time

## Slide 6
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
3 Characterization Facilities
Choke Cavity Field Penetration Facility (RS measurements with 7.8 GHz cavity)
Magnetic Field Penetration Facility
CRAFT Facility (Measurement of flux trapping and flux dynamics)
HP1
HP2

## Slide 7
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
The Choke Cavity Facility
Two-part test cavity in LHe-free cryostat:
  Bulk Nb choke cavity
  Sample:
    planar disk 90 - 130 mm,
    thickness w = 1 – 10 mm
RF-DC compensation  RS (T, B)
VNA measurements  Δf  Δλ
Parameters:
  f0 = 7.8 GHz
  TSample ≥ 4 K
  RF power up to 1 W
  Bsample, pk ≤ 2.5 mT
    To be Bsample, pk ≤ 20 mT after moving to a new CI Bunker
1 sample test Rs(T) in 2 days
Example of results:
effect of magnetron power
for depositing Nb3Sn
Courtesy of O. Malyshev and D. Seal

## Slide 8
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
The Choke Cavity Facility Update milestone 3.1
Courtesy of O. Malyshev and D. Seal
Facility has been moved to a new CI Bunker - completed
  No radiation limit on RF power
    after completing jobs for the gate closing (within a month)
  Cryocooler damaged during relocating in Nov. 2024
    Fixed in Jan 2025
RF rack is being updated:
  ongoing
    f0 = 7.8 GHz
    TSample ≥ 4 K
    RF power up to 1 W
    Bsample, pk ≤ 20 mT in CW mode
    Expected to be larger in pulsed mode
New Magnetic shield
  New drawings agreed, PO sent to manufacturer
  Delivery expected in April 2025
New CI SRF bunker

## Slide 9
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
Courtesy of O. Malyshev, D. Seal and P. McGuinness (ASTeC)
Sample holder redesign to accommodate 3 Hall probes for 3D magnetic field measurements:
  Hall probes and a controller procured
  A 3D Hall probe assembly with a D15 connector has been design and under construction at DL electric workshop
  Sample holder redesigned and is the mechanical workshop - completed (MS-11)
  These all will be produced and tested in March
New magnetic shield designed and ordered
  Delivery expected in April 2025
A design of a 3D Hall probe assembly with a D15 connector
The 3D Hall probe assembly mounted on the sample holder.
New magnetic shield design
The Choke Cavity Facility Update milestone 3.1

## Slide 10
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
The Field Penetration Facility Update
Courtesy of O. Malyshev, D. Seal
Hp2 with Shielding
HP1
HP2
Sample
SC coil
Hall probe for applied field
Hall probe for penetrated field
Hall probe Shielding :
d = 30 mm, w = 1 mm and L = 50 mm
d = 50 mm, w = 2 mm and L = 50 mm
Magnet Housing
Sample Holder
Larger Sample Plate
To accommodate
samples  = 30-100 mm
Split cavity
Parts of cavity up to 100  100 mm

## Slide 11
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
The Field Penetration Facility Update
Courtesy of O. Malyshev, D. Seal
An operation software has been modified to test a residual sample magnetisation as a function of
operation temperature, T
applied magnetic field, B1app

## Slide 12
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
CRAFT Facility Update
Courtesy of O. kugeler
GOAL: Measurement of flux trapping and flux dynamics using the CRAFT and TraMaFlu facilities
Time resolved field mapping during the sc transition in external field
TraMaFlu

## Slide 13: Unexpected problem encountered: cryocoolers can only deal with limited shear forces in horizontal orientation Solution: mechanical relief with a custumized spring system System up and running Turn-around time less than 1 day
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
CRAFT Facility Problem Encountered
Courtesy of O. kugeler

## Slide 14
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
CRAFT Facility First Test
Courtesy of O. kugeler
Thermo currents in Nb3Sn sample during cooldown
Sample: Nb3Sn on copper substrate with Nb buffer layer in between prepared by INFN LNL
Compensate earth’s magnetic field
Cooldown with temperature gradient of
Field at the beginning of the animation (~30µT) are already caused by thermo currents
Strong magnetic fields are generated during cooldown with measured magnitudes up to µT
Onset temperature is around 14.7 K
Numbers next to the arrows show the measured B-field in µT
Numbers next to sample show the Temperature of 8 Cernox sensors which are glued to the sample

## Slide 15
WP3 Nb3Sn on Cu: Task 3.2 Flux Trapping
Comments and next steps
Milestone 3.1 is completed
Choke cavity facility ready for test in 2 months
Magnetic Field Penetration Facility ready (UKRI samples already measured)
CRAFT Facility ready and first INFN samples measured at HZB

## Slide 16
WP3 Nb3Sn on Cu films for 4.2K cavity operation: Task 3.3
RF Tunability (INFN, CEA, HZB, UKRI) – Oliver Kugeler
Objectives
Explore new coating parameters on planar samples and small resonators to enhance the mechanical strength in SC A15 films.
Mechanical film-stability tests with planar samples.
Build cavity tuning system and perform vertical cryo-tests of coated cavities to explore RF performance limits and acceptable tuning without incurring film damage.
Devise cavity tuning schemes for Nb3Sn cavities fulfilling the required tuning parameters while taking into account the constraints of Nb3Sn. The implementation of FE-FRT to assist will be considered.
Deliverable 3.1 Cavity tuning Report on implementation of cavity Q vs F tuning tool - HZB - Report M24
Milestone 3.3 Report on mechanical strength test of SC coatings - Test report M30

## Slide 17
WP3 Nb3Sn on Cu: Task 3.3 RF Tunability
Planar Samples
Courtesy of O. Kugeler
Protocol for mechanical properties test on Nb3Sn coatings defined by CEA
UKRI and INFN: Coating systems ready for first planar samples deposition
First samples exchange expected in the next 2-3 months

## Slide 18
WP3 Nb3Sn on Cu: Task 3.3 RF Tunability
Tuning Facility Characteristics
Courtesy of O. Kugeler
Perform vertical test of Nb3Sn coated Cu-cavity
Integrate tuner into vertical test (no tank)
Investigate performance degradation due to mechanical tuning
Feedback for tuning scheme

## Slide 19: Adapters for tuner integration with INFN Legnaro Nb3Sn-on-Cu cavity manufactured
WP3 Nb3Sn on Cu: Task 3.3 RF Tunability
Tuning Facility Update
Courtesy of O. Kugeler
INFN LASA Blade Tuner
New cavity flange design @LNL

## Slide 20
WP3 Nb3Sn on Cu: Task 3.3 RF Tunability
Tuning Facility Nex Steps
Courtesy of O. Kugeler
Fabricate input and pickup antenna
Wait for cavity from INFN
Vertical test at HZB using SRF infrastructure

## Slide 21
WP3 Nb3Sn on Cu films for 4.2K cavity operation: Task 3.4
Adaptive Layers (INFN, CEA, HZB, UKRI) – Thomas Proslier
Objectives
Develop adaptative layers by atomic layer deposition on Cu that are stable up to 650 °C. Insulating oxides layer: Al2O3, ZrO2, ZrAlOX as diffusion barriers
Compare performance Nb3Sn on Cu with and without adaptive layers on planar samples and QPR.
Deliverable 3.3 Adaptive Layer Report on QPR study of Nb3Sn on Cu & adaptive layers - CEA - Report M38
Milestone 3.2 Developed ALD adaptive layers on Cu - Test report M24

## Slide 22
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
Al2O3 (15 nm) /Cu EP
Courtesy of T. Proslier
After annealing
Before annealing
No cracks, no holes
Al2O3 layer stable after annealing up 700°C in high vacuum and HPR.
No Cu diffusion through the Al2O3
Amorphous before or after annealing. No structure observed by SEM.
After annealing 700°C-2hrs + HPR
XPS

## Slide 23
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
Cu EP / Al2O3 (15 nm) + Nb HiPIMS coating
Courtesy of T. Proslier
Baseline HIPIMS coating recipe:
1.2kW avg
100Hz, 200us HiPIMS pulses
-75V bias voltage
150C
2.5.10-3 mbar Kr
Nb/Al2O3 15 nm
GIXRD
crystallite size,
microstrain,
lattice parameter,
Nb/Cu and Nb/Al2O3/Cu do not show any difference from XRD.
The lower dislocation density can be explained by the thicker layer.
Same superconducting properties measure by tunneling spectroscopy with or without Al2O3 layers.
C. Pereira, S. Leith, G. Rosaz, S. Pfeiffer

## Slide 24
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
Cu EP / Al2O3 (15 nm) / Nb HiPIMS on cavity
Courtesy of T. Proslier
Coating of a 1,3 GHz cavity EP from CERN with 15 nm of Al2O3. Send back to CERN for Nb deposition.
Delamination occured in one beamtube near the flange after HPR.
Another cavity will be sent under inert atmosphere (N2) and coated again at CEA and CERN.

## Slide 25
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
ZrO2 (20 nm) / Cu
Courtesy of T. Proslier
Crystalline ZrO2 grains 5-10 nm as grown or after annealing.
No cracks for ZrO2 films ≤ 20 nm on Cu.
Cubic as deposited and mixture tetragonal after annealing.
No copper diffusion after 700°C-2hrs.
ZrO2/Metallic Cu interface.
After annealing
Before annealing
XPS
XRD
After annealing + HPR

## Slide 26
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
ZrO2 (20 nm) / Al2O3 (5 nm) / Cu
Courtesy of T. Proslier
No cracks
Clear crystallites ( ~10-30 nm)
Cubic + much weaker monoclinic phases.
No copper diffusion after 700°C-2hrs.
ZrO2/Metallic Cu interface.
Maybe slight interdiffusion Al2O3-ZrO2.
Resist Annealing + HPR.
After annealing
Before annealing
XPS
XRD
After annealing

## Slide 27
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
ZrAlOx (20 nm) / Cu
Courtesy of T. Proslier
Intermixing growth 4 cycles ZrO2 -1 cycle Al2O3. Nominal ratio 25% Al2O3-75% ZrO2.
XPS: 27 % Al2O3 - 73% ZrO2 .
No copper diffusion after 700°C-2hrs.
ZrO2/Metallic Cu interface.
Amorphous as grown and very weakly crystalline after annealing.
No cracks.
Resist HPR
After annealing
Before annealing
After annealing + HPR

## Slide 28
WP3 Nb3Sn on Cu: Task 3.4 Adaptive Layers
Comments
Courtesy of T. Proslier
Some layers (crystalline or amorphous): Al2O3, ZrO2, ZrAlOX and bilayers ZrO2 / Al2O3 are stable up to 700°C in high vacuum and HPR on Cu.
No Cu diffusion through the insulating ALD films.
Some oxide films such as Y2O3 or YZrOX (YSZ) and ZrO2 films thicker than 50 nm show some cracks after annealing at 700°C-2hrs.
Next Steps
Test Nb3Sn or Nb deposition: samples sent to CERN, INFN and UKRI for Nb3Sn deposition (HiPIMS and DC-MS)
ZrO2 (20 nm)/Cu.
ZrO2 (20nm) /Al2O3 (5nm)/Cu.
Al2O3 (15nm)/Cu.
AlZrOx (20 nm)/Cu.
HPR tests on Cu/ALD layers/Nb3Sn
Test Al2O3 / Nb deposition by HIPIMS on 1,3 GHz Cu cavity.
Test mechanical stability of Nb3Sn/ALD layer/Cu (tuning).

## Slide 29
WP3 Nb3Sn on Cu films for 4.2K cavity operation: Task 3.5
Working Cavity (INFN, CEA, HZB, UKRI) – Reza Valizadeh
Objectives
Improve I.FAST 1.3-GHz superconducting coating recipe based on Tasks 3.2-3.4 results.
Prepare 1.3-GHz thin film cavities with an optimized coating recipe.
Perform full cavity characterization @4.2 K (Q vs E, Q vs F, and flux trapping in the VTS@SupraLab vertical test stand).
Deliverable 3.4 4.5-K Cavity Report on 4.5-K Cavity performance & tunability tests - INFN - Report M46
Milestone 3.4 Characterization of Nb3Sn reference cavity - Test report M34

## Slide 30
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
2 Coating Facilities for 1.3 GHz elliptical cavities
2’’ Movable Planar Magnetron
Rectangular Magnetron with rotating cavity
Both facilities are in the final commissioning phase

## Slide 31
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
Preliminary Cavity Deposition using Planar Magnetron
Courtesy of R. Valizadeh
100 W Dc , -75 V Bias, 340 °C and 440 °C C, 7 hours , 6 x 10-3 mbar Kr
Tc = 16.22 +/-0.11 K
Nb3Sn
Cu

## Slide 32
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
Cavity heating and shielding assembly
Courtesy of R. Valizadeh
Cavity heating and heat shielding designed
A nock run was successful

## Slide 33
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
New 2” Planar Magnetron
Courtesy of R. Valizadeh
New 2” planar magnetron designed and built in house
Magnetron tested successfully
New double wall chamber is designed and ordered
Other auxiliary parts are ordered and waiting for delivery
Next is to deposit a mock cavity to be coated with the new magnetron to validate the process

## Slide 34
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
Nb3Sn Coating System @LNL
Hybrid coating system for 1.3 GHz cavities
Rectangular fixed magnetron & rotating cavity
Post magnetron configuration with Nb3Sn cylindircal target produced via dipping
Status:
Vacuum sysyem ready and tested
All components commissioned:
  Magnetron and rotation components delivery expected by end of March
  Some auxiliary parts arrive in May

## Slide 35
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
Cavity Support Structure
After heat treatment (4 h @ 600 °C): cavity collapsed during the pumping process
SOLUTION:
4 stainless steel bars (M8) tested successfully, with ongoing design improvements

## Slide 36
WP3 Nb3Sn on Cu: Task 3.5 Working Cavity
Next Steps
Installation and test of cavity coating system at UKRI and INFN
First Coated Cavity expected in June-July

## Slide 37
WP3 Nb3Sn on Cu: plans to achieve milestones & deliverables
M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F
2024 | 2025 | 2026 | 2027 | 2028
D3.1 Cavity tuning Report on implementation of cavity Q vs F tuning tool - Report M24 - HZB
D3.2 Flux trapping Report on flux dynamics study in Nb3Sn on Cu samples - Report M30 - HZB
D3.3 Adapt. Layer Report on QPR study of Nb3Sn on Cu & adaptive layers - Report M38 - CEA
D3.4 4.5-K Cavity Report on 4.5-K Cavity performance & tunability tests - Report M46 - INFN
Y0
Y1
Y2
Y3
Y4
Task 3.1 - Coordination
Task 3.2 – Flux Trapping
Task 3.3 – RF Tunability
Task 3.4 – Adaptive Layers
Task 3.5 - Working Cavity @4.2K
M3.1
D3.1
M3.2
D3.2
M3.3
D3.3
M3.4
D3.4
M3.1 Modification of choke cavity for flux trapping study - Engineering report M12
M3.2 Developed ALD adaptive layers on Cu - Engineering report M24
M3.3 Report on mechanical strength test of SC coatings - Test report M30
M3.4 Characterization of Nb3Sn reference cavity - Test report M34
Milestones & deliverables
on track

## Slide 38
WP3 Nb3Sn on Cu: financial status
Partner | Budget |  |  | FTE |  |  | 
 | EU total contribution | EU Budget spent | Matching Funds | YEAR 1 | YEAR 2 (expected) | YEAR 3 (expected) | YEAR 4 (expected)
CEA | 100 |  |  |  |  |  | 
HZB | 200 |  |  |  |  |  | 
INFN | 200 | 64 1 post-doc hired + dedicated LNL staff | 60 1.3 GHz coating system upgrade |  |  |  | 
UKRI | 200 |  |  |  |  |  | 

## Slide 39
WP3 Nb3Sn on Cu: financial status
Financial status
  Funds engaged in the WP by institute to date, differentiating EU-budget from matching funds
  With highlight of staff dedicating time on the iSAS project, to date & projections if possible
Deviations?

## Slide 40
WP3: Nb3Sn on Cu films for 4.2K cavity operation
1° year milestone delivered in time
2° year milestone and deliverable on track
No project main criticality at the moment
The partners of WP3 are preparing a proposal for I-FAST-2 in continuity with ISAS activity
Conclusion and point of attention

## Slide 41
Thank You!

## Slide 42
A15 are Brittle materials
Complicate Phase Diagram
Low melting point substrate
Substrate preparation
Interface diffusion
Target Production
Coating Parameters
Trapped Flux
Tuning
Nb3Sn on Cu: Multiple challenges

## Slide 43: I.FAST Sinergy
MAIN GOAL (2025): Realize a prototype of high performance 1.3 GHz thin film SRF elliptical cavity Q > 1· 1010 @ 4.5 K
A step forward in TRL
Focus on:
minimizing trapped flux
increasing coating mechanical strength (to allow cavity tunability)

## Slide 44: I.FAST Sinergy
MAIN GOAL (2025): Realize a prototype of high performance 1.3 GHz thin film SRF elliptical cavity Q > 1· 1010 @ 4.5 K
Equivalent to a Q of 9*109 @5 MV/m @4.5 K
5 times better than LHC
Rs of 25 nΩ @ 20 mT @ 4.5 K
Quench >70 mT @ 4.5 K
Last results (March 2023):
4.5 K
QPR Nb3Sn
QPR Nb3Sn
Data of LHC cavities from: W. Venturini, TTC Meeting 2018, Milan (Italy)
G=216 Ω

## Slide 45: Trapped Flux
First ISAS Results:
A. Romanenko, A. Grassellino, O. Melnychuk, D. A. Sergatskov, J. Appl. Phys. 115, 184903 (2014)
Fast cooldown
Slow cooldown
Nb3Sn coating suffer flux trapping
Cooldown procedure influence Rs

## Slide 46: Cavity Tunability
Vapor Tin Diffusion Nb3Sn on Nb cavities can be tuned only at cryogenic T
An interlayer in Nb3Sn on Cu coatings can be added to enhance film mechanical stability and tunability
Eremeev, G. (2023). Tunability/robustness of Nb3Sn (No. FERMILAB-SLIDES-23-402-TD). Fermi National Accelerator Laboratory (FNAL), Batavia, IL (United States).
Strong performance degradation after room temperature tuning for 200 kHz
Nb3Sn is extremally brittle
Little change in the coated cavity performance after tuning up to 1400 kHz at cryogenic temperatures