## Slide 1: Additive manufacturing applied to particle accelerators Nicolas Delerue on behalf of the FA3 project

## Slide 2: What is additive manufacturing?
Building an object by the addition of successive layers of materials (by opposition to traditional manufacturing where material is removed).
Originally made for rapid prototyping but now extended to the production of fully functional objects.
For more details, see, for example, the talk by Lukas Stepien given during the I.FAST collaboration meeting: https://indico.cern.ch/event/1143029/
3D CAD Data
Slicing
Layer-wise build-up
Source: Lukas Stepien, Fraunhofer IWS Dresden
Cost per part
Part complexity
Conventional fabrication
Break even point
Additive manufacturing
Break even point
Batch Size
Cost per part
Additive manufacturing
Conventional fabrication

## Slide 3: What is additive manufacturing?
Easier with polymers but possible with a large range of materials (including metals).
Wide range of technologies. For metals, it is necessary to melt powder or a thin wire of the metal. Can be done with a laser or an electron beam.
More advantageous for small series of complex parts.
The surface of additively manufactured part is often very rough.
Image source: wikipedia

## Slide 4: Additive manufacturing of Copper
For accelerators several metals are of interest:
  Aluminum and Stainless steel are well under control
  Copper is more difficult because of its reflectivity (see separate slide)
  Niobium is difficult because of the high melting point.
Melting copper with an infra-red laser is difficult because of the high reflectivity of Copper at that wavelength
Several strategies exist:
  Use more laser power
  Use a laser with different wavelength (eg: green)
  Add an additive to the powder to make it absorb the laser power
Some attempts we did were unsuccessful as the copper produced had too much porosity.
However this is strongly dependant on the settings of the machine used. More experience needed to understand the acceptable range of machine settings.

## Slide 5: Recognized metal additive manufacturing activities within accelerator community
Chart: year
| 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021
 | 1 | 3 | 3 | 3 | 3 | 4 | 5 | 8 | 10 | 12 | 16 | 21 | 31 | 34 | 41

## Slide 6: Materials used for accelerator parts
Chart: 
| SS | Ti | Cu | Al | Nb
 | 6 | 4 | 8 | 1 | 2

## Slide 7: Collage of metal AM parts within accelerators
Reference links to each of pictures in further slides

## Slide 8: Challenges of additive manufacturing in accelerators
Parts used in particle accelerator have to be adapted to their environment:
  Ultra High Vacuum (UHV)
  Induced electric fields
  High Electromagnetic power
  Sometimes: ultra low temperatures
  …
We demonstrated around the UHV compatibility of Metal (and Copper) AM parts with UHV.
Now the FA3 project wants to address two other challenges:
  Resistance to high electromagnetic power
  Transmission of electric signals outside the vacuum

## Slide 9: The basic: Ultra High Vacuum
Beyond the use of polymer AM parts as support, one of the first challenge to address was Ultra-High Vacuum compatibility.
The rough surface of the stainless steel parts produced was source of concern.
Several UHV tubes were manufactured and measured by our vacuum group (as well as a conventional tube from a regular supplier).
It was demonstrated that surface roughness is not an issue (except for the flanges).
UHV Performances of both types of tubes were similar.

## Slide 10: First diagnostic: Beam position monitor
The next step was to produce a working accelerator part.
The choice was to built a beam position monitor as it is mechanically complex.
Topological optimization was used to improve the design.
The use of additive manufacturing allowed to have thinner electrodes (and thus a better impedance matching).
After production the BPM was validate by our vacuum group and then installed on our photo-injector next to two conventional BPMs.
All measurements showed no difference in behaviour between the three BPMs.
Note: At the moment the electrical feedthrough are still sourced externally and note additively manufactured (R&D on this is in progress).

## Slide 11: Radiofrequence Quadrupole
In the European project I.FAST, Work Package 10 is partly dedicated to the applications of additive manufacturing to particle accelerators.
WP 10 involves Riga Technical University, CERN, Politechnic University of Milano, IWS Fraunhofer, INFN Padova, Talinn Technical University, Trumpf and CNRS.
The collaboration has worked on the design of a segment of an accelerator component called Radiofrequency Quadrupole (RFQ) made of copper.
Validation tests for UHV were successful.

## Slide 12: High power and beam tests
FA3 goal on high EM power:
  We have started internal R&D to produce an accelerating section using additive manufacturing.
  Aim: qualify a copper accelerator component with high power RF and then test it with an electron beam.
  The part we have designed is based on the lab’s experience (a similar part has been produced in traditional manufacturing).
  Current status:
    Technology and supplier identified
    First test parts produced, electrical properties to be measured
    Design of the second test part in progress

## Slide 13: Multimaterials
FA3 goal on multimaterials:
  Build a Beam Position Monitor fully in Additive Manufacturing
  This require a part with inox and ceramics.
  First test on a simple flange
  Collaboration with the Ceram Glass team in Padova.
  Current status:
    First flange produced
    Under tests at the vacuum group

## Slide 14: Advantages of Additive Manufacturing for accelerators
Outlook:
Additive manufacturing has several advantages for accelerators:
  Shapes can be closer from specifications
  Possibility to add cooling channels as close as possible to heat source
  Faster and/or cheaper production (for complex parts).
Some challenges still to be addressed:
  UHV electrical feedthrough
  High power RF
  Accelerating a particle beam with an AM component
  (not addressed here) Application to cryogenics