## Slide 1: Ruthenium speciation during acidification of alkaline solution using a UV-Visible fast detector and an in-situ probe
Mathis Leblanc1, Sarah Baghdadi1, Alexandre Quemet1, Jean Aupiais2
1CEA, DES, ISEC, DMRC, Univ Montpellier, Marcoule, France.
2CEA, DAM, DIF, 91297 Arpajon, France.

## Slide 2: Context: What is it like to work with ruthenium?

## Slide 3: Context: What is it like to work with ruthenium?
-II
0
+I
+II
+III
+IV
+V
+VI
+VII
+VIII
Ex: RuO4
Ex: RuO42-
Ex: RuO2
Solid
Aqueous
Gas
To keep in mind
298 K – 100 kPa (20 °C – 1 bar)
Mousset, F. Ph.D. Thesis, Université Paris VI, 2004.
Experimental results

## Slide 4: Context: Why are we interested in ruthenium?
Fission product
NaOH
Ru - NaOH
RuO4 (g)

## Slide 5: Context: Why are we interested in ruthenium?
Ru - NaOH
Difficult to quantify
Ru – HNO3
Low concentration
Ru - NaOH
Low concentration
ICP-MS
High Na+ level
Low sensitivity
No alkaline standard

## Slide 6: Context: Why are we interested in ruthenium?
Ru - NaOH
Ru - NaOH
Ru – HNO3
ICP-MS
HNO3
Black precipitate

## Slide 7: Context: Why are we interested in ruthenium?
0 – 30% of total Ru
Quantification not reproducible
Ru - NaOH
Precipitate
Ru – HNO3
HNO3
ICP-MS?
Objectives:
Identify and quantify the acidifications byproducts
1
Understand their formation mechanisms
2
Control their formations during the analysis
3
Perform a reliable ICP-MS analysis of ruthenium from an initial alkaline medium

## Slide 8: Methods: Synthesis of a Ru solution in NaOH at a known concentration
Ru metal
K2S2O8
in NaOH 5.0 mol·L-1
Ru – NaOH Stock solution
[Ru] = 850 mg·L-1
[NaOH] = 5.0 mol·L-1
Boil, 1h
But how to confirm the concentration?
UV-Visible quantification
RuO42-
.
.
High concentration

## Slide 9: Methods: Experimental set-up for acidification
Controlled acid addition
Gas outlet
UV-Visible in-situ probe
Fast detector – up to 160 spectra/s
In-situ and real-time monitoring
Massive data acquisition
Deconvolution needed to resolve species
Closed reactor

## Slide 10: Methods: Data treatment
Python automation for large-scale data handling
Multivariate Curve Resolution Alternating Least Squares
MCR-ALS algorithm:
Fed with estimated spectra of pure species:
Ruthenate: RuO42-
Perruthenate: RuO4-
Nitrate: NO3-
Chemical constraint

## Slide 11: Results: Reactor during acidification
Nitric acid
Time

## Slide 12: Results: Raw UV-Visible Spectra
Ruthenate
Perruthenate

## Slide 13: Results: Speciation during acidification
Ratio
RuO42-
RuO4-
Sum

## Slide 14: Results: Speciation during acidification
Ratio
RuO42-
RuO4-
Sum
a RuO42- + b H+ → c RuO4- + d Ru(?)
2 RuO42- + b H+ → 1 RuO4- + 1 Ru(?)
2 Ru(VI) + b H+ → 1 Ru(VII) + 1 Ru(?)
2 Ru(VI) + b H+ → 1 Ru(VII) + 1 Ru(V)
2 Ru(VI) + b H+ → 1 Ru(VII) + 1 RuO2.5
4 RuO42- + b H+ → 2 RuO4-+ 1 Ru2O5

## Slide 15: Results: Speciation during acidification
Ratio
a RuO4- + b H+ → c Ru(?)
1 RuO4- + b H+ → 1 Ru(?)

## Slide 16: Results: Speciation during acidification
2 RuO4- + b H+ → 2 Ru(?)
4 RuO42- + b H+ → 1 Ru2O5 (s) + 2 Ru(?)
Ru solid
K2S2O8
in 25mL NaOH
The precipitate contains 66% of the initial Ru inventory
Where is the remaining 33%?
4 RuO42- + b H+ → 2 RuO4- + 1 Ru2O5 (s)
Solid quantification:
UV-Visible quantification:

## Slide 17: Results:
RuO4 (aq)
RuO4 (g)
Contains 33% of the initial Ru inventory
Where is the remaining 33%?
Increasing Ru concentration reveals the low-epsilon ruthenium tetroxyde
Increasing Ru concentration
Increasing Ru concentration reveals the low-epsilon ruthenium tetroxyde

## Slide 18: Results: Final reaction equations
2 RuO4- + b H+ → 2 Ru(?)
4 RuO42- + b H+ → 2 RuO4- + 1 Ru2O5 (s)
2 RuO4- + b H+ → 1 Solid + 1 RuO4 (aq)
Reaction 1:
Reaction 2:
2 Ru(VII) + b H+ → 1 Solid + 1 Ru(VIII) (aq)
2 Ru(VII) + b H+ → 1 Ru(V) + 1 Ru(VIII) (aq)
4 RuO4- + b H+ → 1 Ru2O5 (s) + 2 RuO4 (aq)
3 Ru(aq) + b H+ → 2 Solid + 1 Gas(dissolved)
66%
33%
2 RuO4- + b H+ → 1 RuO2.5 + 1 RuO4 (aq)

## Slide 19: Results: Final reaction equations
4 RuO42- + b H+ → 2 RuO4- + 1 Ru2O5
Reaction 1:
Reaction 2:
4 RuO4- + b H+ → 1 Ru2O5 + 2 RuO4 (aq)
4 RuO42- + 6 H+ → 2 RuO4- + 1 Ru2O5 + 3 H2O
6 RuO4- + 6 H+ → 1 Ru2O5 + 4 RuO4 (aq) + 3 H2O
Ratio

## Slide 20: Results: Final reaction equations
Reaction 1:
Reaction 2:
4 RuO42- + 6 H+ → 2 RuO4- + 1 Ru2O5 + 3 H2O
6 RuO4- + 6 H+ → 1 Ru2O5 + 4 RuO4 (aq) + 3 H2O
12 RuO42- + 24 H+ → 4 Ru2O5 + 4 RuO4 (aq) + 12 H2O
3 RuO42- + 6 H+ → 1 Ru2O5 + 1 RuO4 (aq) + 3 H2O
3 Ru(aq) + 6 H+ → 2 Solid + 1 Gas (dissolved)
66%
33%
3

## Slide 21: Results: Back to the Ruthenium Analysis
0 – 30% of total Ru
Quantification not reproducible
Ru - NaOH
Ru2O5 (s)
RuO4 (aq)
HNO3
ICP-MS?

## Slide 22: Results: Back to the Ruthenium Analysis
3 Ru(aq) + 6 H+ → 2 Solid + 1 Gas (dissolved)
66%
33%
Time
Variable amount of Ru over time
RuO4 (aq)
0 – 30% of total Ru
Quantification not reproducible
.
.
.
.
.
.

## Slide 23: Conclusion and Outlooks
Acidification of alkaline Ru sample leads to ⅔ of solid Ru2O5
Identify and quantify the acidifications byproducts
1
Another ⅓ react into the highly volatile RuO4 (partially dissolved)
Understand their formation mechanisms
2
Two-steps reaction involving a RuO4- intermediate
Kinetic constants determination in progress
The two reactions are total and fast
Control their formations during the analysis
3
Acidification with hydrochloric acid to form more stable species
Ru - NaOH
HCl
?
⅔ Ru2O5
⅓ RuO4(aq)

## Slide 24: Thank you
Mathis LEBLANC
Marcoule Center – France
mathis.leblanc@cea.fr
PhD supervisors:
Sarah BAGHDADI – sarah.baghdadi@cea.fr
Alexandre QUEMET – alexandre.quemet@cea.fr
Jean AUPIAIS – jean.aupiais@cea.fr