## Slide 1: iSAS Task 3.2: Flux trapping Progress at UKRI/STFC
O.B. Malyshev, D. Seal and L. Smith
R. Valizadeh and C. Benjamin

## Slide 2: iSAS Task 3.2 objectives
completed

## Slide 3: Facilities for Superconducting Properties Evaluation at UKRI/STFC/CI
EXP700: Magnetic field penetration facility (in-vacua)
EXP900: RS measurements with 7.8 GHz cavity
HP1
HP2

## Slide 4: The Choke Cavity Facility (EXP-900)
Two-part test cavity in LHe-free cryostat:
  Bulk Nb choke cavity
  Sample:
    planar disk 90 - 130 mm,
    thickness w = 1 – 10 mm
RF-DC compensation  RS (T, B)
VNA measurements  Δf  Δλ
Parameters:
  f0 = 7.8 GHz
  TSample ≥ 4 K
  RF power up to 1 W
  Bsample, pk ≤ 2.5 mT
    To be Bsample, pk ≤ 20 mT after moving to a new CI Bunker
1 sample test Rs(T) in 2 days
Example of results:
effect of magnetron power
for depositing Nb3Sn

## Slide 5: The Choke Cavity Facility updates
Facility set into operation in a new CI Bunker
  Cryogenics is operating
  RF with VNA - OK
  No radiation limit on RF power
    after completing jobs for the gate closing (long delays due to outside contractor, but progress over last two weeks)
RF rack is being updated:
  ongoing
    f0 = 7.8 GHz
    TSample ≥ 4 K
    RF power up to 1 W
    Bsample, pk ≤ 20 mT in CW mode
    Expected to be larger in pulsed mode
New Magnetic shield
CI SRF bunker

## Slide 6: Magnetic Field Penetration Facility
Magnet Housing
Sample Holder
HP1
HP2
Sample
SC coil
Hall probe for applied field
Hall probe for penetrated field
Large Sample Plate
To accommodate
samples  = 30-100 mm
Split cavity
Parts of cavity up to 100 mm . 100 mm
DC magnetic field
  parallel to the surface
  B ≤ 600 mT
  Field local to the sample surface
    2mm  10 mm

## Slide 7: The ongoing work
Samples:
  Substrates:
    100 mm diameter disks with thickness of 2-3 mm made of Cu or Nb
  Coated with thin film of Nb and Nb3Sn
    Varying deposition parameters: temperature, duration, power, etc.
    Varying Deposition method: DC or HIPIMS
Measuring Rs and Tc-RF of these samples with the choke cavity facility of samples
Testing the same samples with magnetic field penetration facility for full penetration magnetic field Bfp(T), residual magnetisation Bres(T) and Tc-dc
Choke cavity facility
Full magnetic field penetration facility

## Slide 8: Residual magnetisation
Residual sample magnetisation can be measured as a function of
operation temperature, T
applied magnetic field, B1app
Typical magnet residual magnetisation B1res
  stays in the range of B1res = 4 mT and
  does not change with T
Residual sample magnetisation B2res :
  varies from sample to sample and
  depends on T
Examples of residual magnetisation

## Slide 9: Main results for Nb on cupper substrate
Relation between Rs(7.8 GHz), Bres and Bfp
measured at 4.2 K
Corelation between Tc measured by different methods and Bfp measured at 4.2 K

## Slide 10: Main results for Nb3Sn on cupper substrate
Relation between Rs(7.8 GHz) and Bfp
measured at 4.2 K
Corelation between Tc, Bfp measured at 4.2 K
and Bres measured at 4.2 and 10 K

## Slide 11: Main results for Nb3Sn on cupper substrate
Corelation between Tc measured by different methods and
Bfp measured at 4.2 K

## Slide 12: Rs for Nb3Sn on Cu and Nb substrates
Relation between Rs(7.8 GHz) and Tc-mag measured at penetration rig

## Slide 13: Magnetic Field Penetration Facility update - 1
New poles for a c-shaped magnet produced
New ability to test curved surfaces:
  Cuts from 1.3 GHz cavity
  Half of 6 GHz cavity
Ability to relate performance of RF tested cavity to AC/DC characterisation such as
  Bfp(T),
  residual magnetisation
  Tc-dc
Ability of AC/DC characterisation of cavity prototypes
1.3 GHz mock cavity deposited Nb after cutting
1.3 GHz cavity cut
from an equator zone
Cavity cut from a tubular zone

## Slide 14: Results for 1.3 GHz cavity cuts
Bfp (4.2 K) =
= 29*4.1 = 119 mT
K
Bfp (4.2 K) = 132 mT
K
Equator
Tube

## Slide 15: Magnetic Field Penetration Facility update - 2
New poles for a c-shaped magnet produced
New ability to test curved surfaces:
  Half of 6 GHz split cavity
  Half of a cut of 6 GHz cavity from INFN
No damage to 6 GHz split cavity
  Non-destructive test, cavity can be used for future coatings and testings
Ability to relate performance of RF tested cavity to AC/DC characterisation such as
  Bfp(T),
  residual magnetisation
  Tc-dc
Half of 6 GHz cavity deposited Nb
Half of 6 GHz cavity installed for MFP measurements

## Slide 16: Results for half of 6 GHz split cavity
Bfp (4.2 K) = 122 mT
K
Side 1
Side 2
Bfp (4.2 K) = 126 mT
K

## Slide 17
Low Power Cavity Test Facility
Mounted 1.3 GHz cavity & heat link
Heat shield & MLI
OVC
Magnetic shields
LLRF System

## Slide 18: New low power RF testing facility (as a part of Task 3.4)
In CI RF bunker
Vacuum <10-7 mbar
Cryogenics: 3.0 K  Tcav  20 K
Magnetic shield is produced and delivered
Next steps – focus on RF:
  RF testing with VNA of uncoated cavity
    flanges and RF cables will be added next week
  RF testing with VNA of Nb coated cavity from IFAST (laser polished at RTU)
  RF testing with VNA of bulk Nb cavity
    After receiving after processing at CEA
  RF testing with VNA of Nb3Sn coated bulk Nb cavity
    As a part of Task 3.4
  Testing new RF system
    Software is still underdevelopment

## Slide 19
Facility Commissioning
Facility has undergone several cooldowns during cryogenic commissioning:
  Base pressure ~ 10^-7 mbar
  Base temperature ~ 2.7 K
  Cooldown time ~ 14 hours
Successful cooling of a Cu cavity:
  4 Cernoxes mounted to cavity
  Tave ~ 2.9 K
  ∆T < 2 mK
Next steps (May/June):
  Commission RF facility
  Test bulk Nb cavity

## Slide 20
A new 1.3 GHz split cavity
RF design based on single-cell 1.3 GHz TESLA cavity split longitudinally
Al prototype currently being manufactured
Final Cu design ~ 15 kg
Cavity mounted to existing Cu supports

## Slide 21
Current status
1. M16 holes machined on 3-axis machine (block mass ~ 31 kg)
2. Block lifted onto 5-axis machine
3. Rough machining outer profile with ~ 2 mm material on all faces