## Slide 1: Trapped flux generated by thermoelectric currents
22.04.2026
ISAS 2026
Berlin
F. Kramer
Notes: I will be sharing measurement data of trapped magnetic flux generated by thermo-electric currents in Nb3Sn samples.

## Slide 2: Experimental setup to measure trapped flux
2 cryocoolers to cool down sample
Sample (100x60x3)mm3, clamped in copper blocks at either end
Two heaters at the end of the blocks allow for precise control of temperature gradient and cooldown rate
Multiple AMR sensors for magnetic field measurements
grouping of 3 sensors to measure field vector in 3d
15 AMR sensor groups measure magnetic field just above the sample
2 Cernox sensors measure temperature gradient across sample
Active field compensation with three Helmholtz-coils
Minimum flux density at location of reference sensors < 30nT
Maximum flux density 220µT
Setup
Courtesy A. Cierpka

## Slide 3: The samples
SampleS
Name | Substrate | Nb layer [µm] | Nb3Sn layer [µm] | Method
Nb3Sn BL (INFN) | Cu | 30 | 1 | Sputtered
Nb3Sn (INFN) | Cu | - | 1 | Sputtered
Nb3Sn BL (INFN) center | Cu | 30 | 1 | Sputtered
Nb3Sn/Cu (HZB) | Cu | 10 | 1 | Sputtered / Bronze route
Nb3Sn/Nb (HZB) | Nb | - | 1 | Bronze route
Nb/Cu (10µm) | Cu | 10 | - | Sputtered
Nb/Cu (4µm) | Cu | 4 | - | Sputtered
D. Fonnesu
D. Ford
A. Zubtsovskii
M. Lu

## Slide 4: A typical Cooldown with “Nb3Sn/Cu (HZB)”
Set Temperature gradient across sample (∇T = 0.12 K/cm)
Compensate external field Bext 1 µT
Green numbers are the measured flux density in µT
Lower Sample temperature at top and bottom simultaneously
As the sample becomes superconducting large flux densities are measured by the AMR sensors
Pulsing stems from temperature oscillations of cryocoolers
  Final state is not impacted by the oscillations
Measure trapped flux in the final state
Results

## Slide 5: Nb3Sn on copper substate
Zero field cooled
Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown
Increasing flux density with temperature gradient
All samples show large flux density magnitudes several times the earth’s magnetic field
Results
To be published

## Slide 6: Nb3Sn on niobium substrate
Zero field cooled
Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown
Increase with temperature gradient
Flux density 2 orders of magnitude smaller
Results

## Slide 7: Niobium on copper
Zero field cooled
Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown
Trapped flux at 0.085 K/cm
  Nb/Cu (4µm): 3.5 µT
  Nb/Cu (10µm): 33 µT
Results

## Slide 8: Trapped flux orientation
The final state orientation of the trapped flux can be categorized in homogenous and inhomogeneous
All Nb3Sn samples on copper substrate show an inhomogeneous final state
All other samples show a homogeneous final state
Results
Nb3Sn/Nb (HZB)
Nb3Sn/Cu (HZB)

## Slide 9: Overview
Results
Name | TF Orientation | Uniform Tc | Tc [K]
Nb3Sn BL (INFN) | inhomogeneous | no | 
Nb3Sn (INFN) | inhomogeneous | no | 
Nb3Sn BL (INFN) center | - | - | 
Nb3Sn/Cu (HZB) | inhomogeneous | no | 
Nb3Sn/Nb (HZB) | homogeneous | yes | 
Nb/Cu (10µm) | homogeneous | yes | 
Nb/Cu (4µm) | homogeneous | yes | 
Name | TF Orientation | Uniform Tc | Tc [K]
Nb3Sn BL (INFN) | inhomogeneous | no | 
Nb3Sn (INFN) | inhomogeneous | no | 
Nb3Sn BL (INFN) center | - | - | 
Nb3Sn/Cu (HZB) | inhomogeneous | no | 
Nb3Sn/Nb (HZB) | homogeneous | yes | 
Nb/Cu (10µm) | homogeneous | yes | 
Nb/Cu (4µm) | homogeneous | yes | 

## Slide 10: Simulation
Simplified geometry to facilitate meshing:
  3mm copper
  1mm niobium
Seebeck coefficients:
  Nb: Temperature dependent
  Cu: Fixed -9 µV/K
Conductivity:
  Nb: RRR 10
  Cu: RRR 50
  Sc Nb: Increase by 5 orders of magnitude between 9.3 K and 9.2 K
Place transition in the middle of the sample
Compute current density
Currents are suppressed by low conductivity of normal conducting Nb
Results

## Slide 11: Simulation
Simulate flux density generated by the current density
Extract flux density at sensor positions
Compare to measurement
  Nb/Cu (10 μm) Sample
  Partially superconducting
Good qualitatively agreement
Magnitude can change drastically by changing conductivity of the copper
Results
Simulation
Measurement

## Slide 12: Barrier layer
Results
Introducing a barrier layer should increase the resistance on the path the thermoelectric currents take
Two samples:
  One fully coated: electric connection at ends
  One coated only in the center: floating Nb3Sn

## Slide 13: Conclusion
All Nb3Sn samples on copper substrate created large fields during cooldown
Coating of only the center did not fix the low
Simulation shows qualitative agreement with measurement
Electrical conductivity is crucial for thermoelectric currents
Conclusion & Outlook
Outlook
Try different coatings
  Film thickness
  Coating area
  Higher Tc
  Insulating buffer layer
Different substrate materials
Adapt setup for smaller sample sizes (20x30 mm)
outlook

## Slide 14: Backup Slides

## Slide 15: Trapping efficiency
Cool down samples different external fields with constant temperature gradient
Plot trapped flux versus external field
Slope of linear fit is trapping efficiency
No dependency on temperature gradient
  This is in contrast with bulk samples where the trapping efficiency decreases with increasing temperature gradient
Results
All coated samples show trapping efficiencies of 85-92 %
Nb3Sn/Nb (HZB)

## Slide 16: Nb3Sn on niobium substrate
Zero field cooled
Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown
Flux density 2 orders of magnitude smaller than copper substrate samples
Increase with temperature gradient
Since this sample is coated only via bronze route it is coated from both sides
Remove coating on one side to make it comparable to others
No significant difference between the two
Results
Two orders of magnitude less trapped flux

## Slide 17: Nb3Sn on copper substate
Zero field cooled
Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown
All samples show large flux density magnitudes several times the earth’s magnetic field
Increasing flux density with temperature gradient
Other sensors measures largest field with “Nb3Sn (INFN)”
Results
Flux densities 10 earths magnetic field generated

## Slide 18: Cooldown dynamics and Tc
Plot AMR raw data versus time
All 5 sensor rows are discernable
Uniform Tc
K
Results
Nb3Sn/Nb (HZB)
To be published

## Slide 19: Cooldown dynamics and Tc
Plot AMR raw data versus time
Sensor rows are not discernable
Non-uniform Tc
K
Results
Nb3Sn/Cu (HZB)
Name | TF Orientation | Uniform Tc | Tc [K]
Nb3Sn BL (INFN) | inhomogeneous | no | 
Nb3Sn (INFN) | inhomogeneous | no | 
Nb3Sn/Cu (HZB) | inhomogeneous | no | 
Nb3Sn/Nb (HZB) | homogeneous | yes | 
Nb/Cu (10µm) | homogeneous | yes | 
Nb/Cu (4µm) | homogeneous | yes | 
Name | TF Orientation | Uniform Tc | Tc [K]
Nb3Sn BL (INFN) | inhomogeneous | no | 
Nb3Sn (INFN) | inhomogeneous | no | 
Nb3Sn/Cu (HZB) | inhomogeneous | no | 
Nb3Sn/Nb (HZB) | homogeneous | yes | 
Nb/Cu (10µm) | homogeneous | yes | 
Nb/Cu (4µm) | homogeneous | yes | 

## Slide 20: CRAFT vs. mVTS
Results