## Slide 1: EPITA
WP4 on Superconducting TF for SRF cavities
WP coordinator: Oleg B. Malyshev, UKRI/STFC/DL
WP coordinator deputy: Thomas Proslier, CEA

## Slide 2: WP: Superconducting Thin Films coated RF cavities
Objective: Deliver a new class of coated superconducting radiofrequency (SRF) cavities
State-of-the-art: SRF accelerating cavities made from bulk niobium and operated at 2 K are the state-of-the-art system for particle acceleration in modern colliders. Their performance is limited by physical properties of material and by impurities, and their cost is impacted by the scarcity of niobium and the need for complex, low-temperature cryogenic systems. Initial development of innovative superconducting coatings on copper took place in ARIES and I.FAST projects, where assessment of different materials and coating techniques was completed.
Ambition: pioneer a disruptive SRF manufacturing technology through four key elements: advanced manufacturing, material innovation using Nb3Sn coatings on Cu substrates, system integration with a compact conduction-cooled cryomodule, and industrialisation via technology transfer to partners.
Aims: develop and validate a new class of thin-film coated SRF cavities, operated in a horizontal cryostat & cooled by compact cryocoolers:
  design and fabricate high-Q copper cavities coated with Nb3Sn, optimised for 4.2 K.
  demonstrate stable, efficient conduction cooling using commercial cryocoolers to eliminate liquid helium infrastructure.
  integrate and test these cavities in a horizontal cryomodule for industrial, medical, and scientific applications.
  assist Zanon in equipping its manufacturing lines with a new industrial cavity coating facility.

## Slide 3: WP: Superconducting Thin Films coated RF cavities
Success metrics:
  testing of a cryomodule for a 1.3 GHz cavity at 4.2 K.
  copper cavity production and coating with Nb3Sn.
  RF testing of cavity in cryostat to validate readiness for beam operation (Q>1010, field up to 23 MV/m); d) identification of new alloys with high thermal conductivity (>150 W/(m ⋅ K) at 4.2 K) and high temperature stability (>650 °C) for depositing superconducting thin films with critical temperature Tc ≥15 K.
TRL progress: from 5 to 6 (SRF cavity technology validated for operation with a beam).
Specific Objectives
  Develop and validate a novel class of thin film (TF) coated SRF cavities conduction-cooled via compact cryocoolers. This translates into:
  design and fabricate high-Q Nb3Sn-coated copper TF-SRF 1.3 GHz cavities for operation at 4.2 K.
  demonstrate stable, efficient conduction cooling using commercially available cryocoolers.
  Integrate and test TF-SRF cavities in a horizontal cryomodule suitable for industrial, medical, and scientific accelerator applications.

## Slide 4: WP4: List of tasks
Task 4.1: Strategy and Industrialisation
Partners: UKRI, CEA, INFN, HZB, RI
Task leader: Reza Valizadeh, STFC
Milestone: Thin Film SRF workshop and lead roadmap discussion. M10.
Deliverable: Industrialisation. Report on industrialisation perspective and recommendations. M42.
Task 4.2: Horizontal RF test of conduction cooled 1.3 GHz cavity with off-axis couplers
Partners: HZB + RI, CEA, INFN, UKRI
Task leader: Oliver Kugeler, HZB. Final TRL-6
Milestone: Existing cryostat refurbished and commissioned for use with Nb3Sn cavities, coupler adaptation. M28.
Deliverable: Test stand. Horizontal RF test of conduction cooled cavity at CEA and with off-axis couplers at HZB. M46.
Task 4.3: 1.3 GHz cavity production and coating
Partners: INFN + Piccoli, CEA, UKRI, RI, Zanon, Lanc U
Task leader: Cristian Pira, INFN. Final TRL-6
Milestone: Report on different types of 1.3 GHz cavity manufacturing and surface preparation. M22.
Deliverable: Cavities. Report on 1.3 GHz cavity with coupler ports coated. M40.
Task 4.4: Superconducting Thin Film Development
Partners: CEA + CNRS + Paris-Saclay U + Polytechnique, IEE, INFN, DESY/HUH, HZB, HZDR, RTU, Siegen U, UKRI + Lancaster U
Task leader: Thomas Proslier, CEA. TRL-4
Milestone: Test for development of small scale Nb3Sn targets. M36.
Delivery: Targets. Production and tests of Nb3Sn cylindrical sputtering targets. M36.

## Slide 5: Task 4.1: Strategy and Industrialisation
Task 4.1: Strategy and Industrialisation
Partners: UKRI, CEA, INFN, HZB, RI
Task leader: Reza Valizadeh, STFC
Milestone: Thin Film SRF workshop and lead roadmap discussion. M10.
Deliverable: Industrialisation. Report on industrialisation perspective and recommendations. M42.
Develop a long-term strategy to transition TF-SRF technology from R&D to industrial level, targeting higher TRLs and future use in accelerator applications across science, health, and industry.
Industrial partners will help identify current challenges and explore solutions for the industrialisation of TF-SRF cavity production.
The Task will organise a TF-SRF workshop, participate in relevant conferences sessions, and support meetings to coordinate academia and industry efforts toward European TF-SRF industrialisation strategy.

## Slide 6: Task 4.2: Horizontal Cavity Integration and RF Tests
Task 4.2: Horizontal RF test of conduction cooled 1.3 GHz cavity with off-axis couplers
Partners: HZB + RI, CEA, INFN, UKRI
Task leader: Oliver Kugeler, HZB. Final TRL-6
Milestone: Existing cryostat refurbished and commissioned for use with Nb3Sn cavities, coupler adaptation. M28.
Deliverable: Test stand. Horizontal RF test of conduction cooled cavity at CEA and with off-axis couplers at HZB. M46.
Integrate the Nb3Sn-coated SRF cavity from Task 4.3 into a cryostat and test it under beam-relevant conditions, addressing two key challenges:
  a) replacing liquid helium cooling with conduction cooling for a simplified setup, and
  b) using off axis couplers while maintaining adaptable input coupling. The bare cavity will be tested at HZB’s HoBiCaT facility, where thermal contact methods will be optimised and the helium line will be replaced by a cryocooler.
HZB will design a beam-compatible TESLA-type cavity with added ports for a power coupler and pickup antenna, with RI supporting high-power coupler integration.
In parallel, CEA will design a cryostat using a closed-loop liquid helium system for vertical and horizontal testing of 1.3 GHz cavities at 4.2 K. This system will feature a 3D-printed Cu-based double-wall structure embedded in the Nb3Sn coated cavities. The two approaches will assess the impact of microphonics from cryocoolers and helium boiling, respectively, on cavity RF performance and develop mitigation strategies.

## Slide 7: Task 4.3: 1.3 GHz Cavity Production and Coating
Task 4.3: 1.3 GHz cavity production and coating
Partners: INFN + Piccoli, CEA, UKRI, RI, Zanon, Lanc U
Task leader: Cristian Pira, INFN. Final TRL-6
Milestone: Report on different types of 1.3 GHz cavity manufacturing and surface preparation. M22.
Deliverable: Cavities. Report on 1.3 GHz cavity with coupler ports coated. M40.
Deliver single cell 1.3 GHz copper cavities, with integrated power coupler and pick up ports and coated with Nb3Sn superconducting thin films, for use in Task 4.2.
Cavities will be produced through seamless fabrication at INFN and equator Electron Beam welding at Zanon and RI.
Additive Manufacturing will also be explored by CEA and INFN. Cavity polishing will be performed at INFN and, Zanon.
CEA and UKRI will set up surface preparation facilities leveraging partner experience.
Superconducting TF coating will be carried out at CEA, INFN, and UKRI using different setups to reduce failure risk.
Zanon will build a new industrial coating facility based on experience gained in I.FAST, with systems optimised to also coat the power coupler and pickup ports doors.
In parallel, TF deposition on longitudinally split cavity geometry will be explored by UKRI, with the support of Lancaster University.
The baseline coating protocol will follow I.FAST developments, while CEA will assess the possibility of including interlayers via Atomic Layer Deposition (ALD) based on the results of IEE.

## Slide 8: Task 4.4: Superconducting Thin Film Development
Task 4.4: Superconducting Thin Film Development
Partners:
CEA + CNRS + Paris-Saclay U + Polytechnique, IEE, INFN, DESY/HUH, HZB, HZDR, RTU, Siegen U, UKRI+Lancaster U
Task leader: Thomas Proslier, CEA. TRL-4
Milestone: Test for development of small scale Nb3Sn targets. M36.
Delivery: Targets. Production and tests of Nb3Sn cylindrical sputtering targets. M36.
Development of high-purity and high-density Nb3Sn targets via Spark Plasma Sintering (SPS) at CEA, cold powder spray coating at UKRI, and infusion at INFN.
Novel alloys with high-temperature stability and thermal conductivity will also be developed for depositing superconductors with critical temperatures higher than Nb.
R&D activities on superconducting TF deposition and post thermal treatments will be conducted along with characterisation of targets, high-temperature alloys, and planar samples at CEA, IEE, INFN, UKRI with the support of HZDR.
The RF tests of planar samples will be performed on chock (UKRI) and QPR cavities (HZB), while RF tests on 6 GHz elliptical and 6 GHz split cavities will be conducted at INFN, UKRI, and CEA.
Outcomes will feed into Task 4.3 and support the long-term European TF-SRF roadmap outlined in Task 4.1.

## Slide 9: Partners’ expertise, complementary roles, infrastructure
UKRI: TF coating and characterisation in dedicated lab, testing facilities for SC coatings and vertical cavity testing.
  Lanc U.: RF cavity design and testing;
HZB: cavity design, HoBiCaT cavity test stand.
DESY/HUH: QPR
CEA: cryostat design, vertical and horizontal cavity testing, deposition techniques in dedicated lab and film characterisation.
  CNRS + Paris-Saclay U + Polytechnique: TF characterisation
INFN: design and fabrication of copper cavities, TF coating and characterisation in dedicated lab, DC and RF testing facilities for SC.
  Piccoli: fabrication of copper cavities
Zanon, RI: EU leaders in SC cavity preparation, production and welding facilities.
IEE: testing facilities for SC coatings
HZDR: testing facilities for SC coatings.
RTU: Laser treatment
Siegen U: thin film coating and characterisation
Observers :
  Academic: CERN, JLab
  Industrial: Euclid Techlab, NovAccel Co. Ltd, Shakespeare Ltd.