## Slide 1
Superconducting Fluctuations: From Ginzburg–Landau Theory to Fluctuation Spectroscopy I
Andrey Varlamov
CNR-SPIN, Rome, Italy
Academy of Science and Letters, Milan, Italy
The Two-dimensional and Disordered Superconductors
Universitè Paris-Saclay, Institut PASCAL
July 7, 2026

## Slide 2
From Rayleigh-Jeans Waves to Abrikosov Vortex Clusters: qualitative picture
Kamerlingh Onnes vs Gottfried Leibniz
Superconducting fluctuations lifetime via Heisenberg’s uncertainty principle
How many fluctuations Cooper pairs are above Tc?
How their presence changes BCS critical temperature?
What is the physics of the main fluctuation effects?
From thermodynamic to quantum fluctuations
2. A brief excursus on the Ginzburg-Landau Phenomenological Theory of Superconductivity
Landau theory of 2nd order phase transitions
Ginzburg–Landau functional for superconductor
Derivation of GL equations
Main achievements of GL theory
Superconductors of the I and II types
Lecture I. Qualitative picture and Ginzburg Landau description of Superconductivity

## Slide 3: I. Superconducting Fluctuations: Qualitative Picture

## Slide 4: Natura non facit saltus Gottfried Leibniz, New Essays, 1704
Kamerlingh Onnes vs Gottfried Leibniz
… at 4.05 𝐾, the resistance of the sample still remained outside the accuracy of the measurements, with nothing yet to indicate that it is about to rise. Only at 4.12 𝐾 the galvanometer readings indicated the appearance of a non-zero resistance. At the subsequent temperature interval of 0.1 𝐾 the resistance increased almost 400.
From the laboratory Journal of Kamerlingh Onnes, 26 October 1911

## Slide 5: Supeconducting transition in thin TiN films (T. Baturina et al)
1911 100 years passed…. 2011

## Slide 6: Superconducting fluctuations near Tc: qualitative picture

## Slide 7: Concentration of Cooper pairs above Tc

## Slide 8
Superfluid density and averaged square of the order parameter in 2D
Berezinsky

## Slide 9: Superconducting fluctuations near Tc: paraconductivity
v
t

## Slide 10: Superconducting fluctuations near Tc: other physical quantities
Diamagnetic susceptibility:
Free energy
Fluctuation Cooper pairs concentration
Heat capacity
Chemical potential of FCP
Nernst coefficient
A more consistent consideration performed in the framework of the Ginzburg-Landau fluctuation theory confirms this estimate.

## Slide 11
Superconducting fluctuations near Tc: anomalous Maki-Thompson term

## Slide 12: Superconducting fluctuations near Tc: One-electron conductivity renormalization

## Slide 13: Thermal fluctuations near Tc0: summary
Vicinity of Tc | Vicinity of Hc2(0)
?

## Slide 14: Mean
Superconducting fluctuations near Hc2: Quantum phase transition
Mean field picture
Melting of the vortex lattice due to
thermal fluctuations
What happens here?
Thermal fluctuations

## Slide 15: Quantum fluctuations near Hc2(0): qualitative picture
Vicinity of Tc | Vicinity of Hc2(0)

## Slide 16
Above Hc2(0): Snapshot visible
for times shorter than τQF
Below Hc2(0)
Crossing the Hc2(T) line

## Slide 17
Schematic phase diagram of type-II superconductors,
showing the domains of qualitatively different physical behavior

## Slide 18
II. A Brief Excursus on the Ginzburg–Landau Phenomenological Theory of Superconductivity

## Slide 19
Landau theory of 2nd order phase transitions

## Slide 20
has the dimension of the density of states. Candidate: electron density of states ν
The Ginzburg–Landau functional in the absence of a magnetic field
The uncertainty in the normalization of the wave
function: 2m - ?
Order parameter? Hint: wave function of Bose condensate (complex!)

## Slide 21
In the Ginzburg–Landau phenomenological theory, m is taken as the mass of the electron. The corresponding
A more convenient normalization relates the order parameter Δ(r) to the width of the gap in the superconductor’s spectrum. In this case, microscopic theory gives

## Slide 22
The Ginzburg–Landau functional in magnetic field
1. Gauge invariance of the theory
2. Density of energy related to magnetic field
}

## Slide 23
Let us calculate the variational derivative over
Ginzburg–Landau equations
Let's use the relation
Integrating it one finds
Applying the Gauss theorem and assuming
one obtain
:

## Slide 24
This expression is equal to zero for any value
if each of the parentheses is equal to zero on its own:
This is the first GL equation
Corresponding boundary condition for it is

## Slide 25
To obtain the second equation, we calculate the variational derivative of the GL functional with respect to A(r):
In the homogeneous case,
this GL equation reduces to
with
-

## Slide 26
Applying the curl operation to both parts of of the 2nd GL equation
Recalling that
One can identify
we obtain:
and remembering that
First London brothers' theory equation
Second London brothers' theory equation
with

## Slide 27
Introduced a continuous order parameter enabling a spatial description of the superconducting-to-normal transition.
Justified the existence of a finite-thickness interface between superconducting (S) and normal (N) regions, characterized by the coherence length and penetration depth
Provided the first microscopic-independent calculation of the S–N interface (surface) energy:
Ginzburg–Landau Theory: Intermediate State and Surface Energy
Showed that the sign of the surface energy is governed by the Ginzburg–Landau parameter
  → stable macroscopic normal/superconducting domains (intermediate state, Type-I superconductors).
  → interfaces are energetically favored, leading to flux penetration as vortices (mixed state, Type-II superconductors).
The Ginzburg–Landau theory provided the thermodynamic explanation of the intermediate state through the competition between magnetic energy and positive interface energy.
Achievements

## Slide 28: Ginzburg–Landau Theory: Critical Current and Critical Field in Confined Superconductors
Predicted the existence of a depairing (critical) current, at which the superconducting order parameter is suppressed and superconductivity is destroyed. Established the dependence of its density on the coherence length , penetration depth , and temperature:
Demonstrated that geometrical confinement strongly modifies superconducting properties, allowing quantitative predictions for wires and thin films.
Predicted that the parallel critical magnetic field of a superconducting film
increases as the film thickness decreases: showing that very thin films can sustain magnetic fields far exceeding the bulk thermodynamic critical field.
Established a unified framework linking sample dimensions, superconducting coherence, and electromagnetic screening, providing the theoretical basis for the design of superconducting wires, thin films, and micro/nano-scale superconducting devices.
The Ginzburg–Landau theory quantitatively predicted both the maximum dissipation-free current in superconducting wires and the enhancement of the critical magnetic field in thin films, revealing how superconducting performance
is fundamentally governed by geometry and characteristic length scales.

## Slide 29: Ginzburg–Landau Theory: Prediction of Type-II Superconductivity
The existence of mixed (vortex) state was predicted, in which magnetic flux penetrates the superconductor as quantized flux lines while superconductivity persists between them.
Abrikosov established the existence of two critical magnetic fields:
  : onset of magnetic flux penetration,
  : complete destruction of superconductivity.
He predicted that the upper critical field scales as linking the maximum sustainable magnetic field to the coherence length.
Alexei Abrikosov, basing on the Ginzburg–Landau theory, provided the theoretical prediction of Type-II superconductivity -- existence of the mixed (Abrikosov vortex) state and establishing the fundamental role of the parameter . This framework laid the development of high-field superconducting materials.
Structure of an isolated vortex. The top graph shows the distribution of the magnetic field and order parameter amplitude in a cross-section through the vortex. The vector-lines circling the vortex represent the supercurrent screening the magnetic flux of the vortex. The bottom plane-cut shows the distribution of the order parameter. (b) Sketch of the vortex lattice in type II superconductor .

## Slide 30
Let us estimate the values of the two critical fields found by Abrikosov. For simplicity let us assume that , i.e. the London penetration depth is much larger than the coherence length of the Ginzbutg-Landau function . It is easy to do based on dimensional analysis. Indeed, to characterize the critical magnetic fields we have at our disposal the value of magnetic flux and two lengths : and . In our assumption Since the dimensionality of magnetic flux is the product of dimensionality of magnetic field and that one of the square of length: , one can write down two fields:
and
Two critical fields

## Slide 31
Facsimile of Abrikosov’s presentation slide

## Slide 32
The result of experimental observation of vortex lattice at the surface by means of magnetic decoration. Reprinted from U. Essmann and H. Träuble, “The direct observation of individual flux lines in type II superconductors”, Physics Letters A, 24, 526, (1967).
The direct observation of individual flux lines in type II superconductors

## Slide 33: High Jc important for many applications
Power Cables, Electric Grid
Long Island
Wind turbines
Medical MRI
In-Field Applications
Motors & Generators
Transportation MagLev
Fusion Energy, HEP
Magnetic
Energy Storage

## Slide 34: Model: The Ginzburg Landau equation
With total current: J=Js+Jn:
Time dependent GL equations:
Field perpendicular to current
In dimensionless units:
Solver implemented on GPUs, using iterative Jacobi scheme
For more details: J Comp. Phys. 294, 639 (2015)

## Slide 35: Reconstruction of defects
Reconstructed landscape
Extracted positions and radii of (almost) spherical Dy defects in YBa2Cu3O7–δ were used in time-dependent Ginzburg-Landau simulations
2D STEM image at different angles
3D tomogram
Simulated vortex dynamics
Simulation of a Real Pinning Landscape
Sadovskyy et al., Phys. Rev. Applied B, 014011 (2016).

## Slide 36: Simulation of a real sample
3D STEM tomogram superimposed with reconstructed particles
534 × 524 × 129 nm3
Sim Visualization: vortex lines+ inclusions & order parameter amp.
538 × 538 × 134 nm3
A. Glatz et al, Phys. C 469, 2052 (2009)
A. Glatz et al Phys. Rev. Applied 5, 014011 (2016)

## Slide 38: Jc(B): Experiment vs. Simulation
Tomogram resolution ~2.5ξ: added background inclusions = particles of diameter 2ξ occupying 2% of the volume fraction
Direct simulation: Dy0.5
Simulation with background disorder: Dy0.75

## Slide 39: Jc(q): Experiment vs. Simulation
Experiment
Simulation