## Slide 1
Superconducting Fluctuations: From Ginzburg–Landau Theory to Fluctuation Spectroscopy II
Andrey Varlamov
CNR-SPIN, Rome, Italy
Academy of Science and Letters, Milan, Italy
The Two-dimensional and Disordered Superconductors
Universitè Paris-Saclay, Institut PASCAL
July 9, 2026

## Slide 2: Lecture II. Superconducting fluctuations in Ginzburg Landau formalism and beyond
Accounting for superconducting fluctuations in the framework of the GL formalism
0D case
3D case (evaluation)
Ginzburg-Levanyuk criterion
Time-dependent GL equation and its applications for description of the effect of fluctuations on the transport properties
2. The ideas of microscopic description of fluctuation phenomena
3. Fluctuation Spectroscopy: results

## Slide 3: Beyond mean field: accounting for fluctuations
The complete description of its thermodynamic properties can be done through the calculation of the partition function

## Slide 4
The limits of applicability of the Ginzburg–Landau theory.
0-dimensional case: exact solution:
x>>1
One can see that this function is analytic in temperature, therefore fluctuations remove phase transition in the 0D system. The smearing of the heat capacity jump takes place in the region of temperatures in the vicinity of Tc0 where x ∼ 1, i.e.

## Slide 5
The transition remains narrow as long as
E
BCS theory holds as long as the spacing remains small in comparison to
is spacing – average distance between quantum levels in the grain

## Slide 6
Outside the critical region
S. Poran, A. Auerbach, T. Nguyen-Duc, N. Dupuis, A. Frydman & Olivier Bourgeois
Nature Communications 8, 14464 (2017)

## Slide 7
Beyond the immediate vicinity of transition: Qualitative evaluation
ξ(T)
The volume of the specimen may be divided into regions of size ξ(T), which are weakly correlated to each other. Then the whole free energy can be estimated as the free energy of one such 0D specimen
multiplied by their number
This formula gives the correct temperature dependence of the free energy not too close to Tc for the specimens of the even dimensionalities. Example:
3-dimensional case:

## Slide 8
Beyond the immediate vicinity of transition: Perturbation approach
Fourier transform
Partition function

## Slide 9
Fluctuation contribution to the heat capacity:

## Slide 10
The Ginzburg–Levanyuk number

## Slide 11
Broadening of the critical region: dependence of the Ginzburg–Levanyuk number on the magnetic field

## Slide 12
Fluctuation-induced shift of the critical temperature
Ginzburg-Landau penetration length

## Slide 13
Fluctuation-induced shift of the critical temperature

## Slide 14: Fluctuation transport in the Ginzburg–Landau formalism
Time-dependent Ginzburg–Landau equation
The relaxation of the order parameter is described by the equation
Accounting for interaction with thermostat
Gauge invariance requires
Langevin forces

## Slide 15
Neglecting the fourth-order term in the GL functional, this equation can be rewritten
in operator form as
with the TDGL operator and Hamiltonian defined as
In the absence of an electric field one can write the formal solution of this equation as
The correlator of the Langevin forces introduced above must satisfy the fluctuation–dissipation theorem. This requirement is fulfilled if the Langevin forces are correlated by the Gaussian white-noise law

## Slide 16: Paraconductivity

## Slide 17: The quantum mechanical expression for the current
Where is the spectrum of the GL Hamiltonian
After some algebra which we can discuss during Q&A session one can obtain

## Slide 18: The isotropic case

## Slide 19: Diagrammatic description of fluctuation phenomena

## Slide 20
( )=

## Slide 21
Fluctuoscopy: arbitrary temperatures and fields
a) AL
b) MT
c) DOS
d) DcR
1
2
3
5
4
6
9
7
10
8

## Slide 22
Fluctuation propagator in magnetic field and arbitrary temperatures
=

## Slide 23: Fluctuation conductivity at arbitrary temperatures and magnetic fields

## Slide 24: General picture of fluctuation conductivity (A.Glatz,A.Varlamov, V.Vinolur, 2011)

## Slide 25: How is Tc obtained?
Tc is assigned, not determined

## Slide 26: Fluctuoscopy of thin TiN films (II) T. Baturina et al (2011)
Traditional definition of Tc
The determination of Tc as the temperature where R(T) drops to 0.9, 0.5 RN significantly overestimates Tc.
S03: Tc=1.260K
S04: Tc=2.538K

## Slide 27: Electric field control of fluctuations in a two-dimensional superconductor Graham Kimbell, Ulderico Filippozzi, Stefano Gariglio, Marc Gabay, Andreas Glatz, Andrey Varlamov, and Andrea Caviglia (2026)
(a) Superconducting transition at −2 V, comparing the best fit from Aslamazov-Larkin and the full fluctuation conductivity model. (b) Superconducting transition at different gate voltages (colored lines), fit to the full fluctuation conductivity model (black lines).

## Slide 28: Microwave Signature of the Emerging Abrikosov Lattice Above Hc2 (Hang Zhou, Zhanghai Chen, A. A. Varlamov, Andreas Glatz, and Yuriy Yerin, PRL 2026)

## Slide 29: Frequency dependence of conductivity
Normal impure metal (Drude)

## Slide 30: Absorption in low-Tc superconductor.
The characteristic frequency 𝑓𝑐, which is proportional to the strength of the pinning force acting on fluxons and that marks the crossover between the low-frequency, low
dissipation regime and the high-frequency, high dissipation regime. J. I. Gittleman and B. Rosenblum, “Radio-frequency resistance in the mixed state for
subcritical currents”, Phys. Rev. Lett., vol. 16, no. 17, pp. 734-736, 1966.
Superconductor at T=0 (Abrikosov, Gor’kov, Khalatnikov, 1958)

## Slide 31: Quantum fluctuations in a weak electromagnetic field
=
=
)
=
For

## Slide 32: Microwave Signature of the Emerging Abrikosov Lattice Above Hc2

## Slide 33
Giant Nernst effect above the transition line
Hc2(T): vortices or fluctuating Cooper pairs?
Nernst effect in cuprates: the experiments of Ong’s group

## Slide 34
Nernst effect in conventional superconductor

## Slide 35
Qualitative explanation of the Giant Nernst effect due to fluctuating Cooper pairs
(A. V. Kavokin and A. A. Varlamov, 2009)
Nernst effect & chemical potential

## Slide 36: Giant Nernst effect due to fluctuation Cooper pairs M.Serbyn et al (2009): A. Kavokin, A. Varlamov (2009); A. Glatz, A. Varlamov (2018)
=Tc-T

## Slide 38: Comparison of the theory and experiments

## Slide 39: Tunnel Fluctuoscopy: pseudogap opening and low bias anomaly (A.Glatz,A.Varlamov, V.Vinokour, 2011)
Fluctuation renormalization of the DOS (Abrahams et al, 1970)
Tunnel Current Giaver and Mengerle, 1961)
Fluctuation pseudogap (Varlamov, Dorin, 1983)

## Slide 42: Tunneling conductance at H=0, near Tc0 : theory
The non-linear behavior of the second term of the tunnel current is responsible for the fine structure (local maximum) at the center of the gap.
Temperature and voltage dependence of the tunneling conductance due to superconducting fluctuations. The overall behavior of both terms of the tunnel current results in a pronounce pseudo-gap structure of the conductance near the superconducting region.

## Slide 43: Observation of the pseudogap structure in experiments (B. Sacepe et. al., Nature Comm.. 140, 1 (2010))
.
Tunneling conductance STM measurements on 3.6nm (a) 5nm (b) thick TiN films (»¼10nm), Tc=1.27K (a) or 0.98K (b)