## Slide 1
Inhomogeneities in superconductors
Pascal Simon
Laboratorie de Physique des Solides (LPS)
University Paris Saclay & CNRS
TIDES 2026, Institut Pascal

## Slide 2
Anderson’s theorem
P. W. Anderson, J.Phys. Chem. Solids 11, 26 (1959)
In the presence of dirt one can still pair time-reversed members of Kramer’s doublet:
thermodynamics (Tc, gap, sp. ht., …) are not affected by nonmagnetic impurities
In the presence of dirt one can still pair time-reversed members of Kramer’s doublet:
thermodynamics (Tc, gap, …) are not affected by nonmagnetic impurities

## Slide 3
Abrikosov-Gor’kov theory

## Slide 4
Abrikosov-Gor’kov theory (consequences)
Skalski et al, Phys Rev. 136, A1500 (1964)

## Slide 5
Results about non-magnetic impurities

## Slide 6
Magnetic impurity in a superconductor
Yu Lu, Acta Physica Sinica 21, 75 (1965)
see also
H. Shiba, Prog. Theor. Phys. 40, 435 (1968).
A. I., Rusinov, 1969, Zh. Eksp. i Teor. Fiz. 56, 2047, [Sov.
Phys. JETP 29, 1101 (1969)].

## Slide 7
A more direct approach to YSR bound states
From F. Pientka, L. Glazman, F. von Oppen, Phys. Rev. B 88, 155420 (2013)
In this Nambu basis, the Hamiltonian is bloc diagonal in spin space!
Solve the Schoedinger equation in the spin bloc space :
Take
Fourier transform:

## Slide 8
A more direct approach to YSR bound states
F. Pientka, L. Glazman, F. von Oppen, Phys. Rev. B 88, 155420 (2013)

## Slide 9
A more direct approach to YSR bound states
Normalization

## Slide 10
Rusinov’s parametrization (JETP 68’)
Phase shift:
Full wave function:
Spatial dependence governed by:
;

## Slide 11
Rusinov’s parametrization (JETP 68’)
In 3D:
In 2D:
G. Ménard et al., Nature Physics 2015
A. I. Rusinov, Zh. Eksp. Teor. Fiz. Pisma Red. 9, 146 (1968) [JETP Lett. 9, 85 (1969)]
;
;

## Slide 12
Yazdani et al. Science 275, 1767 (1997)
Bound states for magnetic impurities (Mn & Gd) on Nb
No bound states for non magnetic Ag adatoms on Nb
Nb
Mn & Gd atoms
STM tip
The wave function of the
bound states is localized at less
than 10 Å from the impurities
Single magnetic impurities observed by STM

## Slide 13
Shuai-Hua Ji et al. PRL 100, 226801 (2008)
See also N. Hatter et al., Nature Commun. (2015)
Single magnetic impurities observed by STM:
Angular momentum dependence
The number of Shiba peaks depends on the atom nature
Every peak may correspond to a different angular momentum scattering channels for the superconducting electrons.
Extremely local effect of the impurities (a few )

## Slide 14
Band 1
Band 2
2H-NbSe2 as a two-dimensional superconductor
Two-dimensional like bands structure due to the weak Van der Waals interlayer coupling.
Superconducting gap measured at 320 mK
(multigap superconductor)

## Slide 15
The Nb used for the crystal growth contains magnetic impurities :
  175 ppm of Fe
  54 ppm of Cr
  22 ppm of Mn
dI/dV maps at -0.13 mV (320 mK)
G. Ménard et al., Nature Physics 2015
Observation of bound states around magnetic impurities in 2H-NbSe2

## Slide 16
20 nm
Shiba bound states observed over scales of the order of 10nm
Observation of bound states around magnetic impurities in 2H-NbSe2
G. Ménard et al., Nature Physics 2015

## Slide 17
Observation of bound states around magnetic impurities in 2H-NbSe2

## Slide 18
YSR in 2H-NbSe2
YSR in 2H-NbSe2 (F. Massee’s STM in LPS)
U. Thupakula et al., PRL (2022)

## Slide 19
Distance (nm)
Spatial oscillation of Shiba bound states
Electron-hole asymmetry
Oscillations of the local density of states with a phase opposition between positive and negative energy states
Decrease of the Shiba bound states on a size of the order of the coherence length ξ
G. Ménard et al., Nature Physics 2015

## Slide 20
Good agreement with theoretical calculations for Shiba state in a 2D SC
in the asymptotic limit.
The Shiba peaks position relatively to the gap is directly related to the phase shift.
Spatial oscillations and electron-hole asymmetry
G. Ménard et al., Nature Physics 2015

## Slide 21
2nd Case
1st Case
We observe the energy dependence of the phase
Cr or Mn impurity
G. Ménard et al., Nature Physics, 11 1013 (2015)
23
Impurity with bound states at gap edge:
in phase electron-hole oscillations

## Slide 22
Adapted from Franke group : PRL 121, 196803 (2018) and Prog. Surf. Sci. 93, 1-19 (2018)
0
Jc
J
Δ
0
Excitation spectrum in the YSR impurity model
Ground state
Free spin: S=1/2
Excited state
Screened spin: S*=0
Ground state
Screened spin: S=0
Excited state
Free spin: S*=1/2
Quantum parity phase transition

## Slide 23
Exchange coupling (J) modified with tip-sample distance
Franke group: PRL 121, 196803 (2018)
What if there are multiple channels?
Quantum phase transition

## Slide 24
Shape of the YSR wave function ?
M.E. Flatté and J. M. Byers, PRL78, 3761 (1997)
A classical spin in NbSe2
may give rise to a bound state
with a star shaped pattern
M.E. Flatté and D. E. Reynolds, PRB (2000)

## Slide 25
Shape of the YSR wave function ?
Continuous asymptotic model
Direct numerical resolution of the Shiba equation using a
a Bogoliubov-de Gennes tight-binding model extracted from ARPES
Tight binding model
The star shape comes the anisotropy of the Fermi surface
G. Ménard et al., Nature Physics, 11 1013 (2015)

## Slide 26
H.Kim et al.
Nat.Comm. 11, 4573(2020)
La(0001)
β−Bi2Pd
Zaldivar et al. (2020)
U.Thupakula et al.,
Phys. Rev. Lett (2022)
NbSe2
Long-range 2D YSR bound states
G.Menard et al.
Nat.Phys. 11, 1013 (2015)
NbSe2
Quasi-particle focusing of YSR states
Need the real-space form of YSR for any dispersion
(anisotropy, decay&oscillations, symmetry)
Analytical approximation and interpretation
Quantitative match with tight-binding for NbSe2
STM data analysis: an approach

## Slide 27
Quasiparticle focusing in a normal metal
Seeing Fermi surface in real-space
A.Weismann et al. Science 323, 1190(2009)
S.Lounis et al. PRB 83, 035427(2011)
Focusing from
flatter segments
Theory:
Saddle point approximation of normal metal propagator
6nm
Cu(111) surface
Cu[111]
Real-space
Fermi surface
Co impurity
Our work: Generalize to YSR
See also alternative approach by Ortuzar et al., Phys. Rev. B 105, 245403 (2022)

## Slide 28
Deform integration path through a saddle point:
Standard Laplace method along deformed contour:
Generalization to n dimensions (Bleinstein 2016)
with
Complex saddle point

## Slide 29
Complex saddle point
with
Critical points are given by
yielding the saddle point equations:
If critical points must fall
on the Fermi surface
Discard spurious solutions!
t

## Slide 30
Theory: Quasiparticle focusing in superconductors
Perform a complex saddle point approximation

## Slide 31
Quasiparticle focusing in superconductor
Theory: Quasiparticle focusing in superconductors

## Slide 32
In the perturbative limit :
Friedel-like oscillations
Exponential decay
Geometrical prefactor
Saddle pt eq.  Two solutions: , solving
How is the anisotropy encoded?

## Slide 33
In the perturbative limit :
Friedel-like oscillations
Exponential decay
Geometrical prefactor
How is the anisotropy encoded?
Saddle pt eq.  Two solutions: , solving

## Slide 34
In the perturbative limit :
Friedel-like oscillations
Exponential decay
Geometrical prefactor
How is the anisotropy encoded?
Saddle pt eq.  Two solutions: , solving

## Slide 35
In the perturbative limit :
Friedel-like oscillations
Exponential decay
Geometrical prefactor
How is the anisotropy encoded?
Saddle pt eq.  Two solutions: , solving

## Slide 36
Prefactors and decay length are aligned

## Slide 37
Friedel-like oscillations
Exponential decay
Geometrical prefactor
How is the anisotropy encoded?
General implications:
1. Focusing survives in 2D SC
2. Decay length and prefactor are in phase (reasonable FS)
3. Critical point doubling affects oscillations (no SOC)

## Slide 38
Example: Tight-binding toy model
Single Fermi pocket
Fermi surface
LDOS

## Slide 39
Example: Tight-binding toy model
Single Fermi pocket
Fermi surface
Single Fermi pocket

## Slide 40
Analytical model:
Tight-binding fit:
Tight-binding and analytical model
match perfectly!
NbSe2 tight binding (multi-pocket)
D.J. Rahn et al., Phys. Rev. B 85, 224532 (2012)
Spinless three-pocket
Fermi surface
(lowest Nb 4d-band)

## Slide 41
Analytical model:
Tight-binding fit:
Tight-binding and analytical model
match perfectly!
NbSe2 tight binding (multi-pocket)

## Slide 42
Analytical model:
Tight-binding fit:
Tight-binding and analytical model
match perfectly!
NbSe2 tight binding (multi-pocket)

## Slide 43
Analytical model:
Tight-binding fit:
Tight-binding fit and analytical model
match perfectly!
NbSe2: Quantitative test against
tight-binding
See M. Uldemolins, A. Mesaros, PS, PRB 105, 144503 (2022)

## Slide 44
Analyzing STM data on NbSe2: challenge
STM
Matches estimate from Hc2 and vortex core
Nader and Monceau. SpringerPlus 3:16 (2014)
H. F. Hess, R. B. Robinson, and J. V. Waszczak, PRL 64, 2711 (1990)
Tight-binding models
Small gap (1meV) and ARPES fit bands
G.C. Menard et al., Nat. Phys. 11, 1013 (2015)
L.M. Rütten et al., arXiv:2404.16513 (2024)
First principles
D. Sticlet and C. Morari, Phys. Rev. B 100, 075420 (2019)
Abandon the radial fit of and consider the prefactor only

## Slide 45
Analytical model:
Tight-binding fit:
Tight-binding and analytical model
match perfectly!
Analyzing STM data: angular dependence

## Slide 46
Analytical model:
Tight-binding fit:
Tight-binding and analytical model
match perfectly!
Angular dependence results
M. Uldemolins, F. Massee, T. Cren, A. Mesaros, PS, arXiv:2406.14323

## Slide 47
Analytical model:
Tight-binding fit:
Tight-binding and analytical model
match perfectly!
Angular dependence results
M. Uldemolins, F. Massee, T. Cren, A. Mesaros, PS, arXiv:2406.14323

## Slide 48
Prefactor in momentum space
M. Uldemolins, F. Massee, T. Cren, A. Mesaros, PS, arXiv:2406.14323
STM data

## Slide 49
Limiting approximations
of the YSR solution

## Slide 50
Self-consistent SC gap calculation
Due to impurities, the SC gap becomes inhomogeneous
where
Expectation value depends
on the impurity spin
Self-consistent calculation is thus required
For
One can obtain an analytical expression:
In the a << 1 limit,
Quadratic suppression of the gap
Meng, Klinovaja, Hoffman, PS, Loss, PRB (2015)

## Slide 51
SC gap BELOW the impurity
Self-consistent SC gap calculation
Energy of the Shiba state
Meng, Klinovaja, Hoffman, PS, Loss, PRB (2015)
Pi-shift of the SC gap
Self-consistent SC gap calculation

## Slide 52
Sub-gap Shiba BS to Supra-gap Andreev BS
Meng, Klinovaja,Hoffman, PS, Loss, PRB (2015)
Sub-gap Shiba state turns into a
supra-gap state

## Slide 53
Spectroscopic signature ?
Meng, Klinovaja,Hoffman, PS, Loss, PRB (2015)

## Slide 54
Beyond the
YSR model

## Slide 55
Competition between Kondo-screened and free spin ground state
Local exchange interaction:
In a metal, this interaction gives rise to the Kondo effect with a formation of a
Kondo singlet at T << (the Kondo temperature)
In a superconductor, competition between the screening with pairing
>> D
The magnetic impurity is screened (singlet) and no in-gap bound state
<< D
Kondo effet cannot develop and the GS is a doublet  Back to YSR physics
When
Competition between these two GS
T. Matsuura, Progress of theoretical physics 57, 1823 (1977)

## Slide 56
Relation between YSR and Kondo energy scales
for MnPc molecules
K. J. Franke, G. Schulze, and J. I. Pascual, Science 332, 940 (2011)

## Slide 57
Complexity
Classical spin
Quantum spin
Anderson impurity
Large S limit or large longitudinal anisotropy D
SW transformation in the local-moment regime U≥πΓ
Spin fluctuations
Charge and spin fluctuations
Explicit impurity-substrate coupling
Science 332, 6032 (2011)
Nature Commun. 6, 8988 (2015)
Comm. Phys. 3, 1-9 (2020)
Nature Commun. 12, 298 (2021)
Impurity models

## Slide 58
Complexity
Quantum spin
Anderson impurity
Large S limit or large longitudinal anisotropy D
SW transformation in the local-moment regime U≥πΓ
Spin fluctuations
Charge and spin fluctuations
Explicit impurity-substrate coupling
Science 332, 6032 (2011)
Nature Commun. 6, 8988 (2015)
Comm. Phys. 3, 1-9 (2020)
Nature Commun. 12, 298 (2021)
Classical spin
Captures most observations
Widely used to describe YSR states
Multiple YSR states are simply added up
Impurity models
Impurity models

## Slide 59
Complexity
Classical spin
Captures most observations
Widely used to describe YSR states
Multiple YSR states are simply added up
Question: are there experiments for which the classical model does not work ?
Impurity models
Impurity models

## Slide 60
FeTe0.55Se0.45: an exotic superconductor in vogue

## Slide 62
Experimental observations
Assumption: Tip acts as a local gate electrode
T=0.3 K

## Slide 63
Experimental observations
Two key features:
1) Concurrent switch of in-gap states from
hole-like to electron-like
Independent classical YSR
channels
1

## Slide 64
Experimental observations
Two key features:
1) Concurrent switch of in-gap states from
hole-like to electron-like
Independent classical YSR
channels
2
2) Appearance of negative differential conductance (NDC)
Multiple impurity states and Coulomb interaction

## Slide 65
Previous related experiment
See Rubio-Verdiu et al., Phys Rev. Lett. 2021
Interpreted as two YSR channels, caused by two frontier molecular orbitals strongly coupled by Hund coupling.
Magnetic iron-porphyrin on Pb(111)

## Slide 66
Orbital a
Energy levels
Orbital b
Multi-channel
Anderson impurity model

## Slide 67
Orbital a
Energy levels
Orbital b
‘crystal field’ splitting
varies linearly with tip-sample distance
Multi-channel
Anderson impurity model

## Slide 68
Orbital a
Energy levels
Orbital b
‘crystal field’ splitting
varies linearly with tip-sample distance
Hund’s coupling
Multi-channel
Anderson impurity model

## Slide 69
‘crystal field’ splitting
varies linearly with tip-sample distance
Orbital a
Energy levels
Orbital b
Multi-channel Anderson impurity model:
many-body spectrum

## Slide 70
Multi-channel Anderson impurity model:
many-body spectrum
M. Uldemolins et al., Nature Comm 15, 8526 (2024)

## Slide 71
Multi-channel quantum phase transition: large change in occupation
Orbital energy cost compensated by gain of Hund’s energy
Multi-channel
Quantum phase transition

## Slide 72
Calculated LDOS captures STM experiment
Multi-channel
Quantum phase transition
M. Uldemolins et al., Nature Comm 15, 8526 (2024)

## Slide 73
Discontinuous slope at E = 0
Slope changes upon crossing E=0

## Slide 74
Discontinuous slope at E = 0
Slope changes upon crossing E=0
M. Uldemolins et al., Nature Comm 15, 8526 (2024)

## Slide 75
JH = 0 does not match the experiment
Comparison to JH = 0:
orbitals decoupled, similar to independent YSR or Kondo channels
Switching off the Hund coupling
M. Uldemolins et al., Nature Comm 15, 8526 (2024)

## Slide 76
Multi-channel quantum phase transition (MCQPT)
Independent YSR channels not always suitable
High spin impurities (Hund’s coupling)
Large change in ground state occupation at MCQPT
Discontinuity of both the slope and intensities at the transition

## Slide 77
Motivation 1: Local defects as probing tools

## Slide 78
S. Nadj-Perge et al., Science 346, 6209 (2014)
Motivation 2: Engineering exotic states
Kim et al. Sci. Adv., 2 eaar5251 (2018)

## Slide 79
1D effective topological superconductors
using RKKY systems

## Slide 80
Where to look for Majorana excitations ?

## Slide 81
Certain Hamiltonians can support solutions with isolated localized Majorana fermions
They also encode one complex fermion but in a way robust
to any local perturbation
Ideal for quantum bit
Majorana fermions: in short:

## Slide 82
Band structure of a quantum wire

## Slide 83
Equivalent system: Rashba nanowire in B-field :
Turn on the B-field
m
m
Reduce
m
Effective Pairing:
Effective Pairing:
TRIPLET
Sau et al., PRL 104, (2010).
Oreg et al., PRL 105, (2010).
Notes: note: there is a subtlety for CNT: there are 4 helical modes from K and K’ each two. Need to assume that there is no valley
scattering. Flensberg et al. claim that there is substantial valley scattering…If it is a problem, go into valley tuned regime with B field, which suprresses one valley.
Magnetic field:: s-wave

## Slide 84
Majorana fermions in 1D : Quantum wires
Spin-orbit interaction :
Magnetic field :
s-wave superconductivity :
1-Dimensional Semiconducting quantum-wires
Oreg et al., PRL 105, (2010).
Sau et al., PRL 104, (2010).
Topological phase
Majorana:
Sato et al., PRB (2009)

## Slide 85: Can we find other equivalent realization ?
B. Braunecker, G. Japaridze, J. Klinovaja, D. Loss, PRB 82, 045127 (2010)
Change of frame: Gauge transform
Equivalent to a spiral magnetic field

## Slide 86: The spin selective Peirls transition
external periodic potential: spiral magnetic field B(r)
2Δ
backscattering on B(r): gap Δ for one-half
of the conducting modes with opposite spin
by forming a helical spin/charge density wave
  one-half of the system becomes insulating
  one-half remains conducting and forms a spin-filter
B. Braunecker, G. Japaridze, J. Klinovaja, D. Loss, PRB 82, 045127 (2010)

## Slide 87: Where to find a magnetic spiral field ?
B. Braunecker, PS, D. Loss, PRL 2009, PRB 2009
A first option: quantum wires with nuclear spins
Below some critical temperature T*, electrons and nuclear spins
can be tightly bound into an new ordered phase in 1D
Basic
Hamiltonian

## Slide 88: How does it work ?
B. Braunecker, PS, D. Loss, PRL 2009, PRB 2009
- Integrate out electrons (separation of time-scales)
static electron spin susceptibility
RKKY interaction long ranged
Interaction Jq
minimum at 2kF

## Slide 89: Self-consistent mean field approach
effective electron Hamiltonian
effective nuclear spin Hamiltonian
mutual
dependence
self-consistency
novel physics

## Slide 90: Effect of nuclear helical field
B. Braunecker, PS, D. Loss, PRL 2009, PRB 2009
Helical order of nuclear spins :
Nuclear magnetization
Nuclear helimagnet
Nuclear order generates a spiral Overhauser field:
This Overhauser field drives the spin-Peierls instability
and gaps half of electronic degrees of freedom

## Slide 91: Combined electron / nuclear spin order
pinned electron density wave
(electron spin helix)
nuclear helimagnet
Below T* the ordered phases depend on each other:
- independent of system size for realistic samples
- huge renormalization due to electron-electron interactions
- experimentally (challenging but) accessible temperatures
Phase of tightly bound electron & nuclear spin degrees of freedom
B. Braunecker, PS, D. Loss, PRL 2009, PRB 2009

## Slide 92: Experimental consequences
1. Reduction of conductance
Through feedback: Pinning of channels
Blocking of ½ of the conducting channels
Universal reduction of conductance by factor 2
Example: Luttinger liquid adiabatically connected to metallic leads
Conductance:
Maslov & Stone, Ponomarenko,
Safi & Schulz (all in PRB 1995)
number of conducting channels
reduced to n → n / 2
helical phase
lead
lead
Remaining channels are spin-filtered
R ↑
L ↓
B. Braunecker, PS, D. Loss, PRL 2009, PRB 2009

## Slide 93: In proximity of a superconductor
Superconductivity induced by proximity effect is of p-wave type
(projection onto spin-filtered conducting modes)
proximity induced
superconductivity
s-wave superconductor
for nanotubes cf. Le Hur, Vishveshvara, Bena
PRB (2008)

## Slide 94: Expect Majorana edge states ?
Superconductivity induced by proximity effect is of p-wave type
(projection onto spin-filtered conducting modes)
s-wave superconductor
S Gangadharaih, B Braunecker, PS, Loss, PRL 2011
Do we expect Majorana zero modes ?

## Slide 95: How does SC modify the whole locking scenario ?
Same as before but now Hel contains the
proximity induced SC gap
Mean field decoupling
as before
How is the susceptibility/RKKY modified in a 1D SC?
minimum at 2kF
Therefore helical magnetic structure survives
Majorana zero modes expected !
Braunecker, PS, PRL (2013)
Klinovaja et al., PRL (2013)
Vazifeh, Franz, PRL (2013)

## Slide 96: Minimal ingredients and robustness
Recipe ingredients: - Magnetic moments interacting via RKKY interactions
- 1D-like electronic band
- s-wave superconductor
One can include also take electron-electron interactions into account:
This enhances T* but reduces the proximity induced gap (compromise)
This whole locking scenario is also robust versus point-like
non-magnetic disorder !
B. Braunecker, PS, PRL (2013)

## Slide 97: A natural platform: magnetic adatoms on a SC substrate
Recipe ingredients: - Magnetic moments interacting via RKKY interactions
- 1D-like electronic band
- s-wave superconductor
S. Nadj-Perge, I. Drozdov, A. Bernevig, A. Yazdani PRB (2013)
See also T.-P. Choy, J. M. Edge, A. R. Akhmerov, C. W. J. Beenakker,
Phys. Rev. B (2011)
Proposal: magnetic atoms with some
pre-existing spin texture on a SC surface

## Slide 98: How about the 1D band ?
Two limiting cases:
a
1) The dense limit :
The adatoms wave functions overlap and hybridize and form a 1D electronic band on top of the SC substrate
All the conditions are met for our model and we expect our locking scenario to apply!

## Slide 99: How about the 1D band ?
Yu Lu (1965), Shiba (1968), Rusinov (1968)
Shiba in-gap bound state:
2) The dilute limit :
First solve the single spin case

## Slide 100: How about the 1D band ?
Several diluted classical spins impurity band in the SC gap : Shiba band
Shiba (1968)
For a chain of dilute magnetic impurities of given orientations, an effective more complicated tight binding Kitaev-like Hamiltonian can be actually derived which supports Majorana fermions under certain conditions
F. Pientka, L. Glazman, F. vonOppen, PRB (2013)
Shiba band
Results obtained from a tight-binding description for a given magnetic texture
I. Reis, D. Marchand, and M. Franz, arXiv:14065222

## Slide 101: Experimental predictions?
Helical magnetic phase is the ground state: self-sustained helical phase
1) Semi-conducting wires with nuclear spins
GaAs wire:
Forget it !

## Slide 102: Experimental predictions?
Helical magnetic phase is the ground state: self-sustained helical phase
1) Semi-conducting wires with nuclear spins
GaAs wire:
Forget it !
InAs wire:
Maybe !

## Slide 103: Experimental predictions?
Helical magnetic phase is the ground state: self-sustained helical phase
1) Semi-conducting wires with nuclear spins
GaAs wire:
Forget it !
InAs wire:
Maybe !
2) Magnetic Co atoms on a Nb surface
provides a constraint on A0:
reasonable !

## Slide 104: Conclusion of this first part
New platform for Majorana fermions: RKKY systems
- Wires with nuclear spins (however only at very low T= 0(10mK)
- Magnetic atoms on a SC surface
Advantage: self-sustained Majorana phase
(no fine-tuning)
B. Braunecker, PS, PRL (2013)