## Slide 1: Classical and Quantum effects on the vortex lattice in superconducting thin films
Pratap Raychaudhuri
Tata Institute of Fundamental Research Mumbai, India.

## Slide 2
Complex conductivity measurements (kHz-GHz)
2-coil technique
Microwave techniques
Poster
Measurement of absolute value of Superfluid Stiffness (penetration depth)
[2605.28759] Absolute measurement of penetration depth of superconducting thin films using microwave stripline resonators

## Slide 3
Imaging the vortex lattice using a Scanning Tunnelling Microscope
G(V) maps
G(V) map at coherence peak bias
H

## Slide 4
A very soft solid
NbSe2
25 kOe, 460 mK
4.14 K, 8 kOe
T
H
Magnetic field Pressure
Areal vortex density :
460 mK, 8 kOe
Caveat:
No Temporal Dynamics  Amorphous glass

## Slide 5
Energy scales of the problem
Thermal Energy
kBT
Intervortex
interactions
Random Pinning
energy
Promotes order
Favors disorder
t ~ 4 – 100 nm
Thin film
Condensation energy reduces by 4-5 orders of magnitude
Long vortices 
Large condensation energy
Bulk Crystal
H
t ~ 0.1 – 2 mm

## Slide 6
Amorphous MoGe thin film
Films grown through pulsed laser deposition using arc-melted target Thickness: 20 nm
Pinning 5 orders of magnitude smaller than Nb films

## Slide 7
Vortex Creep in the Solid, Hexatic fluid and Isotropic liquid
Solid
Hexatic Fluid
Hexatic Fluid
Isotropic Liquid
The Hexatic Fluid
A fluid that maintains orientational order. First predicted by Berezinski, Kosterlitz and Thouless followed by Halperin Nelson and Young in the 1970s.
Only possible when vortex motion is very slow.
Estimated

## Slide 8
Extreme sensitivity of the Hexatic State
Surajit Dutta et al., Phys. Rev. B 100, 214518 (2019)
Solid to liquid transition: Hexatic Marked by Extreme sensitivity
Hexatic fluid to isotropic liquid
Special thanks: Mumbai B Ashmita Vahini
Transmission frequency:: 500 kHz

## Slide 9
Vortex Phase Diagram in 20 nm a-MoGe thin film
the lamps are different, but the Light is the same; it comes from beyond - Rumi

## Slide 10
thin film (thickness 5 nm)
Stronger vortex pinning than a-MoGe
Pinning further increased by reducing thickness
Surajit Dutta, Vivas Bagwe, Gorakhnath Chaurasiya, et al, Journal of Alloys and Compounds 877, 160258 (2021)
400 mK, 10 kOe

## Slide 11
STS measurement in a pinned vortex liquid
Locally Fluctuating Vortex
No Vortex
Vortex hopping between sites
The intensity of the conductance minimum reflects the amount of time a vortex spends at that location.
Surajit Dutta et al.,
Phys. Rev. B 103, 214512 (2021)

## Slide 12
Vortices with different degree of localisation
Deep minima corresponding to strongly localized vortices
Shallow minima corresponding to weakly localized vortices

## Slide 13
How to calculate the motion paths
Delaunay Triangulate
Join any two neighbouring minima for which,
The value of GN > -0.8
and
(ii) The value of GN along the line joining the minima is < -0.4
Step 1
Step 2

## Slide 14
+
+
+ . . . =
Motion paths over long time-scales
Not the complete story

## Slide 15
1
3
7
Sequence of 10 images at 410 mK, 10 kOe
Complete hop
Incomplete hop
Modified landscape
(Pinning + Interactions)

## Slide 16
+
+
+
. . . =
Motion due to incomplete hops
Superimposed image
+
Global Motion Paths
(in an inhomogeneous liquid)

## Slide 17
Magnetic field evolution at 410 mK
No Signature of vortex solid (crystalline or amorphous)!
T = 0.41 K
T = 2 K
T = 1.2 K
T = 2.8 K
T = 2.5 K
Temperature evolution at 10 kOe
a-ReZr 5 nm
Rishabh Duhan et al., Phys. Rev. B 108, L180503 (2023).

## Slide 18
Moderate Pinning
Very Weak Pinning: 20 nm a-MoGe
Strong Pinning: 5 nm a-ReZr
Moderate Pinning: 20 nm a-ReZr
thin film (thickness 20 nm)

## Slide 19
460 mK

## Slide 20
3 kOe: “Inverse melting” in the range 0.46K 3 K. Regular melting between 3K  4 K.
20 kOe: Vortex lattice disorders slowly with temperature
30 kOe: Vortex lattice disorders rapidly with temperature

## Slide 21
For the agnostic: Direct visualization from raw data
Nature Communications 16, 2100 (2025)

## Slide 22
Inverse melting
Most well known in liquid 3He
Predicted also for vortices
Rev. Mod. Phys. 66, 1125 (1994)
Earlier evidence only in layered high Tc superconductor BSCCO from thermodynamic measurements under shaking:
Nature 411, 451–454 (2001)

## Slide 23
Construction of phase diagram
Melting of the vortex lattice
The peak effect(s)
Inverse Melting of the vortex lattice

## Slide 24
Liquid
Solid
Liquid
20 nm
Inverse Melting
5 nm
20 nm
50 nm
No Inverse Melting
Inverse Melting
Liquid
Solid
Liquid
Normal State
Liquid
Normal
State
Solid
Liq.
[2605.23567] Phase diagram of the vortex state in an amorphous Re6Zr thin film exhibiting inverse melting

## Slide 25
Quantum Nature of vortices: “Zero-point” fluctuation
A
C
B
Spectroscopy of the vortex core
Moderate clean crystal
Very clean crystal
NbSe2

## Slide 26: A-MoGe thin films: Soft gap inside vortex vortex core
5 kOe, 450 mK

## Slide 27
Simulating a conductance map
Assumptions:
Spectra inside core is flat: GA(V)
Spectra far away from core is same as the zero-field spectrum: GB(V)
FWHM
Single vortex
Simulating the vortex Lattice
Zero bias conductance
Coh. Pk. bias conductance
G (V,r)=w(r)GA(V)+(1- w(r)) GB(V)

## Slide 28
Validation of this scheme on NbSe2
5 kOe
Hc2 ~ 42 kOe
x ~ 8.9 nm

## Slide 29
Each vortex is randomly displaced by
Simulating fluctuating vortices
Displace each vortex by a random vector r
Zero Bias
Coh. peak
Sum over 200 such replica

## Slide 30: Matching with experimental results: a-MoGe
450 mK, 30 kOe
= 0.275
Zero Bias
Coh. peak

## Slide 31
Extracting the Amplitude of Fluctuations
Origin: Classical or Quantum?

## Slide 32
Theory: Amplitude and frequency of fluctuation
Harmonic Approximation
Amplitude of thermal motion
Zero Point Fluctuation:
Calculations: Surajit Dutta
a
Difference with our result is a pre-factor of 0.7.

## Slide 33
Zero point motion of vortices
Theoretical Estimate of vortex mass:
Suhl, PRL 14, 266 (1965)
Phys. Rev. B 103, 214512 (2021)

## Slide 35
2 K

## Slide 36
Summary
In nanometer-thick superconducting thin films, vortex liquid phases span a very large region of the H-T parameter space.
The phase diagram shows novel phase resulting from the interplay of fluctuations, pinning and intervortex interactions: Formation of the hexatic, smectic vortex fluid and Inverse melting.
Vortices are quantum in nature: Undergo zero-point fluctuations.
Can there be a quantum vortex liquid?

## Slide 37
Collaborators
Inverse melting
Rishabh Duhan (now in Weizmann)
Subhamita Sengupta (now in Harvard)
Somak Basistha (now at IIT Bombay)
Pritam Das, Anjan Jana, Sulagna Dutta
Hexatic vortex fluid
Indranil Roy (now at Rutgers)
Surajit Dutta (now at Weizmann)
Vortex State in NbSe2
Somesh Ganguly (now at University of Jyväskylä)
STM Instrumentation
Anand Kamlapure (now at QuTech, The Netherlands)
Theory Collaborators
Lara Benfatto & group (Sapienza, Rome)
Chandan Dasgupta (IISc, Bangalore)
Vadim Geshkenbein (ETH)
Amit Ghosal (IISER, Kolkata)
…and special thanks for technical support
Vivas Bagwe
John Jesudasan
Funding Support: Department of Atomic Energy, Govt of India

## Slide 38
Different degree of localization

## Slide 39
Overall Motion paths: Red Network + Blue Network

## Slide 40
Order-disorder transition of the vortex lattice
Scientific Reports 5, 10613 (2015); Phys. Rev. B 93, 144503 (2016).
In conventional superconductors the VL does not melt in 3D!
Nature 375, 373–376 (1995)
Nature 406, 282–287 (2000)
In bulk crystals vortex liquids have been only observed in High Temperature superconductors at temperature > 0.4 Tc

## Slide 41
Development of TIFR-Qmet Cryogenic Nanopositioners (NP)
Point Contact Spec Insert
Review of Scientific Instruments, 95, 113708 (2024)
Example of LabView interface
Customisable for specific requirements
Fully computer controlled electronics
Operating Temperature: 300 K – 1.6 K
Customizable for different applications.
Also Available commercially through Excel Instruments, Mumbai