## Slide 1: Upper critical field and pairing symmetry in 2D Ising superconducting materials
Lena Engström
LPS Orsay, Université Paris-Saclay
TIDES, 16 July 2026
L. Engström, L. Zullo, T. Cren, A. Mesaros, and P. Simon, Upper critical field and pairing symmetry of Ising superconductors, 2025, Physical Review Letters 135, 236004
L. Engström, A. Mesaros, and P. Simon, Upper critical field in few-layer Ising superconductors, 2026, arXiv: 2602.14210

## Slide 2
Upper critical magnetic field
BCS superconductor
Cooper pair breaking
Pauli paramagnetic limit :
Superconductivity cannot survive above this value in BCS superconductors
Upper critical field of a superconductor
de la Barrera et al., 2018, Nature Comm.

## Slide 3: Upper critical field
Condensation energy:
Susceptibility difference:
Clogston, 1962
Chandrasekhar, 1962
Frigeri, Agterberg & Sigrist, 2004
Sigrist, Avella & Mancini, 2009
At the critical field Hc2:
Where W is the thermodynamic potential
Near T=Tc, Hc2 is small enough to expand W :

## Slide 4
Upper critical field of a s-wave superconductor
Paramagnetic limit: Clogstone Chandrasekar
More generally:
Condensation energy:
D = superconducting gap
N(E) = density of states
Clogston, 1962
Chandrasekhar, 1962
Pauli limit
Pauli susceptibility of the normal state
Susceptibility difference:

## Slide 5
Singlet:
Triplet:
Möckli & Khodas, 2020
Ilić, Meyer & Houzet, 2023
Effect of the spin-orbit coupling
Singlet:
Triplet:

## Slide 6
Expansion in D of the susceptibility
Regular singlet superconductor (spin-degenerate normal state)
Triplet superconductor, (spin-degenerate normal state)
Singlet superconductor on spin-split normal state
Can be calculated analytically for parabolic bands

## Slide 7
Hp [T] = 1.86 Tc [K], is proportional to ∆0=1.76 Tc
Cases where Hc > Hp :
Triplet pairing
Strong coupling
Spin-orbit coupling (SOC)
Hc affected by e.g. disorder, but carries information about the pairing symmetry in few-layer compounds
Cao, Y., Park, J.M., Watanabe, K. et al. Nature 595, 526–531 (2021)
e.g. tTLG
Hc > Hp : indicator of pairing symmetry ?

## Slide 8: Ising superconductors

## Slide 9
Haim et al. 2022, PRB.105.024515
Zheng et al., Front. Phys. 18, 53603 (2023)
Series of compounds
Inversion symmetry breaking
Ising SOC
Inversion symmetry
Stacked quasi-2D layers:
Semimetals, insulators, CDW, superconductivity
Unconventional order:
Predicted to be mixed-parity, triplet, and/or topological
Transition Metal Dichalcogenides (TMDs)
, Te

## Slide 10
Ising spin-orbit coupling
Spin-polarized bands
Out-of-plane (z) spin-polarization
Ising spin-orbit coupling
’

## Slide 11
Spin-polarized bands
’
Ising spin-orbit coupling

## Slide 12
de la Barrera et al., 2018 (Nature Comm.)
Xi et al., 2016 (Nature Physics)
Lu et al., 2015 (Science), Lu et al., 2018 (pnas)
Experimental data (mono-layer)

## Slide 13
The compounds have the same symmetries and vary by doping main difference: pocket at Г or not
de la Barrera et al., 2018 (Nature Comm.)
Xi et al., 2016 (Nature Physics)
Lu et al., 2015 (Science), Lu et al., 2018 (pnas)
Experimental data (mono-layer)

## Slide 14
All points at the normal state FS are spin-split (by symmetry) except the 6 nodal points:
At these point the system is a conventional singlet superconductor
The susceptibility difference can be signficantly larger
Band structure in monolayer NbSe2

## Slide 15: Assuming uniform spin-singlet
Compare models:
1. Only K-pockets: bands are split by a constant SOC
2. 3 pockets: one Г-pocket with nodes and K-pockets
Both numerical integration and an effective model for the G-pocket
Strategies
Also compare to spin-triplet pairing

## Slide 16
Effective model description
Assumptions:
Parabolic bands
SOC per pocket :
Compare spin singlet and spin triplet pairing

## Slide 17: Г-pocket K-pockets
Contribution from the different bands
L. Engström, et al., Physical Review Letters 135, 236004 (2025)

## Slide 18
If:
Temperature dependence at H=0 is equal for all pockets
There is only one Hc of the system
solving self-consistently the gap equations
inter-pocket intra-pocket interactions
The Hc of the multi-pocket system is:
Multi-pocket system
One gap:
Two gaps:

## Slide 19
For NbSe2:
Application to NbSe2

## Slide 20
For NbSe2:
Only K-pockets:
Including the Г-pocket:
L. Engström, et al., Physical Review Letters 135, 236004 (2025)
Application to NbSe2

## Slide 21
Singlet vs triplet
L. Engström, et al., Physical Review Letters 135, 236004 (2025)
The upper critical field is lowest for the least exceptional
scenario (no band splitting, singlet pairing).

## Slide 22
For a singlet:
Sqrt scaling with SOC
Г-pocket limits Hc
For a triplet:
Nodal SOC points don’t affect Hc
Cannot generate sqrt scaling
Singlet at Г-pocket explains the data of 1H-NbSe2 & 1H-TaS2
Only consistent with some predicted orders:
Wickramaratne et al., PRX 10, 041003 (2020)
Möckli & Khodas, PRB 101, 014510 (2020)
Siegl et al., arXiv:2412.00273
Shaffer et al., PRB 101, 224503 (2020)
Pairing symmetry in monolayers

## Slide 23
Model parameters from ARPES and STM:
Nakata et al. npj 2D Mater Appl 2, 12 (2018)
Kuzmanović et al., PRB.106.184514 (2022)
de la Barrera et al., 2018 (Nature Comm.)
Xi et al., 2016 (Nature Physics)
Lu et al., 2015 (Science), Lu et al., 2018 (pnas)
L. Engström, et al., Physical Review Letters 135, 236004 (2025)
Comparison with data

## Slide 24
Using values from experiment of SOC and order parameter we closely predict the curves (w/o incl. disorder)
Model parameters from ARPES and STM:
Nakata et al. npj 2D Mater Appl 2, 12 (2018)
Kuzmanović et al., PRB.106.184514 (2022)
Unique scaling with SOC for a spin-singlet
L. Engström, et al., Physical Review Letters 135, 236004 (2025)
Comparison with data

## Slide 25
Scaling of Hc2 for NbSe2 with doping
L. Engström, et al., Physical Review Letters 135, 236004 (2025)

## Slide 26: Multi-layer TMDs

## Slide 27
For an intralayer spin-singlet:
Bilayer NbSe2 with inversion symmetry breaking
 spin
 layer
Around nodes
L. Engström, A. Mesaros, P. Simon, arXiv:2602.14210

## Slide 28
Comparison to data of bilayer TMDs
L. Engström, A. Mesaros, P. Simon, arXiv:2602.14210

## Slide 29
Scaling of Hc2 with interlayer potential
L. Engström, A. Mesaros, P. Simon, arXiv:2602.14210

## Slide 30
At SOC nodes:
signature difference between singlet and triplet pairing is large
Г-pocket:
Explains monolayer data
Necessary to describe multilayer data
Scaling of Hc2 as a way
to narrow down possible pairing symmetry, incl. misfits, Moiré, TMD heterostructures ?
Summary
L. Engström, et al., Physical Review Letters 135, 236004 (2025)
L. Engström, A. Mesaros, P. Simon, arXiv:2602.14210
Summary

## Slide 31
People
Lena Engström
Andrej Mesaros
Ludovika Zullo
Tristan Cren

## Slide 32: Pairing symmetry
Theoretical predictions:
Mixed parity
Induced triplet under field
Nematicity
Topological nodal superconductor under field
Hsu et al., Nat. Com. s8 (14985) (2017)
k
-k
Phonon and/or spin fluctuations (Das et al., 2023)
Wickramaratne et al., PRX 10, 041003 (2020)
Möckli & Khodas, PRB 101, 014510 (2020)
Siegl et al., arXiv:2412.00273
Shaffer et al., PRB 101, 224503 (2020)

## Slide 33: Mixed parity
with
Even with a large triplet component the mixed state response is dominated by that of the singlet component
L. Engström, A. Mesaros, P. Simon, arXiv:2602.14210

## Slide 34: Beyond uniform singlet
Mixed parity, e.g. s+ f or p+ip + d+id
Nodal singlet
Topological nodal singlet
Purely triplet
Purely nematic
In NbSe2, Cho et al., PRL 129.087002 (2022)

## Slide 35: Few-layers: up to N=5
L. Engström, A. Mesaros, P. Simon, arXiv:2602.14210

## Slide 36: Susceptibility
Pauli: from FS
Van Vleck: from band splitting
For singlet order