## Slide 1: Thickness tunes everything: Superconductivity in the H-TMD family
Hadar Steinberg
Racah institute of Physics, Hebrew University, Jerusalem
TIDES, Paris, 16.7.2026
Notes: The story I will present to you is embodied in these 2 graphs, recently published in two papers. Both represent a different effect where thickness tunes the fundamental properties of exfoliated superconductors.

## Slide 2: Steinberg Lab: 2D Superconducting Devices
NbSe2:
Dvir et al., Nat. Comm. 9, 598 (2018)
Dvir et al., Nano Lett. 12, 7845 (2018)
Alpern et al., Nano Lett., 19, 5167 (2019)
M. Kuzmanovic et. al., PRB 106, 184514 (2022).
FeTe0.55Se0.45:
Zalic et al., PRB 100, 064517 (2019).
TaS2:
S. Simon et al., Nature Comm., 15, 10439 (2024).
Dvir et al., PRL 123, 217003 (2019)
Keren et al., Nat. Comm. 11, 3048 (2020)
Devidas et al., Nano Lett. 21, 16, 6931 (2021)
M. Quincke et al., ACS Applied Nano Materials, 5, 8, 11429 (2022).
Devidas et al., PRB 107, 094502 (2023)
Fyhn et al., PRB 102, 024510 (2020)
Dvir et al., PRB 103, 115401 (2021)
Zalic et al, Nano Letters 23, 6102 (2023)
Grynszpan et al., 2D Materials, 12, 041004 (2025).

## Slide 3: VdW Systems: A Laboratory for Thickness Control
4L, 20L TaS2. Shahar Simon, M. Sc. Thesis

## Slide 4: Tunnel Junction Fabrication and Architecture
Superconductor on substrate
Semiconductor on superconductor
Contacted tunnel junction
Trilayer MoS2
4-layer TaS2
(plus partial layer)
Image: Atzmon Vakahi, Sergei Remennik, HUJI center for nanoscience and nanotechnology

## Slide 5: VdW Tunneling at mK Temperatures
Effective filtering
High in-plane field
Transport + Tunneling
Very fine energy precision (few µeV)
Sensitivity to depairing processes
Tunneling
electrodes

## Slide 6: Tunneling Project: The People
Theory
Jonathan Ruhman
Hennadii Yerzhakov
Maxim Khodas
Experiment: Tunneling
Shahar Simon
Tom Dvir
Saclay: Charis and friends
Discussions
Oded Millo
Amit Kanigel
Materials
Sajilesh K. P.

## Slide 7: TMD: Inversion Symmetry Broken Layers
TMD = Transition Metal Dichalcogenide
D. Möckli, M. Khodas, PRB 98, 144518 (2018)
k
𝛆 (crystal field)
BSO

## Slide 8: Tc vs Number of Layers
KF Mak Group, Nat. Phys. 12, 139 (2016)
Theory (YBCO): “interlayer coupling enhances superconductivity”
Schneider et al., EPL 14, 261 (1991).
NbSe2

## Slide 9: TMDs: Ising Superconductivity
Xi, X. et al. Nat. Phys. 12, 139 (2016)
Lu et al., Science 350, 1353 (2015)
Saito et al., Nature Phys. 12, 144 (2016)
De la Barrera et al., Nat. Comm. 9, 1427 (2018)
TMD = Transition Metal Dichalcogenide

## Slide 10: The Many Roles of Thickness:
1. Increase the Ising stability vs. In-plane magnetic field at the thin limit.
1
10
>20
5
15
Ising
Number of Layers

## Slide 11: Orbital FFLO in TMD SC
P. Wan et al., Nature (2023)
Morpurgo / Zhang Groups
Lortz Group, Smet Group

## Slide 12: The Many Roles of Thickness:
Increase the Ising stability vs. In-plane magnetic field at the thin limit.
Onset of orbital FFLO at finite thickness.
1
10
>20
5
15
Ising
Orbital FFLO
Number of Layers

## Slide 13: NbSe2: Two-Bands in In-plane magnetic field
H < HC1: Meissner Current
Note: d < 𝜆, H is uniform
d
HC1 < H Vortex Penetration
Effective method to study tunneling at the presence of current
T. Dvir et al., Nature Comm. 9, 598 (2018)
Notes: A flaky solution 
20-50 nm flakes are just think enough to get “bulk” behavior, and thin enough to suspend Hc1 to significant field.
Is there a calculation for an ’ideal’ flake?

## Slide 14: Bulk: Depairing at In-plane field
Model
Data
Orbital Depairing
Hc1
Large gap: Ballistic
(Fulde, 1965)
Small gap: Diffusive
Large Diffusion Const:
Large VF
(Tinkham Ch. 10)
Dvir et al., Nature Comm. 9, 598 (2018)
Kiss et al. Nat. Phys. 3, 720 (2007)

## Slide 15: From thick to thin…
50 nm
25 nm
20 nm
10 nm
5 nm: 8-10 layers
d
Thickness effects:
1. Gap decreases in size and becomes immune to field
2. Two (three!) gap structure lost
T. Dvir et al., Nature Comm. 9, 598 (2018)
M. Kuzmanović, T. Dvir et al., PRB 106, 184514 (2022)
Two gap -> One Gap
3 gaps -> 2 Gaps

## Slide 16: Fitting Multiple Gaps
NbSe2, 30 Layers
McMillan, Phys. Rev. 175, 537 (1968)
S. Simon et al., PRL, Acceped for Publication.
T. Dvir et al., Nature Comm. 9, 598 (2018)
Δ1 = 1.26 meV
Δ2 = 0.29 meV
Δ1 = 1.05 meV
Δ2 = 0.30 meV
Γ12 = 0.27 meV
Γ12 = 1.35 meV

## Slide 17: The Many Roles of Thickness:
Increase the Ising stability vs. In-plane magnetic field at the thin limit.
Onset of orbital FFLO at finite thickness.
3-band specturm turns to 2-band at the 10-20 nm range.
1
10
>20
5
15
Ising
Orbital FFLO
Number of Layers
3 Bands
2 Bands

## Slide 18: Thin NbSe2 Tunneling at Ultra-High Fields
< 50 mK
1.2 K
< 50 mK
1.2 K
Fit: Abrikosov-Gor’kov theory
Extract Delta
6 Layers
2 Layers
M. Kuzmanović, T. Dvir et al., PRB 2022

## Slide 19: The Many Roles of Thickness:
Increase the Ising stability vs. In-plane magnetic field.
Onset of orbital FFLO at finite thickness.
Two-band specturm disappears at the 10-20 nm range.
Putative onset of a triplet component at high in-plane field.
1
10
>20
5
15
Ising + Triplet?
Orbital FFLO
Number of Layers
3 Bands
2 Bands

## Slide 20: TC and HC2: Story Gets Complicated
KF Mak Group, Nat. Phys. 12, 139 (2016)
Theory (YBCO): “interlayer coupling enhances superconductivity”
Schneider et al., EPL 14, 261 (1991).
NbSe2

## Slide 21: This was NbSe2. Now let’s look at TaS2
Y. Yang et al., PRB 98, 035203 (2018)
Previous work by E. Navarro-Moratalla et al.
Notes: Efren: effect of DOS on screening of the Coulomb repulsion

## Slide 22: Opposite Response to Thickness
De la Barrera et al., Nat. Comm. 9, 1427 (2018)
Y. Yang et al., PRB 98, 035203 (2018)
What is the origin of the different thickness response?
The role of CDW could be important
Any relation between the mechanisms?

## Slide 23: The Many Roles of Thickness:
Increase the Ising stability vs. In-plane magnetic field at the thin limit.
Onset of orbital FFLO at finite thickness.
Two-band specturm disappears at the 10-20 nm range.
Putative onset of a triplet component at high in-plane field.
Change Tc – Reduce for NbSe2, Increase for TaS2.

## Slide 24: Tunneling Spectra of TaS2
T = 25 mK, Low temperature filters
Hard gap
QP peaks weaker at thicker samples (hanlding?)
Trilayer MoS2
4-layer TaS2
(plus partial layer)

## Slide 25: Temperature Dependence of the Spectrum
When Tc is evaluated using the 95% criterion: Gives good agreement with transport data

## Slide 26: Dependence of Tc on Thickness
When Tc is evaluated using the 95% criterion: Gives good agreement with transport data

## Slide 27: Response to In-Plane Magnetic Field

## Slide 28: Response to Out-of-Plane Magnetic Field

## Slide 29: HC2 vs. ∆: Clean vs. Dirty limits
=
Landau Ginzburg:
In the clean limit:
Where:
So:
In the dirty limit:
=
We have a problem: TaS2 is not supposed to be a clean superconductor

## Slide 30: Hc2 vs. Tc2
TaS2
NbSe2
Bulk TaSe2
TaS2
NbSe2
=
Landau Ginzburg:
In the clean limit:
Where:
So:
NbSe2: Xi, X. et al. Nat. Phys. 12, 139 (2016)
Transport
TaS2: Our data (Tunneling)
TaSe2: Yokota et al., Physica B 284, 551 (2000) (Self-inductance)
Slope = 1 over 4 decades
Shared property + Tunable parameter
Bulk
NbS2
16L TaSe2
5L TaSe2

## Slide 31: Questions: Shared vs. Tunable?
Is there any other system which can be tuned like this?
What is the shared property
What is the tunable parameter?
Why is the system clean?
How does the slope depend on vF?

## Slide 32: Is there any other system like this?

## Slide 33: Shared Property: Band Structure
NbSe2, TaS2 are doped versions of the intrinsic TMDs

## Slide 34: Tunable Property: CDW?
The existence of a universal progression through different TMDs suggests that the same mechanism suppresses superconductivity in all of them.
This observation disagrees with model of thickness-dependent coupling
Xi 2016 (NbSe2): CDW not likely to be important.
Yang 2018 (TaS2): CDW IS important.
What are we going to do?

## Slide 35: Theory: Vary CDW
Jonathan Ruhman, Hennadii Yerzhakov, Maxim Khodas
Tight-binding -> TMD Band-structure
CDW is momentum-dependent: J. van Wezel, PRB 2016
(Because smooth CDW would increase TC ).
Band-structure including CDW modification, DOS depends on CDW
Self-consistent determination of Tc (BCS)
HC2 is calculated based on Ginzburg-Landau theory
Notes: We investigate this possibility by employing Gor'kov's theory to compute \Hc close to $T_C$, starting from a tight-binding model including SOC and the 3$\times$3 CDW for both \tas and \nbse parameters.
In this calculation, we assume the attractive phonon-mediated interaction is of equal strength on all three transition metal $d$-orbitals.
We use the strength of the CDW order parameter, denoted by $b$, as the tuning parameter of $T_C$ and $\Delta$.

## Slide 36
vF
Excellent agreement with the HC2 vs TC2 dependence
We exctract vF = 3.2x104 m/s – Too Low!!
How does theory “miss” HC2??
Experiment
Theory
Notes: VF = 3.2e4 m/s in this fit
ARPES: 0.6 to 0.8 in Kiss paper
Greater in TaS2 (Sanders?) paper

## Slide 37: The Many Roles of Thickness:
Increase the Ising stability vs. In-plane magnetic field at the thin limit.
Onset of orbital FFLO at finite thickness.
Two-band specturm disappears at the 10-20 nm range.
Putative onset of a triplet component at high in-plane field.
Change Tc and HC2 along a universal ratio, likely through tuning CDW
1
10
>20
5
15
Ising + Triplet?
Orbital FFLO
Number of Layers
3 Bands
2 Bands
Reduced Tc (Nb)
Increased Tc (Ta)

## Slide 38: Tunneling, Vortices, and Thickness
Guillamon I, 2009, PhD Thesis, UAM
STM
Tunnel Junction

## Slide 39: Tunneling and Vortices: Through CdGM
Dvir, Tom, et al. "Tunneling into the Vortex State of NbSe2 with van der Waals Junctions." Nano Letters 18.12 (2018): 7845-7850.

## Slide 40: Tunnel Junction as Current Sensor
Precision: Few µeV
Shahar Simon, Maya Klang, Submitted
Clean limit Doppler shift:

## Slide 41: Tunneling and Vortices: Through Meissner
Shahar Simon, Maya Klang, Submitted
NbSe2, 15 Layers

## Slide 42: Visually:
Two regimes in increasing field:
: Meissner+vortices increasing
Meissner saturated

## Slide 43: Vortex Entry / Exit Affect Spectra
Two regimes in decreasing field:
: Meissner decreasing to full cancellation
: Vortices exit
Full cancellation regime

## Slide 44: Numerical solution to London equations fits:
Bishop-Van Horn, Logan, and Kathryn A. Moler. "SuperScreen: An open-source package for simulating the magnetic response of two-dimensional superconducting devices." Computer Physics Communications 280 (2022): 108464.

## Slide 45: So far…
At the 10-15 layer range, vortices can be detected at a distance of few µm away, by their signature on the screening current
BUT
What is actually the structure of the vortex at the ultrathin limit in TMD superconductors?

## Slide 46
Scanning SQUID-on-tip microscopy: Anahory Group
Pb
Pb
gap
D. Harlbertal et al. Nature (2016)
Y. Anahory, J. Reiner, et al. Nano Lett. (2014)
D. Vasyukov, Y. Anahory et al. Nature Nano. (2013)
A. Uri et al. Nano Lett. (2016)
G. Romagnoli et al. APL (2023)
Y. Anahory et al. Nanoscale (2020)
Notes: The work I will present here was carried out using a technique that we developed in our group over the last 10 year… It’s a scanning SQUID technique, but not any type… We call it the scanning SQUID-on-tip. -> Here is an SEM picture of the device. It’s a SQUID loop that reside at the end of a sharp pulled pipette -> You can observe here two lead leads separated by a gap. -> There two leads meet at the end of the pipette to form the SQUID loop. -> We can make them in different size, here is our smallest ever made with 46 nm diameter. -> the idea is to mount this into a scanning probe microscope to perform scanning SQUID microscopy -> Let me go through the main features of our device. -> it has suitable for scanning probe because -> we can make them small -> and because we can bring the SQUID loop in close proximity to the sample. -> as a result -> we can achieve outstanding spin sensitivty with 0.38 Bohr magneton, and -> flux sensitivty of 50 nano phi0. In addition, this technique offers also higher spatial resolution and can work up to 2 T which is a few order of magnitude above other techniques.

## Slide 47: Vortices at the Ultrathin Regime

## Slide 48: Encapsulated NbSe2
NbSe2
4
hBN
hBN

## Slide 49: Size of Vortex: Pearl Length
We can measure the Pearl length even when it is greater than the sample size
Bulk Superconductors:
Screening current suppressed exponentially.
Length scale:
Thin Superconductors (d << ):
Screening less effective. It is govered by the Pearl length
It is suppressed polynomically, as near the core, and
… as far from the core (r > ).
We measure at the 1/r regime. Other vortices + edge:
Constant Backgroud -> eliminated by gradient
T = 4.2 K

## Slide 50: Pearl Length vs. Thickness
Transition appears at N = 6
Se band? No. It would give another 1/d term
N < 6: Superfluid density independent of thickness
-> Surface??
T = 4.2 K
Notes: Surface: Rashba or strain due to lattice mismatch.

## Slide 51: Model: Onset of Surface-Bound Order
Order competition: Surface contribution negligible at the thick limit
Takes over at 6 L and below
Where has it been until now?
Not seen in transport, tunneling…
Pristine sample?
Notes: If you measure Tc, you are sensitive to conditions near Tc.

## Slide 52: The Many Roles of Thickness:
Increase the Ising stability vs. In-plane magnetic field at the thin limit.
Onset of orbital FFLO at finite thickness.
3-band specturm turn to 2-band at the 10-20 nm range.
Putative onset of a triplet component at high in-plane field.
Change Tc and HC2 along a universal ratio, likely through tuning CDW
NbSe2: Transition from bulk to surface-dominated Pearl Length at 6 L.
Are these all different effects?
1
10
>20
5
15
Ising + Triplet?
Orbital FFLO
Number of Layers
3 Bands
2 Bands
Reduced Tc (Nb)
Increased Tc (Ta)
Surface-Dominated