## Slide 1
Roy Gaara Cohen
Frydman’s lab
Aviad Frydman (BIU)
Mark Nikolaevsky (BIU)
Claire Marrache-Kikuchi (UPS)
Amity Cohen (NRCN)
Ran Salem (prev. NRCN)
TIDES 2026
Pressure-Induced Anomalous Metal in the Vicinity of the Superconductor-Insulator Transition

## Slide 2
Tuning parameters:
Magnetic field
Thickness
Level of disorder
Chemical composition
Gate voltage
Pressure
2D Superconductivity
Superconductor insulator transition (SIT)
D.B. Haviland, Y. Liu, A.M. Goldman PRL, (1989)
2

## Slide 3
SC Wave function:
Bose Model
Granular systems
Insulator
Superconductor
3
Notes: פונקציית הגל העל מוליך תוארה על ידי גינצורג ולאנדאו. האמפליטודה קובעת את התכונות העל מוליכות כמו הטמפרטורה הקריטית.
פאזה תלויה בצימוד בין חלקים שונים של המערכת, בחומרים גרנולרים ניתן לראות זאת.
במערכת גרנורית כזו יש על מוליכות סופית וקיים פלקטואציות בפאזה בין הגרגירים.
ההפרמטר אשר גורם לצימוד הוא Ec חלקי Ej כאשר הראשון הוא charging energy והשני הוא אנרגיית גוספסון זרם קריטי, פלקס מגנטי. כאשר אי סי שתלוי בגודל הגרגירים גדול מקשה ... ואנרגיית ג'וספסון...
עדיין יש שאלות פתוחות סביב הSIT לדוגמא

## Slide 4
Electronic Granularity
A. Roy, E. Shimshoni, A. Frydman, PRL, (2018)
Bouadim et al, Nature Phys, (2011)
3
-3
0
0.4
0
100 nm
Amorphous InO
Disorder realization
Local pairing amplitude
disorder
3

## Slide 5
Tunneling Experiment
D. Sherman, A. Frydman, PRL, (2012)
100 nm
Amorphous InO
5

## Slide 6
The Insulating State
D. Shahar Z. Ovadyahu, PRB (1992).
Amorphous InO
TiN
T. Baturina, PRL (2007)
Simple activation
Bose insulator
J. Zhang et al, PRB, (1993)
Anderson
insulators
Doped Si
V. Humbert, nature com (2021)
6

## Slide 7
The Insulating State
D. Shahar Z. Ovadyahu, PRB (1992).
Amorphous InO
TiN
T. Baturina, PRL (2007)
Simple activation
Bose insulator
J. Zhang et al, PRB, (1993)
Anderson
insulators

## Slide 8
The Insulating State
D. Shahar Z. Ovadyahu, PRB (1992).
SIT insulators
J. Zhang et al, PRB, (1993).
Variable range hopping
Coulomb interactions
Anderson insulators

## Slide 9
A. Roy, E. Shimshoni, A. Frydman PRL, (2018)
Amorphous InO
I. Tamir Science advances, (2019)
Amorphous InO
T. Baturina, PRL (2007)
TiN
O. Crauste, C.A. Marrache-Kikuchi, et.al, Journal of Physics (2009)
F. Couëdo, C.A. Marrache-Kikuchi, et.al, Scientific Reports (2016)
Direct Transition? Or Metallic State?
4

## Slide 10
A. Roy, E. Shimshoni, A. Frydman PRL, (2018)
Amorphous InO
T. Baturina, PRL (2007)
TiN
O. Crauste, C.A. Marrache-Kikuchi, et.al, Journal of Physics (2009)
F. Couëdo, C.A. Marrache-Kikuchi, et.al, Scientific Reports (2016)
M1
M2
Direct Transition? Or Metallic State?
I. Tamir Science advances, (2019)
Amorphous InO
Anomalous Metal
4

## Slide 11
A. Roy, E. Shimshoni, A. Frydman PRL, (2018)
Amorphous InO
I. Tamir Science advances, (2019)
Amorphous InO
T. Baturina, PRL (2007)
TiN
O. Crauste, C.A. Marrache-Kikuchi, et.al, Journal of Physics (2009)
F. Couëdo, C.A. Marrache-Kikuchi, et.al, Scientific Reports (2016)
Direct Transition? Or Metallic State?
Anomalous Metal
4

## Slide 13: Pressurizing superconductors
Notes: אולי להוסיף שקופית לפני שזה נושא חם. אולי לשים גרף חדש יותר

## Slide 14
Superconducting metallic elements
T. F. Smith, C.W. Chu, Physical Review (1967)
Pressurizing 3D Superconductors
Carbonaceous sulfur hydride
E. Snider, et al. Nature (2020)
(K)
A. P. Drozdov, M. I. Eremets, et al. Nature (2019)
HTC - lanthanum hydride
5

## Slide 15
Diamond Anvil Cell
6

## Slide 16
1GPa = 10,000 ATM
= 1 upside down Eiffel tower
Diamond Anvil Cell
Copper beryllium
7

## Slide 17
1GPa = 10,000 ATM
= 1 upside down Eiffel tower
Diamond Anvil Cell
7

## Slide 18
Diamond Anvil Cell
1GPa = 10,000 ATM
= 1 upside down Eiffel tower
7

## Slide 19
R. Cohen, M. Nikolaevsky, R. Salem, A. Frydman, Rev. Sci. Instrum. 92, 083903 (2021)
15cm
2.6cm Ø
2cm Ø
Our Experimental Setup
low temp
1.5K
Ultra low temp
15mK
Pressurizing in situ
Notes: להלן השרטוט ותמונה של התא שלנו אשר דומה מאוד לתאים רגילים אך הוא בנוי עם בורג אחד בניגוד לתאים רגילים עם מספר ברגים.
לשם הניסוי אנו נדרשים לקרר את התא לטמפ' נמוכות. בכדי לעשות זאת בנינו מוט אשר מאפשר לנו להכניס את התא למערכת קירור בהליום ועדיין לשלוט על הלחץ מבחוץ.
המערכת בנויה עם מוט מרכזי כשאר מסובבים אותו מעלה את הלחץ בתא.

## Slide 20
8

## Slide 21
Pressure Measurement
M. Rivers et al., High Pressure Research (2008)

## Slide 22
Results
30nm InO
9

## Slide 23
Results - Tc vs Pressure
10

## Slide 24
Results – Anomalous Metal
11

## Slide 25
AM + Magnetic Field
12

## Slide 26
Results – Insulating State
13

## Slide 27
Results – Insulating State
Ambient
P > 10GPa
Bose insulator
Anderson insulator
14

## Slide 28
Results – Insulating State
Ambient
P > 10GPa
Bose insulator
Anderson insulator

## Slide 29
Insulating State

## Slide 30
Insulating State
17

## Slide 31
Weak Localization
1
18

## Slide 32
is non monotonic
Pressure Effects
Different type of insulator
Higher resistance
weaker localization
Improves coupling
Reduces SC amplitude

## Slide 33
Pressure Effects
Improves coupling
Reduces SC amplitude
Anomalous Metal
is non monotonic
Different type of insulator
Higher resistance
weaker localization

## Slide 34
Pressure Effects
15

## Slide 35
Pressure Effects
Destroys superconductivity
Enhances superconductivity
is non
monotonic
15

## Slide 36
Pressure Effects
Destroys superconductivity
Anderson
insulator
Enhances superconductivity
Bose
insulator
is non
monotonic
Different
insulator
15

## Slide 37
Pressure Effects
Destroys superconductivity
Anderson
insulator
Weaker
localization
Enhances superconductivity
Bose
insulator
Higher
resistance
is non
monotonic
Unusual
effect
Different
insulator
15

## Slide 38
Pressure Effects
Improves coupling
Destroys superconductivity
Anderson
insulator
Weaker
localization
15

## Slide 39
Pressure Effects
Improves coupling
Reduces SC amplitude
15

## Slide 40
Pressure Effects
Anomalous Metal
15

## Slide 41
Pressure Effects

## Slide 42
Pressure Effects
Enhances coupling

## Slide 43
Pressure Effects
Enhances coupling
Reduce amplitude

## Slide 44
Pressure Effects
Enhances coupling
Reduce amplitude

## Slide 45
Pressure Effects
Bose insulator
Super-conductor
Anomalous metal
Anderson insulator
Enhances coupling
Reduce amplitude

## Slide 46
Coupling
Amplitude
Phase Diagram
Bismuth - thickness
InO - disorder
NbSi - thickness
InO - pressure
16

## Slide 47
Conclusions
Bose Insulator
Anderson Insulator
Superconductor
AM Metal
Strong coupling
Weak SC amplitude
But in the end
It doesn’t even matter
Even diamonds break

## Slide 48
Reversibility

## Slide 49
Preliminary Results
3 nm
5 nm
12.5 nm
Bose → Anderson
insulator
Weaker
insulator
Improve superconductivity
21

## Slide 50
Conclusions
We developed a method to apply pressure on 2D films
Bose Insulator
Anderson Insulator
Superconductor
AM Metal
Thank you
But in the end
It doesn’t even matter
Even diamonds break

## Slide 51
But in the end
It doesn’t even matter
Even diamonds break
Thank you

## Slide 52: Electronic granularity
A. Frydman, Physica C, (2003)
Thickness
100 nm
A. Roy, E. Shimshoni, A. Frydman Physical Review Letter, (2018)
Granular Pb
Disordered InO
disorder
Notes: טעות בכותרת לתקן

## Slide 53: Tunneling experiment
D. Sherman, G. kopnov D. Shahar, A. Frydman, Physical Review Letters (2012).
J.M. valles Jr. et al., Physica B (1994)
Granular Pb
Disordered InO
Notes: תנאי שההתנגדות של המבודד העל מוליך תהיה קטנה בשני סדרי גודל מהמבודד באמצע. להכין שקופית.

## Slide 54
(a)
(b)
Conductance measurements

## Slide 55
Magnetic Measurements

## Slide 56
preliminary Results
5nm

## Slide 58
preliminary Results
12.5nm