## Slide 1: Results From mid-T Bake Applied to 1.5 GHz C75 5-cell Cavities for CEBAF
Pashupati Dhakal, E. Lechner, and G. Ciovati
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics under Contract No. 89243126CSC000213

## Slide 2: Continuous Electron Beam Accelerator Facility (CEBAF)
Currently 400 5/7 cell cavities are installed providing 12 Gev CW electron beam

## Slide 3: SRF cavities @ CEBAF
C20/C50
C75
C100

## Slide 4: Current Status
Quality factor Q0 is not only performance metrics of SRF cavity; it is an operating expense.
Bottleneck: Heat Load
Target High Q0
(2x1010)
 80 W Heat
One of the linac is reaching cryo- capacity
To reach higher energy gradients without tripping the system, we must lower the dynamic heat load

## Slide 5: High Q0 Development (2012- Present)
P Dhakal et al., IPAC '12, 2012
P. Dhakal et al., PRAB 16, 042001 (2013)
A Grassellino et al 2013 Supercond. Sci. Technol. 26 102001
G. Ciovati, Appl. Phys. Lett. 89, 022507(2006)
S. Posen et al., Phys. Rev. Applied 13, 014024 (2020)
E. Lechner et al., Appl. Phys. Lett. 119, 082601 (2021)

## Slide 6: High Q0 Option for CEBAF Cavities
Despite drawbacks, alloyed cavities are expected to outperform baseline cavities in cryomodules.

## Slide 7: High Q0 Option for CEBAF Cavities
~ 33%

## Slide 8: Single Cell Results
T = 2.0 K, f = 1.3 GHz
T = 2.07 K, f = 1.5 GHz
FG
LG
350 C/3h
Cavities were EP’ed prior to each treatment

## Slide 9: Flux Trapping Sensitivity ( @4MV/m)
Heat Treatment Temperature (oC/ 3h)
Flux Trapping Sensitivity (nW/mG)

## Slide 10: High Q0 Option for CEBAF Cavities
CEBAF is in operation, the only way to implement high Q0 on existing cavities are during refurbishment and upgrades:
Currently older C20 are being replaced with new C75 cavities to increase the over all gradient by ~ 55 MeV per cryomodules
Refurbish underperforming C100 (with light EP and HPR) and reinstallation.
C20
C75

## Slide 11: High Q0 Option for CEBAF Cavities
C100, 7-Cell cavity, Fine Grain
C75, 5-Cell cavities, Large Grain

## Slide 12: Flux Trapping Sensitivity
C75, 5-Cell cavities
Single cavities
T = 2.07 K, f = 1.5 GHz
S@20 mV/m  1.45±0.1

## Slide 13: High Q0 Option for CEBAF Cavities
T = 2.07 K, f = 1.5 GHz, Large Grain
Cryomodule integration in progress…

## Slide 14: Challenges for using high-Q cavities in C75 CM
Improvement was made by increasing the distance between the waveguide and cavity cell in C75 Cavities
<Bres> = 7 mG
C75 CONFIGURATION
Cooldown challenge for high Q0 cavities

## Slide 15: Challenges for using high-Q recipes in C100 cavities
A C100 bare cavity has a SS-Nb brazed joint
  The highest temperature it can be annealed as a bare cavity is 600 °C (poor flux expulsion)
A refurbished C100 cavity has a SS He tank welded to it with a heater inside
  Issues with differential thermal expansion and G10 used in heater assy, the highest annealing temperature is ~140 °C
Removal and reweld of Helium vessel is needed

## Slide 16: Summary & Path Forward
High Q0 recipes ( Oxygen alloying with Mid-T bake) have been validated to reduce the dynamic heat load at operating gradients.
Refurbishment is underway for C75 (new) and C100 (legacy) cryomodules, addressing the heat load and other mechanical constraints.
These upgrades ensure CEBAF remains the premier facility for continuous electron beam nuclear physics pushing the energy frontier within existing cryogenic limits.

## Slide 17: Questions
Pashupati Dhakal
dhakal@jlab.org