## Slide 1
Surface treatment platform construction and preliminary experiment for FEL
Shaohua Peng
Institute of Advanced Light Source Facilities, Shenzhen
  09th June, TTC’2026 Meeting, Paris French

## Slide 2
Outline
01
Introduction
02
Surface treatment platform construction
04
Summary
03
preliminary experiment on single cell

## Slide 3
Introduction

## Slide 4
S3FEL: Shenzhen Superconducting Soft x-ray Free Electron Laser
Construction unit: Institute of Advanced Light Source Facilities, Shenzhen (IASF)
Construction site: Guangming District, Shenzhen (Guangming science city, cluster of facilities)

## Slide 5
1
2
3
No. | Nameing
1 | S3FEL
2 | Superconducting Module Test Facility (SMTF)
3 | Linac Test Facility (LTF)
Layout of S3FEL Accelerator

## Slide 6
S3FEL Projects Need of cavities
 | SMTF | LTF | S3FEL | Total
1.3 GHz CM | 1 | 5 | 18 | 24
1.3 GHz-9cell cavity | 10 | 40 | 162 | 212
3.9 GHz CM | 1 | 2 | 2 | 5
3.9 GHz-9cell cavity | 10 | 16 | 19 | 45
Injector CM | / | 1 | 2 | 3
1.3GHz-9cell cavity（double coupler） | / | 1 | 2 | 3
S3FEL need 212 1.3GHz -9cell cavities, 45 3.9GHz -9cell cavities and 3 injector 1.3GHz -9cell cavities in total.
Most 1.3GHz-9cell cavities will be carried out surface-treatment by IASF. 3.9GHz-9cell caivties mainly undergoes BCP and will be carried out by the manufacturer.

## Slide 7
Surface treatment platform construction

## Slide 8
layout
IASF built an EP system, located in Zhongshan City. IASF has set up a Vacuum baking oven、HPR and ultrasonic cleaning machine in the pre-research laboratory . IASF is developing CBP equipment, which is expected to arrive in October.
Equipment | Quantity | Progress | Position
EP | 1 | In use | Zhongshan
HPR | 1 | Debugging completed | Shenzhen
Vacuum baking oven | 1 | In use | Shenzhen
Ultrasonic Cleaner | 1 | In use | Shenzhen
CBP | 1 | Under development | 

## Slide 9
EP
2023.9
Start platform layout diagram
2024.8
Complete factory testing and send to Zhongshan
2025.3
Complete on-site installation
2025.4、5
Carry out on-site water flow commissioning and related modifications
2025.6.20
Held a review meeting for the EP test acceptance plan
2025.8、9
Completed the EP test
Unit | Requirements
Acid supply unit | The materials are all PFA and PVDF materials.
Mixed acid circulation unit | The volume of the circulating cooling tank shall not be less than 200L
 | The acid temperature range is not less than 10~20℃, and the acid temperature accuracy is 1℃
 | Acid solution process flow 1~20 L/min, flow controllable, step size not greater than 0.5 L/min
Cleaning system and hydrogen forced discharge system | Nitrogen flow rate 0~50 L/min
Chiller unit for spray cooling | Cooling capacity 40 kW, used in conjunction with the spray cleaning unit
Chiller Unit for EP Polishing | Cooling capacity 30 kW, water outlet temperature control accuracy ±0.5°C
Spray cleaning unit | Spray flow control, 0~20 L/min, temperature control range not less than 5~20℃
DC power supply | Voltage continuously adjustable from 0 to 50V, maximum current 500A
2025.10.23
Completed the equipment acceptance
The EP equipment was placed in Zhongshan, and has currently conducted polishing experiments on several single-cell cavities. EP equipment can accommodate the polishing of 1.3GHz 9-cell bare cavities, helium cavities, and 1.5m long cavities.

## Slide 10
HPR + Ultrasonic Cleaner
Device Name | HPR
Parameter | Indicator
Effective cleaning length | ＞1300mm
Boom pressure resistance | ＞150bar
Other pipelines under pressure | ＞120bar
Boom rotation speed | 4-20rpm
Spray boom vertical movement speed | 5-500mm/min Adjustable
Load | ≥500kg
Protection level | IP67
Matching filter | Filtration 0.01um accuracy
Matching nozzle | Nine 0.6mm holes
Cleanliness level | Better than ISO-5 (Class 100)
Control method | Automatic/Manual
HPR
Ultrasonic Cleaner

## Slide 11
Vacuum furnace (furnace body、vacuum pump unit、nitrogen filling system、power distribution system and water cooling system), Class 100 cleanroom.
Furnace body area
Front furnace door
Cooling water tank
Vacuum pump unit
Distribution System
Device Name | Vacuum baking oven
Parameter | Indicator
Effective heating area | 0.6m0.6m1.5m
Highest Temperature | ≥1200℃
Operating Temperature | 50-1100℃
Total power | ≥220kW
Heating power | ≥180kW
Temperature control accuracy | ±1℃
Leakage rate | < 110-10Pa m3/s
Cryogenic extreme vacuum (room temperature) | < 210-6Pa
Vacuum level before heating | Long-term suction 510-6Pa
High-Temperature Extreme Vacuum (900℃) | < 310-5 Pa
Pressure rise rate | < 0.05 Pa/h
Temperature uniformity (holding at 900℃) | < ±3℃
Heating and cooling rate | 1℃/min-10℃/min adjustable
Low vacuum pump | Roots Pump +Dry Screw Pump
High vacuum pump | Molecular pump,+cryogenic pump
Maximum furnace load | ＞600kg
Device Name | Vacuum baking oven
Parameter | Indicator
Effective heating area | 
Highest Temperature | ≥1200℃
Operating Temperature | 50-1100℃
Total power | ≥220kW
Heating power | ≥180kW
Temperature control accuracy | ±1℃
Leakage rate | 
Cryogenic extreme vacuum (room temperature) | 
Vacuum level before heating | 
High-Temperature Extreme Vacuum (900℃) | 
Pressure rise rate | < 0.05 Pa/h
Temperature uniformity (holding at 900℃) | < ±3℃
Heating and cooling rate | 1℃/min-10℃/min adjustable
Low vacuum pump | Roots Pump +Dry Screw Pump
High vacuum pump | Molecular pump,+cryogenic pump
Maximum furnace load | ＞600kg

## Slide 12
preliminary experiment on 1.3GHz single cell

## Slide 13
EP
BCP 60
Out BCP 10
900℃ 3h baking
EP 30
VT
EP 200(acid T=10℃)
OITC
IASF
1.3GHz Single cell surface-treatment
900℃ 3h baking
EP 30 (acid T=7℃)
VT
PR-SCTF-SRFC:CAVD-002
Treated by OITC
Treated by IASF
CAVD-002 single cell cavity was treated by OITC. After EP, small pits were found at the welds, then a 60-micron BCP polish was performed. The cathode rod is wrapped with a PTFE porous tube and an additional mesh membrane;

## Slide 14
EP (acid T=10℃)
Out BCP 16
900℃ 3h baking
EP 60 (acid T=7℃)
VT
EP 30 (acid T=7℃)
VT
1.3GHz Single cell surface-treatment
PR-SCTF-SRFC:CAVD-008
Number | Polishing thickness | beamtube Average | Cell Average | Max Polishing Thickness | Min polishing thickness | Max/min
1 | 115 | 127.67 | 84.83 | 145 | 62 | 1.84
2 | 40 | 48.3 | 32 | 57 | 30 | 1.9
3 | 61 | 65.67 | 45.5 | 79 | 40 | 1.975
alcohol ultrasonic cleaning 1h and FM20 ultrasonic cleaning 3h;
alcohol ultrasonic cleaning 24h;
The cathode rod is wrapped with PTFE raw sealing tape at the part corresponding to the beamtube,but the polishing thickness effect of the beamtube and cell part is not very good.
300℃ 3h
Waiting for VT
900℃ 3h

## Slide 15
EP (acid T=10℃)
900℃ 3h baking
Out BCP 10
EP 30 (acid T=7℃)
Waiting for VT
1.3GHz Single cell surface-treatment
BJ-01、BJ02
cavity | Polishing thickness | beamtube Average | Cell Average | Max Polishing Thickness | Min polishing thickness | Max/min
BJ-01 | 200 | 197.5 | 145.3 | 214 | 147 | 1.68
BJ-02 | 200 | 212.9 | 150.76 | 229 | 136 | 1.68
The cathode rod is wrapped with a PTFE porous tube and an additional mesh membrane , and the polishing thickness effect of the beamtube with cell part is better.BJ-01 and BJ-02 citvities are waiting for VT.

## Slide 16
Summary

## Slide 17
Summary
We have basically completed the construction of the surface treatment platform and have carried out surface treatment on several single-cell cavities.
We plan complete the optimization and solidification of the surface treatment process and technology this year. We plan to achieve an production capacity of 40-50 cavities per year.
Future Process Optimization
  We plan to develop vibration equipment to perform ultrasonic vibration desulfurization on superconducting cavities.
  Change the temperature difference between the spray water and acid, and study the effect of the temperature difference on the polishing uniformity.
  Our endoscope has just passed inspection, and we will subsequently add endoscopic examinations before and after EP.

## Slide 18
THANK YOU
深圳市光明区新湖街道
荔湖西路618号
No. 618, Lihu West Road, Guangming District,
Shenzhen, Guangdong, P.R.China