## Slide 1: Update: Enhancement of medium-temperature heat-treated 1.3 GHz SRF cavities for high quality and high gradient
Julia Goedecke for the complete SRF team
TTC 2026, 9.–12. June 2026

## Slide 2: What is new since SRF 2025 in Tokyo?
additional data on mid-T treated cavities with long l
New data, furnace upgrade

## Slide 3: What is new since SRF 2025 in Tokyo?
additional data on mid-T treated cavities with long l
mid-T with soft reset of 900°C
New data, furnace upgrade

## Slide 4: What is new since SRF 2025 in Tokyo?
additional data on mid-T treated cavities with long l
mid-T with soft reset of 900°C
mid-T heat treatment of a nine cell cavity
New data, furnace upgrade

## Slide 5: What is new since SRF 2025 in Tokyo?
additional data on mid-T treated cavities with long l
mid-T with soft reset of 900°C
Nb furnace upgrade
mid-T heat treatment of a nine cell cavity
New data, furnace upgrade

## Slide 6: Characterization of heat treatments
calculated oxygen diffusion length ldif
ldif ;
useful parameter for comparing/characterizing heat treatments
difficult to specify an exact temperature for a given duration with profiles not showing a plateau
heating/cooling ramp is not taken into account when only temperature or time is given
Compare heat treatments using the calculated oxygen diffusion length ldif

## Slide 7: Mid-T heat treatment of 1.3 GHz single cell cavities
diffusion length l in the range of 3500 nm < l < 4000 nm
  translate in approx. 350°C for 4h to 4½h
due to the relatively long l -> decrease in cO in the RF layer, which may result in a decrease of the anti-Q-slope
HFQS can be observed
Cavities with long diffusion length ldif showing HFQS
T = 2 K

## Slide 8: Mid-T heat treatment of 1.3 GHz single cell cavities
HFQS can be observed
usually no breakdown of the cavities compares to mid-T heat treated cavities with l < 2500 nm
still have an improvement with the benefit that the cavities don’t quench
T = 2 K
T = 2 K
Cavities with long diffusion length ldif showing HFQS and no quench

## Slide 9: Enhancement of mid-T heat treated single cell cavities
selecting cavities that showed HFQS after a mid-T heat treatment
applying additional low-T
improvement in the performance for high gradients
old data with l showing HFQS starting at 3500 nm
T = 2 K
T = 2 K
With additional low-T heat treatment

## Slide 10: New mid-T data with long diffusion length ldif
additional new data: 1RI12 (fine grain) & 1Z13 (medium grain)
1RI12 HFQS appears already with a ldif of 2500 nm (approx. 330°C for 3½h)
1Z13 a hint of an HFQS is observed
  consists of MG niobium material from a completely different niobium supplier
  cleanliness of the niobium RF surface of this new cavity is still relatively low
  reflected in the increased annealing pressure 𝑝max = 3.7 · 10−5 mbar (usually 10−7 mbar)
  how pressure during heating affects performance is subject of ongoing research
T = 2 K
1RI12: HFQS with ldif =2500 nm, 1Z13: hint of HFQS

## Slide 11: RBCS resistance of mid-T heat treated cavities
Upward trend of RBCS with increasing ldif
mid-T heat treatments affect the RBCS resistance
  generally lower than RBCS of baseline treated cavities (above 8 nΩ)
  correlation can be observed between the diffusion length and the RBCS
    upward trend of RBCS for ldif > 740 nm
T = 2 K

## Slide 12: RBCS resistance of mid-T heat treated cavities
mid-T heat treatments affect the RBCS resistance
  generally lower than RBCS of baseline treated cavities (above 8 nΩ)
  correlation can be observed between the diffusion length and the RBCS
    upward trend of RBCS for ldif > 740 nm
  new data also fits in very well
    2x800°C -> mid-T
    4x900°C -> mid-T
T = 2 K
Upward trend of RBCS with increasing ldif is also consistent with new data

## Slide 13: Mid-T heat treatment of single cell with 900°C as soft reset
Better performance than an 800°C soft reset
first 900°C soft resets on 1RI01, 1DE11, 1DE04, & 1RI13
soft resets at 800 °C versus 900 °C followed by mid-T heat treatment with similar oxygen diffusion lengths
better performance can be observed in 𝑄0 in each case
T = 2 K

## Slide 14: Mid-T heat treatment of single cell with 900°C as soft reset
first 900°C soft resets on 1RI01, 1DE11, 1DE04, & 1RI13
soft resets at 800 °C versus 900 °C followed by mid-T heat treatment with similar oxygen diffusion lengths
better performance can be observed in 𝑄0 in each case
T = 2 K
Better performance than an 800°C soft reset

## Slide 15: Mid-T heat treatment of single cell with 900°C as soft reset
first 900°C soft resets on 1RI01, 1DE11, 1DE04, & 1RI13
soft resets at 800 °C versus 900 °C followed by mid-T heat treatment with similar oxygen diffusion lengths
better performance can be observed in 𝑄0 in each case
still unclear: no HFQS for long diffusion lengths for a 900°C reset
T = 2 K
Better performance than an 800°C soft reset

## Slide 16: The residual resistance Rres
why do 900°C+mid T perform better than the 800°C+mid T ?
decreasing the Rres for 900°C+mid T instead of 800°C+mid T
  Rres is below 2 nΩ
  pinned magnetic flux affects Rres
    grain boundaries and dislocations can pin the magnetic flux
    by heating grain expand and a reduction of grain boundaries and dislocations
Low resistance for mid-T heat treated cavities with a 900°C soft reset

## Slide 17: Mid-T heat treatment of a nine cell cavity
still needs improvement
improvement after mid-T
expected behavior with long l
  a weak anti-Q slope at higher accelerating gradients (at ~20 MV/m)
but no HFQS is apparent
RBCS between 6 nΩ and 8 nΩ; Rres 2.3 nΩ
temperature gradient in furnace
effect of the treatment less pronounced than for single cell cavities, optimization of the furnace is necessary
T = 2 K
T = 2 K

## Slide 18: Nb retort furnace
temperature gradient
due to heat dissipation through the mechanical connection via furnace flange
  350°C recipe max gradient of ca. 50°C between TR 1 & TR 3
  800°C recipe max gradient of ca. 10°C between TR 1 & TR 3

## Slide 19: Nb retort furnace
Upgrade
TR 1
TR 2
TR 3
TS 1
TS 2
temperature gradient
control loop for the heaters is currently running only through TS2
independent control loops for H1 and H2
additional temperature sensors to map whole length
heater 1
heater 2
gas inlet
temperature gradient

## Slide 20: Nb retort furnace
Upgrade
TR 1
TR 2
TR 3
TS 1
TS 2
temperature gradient
control loop for the heaters is currently running only through TS2
independent control loops for H1 and H2
additional temperature sensors to map whole length
heater 1
heater 2
gas inlet
temperature gradient
gas inlet
oxidation of the surface using clean oxygen rather than air
venting the furnace with gas mixture: O/N, O/Ar

## Slide 21: Summary & Outlook
new mid-T data
fit very well into the existing data
mid-T with soft reset of 900°C
Improvement compared to 800°C
  low Rres was found
mid-T heat treatment of a nine cell cavity
more mid-T nine cell to coming soon
on a good way
Nb furnace upgrade
independent control loops for H1 and H2
venting the furnace with gas mixture: O/N, O/Ar

## Slide 22: Thank you for you attention! Questions?