## Slide 1
Marc Wenskat on behalf of the SRF R&D Team
9.6.2026 - TTC Meeting @ CEA-CNRS-Université Paris Saclay
f-shift properties
as indicator for SRF performance

## Slide 2: fvT has become a standard measurement at DESY
Record S21 resonance spectrum with SA while warming up
  Postprocessing: fit curve with Lorentz distribution
  Also obtain Q0
Contains information on impurity content in rf penetration depth
For this study:
  11 standard treatments (120°C, 800°C, EP as last treatment before test)
  21 midT
  3 midT/lowT
max. P
Not „real“ f0
f0
max. P
Method paper:
[R. Ghanbari et al., arXiv:2604.22596]
Reduced noise around Tc

## Slide 3: Different mfp ℓ in δ vs. λ depth
identity line
Mid-T: near-surface higher concentration of interstitials

## Slide 4: Quenchfield scales with mean free path

## Slide 5: Observation: small dip in Q0 as well
Significant in only two cavities – but which had the largest dip in f → otherwise Q0 dip too small to be outside 3σ
T / K
T / K
T / K
∆f / kHz
∆f / kHz
∆f / kHz
∆f / kHz
Q0
Q0
Q0
Q0

## Slide 6: First comparison with theory is promising
Collaboration with F. Herman
[A. Lebedeva, et al. Physical Review Applied 24.4 (2025): 044007]
250°C treatment differs

## Slide 7: Predictions of dip properties within reasonable limits
Collaboration with F. Herman
AverageN=17 -0.168 ± 0.005
[A. Lebedeva, et al. Physical Review Applied 24.4 (2025): 044007]
Higher concentration of interstitials
T
f
Prediction: = -0.167
Assumption: Dip is symmetric

## Slide 8: fvT with QPR on mid-T treated sample
Dip depth Δf scales with f as model predicts
433 MHz
866 MHz
1300 MHz
2.4 kHz
4.3 kHz
6.4 kHz
Expect:
↔
↔
↔

## Slide 9: Zimmermann BCS: calculation of optical and AC conductivity (RLC circuit)
Disorder in midT too significant to be described by mean-field / „weakly polluted material“ BCS
[F. Bolle, O. Saritas, M. Scheffler et al., arXiv:2602.15003]
[O. Saritas, BSc Thesis, U Stuttgart (2024)]
T / K
T / K
Q0
Q0
∆f / kHz
∆f / kHz
Data
Fit
Data
Fit
Fits okay-ish
  Tc, Δ and σnc are material fit parameters
Intrinsic dip already appears (if σnc < σnc,0 )
Data
Fit
Data
Fit
Modify RLC circuit by adding Tc reduced regions
Based on R. Vagglio & on our microscopic model
[R. Ghanbari et al., TTCMeeting 2023 @ FNAL]

## Slide 10: Conclusion
fvT contains relevant information on material properties within RF penetration depth
Correlation studies „alone“ result in findings as fvT is probing the same volume as QvE
But as f and Q0 are linked by theory, this is also expected → predictive power & model building of fvT
Working with two models to analyze RF response – they are congruent to each other
  Model starts to gradually deviate from data if impurity levels becomes „too large“
  Need additional disorder than „regular“ inhomogeneity to work with our dips

## Slide 11
Marc Wenskat / MSL
marc.wenskat@desy.de
Questions?
Thanks…
to you for listening / your patience
to the conveners to invite me
to the students who did the work
to BMFTR for funding (05H24GU1, 05K25GU3)
Darian Holfert
BSc Student
Rezvan Ghanbari
PhD Student
Carl Weiss
MSc Student
Ozan Saritas
MSc Student
Looking for a position

## Slide 12: Dip depth
Collaboration with F. Herman
Average is -0.133 ± 0.014
Weighted average is −0.168 ± 0.005
−0.167
[A. Lebedeva, et al. Physical Review Applied 24.4 (2025): 044007]
1
=

## Slide 13: Dips in Q0 within 3σ noise floor
Clear trend for all midT treated cavities: Tc from Q0 is always smaller as from f for mid-T
→ Maybe no significant dip, but as a consequence rise in Q0 happens at lower T compared to f

## Slide 14
Microscopic model for disordered superconductor
An increased oxygen concentration reduces Tc of Nb by 0.93K per 1 at.%
- to have a dip minimum at 9.1K we would need ≈ 0.2 at.%
    - „end of dip“ around 8.9K ≈ 0.3 at.%
Solubility limit of O in Nb is 1 at.% @ 500°C and 0.33 at.% at 145°C
We have shown that C diffusion speed in Nb along GB vary with GB orientation, increasing disorder by spatially varying concentration
→ Assume same is true for O: not homogenous distributed within the rf layer, but clusters with uneven O-concentration
→ Expect non-constant (gaussian shaped) Tc reduction
→ Lowest Tc equal to the max. at.% concentration at RT (≈ 0.33 at.%)
→ Only locally saturated – not globally. If SIMS spot size ≈ multiple grains, obtained cO below saturation limit
[Desorbo, W. Phys. Rev. 132 (1963): 107.]
[Kolchin, O.P., et al. Soviet Atomic Energy 45 (4) (1978): p999.]
[Benvenuti, C., et al. 10th SRF (2001): p441.]
[Dangwal Pandey, A., et al. Appl. Phys. Lett. 119(2021): 194102]
Notes: 1nm Nb2O5 can easily saturate several hundred nm of Nb!

## Slide 15
Disordered superconductor show dip
[Barra, M., et al. SUST 18.3 (2005): 271.]
T
Tc,Nb
j
Skin depth
Mathematically speaking, the geomtery constant Γ is not constant
Dip properties cluster distribution causing current redistribution
Observed: Q vs. T still increases at 9.27K
→ Dip caused by clusters and not homogenous O-enriched Nb-layer
Tc < Tc,Nb
Tc < Tc,Nb
<Tc>

## Slide 16
What information is encoded in f vs. T?
T
Tc
j
Skin depth
Frequency shift is sensitive to interstitial concentration
(equation valid for dirty limit)
Δftot for EXFEL type cavities is typcially 5-6 kHz
Mid-T: more interstitials → larger Δf, but yet no dip