## Slide 1: Extending High-Q / High-Gradient Processing to a Novel SRF Cavity Geometry: The Barrel Cell Cavity
Daniel Bafia1, Alexej Grudiev2, Simon Barriere2, Robin Betemps2, Thomas Demaziere2, Alex Netepenko1, Tim Ring1, Davida Smith1
1FNAL, Batavia, USA; 2CERN, Geneve, Switzerland;
June 6, 2026
FERMILAB-SLIDES-26-0089-SQMS-TD
TTC'2026, CEA-CNRS-Universite Paris Saclay

## Slide 2: Extending High-Q / High-Gradient Processing to a Novel SRF Geometry
Barrel Cell Cavity Prototype
Barrel Cell Cavity (BCC)
Developed at CERN1 as an ultra-low-R/Q cavity concept to mitigate beam-loading effects in future accelerators
2 GHz non-TESLA SRF cavity with a large aperture and extended cell length
Requires: operation at high stored energy  high sustained Bp
  Goal: Bp = 200 mT
1A. Grudiev and T. Mastoridis, CERN-ACC-2021-0008, CLIC-Note-1173 (2021).
Can high-Q/high-gradient processing be successfully transferred to this cavity?
R/Q ~ 2 Ω

## Slide 3: Selecting a High-Performance Processing Strategy for the BCC
Large statistics of TESLA-shaped, 1.3 GHz single-cells achieving Bp > 200 mT
Optimized EP + 120C baking on HB 650 MHz
V. Chouhan et al., NIMPRA 1051, 168234 (2023)
D. Bafia, PhD Thesis, IIT, 2020
Cold EP + 75/120 C Modified LTB on 1.3 GHz
Bp = 200 mT
Multiple HB 650 MHz single-cells demonstrate Bp > 200 mT
Bp = 200 mT
Chosen processing strategy: Cold EP + 75/120°C modified bake

## Slide 4: Preparing the BCC for High-Gradient Processing
BCC Processing Required New Infrastructure
Custom electropolishing tooling
Dedicated cavity support fixture
VTS preparation
Applied Surface Treatments
120 um bulk EP
800 C x 3 hr degas in UHV
40 um final EP
Assembly, HPR, evacuation
75 C x 4 hr + 120 C x 48 hr in situ LTB

## Slide 5: Developing an EP Strategy for the BCC
EP development activities
Custom drip tray for BCC dimensions
Full-scale 3D printed cavity mockup for cathode position studies
Thank you to Tim Ring and Davida Smith for EP work
Uniform material removal achieved after 120 μm bulk EP (<50 μm wall-thickness variation)
3-D Printed Mockup for Cathode Positioning
Bulk EP Setup
US Thickness Measurements Pre/Post Bulk EP
Challenge #1: Single prototype
Challenge #2: Uniform material removal required to preserve cavity rotational symmetry

## Slide 6: Applying the Cold EP + Modified Bake Treatment
40 um EP final removal
30 um @ ~22 C
10 um @ 12 C
HPR, assembly, & evacuation
Bake at 800 C x 3 hrs in UHV
75/120 C modified low temperature baking

## Slide 7: First BCC Test Demonstrates Successful Processing Transfer
T = 2 K
Q0 > 1.5e10 at all fields
Quench at 164 mT (U = 12 J)
No x-rays/FE/Mping
  Due to low Esurf/Bsurf
Q0 of BCC Post Cold EP + 75/120 C

## Slide 8: First BCC Test Demonstrates Successful Processing Transfer
T = 2 K
Q0 > 1.5e10 at all fields
Quench at 164 mT (U = 12 J)
No x-rays/FE/Mping
  Due to low Esurf/Bsurf
T = 1.44 K
Q0 > 1e11 at moderate Bp
Quench at 197 mT (U = 17.3 J)!
No x-rays/FE/MPing
Q0 of BCC Post Cold EP + 75/120 C
Near 200 mT operation achieved without field emission or multipacting in the first test.

## Slide 9: Benchmarking BCC Against In-Situ Baked TESLA Cavities
Q0 vs Bp of Cavities with Various f0 Post Cold EP + in situ Baking
BCC 2 GHz
Quench at 1.45 K for 2 GHz BCC

## Slide 10: Benchmarking BCC Against In-Situ Baked TESLA Cavities
Q0 vs Bp of Cavities with Various f0 Post Cold EP + in situ Baking
BCC 2 GHz
TESLA 1.3 GHz
TESLA 2.6 GHz
Cold EP + in-situ bake demonstrates robust performance across multiple f0 and geometries.
BCC falls within envelope established by in-situ baked 650 MHz – 2.6 GHz cavities
Similar Q0 to 1.3 GHz TESLA cavity
  G = 446 Ω enables Q0 comparable to 1.3 GHz cavities despite f0 = 2 GHz
Quench of ~200 mT is within common range of quench fields for cold EP + in situ baked cavities
TESLA 650 MHz
Quench at 1.45 K for 2 GHz BCC

## Slide 11: Comparing RBCS Across f0 and Geometries
RBCS vs Bp of Cavities with Various f0 Post Cold EP + in situ Baking
BCC RBCS(Bp) follows similar field dependence observed in TESLA cavities
BCC 2 GHz
TESLA 1.3 GHz
TESLA 2.6 GHz
TESLA 650 MHz
Notes: If the BCC geometry introduced a new loss mechanism, we would expect either the field dependence or the frequency scaling of 𝑅_𝐵𝐶𝑆to deviate from the TESLA cavity trend. We do not observe either, so our treatment likely worked the first time

## Slide 12: Comparing RBCS Across f0 and Geometries
BCC RBCS(Bp) follows similar field dependence observed in TESLA cavities
Consistent with f0 scaling expectations
No geometry dependence
RBCS vs Bp of Cavities with Various f0 Post Cold EP + in situ Baking
M. Martinello et al. PRL 121, 224801 (2018)
Same underlying RF loss mechanisms govern performance
BCC 2 GHz
TESLA 1.3 GHz
TESLA 2.6 GHz
TESLA 650 MHz
Notes: If the BCC geometry introduced a new loss mechanism, we would expect either the field dependence or the frequency scaling of 𝑅_𝐵𝐶𝑆to deviate from the TESLA cavity trend. We do not observe either, so our treatment likely worked the first time

## Slide 13: Comparing Rres Across f0 and Geometries
At 2 GHz, residual estimates include a non-negligible BCS contribution
Estimated Rres of BCC comparable to similarly treated cavities
  Nearly identical behavior with Bp for 650 MHz – 2 GHz cavities
No evidence of excess residual losses from the BCC geometry
Rres vs Bp of Cavities with Various f0 Post Cold EP + in situ Baking

## Slide 14: Conclusions
High-Q/high-gradient processing successfully transferred to the 2 GHz Barrel Cell Cavity
Field-emission-free operation achieved on the first processing and test campaign
sustained to 164 mT at 2 K; quench field reached 197 mT at 1.45 K
Both RBCS and estimated Rres remain consistent with established data and scaling laws
No evidence that the non-TESLA cavity geometry introduces new RF loss mechanisms
Takeaway:
The same RF loss mechanisms that govern TESLA cavities appear to govern the BCC, demonstrating that advanced SRF processing can be successfully extended across both frequency and cavity architecture.

## Slide 15: Acknowledgements
Alexej Grudiev (CERN) for initiating the collaboration, providing the Barrel Cell Cavity prototype, and valuable technical discussions throughout the project.
Tim Ring and Davida Smith for development and execution of the electropolishing campaign.
Fermilab SRF Processing, Assembly, and Vertical Test teams for cavity preparation and RF testing support.
This work was produced by Fermi Forward Discovery Group, LLC under Contract No. 89243024CSC000002 with the U.S. Department of Energy, Office of Science, Office of High Energy Physics. Publisher acknowledges the U.S. Government license to provide public access under the DOE Public Access Plan DOE Public Access Plan

## Slide 16: Thank you!

## Slide 17: Backup

## Slide 18: Cavity Metric Calculations
From simulations
Accelerator definition of R/Q:
Simulated Cavity Parameters
Circuit Definition
Qext1 = 1.6e10
Qext2 = 1.6e11
Measured Antenna Q’s

## Slide 19: 380 GeV CLIC DR parameters (PRAB22, 091601)
Parameter of DR |  | value | unit
Energy | E | 2.86 | GeV
Circumference | C | 373.7 | m
Revolution frequency | f0 | 802 | kHz
RF frequency | fRF | 2 | GHz
Harmonic number | h | 2493 | 
Energy loss per turn | eVA | 5.8 | MeV
RF voltage | VC | 6.5 | MV
RF stable phase | φ | -26.8 | o
Bunch population | Ne | 5.7 | 1e9
Number of bunches per train | Nb | 352 | 
Number of trains | Nt | 1 | 
Peak beam current | Ib | 1.8 | A
Strict specifications on the bunch spacing variation: δφb < ±1o at 2 GHz (±400μm) for Luminosity loss < 1% (CLIC-Note-1138)
This is difficult to maintain due to strong transient beam loading effects caused by large difference between peak and average beam power values of 10.4 MW and 1.5 MW, respectively
1%
±400μm
A. Grudiev, LCWS’25