## Slide 1: Investigating Impurity-Based Treatments in SRF Cavities through Coupled RF and Materials Characterization
Hannah Hu, Young-Kee Kim, Daniel Bafia
University of Chicago, Fermi National Accelerator Laboratory
June 9, 2026
FERMILAB-SLIDES-26-0058-TD

## Slide 2: Previous Work Comparing Interstitial O and N
RBCS Dependence on Impurity Concentration
10× difference in concentration
Key Takeaways
N and O perform similar roles: Increasing O/N concentration decreases RBCS
N appears 10× more effective than O in reducing RBCS

## Slide 3: Decoupling the Effects of ℓ and Δ on BCS Resistance
Optimization in ℓ
No change in Δ
No change in ℓ
Increase in Δ
Simultaneous change in ℓ and Δ
Different impurity profiles reduce RBCS through different mechanisms
O concentrated near the surface  ℓ optimization
Highly uniform profiles (200 °C x 20 h and N doped)  Δ enhancement
EP
EP
EP
200 °C Baked
120 °C Baked
N Doped

## Slide 4: Surface Engineering For High Q0 and High Eacc
Proposed impurity profile:
Uniform concentration of impurities  Δ Enhancement
Increased concentration in first 100 nm  ℓ optimization and increase in Eacc
Progress towards surface engineered Nb: Co-doping
Co-doping treatments contain both oxygen and nitrogen
Leverage the different diffusion coefficients and activation energies to independently tune N and O concentrations
Co-doping treatment recipe
Start with a treatment that has a uniform concentration (N Doping, Mid-T) as a base
Tune ℓ by adding oxygen without significant change to base concentration

## Slide 5: Co-doping Treatments
Treatment | Recipe | Cavity
N Infused | 800 °C x 3 h + 120 °C x 48 h w/ N2 | TE1PAV012
Mid-T + HF | 340 °C x 2.5 h in-situ + 2 HF | TE1RI015
Mid-T + HF + LTB | 340 °C x 2.5 h + 2 HF + 120 °C x 48 h in-situ | 
N Doped | 3/60 + 10 um | TE1RI006
N Doped + Mid-T* | 3/60 + 10 um + 340 °C x 2.5 h in-situ | 
Goals
Combine oxygen and nitrogen in a controlled manner
Use single impurity models to predict cavity performance from sample material characterizations
* Sample study in progress, used individual N-Doped and Mid-T profiles as an approximation

## Slide 6: ToF-SIMS Depth Profiles
Oxygen Depth Profile
Nitrogen Depth Profile
Independently tune oxygen and nitrogen to achieve layered impurity profiles
Confirmed co-doping effect with presence of both oxygen and nitrogen
Background N

## Slide 7: Predicting Cavity Performance
Combine O + N assuming a simple additive model
RBCS Dependence on Impurity Concentration
Predicted ΔRBCS from Impurity Concentration

## Slide 8: Co-doping: Cavity Performance
Q0 vs. Eacc
RBCS vs. Eacc
16 MV/m
Experimental ΔRBCS

## Slide 9: Predicted vs. Cavity Experimental Values
Correlation Plot
Predicted vs. Experimental ΔRBCS
Additive effect in the reduction in RBCS from both O and N

## Slide 10: Conclusion
Key Takeaways
Co-doping is a promising strategy for reducing RBCS beyond single-impurity limits
Simple additive effect with both O and N
Quantitative impurity profiling can serve as a reliable predictor of RF performance
Further work
Use material characterizations as a guide to further optimize co-doping treatments
Impurity-based predictive modeling in search for alternative impurities

## Slide 11: Thank you!
Acknowledgments: Damon Bice, Vijay Chouhan, Adam Clairmont, Andrew Cravatta, Jae-Yel Lee, Akira Miyazaki, Akshay Murthy, Alexandr Netepenko, Tim Ring, and Davida Smith

## Slide 13: Oxygen vs. Nitrogen
RBCS vs. Eacc
Nitrogen Concentration Depth Profile
Oxygen Concentration Depth Profile