## Slide 1: TTC 2026 WG3-Session 2a
Daniele Sertore INFN Milano - LASA

## Slide 2
Q1. Material:
What is the request for materials which will be used for high pressure vessel? (ex. Mechanical property)
Nb300: see Project Specific
Nb-Ti: NbTi55
Ti: TiGr2
RRR 300 mechanical properties | 
Tensile strength, Rm | > 140 N/mm2 *
Yield strength, Rp 0.2 | 50 < Rp 0.2 < 100 N/ mm2 *
Elongation, AL 30 | ≥ 30 % *
Hardness, HV (min. load 10 N) | ≤ 60
    ESS Nb Specifications
    MECHANICAL PROPERTIES (DIN 50125, DIN EN 10002, DIN EN ISO 6507)
PIP-II Nb Specifications
Mechanical requirements
The final product shall conform to the mechanical properties at room temperature given in Table, defined as per ASTM E-8 and E-384. Where applicable, values given by this specification supersede or add to the requirements of ASTM B393 Annex A1.
Manufacturer shall note that any mechanical anisotropy may be amplified by the intrinsic mechanical anisotropy of niobium itself, i.e. up to a factor of 2 for some properties. Residual texture could produce poor forming and polishing characteristics.
3.9 GHz Eu-XFEL Nb Specifications
Mechanical properties (according to DIN 50125, DIN EN10002, DIN EN ISO 6507)
RRR 300 mechanical properties |  |  | 
 | ASME B393 | Minimum Acceptance | Desired Acceptance
Ultimate Tensile strength, Rm | 95 MPa min | 95 MPa < Rm < 175 MPa | 
Yield strength, Rp 0.2 | 50 MPa min No max | 50 MPa < Rp 0.2 < 95 MPa | 
Elongation, AL 30 | 30 % min | 30 % longitudinal min 30 % transverse min | 50 % longitudinal min 50 % transverse min
Hardness, HV (min. load 10 N) | Average < 60 | Average < 60 | Average < 50
RRR 300 mechanical properties | 
Tensile strength, Rm | > 140 N/mm2 *
Yield strength, Rp 0.2 | 50 < Rp 0.2 < 100 N/ mm2 *
Elongation, AL 30 | ≥ 30 % *
Hardness, HV (min. load 10 N) | ≤ 60

## Slide 3
Q2. Pressure test:
What kind of pressure test are required? And how much is the pressure?
Test with pressurized Nitrogen
PED: 1.43*MAWP
ASME/FNAL: 1.15*MAWP
Project | MAWP | Pressure test (barg) | Directive Regulation
3.9 GHz Eu-XFEL | 4 | 5.72 | PED Category IV
ESS | 1.04 | 1.5 | PED Art. 4.3
PIP-II | 2.05 | 2.38 | ASME
Q3. Industrialization:
How to harmonize each regions/country (how industries comply to foreign pressure vessel codes)?
For 3.9 GHz, external notify body “TUEV Nord” required by Category IV
For PED art. 4.3 and ASME, vendor takes care of the whole qualification process.

## Slide 4
Q4. Welding:
Which kind welding test requested?
3.9 GHz PED Category IV, we followed DESY qualification process with PMA (Particular Material Appraisal) and test pieces (TUEV-Nord).
PED article 4.3: Sound Engineering Practice (SEP)
ASME: where applicable ASME Boiler and Pressure Vessel Code, and/or the ASME B31.3-2014 piping code. X-Ray on Ti-Ti weld of pressure bearing part where applicable.
Q5. Testing:
What kind of tests are required for the completed high pressure vessel?
Category IV: welding test, pressure test
PED article 4.3: pressure test
ASME: X-ray of welding on tank Ti-Ti weld of pressure bearing part where applicable and pressure test