## Slide 1: Challenges with production of HOM Couplers for Hi-Lumi
June 9th, 2026
Naeem Huque
Notes: Tip: Keep titles under 60 characters for readability
To change the photo: Right-click on photo and select change photo

## Slide 2: OUTLINE
Introduction
Design and Fabrication
Raw Materials
E-Beam Welding
Vacuum Brazing
Acceptance Testing
Summary
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 3: INTRODUCTION
Horizontal HOM Dampers (HHOMs) for the HL-LHC RFD crab cavities are fabricated at JLab
HHOMs are installed on jacketed cavities, which are tested and qualified at JLab
Fabrication is conducted as per CERN specification documents and quality requirements
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 4: DESIGN
DN40 BRAZE
DN100 BRAZE
SS HELIUM JACKET
TEE EBW
HOOK EBW
TEE
HOOK
LID EBW
INNER CAN
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 5: FABRICATION
DN100 Brazement
DN40 Brazement
Hooks/Tees
Inner Can Assembly
Hook and Tee Weldment
Final Assembly
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 6: JLAB FACILITIES
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 7: RAW MATERIAL - NIOBIUM

## Slide 8: RAW MATERIAL
Niobium procurement QA/QC was stringent but ultimately worthwhile
Niobium (RRR > 300)
Bought in three forms:
  Plate
  Rod
  Seamless Tube
Ultrasonic Testing (UT) on all pieces
Chemical analysis, mechanical testing, and UT for plates carried out at Nb vendor
UT for rods and tubes carried out at third-party vendor in the US
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 9: HOW TO BUILD A TUBE
NDT
Cutting
Forming
Metrology
EBW
NDT
Machining
Die Design
WPS/WPQR
Metrology
Nb Sheet
Raw material is cheap
Subsequent processes are not
Procurement
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 10: HOW TO BUILD A TUBE
NDT
Machining
Metrology
Nb Tube
Raw material is cheap
Few fabrication steps
Procurement Experience:
Seamless tubes were purchased to test fabrication process
Three out of four tubes failed UT
Procurement
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 11: HOW TO BUILD A TUBE
Nb Rod
Raw material is expensive
Drops can be used for other parts
NDT
Machining
Machining
Metrology
Procurement
Wire EDM
Usable Drop
Strategy will depend on your facility and circumstances
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 12: ELECTRON-BEAM WELDING (EBW)

## Slide 13: EBW DEVELOPMENT
Prototype
Production
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 14: EBW DEVELOPMENT
Ensure sufficient raw material/parts for EBW development
Dedicate a dummy assembly if possible
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 15: EBW DEVELOPMENT
Initial tests did not account for the welding fixture acting as a heat sink
Samples should imitate heat dissipation as well as geometry
The weld begins at -20 degrees, upramps in-place over 0.5 seconds (yellow dot), dwells for 1 second, travels CCW to 180 degrees, then downramps over the next 180 degrees
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 16: EBW QUALIFICATION
Visual Test
Penetrant Test
Radiographic Test
Metallographic Test
Visual Test
Penetrant Test
Radiographic Test
Metallographic Test
Bend Test
Tensile Test
Spec = 0.400 mm
Spec = 0.400 mm
Acceptance Criteria: ISO 13919-2:2001 Level B
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 17: EBW METROLOGY
Serial No. | Gap | Parallelism
001 | 2.7 | 0.0
002 | 2.6 | 0.1
003 | 2.5 | 0.2
Serial No. | Hook Perpend. | Hook Position | Tee Position
001 | 0.3 | 0.3 | 0.2
002 | 0.2 | 0.2 | 0.8
003 | 0.3 | 0.5 | 0.9
Hook/Tee gap (2.5 – 3.1 mm) and parallelism are the most critical dimensions
Fixturing holds the gap, but allows the other end of the hook to drift
Parts still pass RF checks
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 18: VACUUM BRAZING
Stringent qualification process and 100% NDT makes for a robust process
Niobium brazed to 316 LN SS with OHFC wire
  Suggest 65/35 Cu-Ag for future applications
Qualification process included UT and Metallography
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 19: VACUUM BRAZING

## Slide 20: VACUUM BRAZING
Testing showed no significant degradation in RRR or mechanical properties of Nb arising from two-step brazing process
DN100 braze has wire added between two runs, to ensure full coverage
Nb RRR (Spec = 300) |  | 
Sample | Temperature | RRR
Baseline | None | 270
2 | 1040 C | 282
3 | 2X 1040 C | 286
Mechanical Properties |  |  |  |  | 
# | Temp | RP 0.2 (MPa) | RM (MPa) | Ag (%) | ABR (%)
1 | Baseline | 52.1 | 158.8 | 37.2 | 67.4
2 | 1X 1040 C | 48.3 | 136.0 | 27.8 | 35.6
3 | 2X 1040 C | 45.9 | 120.7 | 22.7 | 32.9
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 21: ACCEPTANCE TESTING
Warm RF measurements are used to validate the HHOM fabrication
A test box designed in collaboration with ODU, SLAC, and CERN
S21 in the 390 – 410 MHz range must be below < -61 dB
S21 in the 0.1 – 2000 MHz must be within CERN and AUP mask (bottom image)
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 22: TESTING AND CAVITY INTEGRATION

## Slide 23: CAVITY INTEGRATION – RFD02
HHOM Installed
HHOM Replaced
Installation of HHOM on jacketed cavity caused a drop in Q0
Replacing with a new unit recovered Q0
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 24: CAVITY INTEGRATION – RFD02
RF shielded gaskets must engage ‘lips’, not only seal vacuum
Drop in Q0 likely due to RF leakage through the shielded gasket
Similar effect seen on prototype cavities; torquing closed gaps and recovered Q0
HHOM also failed subsequent warm measurement
  Not capable of lowering Q, but can exacerbate leakage through seal
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 25: SUMMARY
HHOMs are complicated assemblies
Most early fabrication challenges have been addressed
More challenges will arise as cavity integration progresses
Lessons will be invaluable for future projects
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 26: QUESTIONS?
Notes: Before sharing your presentation, confirm:
Fonts are consistent
Images meet quality standards
Charts use template colors
Footer information is current
Spell check completed
Links are working
File size is optimized