## Slide 1
Development of In-Situ Plasma Processing Procedures with the Fundamental Passband on 1.3GHz Multi-Cell SRF Cavities at TRIUMF
William Stokes
TTC2026 – Paris-Saclay
June 11th, 2026

## Slide 2
Advanced Rare Isotope Laboratory (ARIEL) e-Linac
Three 1.3GHz 9-cell SRF cavities (10MeV/cavity) in two cryomodules
ARIEL cavities damp HOMs with beamline dampers, and lack HOM couplers – only fundamental passband available
In-situ plasma processing development underway for removing hydrocarbon-based field emitters
Beamline dampers on end half-cells
(P. Kolb, 2016)
William Stokes

## Slide 3
Developments Transferable to ARIEL Cryomodules
William Stokes
ARIEL prototype - 1.3GHz copper 7-cell
ARIEL mechanical mock-up FPC
On-line (warm):
Qext = 1
Q0 1
1

## Slide 4
William Stokes
RF Coupling
Two coupler positions were used for developing plasma processing methodology
Replicated warm coupling of on-line cryomodules
No bellow displacement; neutral FPC position
Extended bellows; warm ARIEL coupling
Comparable to warm on-line coupling
(Qext= 1 )

## Slide 5
Plasma Processing Schematic
Inline Gases
Power Meters (FWD & REV)
50 Load
Circulator
Amplifier
Combiner
20 dB Attenuator
Signal Generators
Vector Network Analyzer
Cavity
Directional Coupler
Scroll Pump
CDG-500 Capacitance Gauge
Scroll Pump
Ion Gauge
RGA 100
Turbo Pump
Leak Valves
Amplifier
Power Meter
(Pickup)
William Stokes

## Slide 6
Electric Field Distributions of Fundamental Passband Modes
Field profiles were measured for prospective plasma ignition sites
Ignition in 4 cells on pickup end of cavity
Must ignite in all cells for comprehensive cavity cleaning
2𝜋/7
4𝜋/7
5𝜋/7
6𝜋/7
William Stokes

## Slide 7
Plasma Sequence
TTC2026
Symmetric field distributions for plasma movement; modes reused for mirrored cell locations
Dual-tone excitation required for translating plasma between adjacent cells
RF attenuation through plasma permitted upstream ignition locations
6𝜋/7

## Slide 8
Dual-Tone Excitation for Plasma Movement
Combiner
Signal Generators
Cell #:
1
2
3
4
5
6
7
Mode:
6/7
2/7
4/7
5/7
4/7
2/7
6/7
SG1
SG2
William Stokes

## Slide 9
Plasma Translation
William Stokes

## Slide 10
Regulate Cavity Power
Measure Resonant Frequencies
Estimate Plasma Location
Instrument Control System
PCavity = PForward – PReflected
Frequencies increase when plasma ignited
From modal electric field distributions and frequency shifts
Target Power (PCav) to sustain
Measurement of resonant frequencies
William Stokes

## Slide 11
Gas Recipes
95/5 He/CH4 – Plasma Contamination
Cavity contaminated 30min/cell with 95/5 He/CH4 plasma prior to plasma processing experiments (inspired by JLab)
CH4 molecules dissociate in He dominated plasma
Ionized carbon and hydrogen species recombine, forming CXHY chains
Adsorbed and purged from cavity
95/5 He/O2 – Plasma Processing
Cavity processed with 95/5 He/O2 plasma until by-product saturation realized
Ionized He species accelerated across plasma sheath, incident on CXHY chains
Cracked CXHY chains recombine with ionized O2 species forming by-products (H2, H2O, CO, CO2)

## Slide 12
Inaugural Plasma Contamination
Qext = 9.5
140mTorr
RF ON
0.0 hours
95/5 75/25 He/CH4 from gas regulator issue
CH4 O2 ; H2 28 amu (C2H4, CO, N2) 44 amu (C3H8, CO2)
Processing & CXHY formation
William Stokes

## Slide 13
Inaugural Plasma Processing
Qext = 9.5
130mTorr
RF ON
0.0 hours
95/5 90/10 He/O2 from leak valve fault
O2 ; H2 H2O CO CO2
Processing
William Stokes

## Slide 14
Optimizing Plasma Density
Increasing the drive frequency grows plasma density by momentarily improving coupling
ionized species cleaning efficacy
At a maximum frequency tune, , the plasma will collapse
varied for modes and plasma-cell locations
Frequency-Tuning
Drive signal
*Tune*
f
1.
2.
3.
4.
*Tune*
William Stokes

## Slide 15
Warm ARIEL Coupling
(Contamination)
Qext = 1.2
182mTorr
Qext = 1.2
178mTorr
Near identical cavity pollutions
To test processing performance with frequency-tuning and without frequency-tuning
A
B
95/5 He/CH4
William Stokes

## Slide 16
Warm ARIEL Coupling
(Processing)
Not Frequency-Tuned
Qext = 1.2
181mTorr
Frequency-Tuned
0.8()
Qext = 1.2
182mTorr
Stronger by-product recombination signals
Reduced cleaning duration/cell
A
B
95/5 He/O2
William Stokes

## Slide 17
Contribution of H2, CO and CO2 to H2, 28 amu and 44 amu species likely reduced over consecutive cavity pollutions
By-product signals weakened over consecutive pollution trials
Contamination Trials
(He/CH4)
Reduction in processing reactions over He/CH4 trials

## Slide 18
Processing by-product signals weakened over consecutive trials
Reduction in hydrocarbon removal over consecutive processing trials
Minimal adsorption of hydrocarbon pollution from He/CH4 trials
Processing Trials (He/O2) – 7th Cell
William Stokes

## Slide 19
Processing Trials (He/O2) – 4th Cell
Processing by-product signals weakened over consecutive trials
Reduction in hydrocarbon removal over consecutive processing trials
Minimal adsorption of hydrocarbon pollution from He/CH4 trials
William Stokes

## Slide 20
Conclusions
In-situ plasma processing procedures are possible with the fundamental passband, and are ready for on-line cryomodule testing at TRIUMF
Frequency-tuning the driven mode raises the plasma density, thereby increasing chemical recombination and reducing processing time per cell
Frequency-tuning allowances are unique to modes and plasma-cell locations
Hydrocarbons on the cavity interior reduced from consecutive contamination and processing trials, independent of plasma density
Pollution introduced with contamination plasma was minor relative to initial pollution
William Stokes

## Slide 21
William Stokes
wstokes@triumf.ca
Thank you / Merci
TTC2026