## Slide 1
ALD interlayer to suppress thermoelectric currents
TESLA Technology Collaboration (TTC) meeting 2026
On behalf of CEA and CERN collaboration
I. Curci, T. Proslier, G. Rosaz, C. Pereira, C. Hain, K. Brunner, W. Venturini-Delsolaro, S. Leith, S. Pfeiffer, J. Bernardi, A. Steiger-Thirsfeld, L.Vega-Cid

## Slide 2
Coating system for Nb HiPIMS layers: 1.3 GHz cavities and samples
https://doi.org/10.1016/j.surfcoat.2022.128306
Description of the system can be found in the paper :
Context: Nb/Cu cavities coated by HiPims
RF performance of Nb/Cu cavity BM4.3 showing the difference in Q0 between the 2 cooldowns
Thermal gradient at SC transition

## Slide 3: The thermoelectric issue
Al2O3
Nb
Cu
∆
∆
Cu
Nb
current
(6 μm)
(6 μm)
(18 nm)
A thermal gradient between Nb and Cu generates thermoelectric currents at the interface
Solution? → Interlayer (Al2O3) by ALD (excellent uniformity, nanometer-scale thickness control, and conformality)
ALD system at CEA
Notes: Include ALD system, Hipims to introduce, hipims set up reference to publication…
The message to pass: Why thermoelectric currents are detrimental for SRF performance. Why ALD is useful? Monolayer by monolayer control and good confomity in 3D structures.

## Slide 4: Progress made so far…
Depositon of Al2O3 by ALD (CEA) on Cu substrates
Deposition of Nb by HiPIMS (CERN) on Cu and Al2O3/Cu.
Characterization of samples (PCTS, XRD, SEM)
Test RF of Nb/Cu and Nb/Al2O3/Cu cavities(CERN)

## Slide 5
GIXRD 2°
crystallite size,
microstrain,
lattice parameter,
Nb/Cu and Nb/Al2O3/Cu do not show any difference from a defect content point of view.
The lower dislocation density can be explained by the thicker layer.
C. Pereira, J. Bernardi, A. Steiger-Thirsfeld, S. Leith, G. Rosaz, S. Pfeiffer
SEM/XRD results
Al2O3 17 nm (150 cy)
Al2O3 5.5 nm (50 cy)
Nb/Al2O3/Cu samples
Crystallite size D: 50 cy: 280 nm
100 cy: 181 nm
150 cy: 180 nm
Al2O3 11 nm (100 cy)
5

## Slide 6: PCTS results
Similar distributions of Δ and Γ/Δ (around typical values of bulk Nb EP)
Al2O3 layer does not modify the superconducting properties (PCTS) nor structural properties (XRD) good for studying thermoelectric currents
Notes: 2 Tc dans le materiaux. On sait pas pourquoi il a 2 Tc.
Dagassge H2O. Al2O3 introudes impurities comme l’eau qui degasses (groupe OH). Plus tas de surface, plus ta de impurities qui dagass pendant le depot de Nb.
Un echantillon plus petit, moins de surface, moins de impurites qui degass.
24h a 200 °C en principio para preparar la superficie. RGA: rien de different.

## Slide 7: Progress made so far…
Depositon of Al2O3 by ALD (CEA) on Cu substrates
Deposition of Nb by HiPIMS (CERN) on Cu and Al2O3/Cu.
Characterization of samples (PCTS, XRD, SEM)
Test RF of Nb/Cu and Nb/Al2O3/Cu cavities (CERN)

## Slide 8: Magnetic field expulsion tests
In both cases, faster cooling rates create higher → higher thermocurrents → higher B
The intensity of B after SC transition is higher in Nb/Cu cavity (4 µT versus 1 µT ) → Al3O2 layer is effective in reducing thermoelectric currents
Nb/Cu
Nb/Al2O3/Cu

## Slide 9: RF tests
For Nb/Al2O3/Cu the Q slope is more pronounced: Is it because of the Al2O3 layer or some external factor?
The Nb/Al2O3/Cu cavity is less affected by the cooling rate.
Nb/Al2O3/Cu

## Slide 10: F vs T
Both cavities have similar superconducting properties close to bulk Nb.
There is no evidence that the premature quenches are because of bad superconducting properties.
Nb/Cu
Nb/Al2O3/Cu
Tc = 9.28 K
λ0 =51.3 nm
Tc = 9.39 K
λ0 =53.8 nm

## Slide 11: Future work…
Redo the test in another cavity with a better baseline.
Optimize the ALD layer to achieve good electrical insulation and thermal conductivity: try different alloys and vary the layer thickness.
Development of insulating barriers for high temperature deposition (Nb3Sn) → ISAS project

## Slide 12: Future work...
Redo the test in another cavity with a better baseline.
Optimize the ALD layer to achieve good electrical insulation and thermal conductivity: try different alloys and vary the layer thickness.
Development of insulating barriers for high temperature deposition (Nb3Sn) → ISAS project
Thank you!