## Slide 1: From 1.3 GHz to 400 MHz Nb/Cu Cavities: Challenges and Optimisation Strategies
presenter: Caroline Hain
TTC meeting
9-12 June 2026
G. Rosaz, C. Pereira, S. Forel, L. Ferreira, D. Doretto, A. Guyot, A. Vassallo, K. Brunner, G. Pechaud, D. Smekens, B. Dubois, S. Bizzaglia, S. Zadeh, F. Pelloux (and many others from TE, SY, EN)

## Slide 2: Quantitative objectives
4×108 @ 12 MV/m, 4.2 K (scaled 400 MHz FCC specs)
1×1010 @ 20 MV/m, 2 K (R&D goal)
1×1010 @ 25 MV/m, 2 K (R&D goal)
1.3 GHz
400 MHz
2-cell, 3.3×109 @ 12.2 MV/m, 4.5 K (FCC specs, bare)
What is the current status?

## Slide 3: 1.3 GHz R&D progress

## Slide 4: Advancements in 1.3 GHz R&D
example 1.3 GHz cavity
important factors:
surface state/treatment of Cu (polishing + passivation)
compact, high purity Nb coatings, i.e. strict control over level of impurities (e.g. oxygen, hydrogen, particulates)

## Slide 5: Advancements in 1.3 GHz R&D
important factors:
surface state/treatment of Cu (polishing + passivation)
compact, high purity Nb coatings, i.e. strict control over level of impurities (e.g. oxygen, hydrogen, particulates)
electropolished
as-machined, cleaned
EP, Nb-coated
as-machined (AM)
machining marks, high roughness, mechanically damaged near-surface layer
chemical polishing (with SUBU)
mixture of sulfamic acid, hydrogen peroxide, n-butanol and ammonium citrate
removes damaged layer, reduces roughness BUT differentially etches crystallographic orientations, can induce micropitting
electropolishing (EP)
mixture of phosphoric acid and n-butanol
reduces microroughness, more uniformly polished surfaces
example 1.3 GHz cavity

## Slide 6: Advancements in 1.3 GHz R&D
important factors:
surface state/treatment of Cu (polishing + passivation)
compact, high purity Nb coatings, i.e. strict control over level of impurities (e.g. oxygen, hydrogen, particulates)
HiPIMS vs DCMS
high plasma density (approx. 1019 m-3) compared to DCMS (approx. 1016 m-3)
increased probability for ionising collisions
high degree of ionisation of sputtered material
M. Ghaemi et al. Surface & Coatings Technology 476 (2024) 130199
T. Mieno Plasma Science and Technology
EP + HiPIMS
example 1.3 GHz cavity
11th TFSRF Workshop (2024)
PhD work of C. Pereira

## Slide 7: How to transfer this approach to 400 MHz cavities?

## Slide 8: Upscaling to 400 MHz
1.3 GHz
400 MHz
moving from 1.3 GHz to 400 MHz cavities can present a challenge
much larger surface area needs to be treated
object handling becomes significantly more difficult, requiring crane support
switching between process steps is time-consuming
example 1.3 GHz cavity

## Slide 9: Upscaling to 400 MHz
example 400 MHz cavity
important factors:
surface state/treatment of Cu (polishing + passivation)
compact, high purity Nb coatings, i.e. strict control over level of impurities (e.g. oxygen, hydrogen, particulates)
SUBU + DCMS
SUBU + HiPIMS
SUBU surface treatment, DCMS coating → LHC specs met at 4.5 K
SUBU surface treatment, high power impulse magnetron sputtering (HiPIMS) → improvement in Q0, BUT FCC specifications not met yet
moving to EP
so far ALL attempts of EP of 400 MHz cavities have resulted in peel-off
10 mm
20 mm

## Slide 10: Upscaling to 400 MHz
example 400 MHz cavity
important factors:
surface state/treatment of Cu (polishing + passivation)
compact, high purity Nb coatings, i.e. strict control over level of impurities (e.g. oxygen, hydrogen, particulates)
same setup for both 1.3 GHz and 400 MHz cavities
larger volume needs to be treated
insufficient and inhomogeneous rinsing
takes time to mount/dismount the cavity
preventing oxidation is critical
availability of safe passivation solutions is limited
fine Cu powder collected on the outflow side
effective
long-lasting protection
highly toxic
oxidation stains

## Slide 11: Upscaling to 400 MHz
example 400 MHz cavity
important factors:
surface state/treatment of Cu (polishing + passivation)
compact, high purity Nb coatings, i.e. strict control over level of impurities (e.g. oxygen, hydrogen, particulates)
ammonium citrate
(same as for 1.3 GHz)
much safer
not as robust as Cr (VI)
helps control surface chemistry
…and biocompatible!
improvements in monitoring EP bath, passivation solution and environmental conditions
additional high-pressure rinsing
10 mm
0.2 mm
0.2 mm

## Slide 12: summarising

## Slide 13: Summary and ongoing activities
So far…
possible to reach the FCC specifications demonstrated on 1.3 GHz cavities
HiPIMS improves the Q0 of the Nb coatings
biggest challenge related to electropolishing, improvements ongoing
latest processed cavity to be RF tested mid-June
ongoing activities and next steps
improving cavity-EP system interface
studies related to optimising anode design
HiPIMS + cavity biasing (DC and synchronised)
plasma surface treatment: surface cleaning and passivation
courtesy of: C. Kouzios, M. Himmerlich

## Slide 14: From 1.3 GHz to 400 MHz Nb/Cu Cavities: Challenges and Optimisation Strategies
presenter: Caroline Hain
TTC meeting
9-12 June 2026
G. Rosaz, C. Pereira, S. Forel, L. Ferreira, D. Doretto, A. Guyot, A. Vassallo, K. Brunner, G. Pechaud, D. Smekens, B. Dubois, S. Bizzaglia, S. Zadeh, F. Pelloux (and many others from TE, SY, EN)