## Slide 1: Update on Nb & Nb3Sn on Cu Developments at JLab
6/11/26
A.-M Valente-Feliciano, U. Pudasaini, O. Hryhorenko, S. Bira, Minqgi Ge, Eric Lechner, Brandi Redman, Theo Cahall​
​​

## Slide 2: Outline
Update on 1.3 GHz Nb/Cu development
Development of Nb3Sn on Cu and other substrates
Supporting Developments
Summary

## Slide 3: Produce Nb/Cu cavities with HiPIMS at 1.3 GHz and lower frequencies with at least Q~ 2x 1010 at 2K, 15 MV/m
The development of SRF surfaces with other forms of Nb and other superconducting materials have the potential to further improve SRF cavity performance beyond the Nb material intrinsic limit. This combined with higher efficiency and quality control are most relevant for structures required for large instruments and for industrial accelerators
Overcome Q-slope plaguing Nb/Cu cavities by producing high quality Nb films with hyperthermal ions
Goal
Energetic Condensation
ECR
Cylindrical HiPIMS
Energetic Condensation implemented with 2 techniques

## Slide 4: Q-slope mitigation with HiPIMS Nb films
HiPIMS Nb film/Nb results
No degradation in Q compared to bulk substrate though quench limitation early at 12 MV/m
No intrinsic limitation for Nb films
Coating Temperature: 150 ºC
Nucleation at -25 V, subsequent growth -50 V
Δ=1.8935,
Rres=0.1 nΩ
mfp=57.2 nm

## Slide 5: 1.3 GHz Nb/Cu (bulk machined) cavities
Q on bulk machined Cu cavities still low. Tc ~ 9.1 K, low for Nb/Cu films ( Tc expected > 9.35 K)
Origin: film poisoned with N due to leak on Kr injection line - validated with samples
Issue fixed, BUT progress further hindered due to facilities problem: PCW conductivity > 3000 uS/cm due to bacteria contamination, which induce damage with the pulser (currently under repair)

## Slide 6
Nb on Cu optimization: Mitigating Geometrical Field Limitations via Nucleation Energy
Ongoing complementary studies: jc and Hc1 as function of nucleation energy
[1] Lechner, Eric M., et al. Physical Review Accelerators and Beams 26.10 (2023): 103101.
[2] Hryhorenko, O., A-M. Valente-Feliciano, and E.M. Lechner. Superconductor Science and Technology 39.2 (2026): 025014.
See E. Lechner presentation on Tuesday afternoon
Increasing nucleation energy
ECR Nb on Cu
PRELIMINARY
Courtesy B. Redman, E. Lechner

## Slide 7: Single & multilayers structures
Nb3Sn Development – Goals
Binary phase diagram of the Nb-Sn system [2]
[1] André Anders, A structure zone diagram including plasma-based deposition and ion etching, Thin Solid Films, Volume 518, Issue 15, 2010, Pages 4087-4090, ISSN 0040-6090, https://doi.org/10.1016/j.tsf.2009.10.145.
[2] Charlesworth JP, Macphail I, Madsen PE. Experimental work on the niobium-tin constitution diagram and related studies. Journal of Materials Science. 1970 Jul 1;5(7):580-603.
[3] Takayuki Kubo, Yoshihisa Iwashita, Takayuki Saeki; Radio-frequency electromagnetic field and vortex penetration in multilayered superconductors. Appl. Phys. Lett. 20 January 2014; 104 (3): 032603. https://doi.org/10.1063/1.4862892
Why Nb3Sn?
Tc ~ 18.3 K (9.25 K for Nb)
Hsh 400 mT (twice of Nb)
The ultimate goal is the development of energetic condensation technique to improve Nb3Sn film structures
Process development
Target commissioning
Film production with a variation of the deposition energy, temperature, and thickness to get a niobium-tin stoichiometry in the range of 18-26 At % within deposited layers
Single & Multilayers (SIS structures) development
Use lower temperatures compared to tin vapor diffusion technique (Cu cavities coating)
Material control:
Surface evaluation with EDS, measurement, XRD-GXRD, and topography evaluation to correlate fundamental growth and superconducting performance
Film structure [1]
Multilayer coating[3]

## Slide 8: Nb3Sn film deposition
Reacted during coating
Required Sn % = 24 to 25 at. %
Adequate coating temperature needed to provide energetics necessary to form A15 phase
Nb3Sn on Cu at the beginning of the road.
1) Thermal budget is limited due to Cu substrate, Nb3Sn requires high energetic budget : need to compensate with ion energy
2) Need for an interlayer : Cu affinity with Sn and Cu high mobility above 600 °C make a barrier layer (Ta, Nb…) a must.
3) Pay attention to materials used for sample holder ( need to switch from Cu to Mo)
4) Use same setup geometry as HiPIMS deposition for cavities (need for cylindrical target)
Good Tc on ideal substrate required : Nb3Sn/Al2O3
A15 phase
narrow window

## Slide 9
Nb3Sn film deposition
50 W/620C -1e-2mbar
Post-annealing @ 950C
Ta/Al2O3
ECR Nb/Al2O3
a-Al2O3
c-Al2O3
Nb3Sn on Cu (with Nb & Ta interlayers) and bulk Nb under characterization
Alloyed NbSn target
Power increase leads to reducing Sn content at the same annealing conditions, but also reduces Tc
Additional ex-situ annealing at 950 °C for 1h resulted in Sn content drop, also improves Tc (17.7K).
Coating @ 620 °C yields Tc~15-16 K without ex-situ annealing
Increase of Ar working pressure yields further improved stoichiometry and Tc>16 K without ex-situ annealing on Al2O3, Ta/ Al2O3, ECR Nb/ Al2O3
EDS
SEM
Nb3Sn/ECR Nb/Al2O3
Nb3Sn/a-Al2O3
Tc

## Slide 10
Development required for implementation of PVD for cavity geometries
2 approaches in parallel for cylindrical stoichiometric targets
Sn diffusion into Nb cathode tubes
JLab/FSU/Ames Lab
Alloyed Target starting from powders mix
Nb3Sn Cylindrical Cathode Development

## Slide 11
Other limiting mechanisms likely concurrent:
Non-stoichiometry
Tin droplets
Patchy regions
Supporting Developments
Cu Cavity Electropolishing
QPR Facility for sample RF measurements
Demonstrated Key RF performances by Rs vs Bpk and Rs vs T at multiple temperatures (up to Tc) for 4 modes
Achieved 1 nΩ resolution at 10 mT for bulk Nb at 2.5 K;
Achieved ~20 nΩ for the regular bulk Nb sample;
Achieved 60 mT for the bulk Nb sample without quenching;
Extended QPR frequency range to 1.6 GHz, near the CEBAF frequency;
Completed comprehensive error analysis and resolution estimation;
The measured frequencies of all quadruple modes are consistence with CST simulation.
M. Ge et al.
S. Bira, N. Gale
  Design cavity support structures
  Design cathode handling system
  Design electrical safety system
  Electrical Safety Review
  Fabricate proof of concept system
  Water test system
  Incorporate power supply
  Final electrical safety check
  Electropolish cavity
Design & Fabrication of a cavity electropolishing system integrating all the steps required for Cu substrate preparation for cavity deposition​

## Slide 12
No intrinsic limit for the mitigation of Nb thing film Q-slope
The devil is in the details. Constant attention is necessary to maintain adequate deposition conditions
Nb3Sn DC sputtering with alloyed stoichiometric target requires substrate temperature above 600 C, high Ar pressure (1e-2 mbar), low current density
Nb3Sn on Cu (with Nb & Ta interlayers) and bulk Nb under characterization
Refine deposition process for denser, more uniform and relaxed material for thick and thin layers, switch from Ar to Kr
RF measurements with QPR samples
Implement Nb3Sn cavity deposition with cylindrical cathode developed
Summary & Next Steps

## Slide 13: Merci Thank You