## Slide 1
TTC 2026 · TESLA TECHNOLOGY COLLABORATION · GIF-SUR-YVETTE, 9–12 JUNE 2026
Nb₃Sn-coated copper cavities
from an optimized film to a 1.3 GHz coating system
Matteo Lazzari
INFN – Legnaro National Laboratories · Università degli Studi di Padova
on behalf of the LNL Surface Treatments & Superconductivity Team
◆ PhD scholarship fully funded by Zanon Research & Innovation
SUPPORTED BY
EU Horizon — iSAS (GA 101131435) & I.FAST (GA 101004730). INFN CSN5 SuperMAD · CSN1 SRF, RD_FCC.
HOSTED BY · PROJECTS & COLLABORATIONS

## Slide 2
ACKNOWLEDGEMENTS
LNL SRF R&D — a collaborative effort
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
02 / 17
EU HORIZON PROGRAMMES
INFN ACCELERATOR R&D
INTERNATIONAL PARTNERS
INFN–LNL
C. Pira, O. Azzolini, E. Chyhyrynets, E. Cremonesi, T. M. Ezeaba, D. Fonnesu, D. Ford, G. Keppel, M. Lazzari, F. Stivanello
INFN PD · RM3 · TO · LNF
A. Pepato, P. Rebesan · N. Pompeo, E. Silva · G. Ghigo · C. Gatti, G. Maccarrone, D. Di Gioacchino
CEA
C. Z. Antoine, I. Curci, Y. Kalboussi, T. Proslier
CERN
G. Rosaz, W. Venturini
DESY
M. Wenskat
HZB
S. Keckert, O. Kugeler, J. Knobloch
HZDR
S. Prucnal, S. Zhou
Jefferson Lab
A. M. Valente Feliciano
IEE SAS
E. Seiler, R. Ries
STFC / UKRI
O. B. Malyshev, R. Valizadeh, C. Benjamin, T. Sian, L. Smith
Lancaster · Liverpool · Siegen
G. Burt, N. Leicester, S. Marks, D. Seal · W. Bradley, S. Simon · X. Jiang, T. Staedler, A. Zubtsovskii
Riga Tech. Univ. · Piccoli
A. Medvids · R. Berton, D. Piccoli, F. Piccoli, G. Squizzato, F. Telatin

## Slide 3
TECHNOLOGY READINESS LEVEL
Each EU project, a step up in TRL
Nb₃Sn-on-Cu has climbed the TRL ladder through successive European programmes.
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
03 / 17
TRL 3–4
Validated in the laboratory
Study on planar samples + first RF test on QPR
TRL 4–5
Validated in relevant env.
Flux trapping & tunability
TRL 6
Demonstrated in operation
Conduction-cooling cryomodule
TRL SCALE
1
Basic principles
2
Concept
3
Proof of concept
4
Lab validated
5
Relevant env.
6
Demonstrated
7
Operational prototype
8
Qualified
9
Proven in operation

## Slide 4
01
PART 01
Film & technical solutions
Film stoichiometry & Tᴄ, the copper substrate and Nb buffer layer — and the measurements that validate the recipe.
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
04 / 17

## Slide 5
WHY Nb₃Sn ON COPPER
A route to efficient, 4.5 K SRF accelerators
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
05 / 17
4.5 K
Target operating temperature
÷ 3
Cryo grid power vs Nb @ 2 K
The copper substrate — coated by PVD
Mature PVD heritage — Nb/Cu by sputtering proven on LEP2, LHC, HIE-ISOLDE → FCC-ee
Thermal stability — excellent heat evacuation → conduction-cooling ready
Low cost — OFE Cu is 20–100× cheaper than RRR-300 bulk Nb
Nb @ 2 K → Nb₃Sn @ 4.5 K cuts cryogenic power ×3 (Thin-Film SRF Roadmap, I.FAST D9.1)

## Slide 6
THE PROBLEM
Nb₃Sn on Cu: four coupled challenges
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
06 / 17
1 Brittle A15 phase
Tᴄ follows Sn% (18–26 at%); A15 is brittle → thin film only
2 Low-melting substrate
Cu weakens above ~400 °C → hard limit T ≤ 600–650 °C
3 Tight geometry
Small aperture of 1.3 GHz cavities makes uniform coating hard
4 Sn–Cu interdiffusion
Sn and Cu are miscible → an intermediate buffer layer is mandatory
A15 forms as a single phase only above ~930 °C — well beyond the copper limit: the coating strategy must work around it.

## Slide 7
INFN LNL SOLUTION
DC magnetron sputtering — a -driven recipe
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
07 / 17
DCMS from a single stoichiometric Nb₃Sn target *
Simple set-up · full parameter control · coating and interface decoupled · Tsubstrate ≤ 650 °C
1
Low cathode power ~250 mW/cm²
2
High deposition pressure 2×10⁻² mbar
3
Deposition temperature 600–650 °C
4
No post-annealing
5
Nb buffer layer ~30 µm — thermal stress mitigation+ accommodation layer
vs cathode power · vs deposition/annealing T · XRD and lattice/Tᴄ vs Nb-buffer thickness
* D. Fonnesu et al., Recipe optimization and SRF test of Cu-compatible Nb₃Sn films by DCMS, Sci. Rep. 16, 3539 (2026).
> 17 K on Cu

## Slide 8
CHARACTERIZATION
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
08 / 17
SC energy gap — tunneling spectroscopy across deposition methods
HiPIMS
Broad gap distribution
inhomogeneous, many low-gap states
DCMS · INFN LNL recipe
Δ = 2.47 ± 0.27 meV
single clean gap · BTK / Usadel fits
VTD
Sub-gap “mini-gaps”
residual states below the gap
Courtesy of T. Proslier, I. Curci

## Slide 9
CHARACTERIZATION
The optimized film holds up to scrutiny
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
09 / 17
Base film · stoichiometric matrix
Nb 76%
Sn 24%
NbBL-10
NbBL-30
NbBL-40
Bulk Nb
Islands · Sn-rich phase
Nb 61%
Sn 39%
NbBL-10
NbBL-30
NbBL-40
Bulk Nb
Nb₃Sn islands on bulk Nb (SEM)
# islands by substrate
Sapphire
Bulk Nb
Nb buffer
Cu
most
fewest — good for Cu cavities
Courtesy of A. Zubtsovskii

## Slide 10
RF VALIDATION
A specific RF Measured on tailored samples
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
10 / 17
Surface resistance vs peak RF field · 4 K, 400 MHz (courtesy O. Kugeler, S. Keckert, HZB)
10 cm
COOL-DOWN BEHAVIOUR
→ Slow cool-down data suggest flux trapping
→ Steep rise > 40 mT → likely thermal dissipation
QPR sample · ⌀ ≈ 10 cm
Same sample, two cool-downs
Slow vs fast cool-down on one QPR sample isolates trapped-flux losses from the intrinsic surface resistance.

## Slide 11
RF VALIDATION
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
11 / 17
Rₛ vs peak RF field
Q vs Eacc · reaching the FCC-ee target
Sample
Tᴄ
Quench
Rs @ 4K
vs VTD
Sample #1 · bulk Nb · BCP
17.2 K
> 70 mT
~ 25 nΩ
≈ to 40 mT
Sample #2 · bulk Nb · EP + pol.
17.45 K
> 85 mT
< 9 nΩ
better, ≤ 50 mT
Sample #3 · full Cu · NbBL30
prelim.
—
—
first on Cu
Surface preparation matters
EP (#2) cuts low-field Rₛ >2× and lifts quench vs BCP (#1); Q ≈ 10× LHC.
#3 — first full-Cu QPR coating: very preliminary.
4 K · 400 MHz · courtesy O. Kugeler, S. Keckert (HZB)
Recipe confirmed on QPR samples
Defects during NbBL deposition

## Slide 12
02
PART 02
Upscaling to 1.3 GHz
From flat samples to a real TESLA-shaped cavity: building the deposition system that makes it possible.
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
12 / 17

## Slide 13
THE 1.3 GHZ COATING SYSTEM @ LNL
Fixed rectangular magnetron, rotating cavity
02 · Upscaling to 1.3 GHz
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
13 / 17
A geometry built for uniformity
Fixed planar magnetron — a rectangular cathode runs along the cavity axis
Rotating cavity — the 1.3 GHz cavity turns around it for an even coating
Stoichiometric target — same Nb₃Sn recipe validated on QPR, now in 3D
Design reference
M. Lazzari et al., “A new system for Nb₃Sn thin-film deposition on 1.3 GHz cavities”, SRF2025, TUP31
Coating chamber · rotating 1.3 GHz cavity

## Slide 14
COMMISSIONING
System assembled — magnetron characterized
02 · Upscaling to 1.3 GHz
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
14 / 17
CURRENT STATUS
✓
Vacuum system — assembled & tested
✓
Heating system — completed & tested
✓
Magnetron — first Nb-target ignition
Rotating-cavity system — design phase
MAGNETRON CHARACTERIZATION
Three magnet sets — 0.68 / 0.92 / 1.02 T tested
Up to 1 A — classical power-law discharge confirmed
Rate mapping — DR₂(equator) ≈ 4× DR₁ · Med vs straight magnets compared
Discharge power law (V–I)
Deposition rate DR₁ / DR₂ along the cavity
Ignited Nb plasma
1
2
3
4
5
6
7

## Slide 15
ROADMAP
Next steps
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
15 / 17
Follow the beam: where the particle sits is today; its path traces the road to a working 4.2 K cavity.
working cavity
1° semester 2026
2° semester 2026
End of
2026
Full
2027
First Nb coating on a dummy cavity
Coating of Nb3Sn on a dummy cavity
Coating of Nb3Sn on a Nb bulk cavity
Coating of Nb3Sn on a Cu cavity
◆ we are here

## Slide 16
SUMMARY
Where we stand on Nb₃Sn on Cu @ 1.3 GHz
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
16 / 17
1
Optimized recipe
DCMS from a stoichiometric target — Tᴄ > 17 K on copper, validated.
2
RF-proven film
Rs < 9 nΩ @ 4 K and quench > 85 mT on QPR — beats the VTD reference.
3
1.3 GHz system built
LNL rotating-cavity magnetron commissioned; first cavities being coated.
4
Clear path ahead
Nb (2026) → Cu prototype (2027) → 4.2 K vertical test.

## Slide 17
Thank you
Matteo Lazzari · malazzar@lnl.infn.it
LNL Surface Treatments & Superconductivity Team · INFN-LNL · PhD funded by Zanon Research & Innovation
KEY REFERENCES
D. Fonnesu et al., “Recipe optimization and SRF test of Cu-compatible Nb₃Sn films by DCMS”, Sci. Rep. 16, 3539 (2026).
M. Lazzari et al., “A new system for Nb₃Sn thin-film deposition on 1.3 GHz cavities”, SRF2025, TUP31.
SUPPORTED BY
iSAS (GA 101131435) · I.FAST (GA 101004730) · INFN CSN5 SuperMAD / CSN1 SRF, RD_FCC · Zanon R&I

## Slide 18
BACKUP
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
Nb3Sn/30 μm Nb BL/Cu and Nb3Sn/Cu
30 μm Nb BL/Cu
proved better than bulk Nb
From measurement at 1.8 K:
Limited reduction of thermal transmittance of Nb BL compared to Cu
Thermal transmittance

## Slide 19
BACKUP
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
Morphology — Nb₃Sn on bulk Nb

## Slide 20
BACKUP
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
Nb3Sn/bulk Nb
Sample #1 (just seen)
Nb3Sn/bulk Nb
Sample #2
Surface preparation:
BCP
Surface preparation:
Metallographic polishing + EP
QPR sample comparison

## Slide 21
BACKUP
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
1.3 GHz cavity assembly