## Slide 1: Towards Nb3Sn coated copper cavities for energy efficient SRF application
Márton Major, Alexey Arzumanov, Amir Farhood, Dorothea Fonnesu, Michaela Arnold, Norbert Pietralla, and Lambert Alff
Technical University of Darmstadt, Darmstadt, Germany
TTC 2026 Meeting, CEA-CNRS-Université Paris Saclay 2026, France
11. June 2026

## Slide 2: Introduction
Charlesworth, Macphail, Madsen, J Mat. Sci. 5 580 (1970) DOI: 10.1007/BF00554367
Cubic A15 phase Tc ~ 18.3K, brittle
Sn
Nb

## Slide 3: Motivation
Lee et al., Acta Materialia 188 155 (2020) DOI: 10.1016/j.actamat.2020.01.055
Early quenching of Nb3Sn coated cavities

## Slide 4: MEthod
Nb3Sn co-sputtering
Nb
Nb3Sn
Sn Target
Nb Target
Argon
Heater
MFC
Butterfly valve
Substrate
Exhaust
Schäfer et al., J. Appl. Phys. 128 133902 (2020) DOI: 10.1063/5.0015376
Nb3Sn co-sputtering = same time deposition of two materials (here the elements Nb and Sn) from two independent sources (targets)

## Slide 5: MEthod
Nb
Nb3Sn
Sn Target
Nb Target
Argon
Heater
MFC
Butterfly valve
Substrate
Exhaust
Nb3Sn co-sputtering at low substrate temperature (starting at 500 °C)
Direct synthesis of Nb3Sn without annealing
Control of stoichiometry by sputtering rate and energy
Independence from substrate
Fast film growth by high sputtering rates
High kinetic energies form phase pure film at low deposition temperature (500 °C), compatible with Cu substrate
No tin segregation
Schäfer et al., J. Appl. Phys. 128 133902 (2020) DOI: 10.1063/5.0015376

## Slide 6: Equipment
Nb
Sn
Sputter chamber with up to three targets
Exchangeable sample holder for i) small flat samples, ii) smaller objects up to QPR cups and possible upgrade to iii) inner coating of complete 1.3 GHz single cell cavities

## Slide 7: Results I
Schäfer et al., J. Appl. Phys. 128 133902 (2020) DOI: 10.1063/5.0015376
Grazing incidence (ω = 5°) XRD patterns of Nb3Sn films grown on fused silica substrate. The sputtering power ratio (of Nb/Sn) was set to 5.25. Substrate temperature during growth was 320 °C.

## Slide 8: Results II
Schäfer et al., J. Appl. Phys. 134 043903 (2023) DOI: 10.1063/5.0145181
Comparison of two Nb3Sn films grown at 320 °C, measured at 4 K. The sample grown at high sputtering energies (30 W Sn/158 W Nb) shows almost no variation in critical current vs H, while the sample grown at low sputtering energies show a variation in critical current, typical for weak-link superconducting behavior.
Normalized resistance of Nb3Sn films grown with different source power. Substrate temperature was 320 °C.

## Slide 9: Nb3Sn Coating
On copper HOM antenna In cooperation with Johannes Gutenberg University of Mainz, Florian Hug’s group
Coating of Nb disc
In cooperation with University of Hamburg, Marc Wenskat
Wenskat et al., Physica C 632 1354694 (2025) DOI: 10.1016/j.physc.2025.1354694
Roughness before coating (AFM)
Roughness after coating (AFM)
Plattner et al. IPAC ‘24 Nashville 2760 DOI: 10.18429/JACOW-IPAC2024-WEPS32

## Slide 10: Nb3Sn Coating
On copper HOM antenna In cooperation with Johannes Gutenberg University of Mainz, Florian Hug group
On top Tc,0 ≈ 14.5 K
At side Tc,0 ≈ 14.0 K
At bottom Tc,0 ≈ 13.0 K
Conclusion: TC,0 > 13 K at every region of the surface
Plattner et al., IPAC’23 Venice 3029 DOI:10.18429/JACOW-IPAC2023-WEPA164
[1] Plattner et al., IPAC ‘24 Nashville 2760 DOI: 10.18429/JACOW-IPAC2024-WEPS32
Normalized voltage (shielding effect) on a coated Cu foil at the top of a dummy antenna
Thermal simulation with a static load of 330mW at the antenna tip. The temperature at the tip is with 9.21K, which is close to the critical temperature of Nb [1].

## Slide 11: role of substrate
Farhood, Arzumanov, Major, Arnold, Pietralla, and Alff, IEEE Trans. Appl. Supercond. 36 7500607 (2026) DOI: 10.1109/TASC.2026.3662680
Critical temperature as shown by the shielding effect of thin films deposited on different substrates at a substrate temperature of 500 °C
Critical field Hc1 determined from the lowest magnetization in magnetization versus external field measurements as a function of temperature

## Slide 12: X-ray diffraction measurement
Critical temperature as shown by the shielding effect of thin films deposited on different substrates at a substrate temperature of 500 °C
XRD patterns of deposited Nb3Sn films at 500 °C on different substrates
Farhood et al., IEEE Trans. Appl. Supercond. 36 7500607 (2026) DOI: 10.1109/TASC.2026.3662680

## Slide 13: Nb3Sn unit cell, powder XRD
110
200
210
211
220
Pmn (#223)
Nb: 6c Sn: 2a
Calculated powder XRD pattern of Nb3Sn (by VESTA)

## Slide 14: Long Range Order (LRO)
S: Bragg Williams long range order parameter. For complete order S = 1, all Nb atoms are on Nb position, all Sn on Sn position, no vacancy.
Complete disorder: S = 0.
Van Reuth and Waterstrat, Acta Cryst. B 24 186 (1968) DOI: 10.1107/S0567740868001937
Complete order (S = 1)
Complete disorder (S = 0)

## Slide 15: Long Range Order (LRO)
ordered
disordered
S: Bragg Williams long range order parameter. For complete order S=1, all Nb atoms are on Nb position, all Sn on Sn position, no vacancy.
Complete disorder: S=0.
110
200
210
211
220
Complete disorder (S = 0)

## Slide 16: Preferred orientation (texture)
XRD peak intensities depend on
Structure factor (long range order)
Preferred orientation (texture)
Texture
Order

## Slide 17
Texture measurement
Peak – Plane
200 – (100)
210 – (210)
211 – (211)
Peak | Plane | 2 (deg)
200 | (100) | 33.89
210 | (210) | 38.06
211 | (211) | 41.85
110
200
210
211
220
Picture: Gabi Haindl

## Slide 18
Texture measurement
Peak – Plane
200 – (100)
210 – (210)
211 – (211)
Peak | Plane | 2 (deg)
200 | (100) | 33.89
210 | (210) | 38.06
211 | (211) | 41.85
110
200
210
211
220
XRD patterns of deposited Nb3Sn films at 500 °C on different substrates
Farhood et al., IEEE Trans. Appl. Supercond. 36 7500607 (2026) DOI: 10.1109/TASC.2026.3662680
Powder XRD pattern of Nb3Sn

## Slide 19
Texture measurement on r-cut sapphire

## Slide 20
Texture measurement on copper

## Slide 21
Texture measurement on fused silica

## Slide 22
-scans (XRD on tilted sample)
On glass: strong (100) texture
On copper: no texture (polycristalline)
Angle between (100) and (211) is 35.3°

## Slide 23
Conclusion
Critical temperature (shielding)
Critical field Hc1
A. Farhood, A. Arzumanov, M. Major, M. Arnold, N. Pietralla, and L. Alff, IEEE Trans. Appl. Supercond. 36 (2026) 7500607
XRD patterns of Nb3Sn films
Conclusion: superconducting properties (Tc and Hc1) depend on microstructure of the deposited film, which is inherited from the substrate. Unexpected: on amorphous substrate (fused silica) strong (100) texture.
Next steps: check long range order for other substrates (single crystalline MgO), micro and macro strain (peak shift and broadening) as seen by XRD.
Final goal: Nb3Sn coating on Cu with close-to-bulk superconducting properties by low-temperature co-sputtering.

## Slide 24: Acknowledgement
Thank you for your attention!
Funded by BMBF Project 05H21RDRB1 and the German Research Foundation (DFG) through grant GRK2128 (AccelencE)