## Slide 1: Optimization of Bronze-Route Nb3Sn Films on Cu Substrates for Quadrupole Resonator (QPR) Testing
Ming Lu
11.06.2026
TTC2026 Meeting, France

## Slide 2: Outline
1. Introduction of Nb3Sn coatings via bronze route
2. Nb3Sn QPR sample Fabrication and RF test
3. Small Sample Characterization and Analysis
4. Summary and Future work

## Slide 3: Introduction of Nb3Sn/Cu by bronze route
Nb3Sn film on Cu by bronze route
Phase diagram of Nb-Cu-Sn ternary system at 700℃
Precursor structure for bronze route
The optimization of Cu-based Nb3Sn coating involves combining two key aspects: Nb3Sn/Nb and Nb/Cu.
Cu substrate
Nb layer
Nb substrate
Nb3Sn layer
Cu substrate
Nb layer
Nb3Sn layer
Nb3Sn on Cu
Nb3Sn on Nb
Nb on Cu
bronze route
HiPIMS+baking
Cu-based Nb3Sn: A suitable Nb barrier layer (>10 μm) is required to prevent Cu diffusion into Nb3Sn, Sn diffusion into Cu, and Cu/Nb3Sn lattice mismatch (low Tc).
Cu-based Nb3Sn QPR sample preparation at HZB

## Slide 4: Nb3Sn/Nb QPR sample fabrication process
Bronze layer
Nb substrate
Nb substrate
Nb3Sn layer
Nb substrate
Nb3Sn layer
BCP 120μm + baking
Coating bronze
Synthesized Nb3Sn
Removing bronze
Nb QPR sample
Nb₃Sn/Nb preparation via bronze route
120 μm BCP + 700 °C (20h) baking to remove hydrogen and release stress;
Before bronze electroplating, the sample need activation and tilting to avoid trapped bubbles.
Increasing annealing temperature from 700 °C to 750 °C, enlarged Nb3Sn grain size and reduced surface impurities.

## Slide 5: Nb3Sn/Cu QPR sample fabrication process
Nb layer
Bronze layer
Cu substrate
Cu substrate
Nb3Sn layer
Cu substrate
Nb3Sn layer
Nb₃Sn/Cu preparation via bronze route
30 μm EP + 700 °C (20h) baking to increase the Nb layer density and release stress;
Due to the thin Nb film at the bottom (<1 μm), the bronze layer was deposited only on the top surface.
The sample still need activation and tilting to avoid surface trapped bubbles.
Sputtering Nb
Coating bronze
700℃ Heat treatment
Removing bronze
Electropolishing Cu

## Slide 6: Nb3Sn QPR sample Rs-T test comparison
At 4 K, the Cu-substrate Nb3Sn sample exhibit an Rs value 29 nΩ higher than that of the Nb-substrate Nb3Sn sample. Both samples show severe Q-slope, and simplified BCS model fitting was performed.
Rs=46.0 nΩ @4 K, 20 mT, 413 MHz
Rs=17.1 nΩ @4 K, 20 mT, 417 MHz
Nb3Sn on Nb
Sebastian Keckert
Nb3Sn on Cu
Corresponds to

## Slide 7: Nb3Sn QPR sample Rres fitting comparison
Compared with the Nb-substrate sample, the Cu-substrate Nb3Sn shows ~20 nΩ higher Rres at 20 mT, a lower Δ across all fields, and a smaller A parameter with weaker field dependence.
Rres=36.37 nΩ @ 20 mT, 413 MHz
Rres=16.04 nΩ @ 20 mT, 417 MHz
Nb3Sn on Nb
Nb3Sn on Cu

## Slide 8: Nb3Sn QPR sample thermal cycle comparison
The both Rs​ shows only a minor dependence on the cooling rate, indicating that Rs​ via bronze route is not sensitive to the thermal cycling conditions.
ΔRs=1.5 nΩ @ 4K, 20 mT, 417 MHz
ΔRs=0.8 nΩ @ 4K, 20 mT, 413 MHz
Nb3Sn on Nb
Nb3Sn on Cu

## Slide 9: Nb3Sn QPR sample penetration depth comparison
Compared with the Nb-substrate Nb3Sn (18.0 K), the Cu-substrate sample shows a lower λ(0) and lower Tc (14.7 K).
λ(0) = 166.78 ± 3.91 nm
Tc = 18.026 ± 0.025 K
λ(0) = 123.6± 5.4nm
Tc = 14.71± 0.06 K
Nb3Sn on Nb
Nb3Sn on Cu

## Slide 10: Nb3Sn QPR sample critical field comparison
The temperature-dependent quench field data near Tc was described by a T2 fit.
The Cu-substrate Nb3Sn exhibits a lower Bc(0) (56.3 mT) compared with Nb-substrate Nb3Sn (102 mT).
Nb3Sn on Nb
Nb3Sn on Cu
B0=56.3mT
Sebastian Keckert

## Slide 11: Outlines
1. Introduction of Nb3Sn coatings via bronze route
2. Nb3Sn QPR sample Fabrication and RF test
3. Small Sample Characterization and Analysis
4. Summary and Future work

## Slide 12: SEM characterization of Cu-based Nb3Sn
Several problems on Nb3Sn/Cu:
Copper particle contamination – removable by aqua regia.
Nanofiber contamination – likely from O (Nb layer) and P (bronze layer) impurity precipitation after heat treatment; not observed on Nb substrate samples; under investigation.
Nb oxide contamination – removable by 4% HF + H₂SO₄ solution.
Nb3Sn on Cu
Nb3Sn on Cu
Nb3Sn on Cu
Nb3Sn on Nb
Alena Prudnikava

## Slide 13: Upgrade of Cu-based Nb3Sn coating recipes
Step | Process | Original Parameters | Upgrade Parameters
1 | Mechanical polishing | Up to 100 µm removal | Up to 100 µm removal
2 | Degreasing | 1% Citranox®, 1 h | 1% Citranox®, 1 h
3 | Cu Electropolishing (EP) | ≈30 µm | ≈30 µm
4 | HiPIMS Nb (sputtering) | Tsub ≈ 180 °C, Ar = 2 Pa, Power = 600 W, Thickness ≈ 10 µm | Tsub ≈ 180 °C, Ar = 0.8 Pa, Power = 400 W, Thickness ≈ 10 µm
5 | High-temperature baking | 700 °C, 20 h | 700 °C, 20 h
6 | Bronze electroplating | ≈10 µm bronze | ≈10 µm bronze
7 | Vacuum Heat treatment | 700 °C, 30 h | 750 °C, 30 h
8 | Surface bronze removal | Aqua regia about 5 min | Aqua regia about 10 min
Optimized steps 4 (denser Nb barrier layer), 7 (large grain size) and 8 (fewer impurities):
Sample 1: baseline process, Nb3Sn/Nb/Cu ≈ 1.0 µm / 10 µm / 3 mm
Sample 2: optimized steps 4+7+8, Nb3Sn/Nb/Cu ≈ 1.0 µm / 10 µm / 3 mm

## Slide 14: PPMS characterization of Cu-based Nb3Sn
Baking the Nb film (HiPIMS) at 700℃(20h) and then increase heat treatment of bronze route at 750℃ can increase the Tc (15.0 K->16.1 K).
New Nb3Sn on Cu substrate
Origin Nb3Sn on Cu substrate

## Slide 15: GIXRD characterization of Cu-based Nb3Sn
GIXRD only detects Nb3Sn phase.
Other impurities are below the detection limit or amorphous.
GIXRD
New Nb3Sn on Cu substrate
Alena Prudnikava
Cu substrate
Nb barrier layer
Nb3Sn layer
NbSn2
Cu,CuOx
NbOx,SnOx,C-H

## Slide 16: Thermal current test of Cu-based Nb3Sn surface
New Nb3Sn on Cu substrate
CRAFT Test conditions: Zero field cooled, Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown (CRAFT details: Alex Cierpka, TTC2026 WG1 S4).
Under the 0.05 K/cm temperature gradient, flux trapping in the new sample decreased from 200 μT to 25 μT, even below Nb films (35 μT), indicating suppressed thermoelectric currents due to improved coating homogeneity and weaker flux pinning.
Comparison with previous results
Felix Kramer
F. Kramer,
SRF2025

## Slide 17: Analysis of Cu-based Nb3Sn coating recipes
Increasing the niobium barrier layer’s density or thickness improved the Nb3Sn film quality on copper, approaching the quality of Nb3Sn on high-purity Nb.
Samples type | Nb layer parameters | Treatment process | Min. growth temp. of Nb3Sn | Rs@4K, 20mT, 416MHz | 0.05 K/cm trap flux (zero field) | Nb3Sn film quality
Nb3Sn/Cu samples (Sasha) | 180℃/10μm, 2.0Pa, 600W | pre-annealing 700℃ 20h +bronze route 30h | 700℃ | 46.0 | large, 200 μT | Tc=14.6K,normal
Nb3Sn/Cu samples (Sasha) | 180℃/10μm, 0.8Pa, 400W |  | 750℃ | ? | ~25 μT | Tc~15.3K
Nb3Sn/Nb samples (IMP, China) | Nb substrate, RRR>300 |  | 750℃ | 17.1 | Small, 5 μT | Tc=17.7K,perfect
Samples type | Nb layer parameters | Treatment process | Min. growth temp. of Nb3Sn | Rs@4K, 20mT, 416MHz | 0.05 K/cm trap flux (zero field) | Nb3Sn film quality
Nb3Sn/Cu samples (Sasha) | 180℃/10μm, 2.0Pa, 600W | pre-annealing 700℃ 20h +bronze route 30h | 700℃ |  | large, 200 μT | Tc=14.6K,normal
Nb3Sn/Cu samples (Sasha) | 180℃/10μm, 0.8Pa, 400W |  | 750℃ | ? | ~25 μT | Tc~15.3K
Nb3Sn/Nb samples (IMP, China) | Nb substrate, RRR>300 |  | 750℃ |  | Small, 5 μT | Tc=17.7K,perfect
SUST, DOI: 10.1088/1361-6668/ae496a
Origin Sample 1
Upgrade Sample 2

## Slide 18: Work summary and future work plan
Future work plan:
  Prepare two new Cu-based Nb3Sn QPR samples (RF test) and two 100 × 60 × 3 mm³ flat samples (trapped flux test).
  Optimize the Nb layer thickness and density to reduce strain in Nb3Sn and thereby further enhance Tc.
  Use higher Sn content (10→15 at%) bronze, and longer annealing (750 °C, 30→50 h).
  Use EP-treated Nb substrate and Nb3Sn, and optimize bronze etching recipe.
  Develop laser treatment, PEP, FE treatment, high-T baking, plasma cleaning to improve the surface quality of Nb3Sn.
Work summary:
  The fabrication process, RF performance, and material characteristics of Nb3Sn samples prepared on Cu and Nb substrates were compared, and possible optimization strategies for further improvement were proposed.

## Slide 19
Thanks for your attention.