## Slide 1: Challenges to the vapor diffusion Nb3Sn coatings: A Materials Analysis
Nikki Tagdulang
Title
Month Day, Year

## Slide 2: The case of vapor diffusion Nb3Sn coatings
Nb3Sn promises high-Q and high-field gradient for future high-energy colliders.
Limited RF performance yet in Nb3Sn-coated cavities and reproducibility remains a concern.
Highest is above 20 MV/m
High T Nucleation promotes shiny, thinner films

## Slide 3
What is the effect of Ti to Nb3Sn coatings?
Towards understanding the potential factors affecting Nb3Sn-coated cavities
We closely monitor the impurities in our Nb3Sn coatings through materials analysis, in particular, Ti levels which is assumed to be one of the factors degrading cavity performance.
Witness sample
Flange cover
What is the effect of native oxides to Nb3Sn coatings?
We first identify the temperature to which oxide fully dissolved through successive heat treatment and in-situ time-of-flight secondary ion mass spectroscopy to a representative Nb3Sn. Apply potential heat-treatment to Nb3Sn-coated cavity.

## Slide 4
What is the effect of Ti to Nb3Sn coatings?
Towards understanding the potential factors affecting Nb3Sn-coated cavities
We closely monitor the impurities in our Nb3Sn coatings through materials analysis, in particular, Ti levels which is assumed to be one of the factors degrading cavity performance.
Witness sample
Flange cover

## Slide 5: Ti level analysis approach
Witness sample
Flange covers
Flange covers and foils are used to minimize as much as possible Ti diffusion into the inner surface of the cavity. Ti impurities still persist and needs to be quantified.
Witness samples are placed inside the source tube and at the end of the cavity.
Time-of-flight secondary ion mass spectrometry is used to monitor Ti levels
Sputter rate estimated from the thickness of the Nb3Sn, about ~0.3 nm/s.
O2+ sputter source with 2keV energy in a 200 x 200 um analysis area.

## Slide 6: Comparative analysis of Ti levels in witness samples
No correlation between current titanium levels and RF performance
Cavities | f [MHz] | [mT] | 
B9AS-AES-002 (Baseline) | 650 | 62 | 66
QWR 218 | 218 | 74 | 155
QWR 145 | 145 | 100 | 63
Cavities | f [MHz] |  | 
B9AS-AES-002 (Baseline) | 650 | 62 | 66
QWR 218 | 218 | 74 | 155
QWR 145 | 145 | 100 | 63
QWR 145 achieved the best ever Bpk,max in Nb3Sn coated cavities

## Slide 7: Summary and Outlook
We show initial results of the Ti levels and understand how it affects RF performance of the Nb3Sn-coated cavities. We don’t see a correlation of the Ti-levels with the RF performance of the Nb3Sn-coated cavities.
Understand if we do really need to use flange covers.
Flange covers

## Slide 8
Towards understanding the potential factors affecting Nb3Sn-coated cavities
What is the effect of native oxides to Nb3Sn coatings?
We first identify the temperature to which oxide fully dissolved through successive heat treatment and in-situ time-of-flight secondary ion mass spectroscopy to a representative Nb3Sn. Apply potential heat-treatment to Nb3Sn-coated cavity.
Cano et al., J. Phys. Chem. C 2023, 127, 19705−19716

## Slide 9: Native oxide dissolution analysis approach
Time-of-flight secondary ion mass spectrometry is used.
Cs- sputter source with 1keV energy in a 200 x 200 um analysis area.
Nb3Sn sample as-received.
TOF-SIMS analysis
Baked at 325 oC/1h
TOF-SIMS analysis without breaking vacuum.
Baked at 500 oC/1h
.
.
.

## Slide 10: Native oxides depth profile
Native oxides dissolve at 800 oC/1h.
A Nb3Sn sample is baked at each temperature for 1 h and measured using TOF-SIMS without breaking vacuum.
Cano et al., J. Phys. Chem. C 2023, 127, 19705−19716

## Slide 11: After exposing to atmosphere..
Native oxides regrows after exposing to atmosphere. We confirmed by baking longer at 800 oC the background level of the oxides.

## Slide 12: After exposing to atmosphere..
Native oxides regrows after exposing to atmosphere. We confirmed by baking longer at 800 oC the background level of the oxides.
Is the Sn concentration retained after 800 oC/1h baking?

## Slide 13: Sn concentration analysis
The Sn concentration after 800 oC heat treatment is within an acceptable level.
Stoichiometric Nb3Sn layer
X-ray photoelectron spectroscopy (XPS) was used.
Sputtered using a 5 kV mono-chromatic Argon
In-situ baking was performed at 700 oC/5h only instead of 800 oC/1h, limited by the instrument.

## Slide 14: Outlook
We performed successive baking of a Nb3Sn sample up to 800 oC to confirm up to which temperature the native oxides (Nb2O5 and SnO2) dissolve. We found 800 oC/1h enough to dissolve oxide. Moreover, Sn concentration level remains within acceptable range.
In-situ heat treatment set-up is ongoing for this level of temperature.
Perform oxide dissolution on Nb3Sn-coated cavities

## Slide 15: Acknowledgements
Brad Tennis, Damon Bice, Daniel Bafia, Grigory Eremeev, Sam Posen
Jae-yel Lee, Zu-hawn Sung, Akshay Murthy, Weislawa Diedzic-Misiewicz, Adam Clairmont
FNAL technical staff
Troy Peterson and Mike Kelly (ANL)

## Slide 16
Thank you for listening!

## Slide 18: How to de-contaminate coating chamber from Ti?
Burn-out alone will not remove the Ti impurities in the set-up. Instead, we routinely perform BCP.
Integrated counts of Ti was calculated until it reaches background.
Heat-treatment at 1200 oC/3h of the coating set-up was performed.