## Slide 1: EWPAA 2024 Highlights Rong Xiang (HZDR)

## Slide 2
7 oral sessions 26 presentations 1 speed talk session 1 Poster session lab tour
63 registered participants

## Slide 3: 1. Overview session

## Slide 4: 2. Photocathode Performance in Accelerator Applications
Boosting Photocathode Performance through Plasmonic Effects
and In-Situ Rejuvenation Techniques
Eduardo Granados (CERN)
photocathode lab been supporting accelerator operations for 25 years – Different cathodes, different accelerators
Rejuvenation of <aged> CsTe cathodes which have delivered nC bunches through re-deposition
Plasmonic photocathodes studied theoretically and experimentally
Notes:   CEIT’s photocathode shows consistent spatial distribution, but only 5x enhancement
  IOM’s photocathode: wasn’t possible to spatially resolve the checkerboard, but 25x enhancement
  Assessment of surface composition was realized with XPS, pointing at oxidation issues during laser treatment

## Slide 5: 2. Photocathode Performance in Accelerator Applications
Honest presentation, wanting to raise open questions and discuss solutions:
  LCLS Experiencing issues with dark current
  Cathode damage mechanism
A cryogenic ‘momentatron’ is currently being commissioned at SLAC.
Photocathodes performance for LCLS-II
Theo Vecchione (SLAC)

## Slide 6: 2. Photocathode Performance in Accelerator Applications
mA Current Level Operation of K2CsSb Photocathode in DC-SRF-II
Huamu Xie (PKU)
Fast caesiation during cathode preparation
Successful operation in DC-SRF gun, CW Operation up to 3 mA demonstrated
Big loss of QE observed in low temperature, QE increased under high charge operations
Preliminary result: K2CsSb intrinsic emittance ~ 0.5 mm at room temp., ~ 0.4 mm at 30 K

## Slide 7
High QE photocathode preparations and tests at SHINE
Li Xudong (Shanghai Advanced Research Institute)
Two Cs-Te recipes were developed, and the QE is typically >5%@265nm.
1 MHz beam was generated at the SHINE gun.
Further optimize the cathode recipe based on the gun operation results (thermal emittance, lifetime, dark current, QE uniformity…).
Explore other high QE photocathodes (UV and green photocathodes).
2. Photocathode Performance in Accelerator Applications

## Slide 8
3. Novel Concepts and Lasers
Overview of the SwissFEL photocathode lasers and cathode R&D
Alexandre Trisorio (PSI)
Introduce Twins laser systems: Alcor (2014) and Mizar (2019)
Successful operation of the gun lasers: >99% uptime over 2019-2024
Laser arrival time stabilization
Excellent flattop current for high and low charge operation:
10 ps FWHM, 3.7 ps FWHM
10 ps FWHM
3.7 ps FWHM
Cu_31 co-evaporated

## Slide 9
Laser Plasma Accelerator → Compact electron source to drive free-electron laser (FEL)
Spatio-temporal overlap between plasma wave and injection laser  very tricky!
Plasma emission observed when the overlap achieved
Injection observed within ~ 100fs time window matching nicely with one plasma cavity
Laser-plasma based electron sources for FEL applications
Arie Irman (HZDR)
3. Novel Concepts and Lasers
Gas target: 50% helium and 50% hydrogen

## Slide 10
3. Novel Concepts and Lasers
Novel plasmonic and photonics integrated photocathodes
Alimohammed. S.H. Kachwala (ASU)
Small emission area plamonic photocathode
Achieve nanoscale electron emission area from plasmonic gold spiral
Confined emission down to 1 µm!

## Slide 11
4. Low emittance application
Photocathodes for low emittance injector
John Smedley (LCLS)
LCLS-II HE Gun lower emittance => Electric field on cathode of 30 MV/m to achieve 0.1 um emittance for 100 pC
Epitaxial Green cathode (KCs2Sb): low roughness, MTE < 184 meV
Overview of low emittance application. Outstanding questions:
How long will a cathode last in a real SRF gun?
Will MTE performance degrade in gun?
Will the cathode pose an operational risk to the SRF Gun?

## Slide 12: Relativistic Ultrafast Electron Diffraction and Imaging Tim Noakes (STFC)
New Facility for Ultra Fast Electron Diffraction :
S-band gun for 4 MeV and 8 fs pulses, copper gun back plane, 0.2 fC/mm2mrad2
New Facility of 130 M$, commissioning planned for 2029
4. Low emittance application

## Slide 13: Pulsed laser deposition for epitaxial growth of photocathodes Kali Prasana Mondal (BNL)
BNL UHV photocathode growth system for Cs2Te, Cs from effusion cell and Te from PLD
Large diagnostic capability: RHEED, XRD, XRR, XRF
Results:
Highly ordered crystaline domains obtained
Rougness less than 1 nm for 7 to 20 nm layer thicknesses
QE > 15% at 265nm for 4H-SiC, Gr/4H-SiC and Gr/SiO2/Si
4. Low emittance application

## Slide 14: PhotEx Photoemission and Transverse Energy Experiment Jonas Dube (HZB)
Photoinjector of Superconducting RF Electron Accelerator Laboratory (SEALab) goes into operation this year
Emittance of the accelerator is limited by the electron source
PhoTEx allows characterization of photocathodes before they are transferred to the accelerator
New instrument to measure MTE, QE, reflection and lifetime: 40 meV < MTE <5600 meV
4. Low emittance application
Fig. 2: Photoinjector at SEALab, Source: HZB

## Slide 15
5. ‘Green’ Photocathodes
Promoting Epitaxy in Alkali Antimonides Jared Maxson (Cornell University)
“Promoting epitaxy” in the alkali antimonides :
  Extremely flat surfaces, interference enhancement, high QE while very thin
  Atomic scale layer engineering: heterostructures, polarized cathodes?
  MTEs dominated by band structure? (Particularly for thin cathodes)
X-ray and electron beam probe suites are vital for epitaxial growth
Epitaxy enables precise understanding of materials properties and detailed comparison to ab-initio theory.

## Slide 16
5. ‘Green’ Photocathodes
Atomically smooth films of CsSb: a chemically robust visible light photocathode
Alice Galdi (University of Salerno, Italy)
MBE can be used as an exploratory tool to discover new phases with desirable properties
Cs1Sb is an example of an overlooked visible light photocathode
  atomically smooth surfaces, more robust than Cs3Sb
  Low emittance? MTE measurements needed!
Band dispersion measured in ARPES despite in-plane disorder

## Slide 17
5. ‘Green’ Photocathodes
Development of Multialkali antimonides photocathodes
for high-brightness photoinjectors
Sandeep Kumar Mohanty (DESY)
3 KCsSb cathodes and 1 NaKSb(Cs) cathode have been produced for testing in the PITZ RF gun.
KCsSb cathodes with sequential deposition, recording QE of 8-9.6% at 514 nm.
Controlling K thickness was crucial for achieving cubic orientation in KSb compounds
Previous XRD confirms that Cs reacts effectively with cubic KSb to form predominantly cubic KCsSb

## Slide 18
NaKSb Photocathodes for High Brilliant Electron Beams
Chen Wang (HZB)
Demonstrated development of NaKSb photocathodes (more chemically stable than CsKSb)
Crucial to achieve high QE with long lifetime and good thermal stability (25W laser power)
Study effects of temperature on QE, K/Sb : Na/Sb ratio is a good QE predictor
5. ‘Green’ Photocathodes

## Slide 19: Machine learning-assisted design of Cesium-based photocathodes Holger-Dietrich Sassnick (Univ. Oldenburg)
Using machine learning to speed up scanning of structures
The Coord. ET and the M3GNet models show the best performance.
The implementation can be readily applied to any other material-system
The source code is published and freely available (https://aim2dat.github.io/aim2dat/).
6. Photocathode theory and characterisation

## Slide 20: OptaDOS Photoemission- The Good, The Bad and The Interesting Felix Mildner (Imperial college London)
OptaDOS Photoemission: K-resolved modelling of Photoemission
currently working on: supercell representation, weighted MTE calculation
Good: Improved physics in the code (3-step and 1-step), fixed issue with vacuum gap, OptaDOS distribution freely available…
Bad: Issues with supercells related to band folding
Interesting: broad agreement between theory and experiment
6. Photocathode theory and characterisation

## Slide 21: An overview of MTE measurement techniques and photocathode R&D at Daresbury Laboratory Lee Jones (STFC Daresbury Laboratory)
Overview MTE measurement techniques
Many different instrument have been developed (low energy, higher energy)
Photocathode R&D at Daresbury Laboratory
Cathodes for the CLARA accelerator
Cathode concepts for RUEDI and UK XFEL design project
6. Photocathode theory and characterisation

## Slide 22: Photocathode characterisation using a UV-tunable ultrashort pulse radiation source Andreas Schroeder (University of Illinois Chicago)
Photocathode characterization system at UIC
Key components: tunable UV radiation source, DC gun 10-20 kV DC gun, electron detection
Calibration and performance: QE ~ 10-10 and MTE 1-2meV
UV cleaning of metal photocathodes: reduction of the surface work function mechanisms (surface and ‘bulk’ desorption)?
6. Photocathode theory and characterisation

## Slide 23
Activation studies for GaAs photocathodes at Photo-CATCH
Maximilian Herbert (TU Darmstadt)
GaAs photocathodes require activation with NEA layer to reduce work function
Automated procedure successfully tested for cathode activation
  Using python, Co-deposition of Cs and O2
Automated procedure for QE scan
Implementation of Lithium-enhanced activation, significant increase in lifetime
Activation cycle
Pulsed Li-enhanced activation cycle
Improved lifetime
7. Cathodes for polarized electron sources

## Slide 24
High intensity polarized beam to drive a positron source
Carlos Hernandez-Garcia (Jefferson lab)
Driving a polarized positron source requires1 mA CW beam of electron with high polarization (90%)
Considering the amount extracted charge, 1/e charge lifetime should be >1 kC
overcome ion-back bombardment on the delicate strained-superlattice photocathode (limiting factor)
JLab develops large conical inverted geometry insulators to operate at > 300 kV
Days
CEBAF (<1 mm2)
4𝜎 ~ 1 mm
Trend we want to realize
4𝜎 ~ 10 mm
Test performed with un-biased anode
250 kV
R28
375 kV
R30
500 kV
concept
CEBAF
GTS
Achieved!
SF6 intervening volume test
7. Cathodes for polarized electron sources

## Slide 25
Cathodes with optimized QE for driving a spin polarized positron source
Kurt Aulenbacher (J.G.-Mainz University)
Production of spin polarized positron beams well understood
  spin polarized electrons beams in the multi-MeV regime
  Large polarization transfer to positron, polarized positron beams with good beam quality
Sustainable supply of GaAs/GaAsP superlattice photocathodes is of vital importance
QE and Polarization tests to performed at Mainz (high current) & TU-Darmstadt
7. Cathodes for polarized electron sources
Superlatticecathodes

## Slide 26
Photocathodes for electron sources for EIC
Omer Rahman (BNL)
Distributed Bragg Reflector (DBR) SSL GaAs developed (ODU, JLab and BNL)
Tested in 300 kV DC gun at BNL : peak QE ~1% at 780 nm with 90% polarization
Extraction of 11.6 nC bunch charge maximum  Exceeds EIC requirement
For DBR SSL GaAs, lifetime is wavelength dependent
Increasing laser spot size did not linearly increase SCL  consider SCL a 3D problem instead of 1D
7. Cathodes for polarized electron sources

## Slide 27
  Acknowledgement
  Many thanks to EWPAA Scientific Program Committee
  Maud Baylac (CNRS-LPSC) Caterina Cocchi (Universitat Oldenburg) Romain Ganter (PSI) Lee Jones (UKRI STFC) Julius Kühn (HZB)
  Laura Monaco (INFN Milano - LASA) Tim Noakes (UKRI STFC) Daniele Sertore (INFN Milano - LASA)
  Rong Xiang (HZDR)
  Special thanks to the Local committee and ELBE colleagues
  Nicki Fischer (HZDR)
  Anton Ryzhov (HZDR)
  Henryk Berndt (TU Dresden)
  Martin Starek (TU Dresden)
  Andreas, Gowri, Raffael, Mike... (HZDR)

## Slide 28
EWPAA2024 proceeding is published:
ISSN: 2191-8708, eISSN: 2191-8716 (https://www.hzdr.de/publications/PublDoc-25684.pdf)