## Slide 1: Cesium Telluride Photocathodes for the Eu-XFEL and FLASH
Anna Winiarska-Bialk, Lutz Lilje, Nils Plambeck, Hamed Achour, Mario Lengkeit
Orsay, 21/09/2026

## Slide 2: Agenda
01 Introduction
DESY accelerators
Deposition setup for photocathodes
02 Cs2Te photocathode
Plugs
Deposition parameters
Coating thickness deviations
03 Overview of past coatings
Thick coating
Performance and lifetime in the machines
04 QE measurements
Degradation and recovery FLASH
Degradation and recovery XFEL
05 Conclusions
06 Appendix

## Slide 3: Introduction
DESY accelerators
Accelerator & Projects at DESY
European XFEL
PETRA III
FLASH
REGAE
DESY II
PITZ
ARES
PETRA IV (future project)
European XFEL
FLASH
ARES
REGAE
PITZ

## Slide 4
FLASH → FLASH2020+
Extensive refurbishment of FLASH and the accelerator tunnel until August 2025
First soft X-ray FEL user facility that operates two undulator beamlines simultaneously
Improved photon- and electron beam parameters
parameter | unit | value
facility length | m | 315
energy | GeV | 1.35
bunches per second | Hz | 5000
emittance | µm rad | 0.4
bunch charge | nC | 0.01... 1.2
photon wavelength | nm | 51... 3.4
ph. pulse duration | fs | 30... 200
Introduction
DESY accelerators
old
new

## Slide 5: Introduction
DESY accelerators
parameter | unit | value
facility length | m | 3.4
energy | GeV | 17.5
bunches per second | Hz | 27000
emittance | µm rad | 0.8
bunch charge | nC | 0.02... 1.0
photon wavelength | nm | 4.7... 0.05
ph. pulse duration | fs | <100
RF gun
injector
bunch compression
main linac
collimation
SASE1
SASE2
SASE3
5 MeV
150 MeV
600 MeV
2 GeV
17.5 GeV
0.05...0.4 nm
0.4...4.7 nm
European XFEL
Laser driven RF-gun
3 bunch compressors
96+2 1.3 GHz superconducting accelerator modules
Up to 600 kW beam power
Three variable gap undulators
  SASE1 and SASE2
    175 m magnetic length
    0.05 – 0.4 nm wavelength (25 keV – 3 keV)
  SASE3
    105 m magnetic length
    0.4 – 4.7 nm wavelength (3 keV – 0.26 keV)

## Slide 6: Introduction
Deposition setup for photocathodes
INFN LASA deposition system design
Assembled by LASA in close collaboration with DESY
All components are 100 % compatible with the Milano system

## Slide 7: Introduction
Deposition setup for photocathodes
Deposition system improvements
Reduced system length
Rectangular flange geometry
Cutout in the rail for better view
Improved temperature monitoring
Optimized antenna positioning
Omitted metal sheet between orifice and cathode plug

## Slide 8: Cs2Te photocathode
FEL
UED FPR
PITZ/XFEL
Plugs
Material and design
Molybdenum plugs
FEL
    elliptical (before circular)
PITZ/XFEL
UED FPR
    elliptical (before circular)

## Slide 9: Cs2Te photocathode
Deposition parameters
Standard parameters - recipe from INFN Milano
Plug is heated to 450 °C then kept at 120 °C
Temperature during deposition: 100-110 °C
Duration of the whole process: ~2 h
Spot size ca. 5 mm
Thickness:
  Te: 10 nm - 1st layer
  Cs: ~50 nm - 2nd layer
13.07.2022 0727.2
QE 12,96%
I(Te) 3,24 A 10nm I(Cs) 4,7 A 50nm
14.07.2022 0748.1
QE 9,8%
I(Te) 3,24 A 10nm I(Cs) 4,85 A 50nm

## Slide 10: Cs2Te photocathode
Chart: Dispenser Currents (A)
Coating thickness deviations
Problems with thickness monitor...
Measurement range of thickness monitor (Inficon SQM-160) set too high for direct readout
Area factor of quartz crystal microbalance (QCM) not always or falsely considered in LabVIEW programs
The problem was indicated by changing dispenser currents (3.0→3.2 A) and lifetimes (5→10+ coatings)
  Same Te dispenser used since beginning!
  Te dispenser current dropped in 2020 and 2023 while the Cs lifetime increased significantly (usually 4-5 coatings)
Most coatings in the past were much thicker than indicated by the programs! (rate increased by area factor)
QCM in (for calibration)
QCM out (during deposition)
dispenser
orifice (cathode)
Chart: Indicated Thickness (nm)

## Slide 11: Overview of past coatings
Thick coating
Improved coating thickness control
A new coating thickness determination method was introduced after identifying issues with the area factor
The new approach provides more accurate and consistent thickness measurements
It enables better monitoring and comparison of coating variations between photocathodes
05.05.2026 1117.3 QE 17.1% QE(map)18% I(Te) 3,38 A 27nm I(Cs) 5,20 A 147nm Temp. 103°C
15.06.2026 734.2
QE 13,5% QE(map) 16,8%
I(Te) 3,28 A 15nm I(Cs) 4,96 A 96nm Temp. 91,5°C

## Slide 12: Overview of past coatings
Performance and lifetime in the machines
FLASH:
#76.3 around 150 days in operation
#91.2 around 130 days in operation
#77.2 around 175 days in operation
#98.2 around 70 days in operation
#90.3 around 55 days in operation
#114.2 around 100 days in operation
#618.3 since December 2013 until February 2015- 439 days in operation
#73.3(Milano) since February 2015 until December 2018 - 1413 days in operation
#105.2(Milano) since December 2018 until now
2009-2012

## Slide 13: Overview of past coatings
Performance and lifetime in the machines
XFEL:
#680.1 since December 2015 until July 2018 -1452 days in operation
#681.1 since January 2020 until June 2022
#681.1 since July 2022 until October 2022 (180 deg rotated in comparison the last time)
#685.1 since October 2022 until July 2025
#724.4 since November 2025 until July 2026
#1117.3 since July 2026 until now

## Slide 14: QE measurements
Degradation and recovery FLASH
Jan. 2019
Mar. 2020
Dec. 2020
Feb. 2021
Oct. 2021
Sep. 2022
Jan. 2023
Sep. 2025
Jan. 2024
Sep. 2026

## Slide 15: QE measurements
Degradation and recovery XFEL
26 May 2026
7 May 2026
18 May 2026
10 Jan. 2026
2 Jun. 2026

## Slide 16: Conclusions
Deposition system: new design with improved functionality and usability
Plugs: continuous development driven by evolving RF gun requirements
Coating thickness: improved monitoring enables systematic investigation of thickness–performance correlations
Cs₂Te: high QE + long lifetime → well suited for FLASH & European XFEL

## Slide 17
Anna Winiarska-Bialk
MVS
anna.winiarska@desy.de
+49 40 8998 (9)3442
Thank you
Grateful acknowledgment is made to Juliane Rönsch-Schulenburg and Frank Brinker for their vital support in performing the measurements and providing the data.

## Slide 18: Appendix

## Slide 19: Appendix
ELAS (ELectron Analysis System)
Compatible with our cathode transport boxes
Main chamber equipped with
  PHOIBOS 100 (SPECS)
  EGG-3101 (Kimball Physics Inc.)
  RS 40B1 (PREVAC)
  X-ray Photoelectron Spectroscopy (XPS)
  Auger-Electron Spectroscopy (AES)
Mean Transverse Energy (MTE) measurement via attached TEMA setup
Complementary XPS and AES measurements
Load Lock

## Slide 20: Appendix
TEMA (Transverse Energy Momentum Analyser)
Adapted to TESS design
  Developed at ASTeC STFC Daresbury see also: DOI 10.1063/5.0109053
Complementary XPS and AES measurements
UA : | Acceleration voltage applied across the gap
d : | Cathode to detector acceleration gap distance
σdet : | RMS radius of electron spot measured on the detector screen
σ0 : | RMS radius of the focused laser spot on the cathode surface
camera
Detector
Lens
Photocathode
grid
multiplier
screen

## Slide 21: Appendix
Complementary XPS measurements
ELAS (XPS Cs2Te):
Cs
Te
O
C
Mo
Surveys:
High resolution (Te 3d) < 0.5 mm spot size:
Larger spot size, 1-2 mm:
Te 3d3/2 2- (Cs2Te)
Te 3d3/2 0
(Metallic)
Te 3d5/2 2-
Te 3d5/2 0
Te 3d3/2 2- (Cs2Te)
Te 3d3/2 0
(Metallic)
Te 3d5/2 2-
Te 3d5/2 0

## Slide 22: Appendix
Complementary XPS measurements
ELAS (XPS Cs2Te):
Cs
Te
O
C
Mo
Surveys:
Te 3d3/2 2-
Te 3d3/2 0
Te 3d5/2 2-
Te 3d5/2 0

## Slide 23: Appendix
Complementary XPS measurements
ELAS (XPS Cs2Te):
Cs
Te
O
Mo
Surveys:
Te 3d3/2 2-
Te 3d3/2 0
Te 3d5/2 2-
Te 3d5/2 0