## Slide 1
Accelerator: Science, Technology & Applications
Aim: A premier Open-Access journal for dissemination of high-impact research across the full spectrum of particle accelerator science, technology, and its transformative applications. APC is free before 2030.
Accelerator Physics & Concepts
Advanced Accelerator Technologies
Accelerator Facilities & Applications
Medical & Industrial Applications
Cross-Disciplinary Integration
Welcome to submit your contributions!
Editor-In-Chief: Prof. Zhentang Zhao
Executive Editor-In-Chief: Prof. Haixiao Deng
Research Article, Review, Letter, Perspective, Dataset, Editorial, Erratum
Expected IF: ~5.0

## Slide 2
Renkai Li
Tsinghua University
September 22, 2026
UED sources and photocathode R&D at Tsinghua University

## Slide 3
Acknowledgement
Collaboration and discussions with many colleagues, especially at Cornell, UCLA, and SLAC
Colleagues at Tsinghua & team members: C. X. Tang, W. H. Huang, Y. C. Du, L. M. Zheng, L. M. Zheng, P. W. Huang, Y. N. Yang, P. Lv, Z. Y. Wang, B. T. Song, Z. X. Liu etc.
Funding agencies

## Slide 4: Outline
Introduction
FORTRESS beamline
few-fs e-beam control
Ultrahigh-vacuum S-band gun
Alkali-antimonide at high-field

## Slide 5: Ultrafast electron diffraction
G. Mourou and S. Williamson, APL 41, 44 (1982)
S. Williamson, G. Mourou and J. C. M. Li, PRL 52, 2364 (1984)
Full potential of (MeV) UED are being explored: science and instrument
https://lcls.slac.stanford.edu/instruments/slac-mev-ued/mev-ued-publications
Sensitive to Coulomb fields, large cross sections, large q-range, low radaition damage…

## Slide 6: An R&D facility for bright beams research
High resolution spectrometer
Beam study
Liquid/gas phase chamber
Gun and load-lock
FORTRESS
Facility fOr Relativistic Time-Resolved Electron Sources and Scattering
Gun
Sources and cathodes
Low emittance
fs bunch and timing
Advanced diagnostics
UED/UEM
Training students
Solid state chamber

## Slide 7: Construction of FORTRESS
Zhiyuan Wang
1st yr grad.
Peng Lv
2nd yr grad.

## Slide 8: Temporal resolution and challenges
: space-charge effects
pump laser
cathode laser
e- bunch
Long bunch
Short bunch
Filippetto, Musumeci, Li et. al., RMP 94, 045004 (2022)
: fluctuations due to RF amp. and RF phase-laser jitters

## Slide 9: Criteria for temporal control
inevitable, try make R560
RF phase-to-laser jitter can still cause TOF jitter
Rotate LPS w/o affecting centroid TOF (no ‘active’ EM fields)
Fix cathode-target TOF
Compress bunch duration
pump laser
cathode laser
e- bunch
Simultaneous sync. & comp.
Preserve beam brightness Simple, reliable, clear

## Slide 10: a new method for few-fs control
High-gradient -magnet
Low-jitter photoinjector
Yining Yang
Now postdoc @ UCLA

## Slide 11: Low-jitter photoinjector
Large ToF jitter
Large energy jitter
RF amp.
momentum
ToF
Much less impact from
Conventional gun (1.6 cell)
New geometry (1.4 cell)
R56

## Slide 12: What is an -magnet?
SSRL injector
Top view
Side view
Harald Enge, proposed in 1963
Michael Borland’s
PhD Thesis, 1991
GPT tracking results

## Slide 13: THz streaking
Strong linearly polarized THz generated by and intrinsically synchronized with ultrafast lasers
Map temporal distribution into transverse profile
Measure bunch duration and relative-to-laser timing jitter
Laser-generated THz pulse
R. K. Li et al., PRAB 22, 012803 (2019)
ToF resolution
Bunch duration resolution
when beam size differ from unstreaked beam size by
0.51 fs rms
2.55 fs rms

## Slide 14: Phase space evolution
Courtesy of Yining Yang

## Slide 15: ToF tuning and compression
ToF
ToF control
Compression
Phase-space selection
slit

## Slide 16: Robust, sub-5 fs control
Simple, clear, compact, reliable
Minimal number of elements
Emittance preserved for high brightness
Bunch duraiton
TOF-to-laser jitter
20 minutes data
fs rms
fs rms
5D brightness
Energy spread
Momentum jitter
Bunch charge
1.6 fC (~104 e-)
Y. Yang et al., arXiv:2508.03946

## Slide 17: UED measurements
Single image (500 bunches)

## Slide 18: Dependence on photocathodes
Currently operating with Cu
Compression depends on bunch charge
Initial bunch duration also affect LPS evolution

## Slide 19: Outline
Introduction
FORTRESS beamline
few-fs e-beam control
Ultrahigh-vacuum S-band gun
Alkali-antimonide at high-field

## Slide 20: Ultrahigh vacuum & high gradient
>10 times better vacuum at cathode
P. W. Huang et al., NIMA 1051, 168251 (2023)
New gun
Earlier version
Pengwei Huang
Now Assoc. Prof. @ Sichuan University

## Slide 21: Some details of the design
Shaping the edge of the cathode plug to optimize field enhancement

## Slide 22: New gun installed
full cell
half cell
vacuum cell
to load-lock

## Slide 23: Vacuum test and rf conditioning
7.7e-9 Pa
(w/o loadlock)
1.3e-8 Pa
(w/ loadlock)
1.7e-8 Pa
(～2.2e-8 Pa at cathode)
<2.1e-9 Pa
<2.1e-9 Pa
<2.1e-9 Pa
1.4e-8 Pa
<2.1e-9 Pa
2.2e-8 Pa
Faraday cup
rf reflec.
rf forward
Base/operation pressure
rf conditioning after 24 hrs
Dark current 0.5 nC @ Ez～105 MV/m
Cs2Te
QE 4~5% over 6 months

## Slide 24: Fabrication of Alkali Antimonide etc.
Evaporation sources
A newly commissioned deposition system for Alkali Antimony cathodes (Cs-Sb, K-Cs-Sb, etc.)
Baseline vacuum 5.9e-9 Pa
Study of QE, MTE versus deposition recipes
Started fabrication of K2CsSb cathodes
K2CsSb QE 4-6%@532 nm

## Slide 25: Load-lock system w/ green cathodes
Ultrahigh vacuum gun
Load-lock chamber
Cathode suitcase
Loaded 4 K2CsSb cathodes
No. | QE@532 nm
#1 | 5.6%
#2 | 4.5%*
#3 | 5.7%
#4 | 4.1%**
* swapped Cs source, outgassing
** run out of Cs

## Slide 26: K2CsSb at high field
K2CsSb survived and characterized at ~100 MV/m
K2CsSb in ultrahigh-vacuum S-band gun @ 100 MV/m
>1% for 2 weeks
Potential benefits for FEL and others, P. Huang, NIMA 1051, 168251 (2023)
Measured QE and MTE at different laser wavelength, P. Huang et al., to be submitted

## Slide 27: MTE measurement
P. Huang et al., to be submitted
Field-dependence of MTE
～ 2 nm

## Slide 28: VHF gun
VHF gun, design pioneered at APEX and motivated by CW XFEL application
5 guns fabricated, commissioned, improved since 2019 (Profs. Chuanxiang Tang, Yingchao Du, Lianmin Zheng, etc.)
Test beamline repurposed for UES and photocathode R&D
Key parameters | Values
Gun gradient | 29.9 MV/m @ 82 kW
Gun voltage | 856 kV
rf amp. stability | 3.3×10-5
rf phase stability | 0.0033 deg
Dark current | 6.8 nA
Vacuum | 4e-9 (RF off)/2.2e-8 (RF on) Pa
Prof. Lianmin Zheng
Prof. Yingchao Du
Installed at SHINE

## Slide 29: Photocathode R&D infrastructure
Photocathode preparation system
Ultrahigh vacuum S-band gun up to 100 MV/m
VHF gun, CW, ~30 MV/m
200 keV DC gun, 7.5 MV/m

## Slide 30: Summary and outlook
Source & beam shaping R&D
Flexible test facility for photocathodes and beams R&D, and UED experiments
High-field testing of alkali-antimonide photocathodes
New photocathodes will support improved shaping and brighter beams
Few-fs beam control, depends on high-performance cathode
K2CsSb at high-field
Thank you!
Stable, versatile test facility
Testing in high-field, high-vacuum real guns