## Slide 1: Field emission and plasmon-assisted photocathodes: from emitter arrays to graphene-edge cathodes
Soichiro Tsujino*
Photocathodes for Accelerator Science in Europe (PhASE 2026)
Sep 22, 2026: Auditorium Joliot Curie (IJCLab), Orsay France
* also at Shizuoka University, Hamamatsu, Japan.

## Slide 2: Outline
Double-gate field emitter array (FEA) as a low-emittance cathode
Surface-plasmon-polariton (SPP) asssited FEA photocathode
Spatial coherence of field emitters: field-emission wave packet
Recent developments: 2D material-edge field-emitter
Summary

## Slide 3: Double-gate field emitter array (FEA) as high-current, low-emittance cathode
5 nm
Field emission Mo nanotip
Collimagion gate
Extraction gate
Vge > 0
Collimated beam
Vge > 0
kcol = Vcol/Vge = 0
Diverging
S. Tsujino et al. Nat Comm (2016).
Transverse moment px/pz
Case: ΔEt = 0.12 eV
Transverse moment px/pz
Case: ΔEt = 11 eV

## Slide 4: Double-gate FEA: emittance reduction
FEA1: as-fabricated
FEA2: as-fabricated
Spindt-FEA
FEA3: Ne-conditioned
Collimated beam (k=1)
ɛ = 0.13 μm
Et = 0.13±0.06 eV (k = 1)
Uncollimated
Beam (k=0)
ɛ = 1.2 μm
Et = 11.8 eV (k = 0)

## Slide 5: Enhanced local electric field via plasmon resonance and electron energy
Keldysh parameter:
Ponderomotive energy
Barrier height 𝛷 /ionization potential (Ip)
Photoemission (perturbative)
Plasmonics modulate Eloc,
hot-electron
Field-driven emission & acceleration
High-harmonic generation:

## Slide 6: Example: strong-field electron dynamics at nanotip & SPP
[5] Irvine et al. (2004): SPP on Au via grating
Field-driven emission & acceleration
High-harmonic generation:
[3] Herink et al. (2012): gold nanotips, 0.8-8 um pulses

## Slide 7: SPP for enhancing QE at moderate excitation:
[7] Li et al. (2013): SPP Cu
in = 1.4 mm mrad/mm rms (~1eV)
sp > 10
in = 0.8-1.0 mm mrad/mm rms (0.33-0.51 eV)
sp >> 1
(Eloc ~0.5 GV/m)
[9] Kachwala et al. (2024): SPP focusing/interference for Cu
 ~ 1E4
UV (266 nm)
[11] Martinez-Calderon et al. (2023):
localized plasmon exc. & hot-carrier

## Slide 8
SPP-assisted FEA photocathode (
EOT through sub-  apertures
+
Photo-field emission
(APL 2008/2009/2011-2, SciRep 2012, APEX 2013, JVST2015)
10^6 tips, 1 µm-pitch, NIR (800 nm)
Copper double-gate struc. QE ~ 10-5
~25 µJ for 200 pC.
cf. Cu QE (flat cathode)~ 6×10-5
by UV pump
(less stability, uniformity, efficiency)

## Slide 9: Field emission wave packet
r
z
kx
ky
kz
Tunnelling allowed for states with kz ~ kF
Planar point-emitter case
-conservation of crystal momentum
-summation over available states
r (nm)
z (nm)
~ 1/
wave packet expansion
~ free space

## Slide 10: Field emission wave packet: fully coherent case
‘Point’-emitter
Finite-initial beam size 𝜎0
( ~ 1/momentum spread)
Angular spread ~ 𝜃0
Fully-spatially coherent-emitter (size r):
Angular spread ~ 𝜃0 x (𝜎0 / r)
JAP (2018); JVSTB(2022); JAP (2026)

## Slide 11: Field emission wave packet from Surface State of Topological Insulator
Total beam intensity
𝓁=0 + 𝓁=1
𝓁=0 component
𝓁 =1 component:
vortex beam
Tsujino, Mussler, Hajibaba (2026): submitted

## Slide 12
Suspended Graphene-Edge Field-Emitter

## Slide 13
Suspended Graphene-Edge Field-Emitter

## Slide 14: Summary
SPP-assisted FEA photothode:
  low-emittance, ultrafast cathode?
Field emission wave packet:
  window of solid state into vacuum?
2D Film-edge emitter

## Slide 15
Funding
SwissFEL/PSI-XFEL project, PSI
Swiss National Science Foundation
Max Planck Institute for structure and material dynamics
Swiss Nanoscience Institute, Uni. Basel
Seite 15
Chiwon Lee
D. R. J. Miller
P. Das Kanungo
P. Helfenstein
V. Guzenko
M. Monshipouri
M. Paraliev
Albin Wrulich
Jens Gobrecht
Y. Oh
A. Mustonen
S. Leemann
Hans-H Broun
Thomas Feurer
E. Kirk
H.-W. Fink
P. Beaud
Pooja Thakkar
Penghan Lu (FZJ)
Rafal Dunin-Borowski (FZJ)
Soheil Hajibaba

## Slide 16: FEA emittance measurement
Solenoid lens
Anode (ground)
phosphor screen
Faraday cup
FEA at – 20kV
L = 0
L
Focused beam (by solenoid)
[un-collimated, kcol = 0]
Focused beam
[collimated, kcol = 1]
Double-Gate FEA
10 µm-pitch, 104 tips
1 mm-dia
Uncollimated
Beam (k=0)
ɛ = 1.2 μm
Collimated beam (k=1)
ɛ = 0.13 μm
Et = 11.8 eV (k = 0)
Et = 0.13±0.06 eV (k = 1)
S. Tsujino et al. Nat Comm (2016).
camera

## Slide 17: Is FEA beam coherent?...test with diffraction
Direct beam
s0 = 59 µm-rms
e-
MCP
L = 5 mm
50 mm
Phosphor
Screen
V0=0.8 kV
Single-nanotip double-gate
field emitter
- Beam potential set by sample voltage
- No additional optics ~ relying on the small velocity spread
of collimated double-gate field emitter beam
Suspended 1 ML graphene (on TEM grid)
Lee, Appl Phys Lett (2018).
Lee, Appl Phys Lett (2018).

## Slide 18: Relationship between the spot size, crystal size, & transverse coherence length
σc = 4 nm
2 nm
0.4 nm
0.2 nm
Lc
When crystal is larger than wave function (transverse coherence length Lc)
Lc
1.1 Lc covers a few lattice: large spot size
1.2 Lc >> lattice size : small spot size
Lc
Bragg spot absout same size as the direct beam spot

## Slide 19: Relationship between the spot size, crystal size, & transverse coherence length
When crystal is larger than wave function (transverse coherence length Lc)
Lc
1.1 Lc covers a few lattice: large spot size
1.2 Lc >> lattice size : small spot size
Lc
σc = 4 nm
2 nm
0.4 nm
0.2 nm
dB  Lc ≳ 2 nm
dsat ≲ dmain/10
 Lc ≳ 20 nm
dB  Lc ≳ 2 nm
~ beam size (60 µm)
Lc ≳ 20 nm
~ 6 µm domain
=> 6 µm > Lc ≳ 20 nm