## Slide 1
Photocathodes for Accelerator Science in Europe (PhASE26) Workshop
IJC Lab, Orsay, France, September 21-23, 2026.
Semiconductor Photocathodes:
Modeling of Electron Emission Processes
W. Andreas Schroeder
Louis A. Angeloni and Ir-Jene Shan
Physics Department, University of Illinois Chicago
Lee B. Jones
ASTeC, STFC Daresbury Laboratory, United Kingdom
Department of Energy
DE-SC0020387
Theodore Vecchione
SLAC
UIC

## Slide 2
Outline
Two photoemission processes
(i) ‘Normal’ one-step direct band photoemission
 Energy (E) and transverse momentum (pT) conserving
(ii) Optical phonon mediated Franck-Condon (FC) electron emission
 Energy (E) and momentum (p) resonant
… Photoemission by inelastic phonon scattering
Polar semiconductor photocathodes
 MTE and QE measurements vs. FC emission theory:
Cs:GaAs at 808 nm (long transport regime); Te → Tlattice
GaN for ħω > Eg (short transport regime); kBTe = f(ħω  Eg)
Fe:Ga2O3(010) photocathode
 Ultracold photoemission: MTE  6 meV at 300 K
 Evidence for Te increase due to polaron formation

## Slide 3
Prior work: H-terminated diamond(001)
J.D. Rameau, J. Smedley, E.M. Muller, T.E. Kidd, and P.D. Johnson, Phys. Rev. Lett. 106, 137602 (2011)
Emitted electrons from NEA CBM
eff = Evac – (ECBM  għ)  0.96 eV
… għ is real part of the electron-
polaron self energy and the
dimensionless Fröhlich coupling
constant for diamond g = 1.1
Emission ‘bands’ are replicas of electron distribution in CB separated by ħ = 165 meV optical phonon energy
I(n) = e-ggn/n! Poisson statistics govern emission strength for nth phonon band
(n = 0, 1, 2, …)
 ARPES measurement; ħω = 6.01 eV (208 nm)  α  4000 cm-1 (absorption depth  2.5 m)
n = 0
n = 1
n = 2
n = 3
.
.

## Slide 4
Franck-Condon mechanism in photoemission
Energy and momentum resonant emission:
… intermediate scattering optical phonon(s)
of energy ħΩ and momentum q
Effective internal () and emitted vacuum () electron momenta matched; so that
q
p0
p

x,y
z
Photocathode
Vacuum
n = 1
 Phonon scattering based electron emission from semiconductor photocathodes

## Slide 5
Franck-Condon emission theory
W.A. Schroeder, L.A. Angeloni, I-J. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
 Analytical evaluation in parabolic band approximation with thermalized electron distribution at Te; ħΩ → 0
PEA
( > 0)
NEA
( < 0)
p0
E
p
E

vacuum
bulk
p0
E
p
E

vacuum
bulk
p0 = p + nq
p0 = p + nq

## Slide 6
Cesiated p-GaAs photocathode
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
 Measurements performed using TESS (Daresbury Laboratory, U.K.);  = 808 nm, T = 300 K
Absorption depth ~1 μm at 808 nm
 Long transport limit with low excess photo-
excitation energy in CB (ECB < 100 meV)
 Expect kBTe  25 meV due to rapid carrier
cooling during drift to emission face
Surface depletion region wd  10 nm traversed in less than ~200 fs optical phonon emission time by 25 meV electrons (m* = 0.067m0)
Controlled oxygen ‘poisoning’ of cesiation used to vary electron affinity  from 0.1 eV to +0.2 eV
BOTH QE and MTE measured as a function of 
VB
CB
[Zn] = 1019 cm-3
Evac.

ħω
wd

## Slide 7
Cesiated p-GaAs: Theory vs. Experiment
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
PEA
NEA
 = * + 60meV
PEA
NEA
 Fits to experimental data use kBTe = 27 meV (> 25 meV) due to drift transport in E  3 kV/cm acceleration field
NOTE:  = * + 60 meV shift due to error in assumption of instrument resolution
MTE  kBTe
for large PEA
QE  exp[/kBTe] for large PEA

## Slide 8
Mg-doped p-GaN(0001) photocathode
W.A. Schroeder, L.A. Angeloni, I-J. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
 Spectral measurements performed at UIC;  = 230-410 nm, T = 300 K
Absorption depth 50-100 nm (ħω > Eg) and wd  40 nm
 Short transport limit in strong depletion field
with excess photo-excitation energy in CB
equipartitioned with l = 6 optical phonon modes:
… Electrons emitted in less than ~1 ps
optical phonon decay time
Electron affinity   +2.4 eV for lower CB
 Emission from population in upper CB
with DFT calculated =  0.1(0.2) eV
BOTH QE and MTE measured as a function of ħω
VB
CB
[Mg] = 5x1017 cm-3
Evac.

ħω
wd
Upper CB
2.5 eV

## Slide 9
GaN(0001): MTE
W.A. Schroeder, L.A. Angeloni, I-J. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
Eg = 3.4 eV
Eg = 3.4 eV
NOTE: Untreated epi-polished GaN wafer (Ra < 1 nm)  Surface roughness effects negligible
 Fits to experimental data use ; polaron formation energy għ  75 meV
NEA with   0.3 eV
FC emission within
~10 nm of surface
due to photoexcitation from Mg acceptor states

## Slide 10
Fe-doped Ga2O3(010): Band structure
Thin-slab calculations give Evac. = 6.0(0.2) eV above valence band  point
 Lower CB   +1.2 eV
AND first ‘closed’ upper CB   1.1 eV
Photoexcitation into lower CB primarily from
(i) Two Fe dopant states (ħω < Eg)
([Fe]  1018 cm-3 for semi-insulating behavior)
(ii) Valance band (ħω > Eg)
 Amsterdam Suite with rSCAN functionals
LCB
UCB

## Slide 11
Fe-doped Ga2O3(010): Absorption α(ħω)
BOTH electron transport regimes expected in one photocathode:
‘Long’ transport for ħω < 4.5 eV
 Absorption depth > 400 μm;
Fe dopant state to CB transitions
‘Short’ transport for ħω > 4.5 eV
 Absorption depth < 100 nm;
band-to-band transitions
NOTE:
Strong Eg(T) variation, Urbach absorption
tail, and anisotropic valence band
contribute to Eg,eff.  4.5 eV at 300 K
L.A. Angeloni, I-J. Shan, J.H. Leach, and W.A. Schroeder, Appl. Phys. Lett. 124, 252104 (2024)
 Sample thickness: 450(50) m
‘short’ transport
‘long’ transport
αl

## Slide 12
Fe-doped Ga2O3(010): Two emission signals
Inner signal from direct LCB emission: = 6-7 meV … m* = 0.24m0 at
Dominant outer signal from multi-phonon (g > 1) Franck-Condon emission from NEA UCB (  1.1 eV)
 Two Gaussian decomposition reveals sub-thermal emission signal !!
ħω = 4.33 eV
pT
Inner signal
MTE  6 meV
Outer signal
MTE  280 meV
300 K
Long transport regime
(ħω < Eg  4.5 eV)
 Te → Tlattice
Transport analysis in
internal drift field gives
kBTe  27 meV
L.A. Angeloni, I-J. Shan, J.H. Leach, and W.A. Schroeder, J. Appl. Phys. 139, 095706 (2026)

## Slide 13
Fe-doped Ga2O3(010): MTE
Two emission signals evident throughout
 Inner low MTE signal from lower CB ( > 0)
 Outer high MTE signal from upper CB ( < 0)
MTE is constant in ‘long’ transport regime
 kBTe  27 meV is constant
MTE increases with ħω in ‘short’ transport regime
 Equipartition of energy with l = 6 dominant
optical phonon modes (c.f. Mg:GaN(0001))
Observe step increase in MTE at ħω  Eg
 Evidence for Te increase due to polaron
formation energy;
AND inner signal converts to FC emission
from lower CB
Outer signal
Inner signal
25meV
‘Long’ transport
‘Short’ transport

## Slide 14
PEA:
NEA:
… N less than ||/(ħΩ)  g
NOTE:
… important when
Modified FC analysis: Multi-phonon emission
 Large Fröhlich coupling constant g and finite ħΩ
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, Phys. Rev. Accel. & Beams 28, 123401 (2025)
:
Emission
CB
Polaron
ħω
n = 0
n = 1
n = 2
ħΩ
ħΩ
għΩ

## Slide 15
Summary
Momentum-resonant Franck-Condon (FC) electron emission mechanism
 Mediated by (optical)phonon scattering in semiconductors (q)
Comparison of FC emission theory with experimental data
− Good agreement with MTE and QE measurements for Cs:GaAs and GaN
Fe:Ga2O3(010) photocathode
 Emission consistent with FC mechanism; including polaron formation self-energy
PLUS: Observation of 6 meV MTE ultracold electron emission at 300 K
consistent with for one-step direct band photoemission
Expect dominant FC emission for all polar semiconductor photocathodes
 III-V materials, Cs3Sb, bi-alkali antimonides, Cs2Te … and diamond
NOTE: “Evidence for Umklapp electron scattering emission from metal photocathodes”
I-J. Shan, L.A. Angeloni, and W.A. Schroeder, APS Open Science (accepted for publication)

## Slide 16
Cesiated GaAs: Sub-thermal emission
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
NOTE
Other reports:
G. Vergara et al., J. Appl. Phys. 80, 1809 (1996)
V. Bakin et al., JETP Lett. 77, 167 (2003)
Z. Liu et al., J. Vac Sci. & Tech. B 23, 2758 (2005)
Evidence for direct band contribution?
Less than 5% of total emission
BUT MTE < 25 meV
[m*  0.067m0 for GaAs
with m*(E)  m*()]

## Slide 17
Beam brightness: FC emission prediction
Chart:  (eV)
| -0.5 | -0.45 | -0.4 | -0.35 | -0.3 | -0.25 | -0.2 | -0.17499999999999999 | -0.15 | -0.125 | -0.1 | -7.4999999999999997E-2 | -0.05 | -2.5000000000000001E-2 | -0.01 | 0 | 0.01 | 2.5000000000000001E-2 | 0.05 | 7.4999999999999997E-2 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5
B 300K | 0 | 0.99588 | 0.99502 | 0.99387 | 0.99225 | 0.9899 | 0.9863 | 0.98039 | 0.9759 | 0.9697 | 0.96078 | 0.94737 | 0.92593 | 0.88889 | 0.81818 | 0.74227 | 0.66667 | 0.5678 | 0.41386 | 0.21654 | 0.10372 | 0.047097 | 0.0088133 | 0.0015248 | 0.00025145 | 4.0142e-05 | 6.2609e-06 | 9.5951e-07 | 1.4505e-07 | 2.1687e-08
B 100K | 0.11554 | 0.11552 | 0.1155 | 0.11548 | 0.11543 | 0.11537 | 0.11525 | 0.11515 | 0.115 | 0.11478 | 0.11439 | 0.11366 | 0.11199 | 0.10685 | 0.096477 | 0.077067 | 0.04306 | 0.012542 | 0.0011273 | 8.4316e-05 | 5.7662e-06 | 2.3423e-08 | 8.582e-11 | 2.9651e-13 | 9.8636e-16 | 3.1953e-18 | 1.0151e-20 | 3.1764e-23 | 9.8216e-26
B 500K | 2.7935 | 2.7879 | 2.7805 | 2.7705 | 2.7564 | 2.7359 | 2.7041 | 2.6814 | 2.6516 | 2.6115 | 2.556 | 2.4768 | 2.3589 | 2.1762 | 2.017 | 1.8816 | 1.7205 | 1.4578 | 1.0424 | 0.70862 | 0.46541 | 0.18742 | 0.071071 | 0.025915 | 0.0091937 | 0.0031959 | 0.0010937 | 0.0003697 | 0.00012371
B 400K | 1.8364 | 1.8338 | 1.8303 | 1.8254 | 1.8186 | 1.8083 | 1.7919 | 1.7799 | 1.7638 | 1.7415 | 1.7096 | 1.6617 | 1.5862 | 1.4595 | 1.3403 | 1.2331 | 1.101 | 0.88797 | 0.57256 | 0.34615 | 0.20068 | 0.062241 | 0.018037 | 0.0050066 | 0.0013491 | 0.00035572 | 9.2259e-05 | 2.362e-05 | 5.9839e-06
50 meV | 0.0095173 | 0.036258 | 0.13163 | 0.26847 | 0.43119 | 0.6055 | 0.77784 | 0.93512 | 1.0041 | 1.0644 | 1.1144 | 1.1524 | 1.1767 | 1.1852 | 1.1793 | 1.1469 | 1.084 | 0.9897 | 0.86576 | 0.71747 | 0.55433 | 0.39008 | 0.24131 | 0.12407 | 0.048255 | 0.010045
B 200K | 0.46146 | 0.46126 | 0.46099 | 0.46059 | 0.46002 | 0.45911 | 0.45757 | 0.45636 | 0.45464 | 0.45206 | 0.44798 | 0.44095 | 0.42739 | 0.39655 | 0.35609 | 0.30827 | 0.23969 | 0.14314 | 0.050169 | 0.01556 | 0.0045092 | 0.00033726 | 2.3065e-05 | 1.496e-06 | 9.3692e-08 | 5.724e-09 | 3.4328e-10 | 2.0294e-11 | 1.186e-12
25 meV | 0.0090645 | 0.032908 | 0.067117 | 0.1078 | 0.15137 | 0.19446 | 0.23378 | 0.2661 | 0.28811 | 0.2963 | 0.29483 | 0.271 | 0.21644 | 0.13858 | 0.060327 | 0.012064 | 0.00033515 | 2.9615e-09
100 meV | 0.0097545 | 0.083588 | 0.22118 | 0.78351 | 1.5555 | 2.422 | 3.2763 | 4.0163 | 4.2575 | 4.4576 | 4.6097 | 4.7066 | 4.7407 | 4.7393 | 4.7172 | 4.6672 | 4.5877 | 4.336 | 3.7248 | 2.8699 | 1.8854 | 0.96523 | 0.32313 | 0.047863 | 0.00012081 | 1.4293e-18
Chart:  (eV)
| -0.5 | -0.45 | -0.4 | -0.35 | -0.3 | -0.25 | -0.2 | -0.17499999999999999 | -0.15 | -0.125 | -0.1 | -7.4999999999999997E-2 | -0.05 | -2.5000000000000001E-2 | -0.01 | 0 | 0.01 | 2.5000000000000001E-2 | 0.05 | 7.4999999999999997E-2 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5
B 300K | 0 | 0.99588 | 0.99502 | 0.99387 | 0.99225 | 0.9899 | 0.9863 | 0.98039 | 0.9759 | 0.9697 | 0.96078 | 0.94737 | 0.92593 | 0.88889 | 0.81818 | 0.74227 | 0.66667 | 0.5678 | 0.41386 | 0.21654 | 0.10372 | 0.047097 | 0.0088133 | 0.0015248 | 0.00025145 | 4.0142e-05 | 6.2609e-06 | 9.5951e-07 | 1.4505e-07 | 2.1687e-08
B 100K | 0.11554 | 0.11552 | 0.1155 | 0.11548 | 0.11543 | 0.11537 | 0.11525 | 0.11515 | 0.115 | 0.11478 | 0.11439 | 0.11366 | 0.11199 | 0.10685 | 0.096477 | 0.077067 | 0.04306 | 0.012542 | 0.0011273 | 8.4316e-05 | 5.7662e-06 | 2.3423e-08 | 8.582e-11 | 2.9651e-13 | 9.8636e-16 | 3.1953e-18 | 1.0151e-20 | 3.1764e-23 | 9.8216e-26
B 500K | 2.7935 | 2.7879 | 2.7805 | 2.7705 | 2.7564 | 2.7359 | 2.7041 | 2.6814 | 2.6516 | 2.6115 | 2.556 | 2.4768 | 2.3589 | 2.1762 | 2.017 | 1.8816 | 1.7205 | 1.4578 | 1.0424 | 0.70862 | 0.46541 | 0.18742 | 0.071071 | 0.025915 | 0.0091937 | 0.0031959 | 0.0010937 | 0.0003697 | 0.00012371
B 400K | 1.8364 | 1.8338 | 1.8303 | 1.8254 | 1.8186 | 1.8083 | 1.7919 | 1.7799 | 1.7638 | 1.7415 | 1.7096 | 1.6617 | 1.5862 | 1.4595 | 1.3403 | 1.2331 | 1.101 | 0.88797 | 0.57256 | 0.34615 | 0.20068 | 0.062241 | 0.018037 | 0.0050066 | 0.0013491 | 0.00035572 | 9.2259e-05 | 2.362e-05 | 5.9839e-06
50 meV | 0.0095173 | 0.036258 | 0.13163 | 0.26847 | 0.43119 | 0.6055 | 0.77784 | 0.93512 | 1.0041 | 1.0644 | 1.1144 | 1.1524 | 1.1767 | 1.1852 | 1.1793 | 1.1469 | 1.084 | 0.9897 | 0.86576 | 0.71747 | 0.55433 | 0.39008 | 0.24131 | 0.12407 | 0.048255 | 0.010045
B 200K | 0.46146 | 0.46126 | 0.46099 | 0.46059 | 0.46002 | 0.45911 | 0.45757 | 0.45636 | 0.45464 | 0.45206 | 0.44798 | 0.44095 | 0.42739 | 0.39655 | 0.35609 | 0.30827 | 0.23969 | 0.14314 | 0.050169 | 0.01556 | 0.0045092 | 0.00033726 | 2.3065e-05 | 1.496e-06 | 9.3692e-08 | 5.724e-09 | 3.4328e-10 | 2.0294e-11 | 1.186e-12
25 meV | 0.0090645 | 0.032908 | 0.067117 | 0.1078 | 0.15137 | 0.19446 | 0.23378 | 0.2661 | 0.28811 | 0.2963 | 0.29483 | 0.271 | 0.21644 | 0.13858 | 0.060327 | 0.012064 | 0.00033515 | 2.9615e-09
100 meV | 0.0097545 | 0.083588 | 0.22118 | 0.78351 | 1.5555 | 2.422 | 3.2763 | 4.0163 | 4.2575 | 4.4576 | 4.6097 | 4.7066 | 4.7407 | 4.7393 | 4.7172 | 4.6672 | 4.5877 | 4.336 | 3.7248 | 2.8699 | 1.8854 | 0.96523 | 0.32313 | 0.047863 | 0.00012081 | 1.4293e-18
Brightness (a.u.)
 (eV)
= 500 K
400 K
300 K
200 K
100 K
MTE = 100 meV
MTE = 50 meV
MTE = 25 meV
 Optimum  for maximum beam brightness: Analytical evaluation in ħΩ  0 limit for one emission band
For any polar semiconductor
photocathode maximum beam
brightness achieved for   0
at a fixed desired MTE
Plotting transverse beam brightness
as a function of  reveals:
Higher for higher
 Cooling may not help unless one wants low MTE
(ii) MTE = 25 meV cannot be attained for 300 K
BUT: MTE 50 meV is readily achievable for
room temperature photocathodes
(e.g., in long transport limit)

## Slide 18
Thank You !

## Slide 19
One-step photoemission analysis
W.A. Schroeder and G. Adhikari, New J. Phys. 21 (2019) 033040
pz
pz
pz
E
E
E
Vacuum states
Virtual states
Bulk states
ħω
Vacuum
(m0)
Crystal
(mz , mT)
qEcath.z
ԐF
ΔE
Photoemission
Field emission
Exact 1-D quantum solution for triangular barrier
 Above and below threshold emission
Extension for photoemission simulation includes:
i) pT conservation
ii) Band dispersion fits; e.g.
iii) Fermi-Dirac population distribution; Te
iv) Bulk local DOS
v) Vacuum density of states

## Slide 20
Metallized diamond(001): A hybrid photocathode
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, arXiv.2506.12550 (accepted for publication in PRAB)
 0.5 mm-thick CVD diamond: Back surface metallized [annealed C-Ti (+Pt+Au)]
Back surface photo-injection from Ti into diamond CB for ħω > 3.2 eV
Electron drift transport to emission face due to applied DC gun field
 kBTe  30 meV
… E  3kV/cm, ħΩ = 165 meV
Emission from upper (  0.8 eV) and lower (  0.8 eV) CBs
 Two emission signals

## Slide 21
Metallized diamond(001): MTE and QE
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, arXiv.2506.12550 (accepted for publication in PRAB)
Upper CB
Lower CB
MTE
Total QE
 Multi-phonon emission: g = 1.1, ħΩ = 165 meV, plus polaron self energy
Back surface injection efficiency with Ti DOS