## Slide 1: High polarization photocathodes at Mainz
Kurt Aulenbacher for the MESA Team
Institut für Kernphysik
JGU Mainz
ERL Workshop, Orsay, 22. 09. 2026

## Slide 2: Outline
MESA Photocathode requirements
Cathode for ERL-commissioning
Surface Photovoltage
Cathode supply chain problem
Ion backbombardment mitigation

## Slide 3: MAINZ ENERGY-RECOVERING ACCELERATOR (MESA)
Op-mode | Target | Av. Beam current/Charge lifetime | Polarisation requirement
Ext. Beam (EB) „P2 Experiment“ | Solid/ Liquid | 0.15mA/ >1000C | >80%
Energy recovery(ERL) | Gas-jet | >1mA (10 mA later) >1000C | Not yet
P2 Experiment
80 Meter

## Slide 4: Experiment P2
D. Becker et al. Eur. Phys. J. A 54 (2018) 11, 208
DOI: 10.1140/epja/i2018-12611-6 &166,
Weak charge of the proton:
A weak charge measurement with accuracy 1.4%
yields an accuracy Dsin2(qW)/sin2(qW) =0.16%.....
The asymmetry is
10000 hours of data taking needed when P>85% and current 0.15mA

## Slide 5: DC-Sources at MAINZ
„old MAMI source, PKA1“ ; 2 in operation (3 until 2022)
MESA source „STEAM“ (inverted, no HV-cage)
– in comparison to
MAMI source ( shown without HV- cage)
STEAM=
Small Thermalized-Source At Mainz

## Slide 6: STEAM Synchro-Laser Systems
TYPE | Wavelength | Time structure | Av. power | Remark
Gain Switched Diode „TAIKO“ | 405nm | Single shot to 100MHz 50ps or DC | 0.05 W (0.5nJ /pulse) | Tuning of MESA Unpolarized QE for 10pC: 6%
Er:doped fiber MOPA „MANNY“ | 778 nm | 1300MHz/2N N<10 50-200ps | >3 W >100nJ /pulse | Polarized beam QE for 10pC: 0.2%
TAIKO-Laser at test installation
Size about 10cm
Injected by „side window“

## Slide 7: MESA source in operatiON (SO FAR)!
Spin rotator and beam diagnostics
for Parity experiment
Normalized Emittance measured
(405nm, DC, low current):0.09 mm.
3*larger than expected)

## Slide 8: High bunch charge cathode FoR MESA?
5nm-GaAs:C 5e19cm-3 auf 1μm-GaAs:C 5e17cm-3
5nm-GaAs:Be 5e19cm-3 auf 1μm-GaAs:Be 5e17cm-
Cooperation with Heinrich Hertz Institut /Fraunhofer Gesellschaft
Goal to reproduce high polarization cathodes
First issue gradient doping: high QE low SPV, low depolarization
Test structures delivered by Heinrich Hertz Institut Berlin:
Low doped
GaAs
High doped
GaAs
Photocurrent
Diff current
Majority of diffusion current ends up in surface zone/band bending region
High doping required for fast recombination (nanosecond time scale)
High doping for thin band bending region
Photons

## Slide 9
-QE good enough for 10pC bunches
(15% at 650nm)
-thin enough for resonable bunch length
-very suitable for optimization of MESA with TAIKO Laser in single bunch mode
But polarization too low (est. 40-45 %)

## Slide 10
1mm suitable for 80ps long laser pulses from MESA lasers

## Slide 11: Surface photO-voltage?
N. Scahill, PhD thesis Mainz 2022
Experiment: Bulk GaAs, doping 2E19cm-3 l=800nm
Produce short pulse with
constant Fluence of 2*10-4 pC/mm2 at varying QE
Pulse Tail supression below QE=10-4 %
QE is reduced after a certain fluence of diffusion current is reached
Effect is attributed to surface photovoltage, see Mulhollan et al :Physics Letters A, 282(4-5):309–318, 2001.
To produce 0.1pC/mm2 for MESA polarized beam requirement we need a QE of > 0.05%.
Low doped
GaAs
High doped
GaAs
Photocurrent
Diff current

## Slide 12: Commercial Cathode at MAMI
Manufactured by SVT company until 2015
Last deliveries: too low polarisation
Surface defects?
N. Scahill and K.A:
J. Appl. Phys. 132, 185702 (2022); doi: 10.1063/5.0108675

## Slide 13: SVT Cathode in USE aT MAINZ
Mott scattering asymmetry measured at 44 keV
Very low analysing power
 Polarisation 80-90% in maximum
QE~0.5%-0.9% at maximum Polarization
The strained superlattice cathode from SVT can do the job at MESA….
But …….
It is no longer possible to purchase from company … Our Stocks are empty
N. Scahill and K.A:
J. Appl. Phys. 132, 185702 (2022); doi: 10.1063/5.0108675

## Slide 14: SVT Cathode Alternative
Chinese Company ACKEN:
Quarter of a Wafer delivered
Defects on surface visble
Polarisation as good as SVT, measured in direct comparison at MAMI
QE a bit lower
activation problem? wavelength?
High linear analysing power (6%)
 inhomogeneous strain relaxation?

## Slide 15: Charge Lifetime –Ion backbordment
Best result of MAMI-source PKA1 (2004)
Vacuum lifetime >1000 hours
Charge lifetime 200C (*)
 Cathode would be reactivated every 2 weeks for P2 (13Coulomb/day)
MESA-source „STEAM“ (**): (2026)
Vacuum 3*10-10 Pa
Vacuum-lifetime >10000 h (405nm)
Charge lifetime: ???
(*): achieved with bulk GaAs (>10mA/Watt) to avoid heating
(**) STEAM= Small Thermalized-Source At Mainz

## Slide 16: How to Cope with Ion Backbombardment /outlook:
+ Pressure level in MESA source „STEAM“ probably lower than at MAMI (longer vacuum lifetime observed)
+ shorter acceleration stage in STEAM compared to MAMI/PKA1
+ repeller available in STEAM to supress ion backstreaming from beamline
If all this does not help, possibilities nevertheless remain :
Larger and more excentic laser spot (Fluence lifetime at MAMI ~2500C/mm2 )
BUT: Keep beam losses low!
Idea: Less sputtering by using heavy Activation/Protection CsBr/CsTe
Materials with large value of negative affinity: GaN/AlGaN superlattices?

## Slide 17: SUMMARY/OUTLOOK
Challenging cathode requirements from the PV-experiments at MESA/MAINZ, in particular charge lifetime
Qbunch/Pulse Energy linearity (surface photovoltage) requires relatively high QE at maximum P
Commercial vendor for GaAs/GaAsP found
Research activities concerning higher charge lifetime: beam dynamics, acivation layers, alternative material with high NEA value.

## Slide 18: Thank You !

## Slide 19: MESA spin polarized photosource „STEAM“
First beam from
Spin-polarized
Photosource
„STEAM“
STEAM
Spin-polarized cathodes are „activated“ on-site and transferred
to source in UHV
Laser | 
type | Er-doped fiber
wavelength | 780nm
Av. power | Up to 4 Watt
Rep-rate | 5-1300 Mhz
Pulse length | 50-250ps
photocathode | 
type | GaAs/GaAsP SL
wavelength | 780nm
Spin-polarization | 80-90%
Quantum efficiency | ~0.5% (3mA/Watt)
Response time | ~1ps
Beam current | 150mA
Charge lifetime | >100 Coulomb
Laser

## Slide 20: MESA Phot0cathode requirements
Source | Operation Voltage | Laser/Time structure | Av. Laserpower/Wavelenght/Pulselenght | Remark
PKA1 | 100kV | Semiconductor MOPA , 2.449 GHz CW. | 0.3W/778nm /80ps | Serves MAMI Accelerator
PKA2 (copy of PKA1) | 100kV | Semiconductor DC | 0.05 W, 808/786nm | Test source for pol. photcathode developments
PKAT (copy of PKA1) | 100kV | Ti:SP, Mode-locked 78 MHz CW | 0.5 W 750-850 nm DC or 0.1ps | Time resolved measurements Dismantled in 2022!
STEAM(*) | 100-150 (200)kV | Er:Fibre MOPA 1-1300MHz CW | >3 W 778 MHz 50-200 ps | Serves MESA Accelerator Alternative laser: Diode 405nm