## Slide 1: Simulation study of nanostructured plasmonic metallic photocathodes
M.Bulgacheva, E.Gjonaj
Technical University of Darmstadt, Germany

## Slide 2: Motivation & workflow
The open question: what impact does the enhanced emission have on the beam quality?
Nanostructured copper photocathodes use surface-plasmon field enhancement to increase QE and therefore photocurrent, which means: the laser energy needed to generate the bunch can be reduced.
Electromagnetic
(Absorption)
Photoemission model
PIC beam dynamics
Workflow:

## Slide 3: Surface-plasmon-enhanced photoemission
Periodic structure
Laser pulse
Increased local absorption
+
Surface Plasmon Polariton (SPP) modes

## Slide 4: Electromagnetic characterization
Geometry: conical nanoholes
Periodic boundary conditions
Plane wave excitation
Optimization objective:
Reflectance minimization at given λ
3 drive wavelengths:
257 nm (UV), 515 nm (green), 800 nm (IR)

## Slide 5: Nanostructured photocathode simulation
Fowler-Dubridge photoemission model
Pλ — absorbed power from FIT (spatially resolved)
Φ(r) — work function, lowered by the Schottky effect
n — photoemission order from local work function
Electromagnetic simulation
  FIT-TD with plane wave excitation
  Geometry optimization
Photoemission model
  Spatially-resolved photocurrent calculation including Schottky
  Emission samples (particle interface)
Beam dynamics simulations
  Near-cathode PIC
  Micro- to macroscale
Power loss density
Fowler-Dubridge + Schottky
Normalized current density

## Slide 6: Charge yield grows sharply with photon order
Which NS cathode requires less pulse energy
to produce a 100pC/250pC bunch?
  UV
  When noting IR→DUV conversion: IR
1-photon
2-photon
3-photon
1-photon (257 nm)
~ 1.2×
2-photon (515 nm)
~ 6×
3-photon (800 nm)
~ 10⁵×
a_n caveat: the multiphoton coefficients are empirical, with a spread of about an order of magnitude. They affect absolute yields and the comparison between emission orders, not the NS-vs-flat ratio at a fixed wavelength.

## Slide 7: Beam dynamics near the cathode
Asymmetric transverse phase space aligned with laser polarization due to SPP field localization at nanohole edges
Larger energy spread than flat Cu: low-energy tail from electrons emitted deep inside the nanohole
Schottky effect suppresses low-energy tail by enhancing top-surface emission
The geometry causes a charge loss inside the UV nanostructure
UV (257 nm) cathode

## Slide 8: Anisotropy vs. photoemission order
With the photoemission order increasing, the beam asymmetry also increases because of the stronger enhanced field localization on the rims of the nanohole.

## Slide 9: Anisotropy vs. photoemission order
With the photoemission order increasing, the beam asymmetry also increases because of the stronger enhanced field localization on the rims of the nanohole.

## Slide 10: Charge loss is geometric
 | 100 pC | 250 pC
transverse | flat-top, σ = 0.16 mm | flat-top, σ = 0.25 mm
temporal | Gaussian, σ_t = 7 ps | Gaussian, σ_t = 3 ps
Transmission at 100 pC (10 nm plane): flat cathode 99% at all wavelengths; NS: 92% (UV), >98% (green, IR).
UV: the deep nanohole (360 nm) traps electrons emitted from the inner walls: about 8% are lost, plus a further 1% during the drift to 500 nm → the loss is geometric.
IR, green: negligible charge loss at 100 pC and 250 pC.
Space charge maximum is located at roughly 100 nm above the surface; inside the cones the charge density decreases.

## Slide 11: Micro- to macroscale: scale-up procedure
PIC near-cathode simulation (micro-scale)
Full-scale e-gun simulations (cluster)
Homogenization with ML and scale-up
Virtual cathode
Planar reference plane at a distance above the nanostructure.
Discrete 6D data
Macroparticle distributions from single-cell PIC runs.
Normalizing flows
Invertible network mapping particles → continuous 6D density.
Full-cathode seeding
Model replicated across the cathode, weighted by the laser intensity profile.
Notes: This is an invertible neuronal network, which is trained by the particle data

## Slide 12: Conclusions
Charge yield increases sharply with photon order: nanostructuring increases the charge by ~1.2× (1-photon, 257 nm), ~6× (2-photon, 515 nm), and ~105× (3-photon, 800 nm) vs flat copper.
Nanostructuring leads to beam quality degradation: emittance and energy spread increase over flat copper; the Schottky effect partially compensates by suppressing the low-energy tail.
UV charge loss is geometric: geometric trapping in the deep UV structure (92% transmission), independent of bunch charge; no space-charge-driven loss at any wavelength.
Electromagnetic optimization (max. QE)
Beam dynamics optimization (min. emittance)
TRADEOFF