## Slide 1: Photoemission from ab initio slabs
Finding a happy medium between effort and fidelity.
Felix Mildner, Prof Nicholas Harrison
23/09/2026

## Slide 2: Emission Modelling
Comp. requirements vs granularity
Dowell - Schmerge model
extended Dowell - Schmerge
Vecchione, et al. DOS dependent Saha et al. Full Scattering Formalism
Pendry
D. H. Dowell and J. F. Schmerge, Physical Review Special Topics - Accelerators and Beams, 2009, 12, 074201.
T. Vecchione, D. H. Dowell, W. Wan, J. Feng and H. A. Padmore, New York, 2013.
P. Saha, O. Chubenko, J. Kevin Nangoi, T. Arias, E. Montgomery, S. Poddar, H. A. Padmore and S. Karkare, Journal of Applied Physics, 2023, 133.
J. B. Pendry, Surface Science, 1976, 57, 679–705.

## Slide 3: Emission Modelling
Comp. requirements vs granularity
Dowell - Schmerge model
extended Dowell - Schmerge
Vecchione, et al. DOS dependent Saha et al. Full Scattering Formalism
Pendry
D. H. Dowell and J. F. Schmerge, Physical Review Special Topics - Accelerators and Beams, 2009, 12, 074201.
T. Vecchione, D. H. Dowell, W. Wan, J. Feng and H. A. Padmore, New York, 2013.
P. Saha, O. Chubenko, J. Kevin Nangoi, T. Arias, E. Montgomery, S. Poddar, H. A. Padmore and S. Karkare, Journal of Applied Physics, 2023, 133.
J. B. Pendry, Surface Science, 1976, 57, 679–705.
Happy medium? – slabs with DFT + individual band excitations

## Slide 4: The specifics of our approach
Slabs vs Bulk, DOS vs Single K
Cu Bulk
Cu(100) 16 layers

## Slide 5: The specifics of our approach
Slabs vs Bulk, DOS vs Single K
Cu Bulk
Cu(100) 16 layers

## Slide 6: The specifics of our approach
Slabs vs Bulk, DOS vs Single K
Cu Bulk
Cu(100) 16 layers
Expectations:
can explicitly model surfaces and surface features
largest uncertainties at threshold
QE/MTE curves noisy without broad smearing

## Slide 7: Emission model
Layer dependent contributions
Depth dependent light intensity Depth dependent excitation probability Depth dependent transmission + emission probability
- reflection of slab
- Absorption of layer i
Fermi’s Golden Rule
Ag(100) 10L

## Slide 8: Emission model
Layer dependent contributions
Depth dependent light intensity Depth dependent excitation probability Depth dependent transmission + emission probability
- reflection of slab
- Absorption of layer i
Fermi’s Golden Rule
Ag(100) 10L

## Slide 9: Emission model
Layer dependent contributions
Depth dependent light intensity Depth dependent excitation probability Depth dependent transmission + emission probability
- reflection of slab
- Absorption of layer i
Fermi’s Golden Rule
Ag(100) 10L

## Slide 10: Workflow
From DFT to Curves

## Slide 11: Calculating Metallic Surfaces
Cu data

## Slide 12: Calculating Metallic Surfaces
Cu data

## Slide 13: Calculating Metallic Surfaces
Cu data

## Slide 14: Supercell Structures
Doing interesting material combos!
Ag/MgO(100)
primitive cell
Cu(100) 1x1
CO on Cu(100)
super-cell structures
Cu/MgO(100)

## Slide 15: Supercell Emission
Mapping to reclaim PC behaviour
primitive cell Cu(100) 1x1 Ag/MgO(100)
super-cell Cu(100) 2x2 Cu/MgO(100)

## Slide 16: Supercell Emission
Contributions in Basis Set

## Slide 17: Supercell Emission
Mapping to reclaim PC behaviour
primitive cell Cu(100) 1x1 Ag/MgO(100)
super-cell Cu(100) 2x2 Cu/MgO(100)

## Slide 18: Heterostructure Photocathodes
MgO(100)/Cu(100) Interface – 3step

## Slide 19: Semiconducting Photocathodes
PRELIMINARY – monoclinic -CsSb
3-step Model
R2SCAN, ultra-soft PS (RSCAN), 600eV cutoff
Gap: indirect, 0.77 eV
C. T. Parzyck et al., APL Mater. 11, 101125
Bulk bands

## Slide 20: More current + future work
Have we found a happy medium?
higher energy response curves for Bloch and PW final states (3-step vs 1-step)
photo-response of other heterointerface structures
More detailed analyses
Open questions / ToDo :
OptaDOS module code due to be released!
What is the IMFP of an electron a few eV above actually?
adsorbates, gases, oxidation
NEA, spin-polarised emission

## Slide 21: Thank you!
Photoemission from Ab initio slabs 23/09/2026
Prof Nicholas Harrison
and the other members of the
Computational Materials Science Group
Dr Tim Noakes, Dr Lee Jones,
Dr Chris Benjamin, Hugh Churn
Prof Sam Cooper

## Slide 22: Metal Photocathodes
Cu(100)

## Slide 23: Metal Photocathodes
Cu(110)

## Slide 24: Metal Photocathodes
Cu(111)

## Slide 25: Heterointerface Photocathode
MgO(100)/Ag(100) interface

## Slide 26: Higher Energy EDCs
Ag(100)

## Slide 27: 1Step Emission