## Slide 1
Photocathode for Accelerator Science in Europe (PhASE26) Workshop
IJC Lab, Orsay, France, September 21-23, 2026.
Photocathode Physics:
A Band Structure Perspective
W. Andreas Schroeder
Professor of Physics (retired)
University of Illinois Chicago
Department of Energy
DE-SC0020387
Theodore Vecchione
SLAC
UIC researchers: Gowri Adhikari
Louis A. Angeloni
Ir-Jene Shan
Lee B. Jones
ASTeC, STFC Daresbury Laboratory, UK

## Slide 2
Outline
Introduction
Direct ‘one-step’ band photoemission
 Physics of emitting band states and recipient vacuum states
 Comparison to Cu(001) and Cu(111) data
Optical phonon mediated Franck-Condon (FC) electron emission
 Energy (E) and momentum (p) resonant
 Examples: Cesiated GaAs, GaN(0001), and Fe:Ga2O3(010)
… includes observation of ultracold emission: MTE  6meV at 300K
Umklapp electron scattering FC emission
 Reciprocal lattice vector (G) mediated
 QE and MTE measurements: Cu(001) vs. W(111)
Summary

## Slide 3
A brief (and incomplete) history of photoemission
1887 H. Hertz observed the photoelectric effect
1888 A. Stoletov’s law:
1902 P. Lenard: Emitted electron energy independent of
1905 A. Einstein: (Nobel prize 1921)
1914 R.A. Millikan verified Einstein’s photoemission relation
(Nobel prize 1923)
21st century P. Agnostini, F. Krausz, and A. L’Huillier (Nobel prize 2023)
… and others (with phase-locked sub-fs high harmonic pulses)
~100 as (~0.1 fs) required to ‘liberate’ a photoelectron from tungsten
A.L. Cavalieri et al., Nature 449, 1029 (2007)
M. Ossiander et al., Nature 561, 374 (2018)

## Slide 4
Metal photocathodes: Response time
D. Gall, J. Appl. Phys. 119, 085101 (2016)
Simplified analysis:
DFT-based evaluation of Fermi velocity for metals
indicates m/s
… consistent with Sommerfeld free-electron
model of metals;
Typical UV absorption depth  10 nm
 Average emission time  10 fs
… a response time much shorter than typical
employed incident laser pulse durations;
i.e., effectively instantaneous

## Slide 5
A brief history of contemporary photocathode physics
1964 C.N. Berglund & W.E. Spicer: 3-step photoemission model
(i) Electron photoexcitation
(ii) Electron transport to emission face
(iii) Electron emission
1970 G.D. Mahan: One-step photoemission model
 A quantum approach linking interior bulk and vacuum states
2009 D.H. Dowell & J.F. Schmerge (DS) photoemission analysis:
2013 T. Vecchione et al.: Temperature extension of DS model
 MTE  below threshold (E < 0)
C.N. Berglund & W.E. Spicer, Phys. Rev. 136, A1030 (1964)
G.D. Mahan, Phys. Rev. B 2, 4334 (1970)
D.H. Dowell & J.F. Schmerge, Phys. Rev. ST Accel & Beams 12, 074201 (2009)
T. Vecchione et al., paper TUPSO83 in Proceedings of FEL2013 (JaCOW Publishing, NY)

## Slide 6
One-step photoemission analysis
W.A. Schroeder and G. Adhikari, New J. Phys. 21 (2019) 033040
pz
pz
pz
E
E
E
Vacuum states
Virtual states
Bulk states
ħω
Vacuum
(m0)
Metal
crystal
(mz , mT)
qEcath.z
ԐF
ΔE
Photoemission
Field emission
Exact 1-D quantum solution for triangular barrier
 Above and below threshold emission
Extension for photoemission simulation includes:
i) pT conservation
ii) Band dispersion fits; e.g.
iii) Fermi-Dirac population distribution; Te
iv) Bulk local DOS
v) Vacuum density of states

## Slide 7
Cu(001): A ‘canonical’ metal photocathode
Occupied X emission states near Fermi level exist for all (until E exceeds about 10 eV)
  Bulk band structure does not
  restrict MTE
Bulk DOS are relatively constant for emitting states around E  0
 Close to DS model conditions
www.hzdr.de/projects/fermisur/cu.html

## Slide 8
Cu(001): Fits to emitting bands
 DFT evaluation of electronic structure; Amsterdam suite with r2SCAN potentials
Transverse (T)
Longitudinal (z)
with n = 3

## Slide 9
Cu(001): Experiment vs.Theory
Experiment(s) and theory (red line) agree
that below threshold MTE decreases to
28-29 meV rather than = 25 meV
  Effect of recipient vacuum DOS !!
… The probability of transition into
recipient vacuum states proportional
to  a bias to higher
vacuum energies leading to
somewhat higher MTE values
 Experimental data from LBNL and UIC at 300 K
Any photocathode emission
model must include the physics
of the recipient vacuum states
Chart: E (eV)
| -0.2 | -0.15 | -0.1 | -0.05 | -2.5000000000000001E-2 | 0 | 2.5000000000000001E-2 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.4 | 0.5
Theory | 27.63 | 27.98 | 28.52 | 29.4 | 30.21 | 31.67 | 33.99 | 37.29 | 46.66 | 58.45 | 71.52 | 85.07 | 99.02 | 127.1 | 155.26
Expt.1 | 400.717 | 388.8915 | 387.3375 | 405.552 | 226.5808 | 157.8764 | 100.5294 | 67.162 | 53.8533 | 39.1393 | 24.8061 | 28.9013 | 29.1756
LBNL | 29.3 | 30 | 33 | 39 | 48.5 | 60.5 | 73
UIC | 29 | 39 | 54 | 68
dE/3 | 0 | 83.3333
LBNL
UIC
UIC
25 meV

## Slide 10
Cu(111) photocathode
E. Pedersoli et al., Appl. Phys. Lett. 93, 183505 (2008)
L-point hole in Fermi surface
  NO occupied states at Fermi level
  for = 0
DFT-based ‘thin-slab’ calculations and literature indicate = 4.95(±0.2) eV
BUT
Emission observed for ħω < 4.9 eV
... Due to rapidly thermalized electron
distribution photoexcited into
upper conduction band at L-point

## Slide 11
Cu(111): Photoexcitation
① Photoexcitation threshold
 Fermi level to Band 2
 Finite thermalized electron temperature
② L-point photoexcitation ( = 0)

 Minimum for
③ photoexcitation
 Largest thermalized electron temperature
due to strong band dispersion
 Expect “ √ ” shaped spectral MTE
dependence based on predicted
①
②
③

## Slide 12
Cu(111): MTE
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, AIP Advances 12, 105129 (2022)
①
③
②
Experimental MTE data consistent with theoretical expectations (red line) using = 0.38 eV, = 4.16 eV, and determined band effective mass values
  0.8 eV
Deviation from theory for ħω > 4.7 eV due to anisotropic electron thermalization
MTE turn-over for ħω > 5 eV due to ‘cold’ electrons from direct photoemission
Band dispersion(s) and energetic
positions determine initial of
thermalized photoexcited electron
distribution

## Slide 13
Cu(111): QE
Observed ‘kink’ in QE measurements consistent with two emission mechanisms:
  Thermalized electron emission from UCB
  Direct band emission for ħω >
Spectral QE dependence not quadratic;
DO NOT expect
DO expect multiple (simultaneous)
photoemission processes
(eV)
G. Gobeli and F. Allen, Phys. Rev. 137, A245 (1965)

## Slide 14
Semiconductor photocathodes
Photoemission usually described using Spicer’s 3-step model
BUT NOTE
Nearly all studied semiconductor photocathodes are strongly polar
 Significant optical deformation potential scattering
(i.e., electron-(optical)phonon or Fröhlich scattering)
(i) Photoexcitation: Determines electron’s initial excess conduction band energy
(ii) Transport (and thermalization physics): Determines at emission
 Long and short transport length limits
 Optical phonon scattering dynamics and drift transport play a pivotal role
(iii) Emission: Two mechanisms have been observed
 Direct band emission
 (Optical)phonon-mediated Franck-Condon emission
 Polar semiconductors: Cs:GaAs, GaN, CsTe, alkali antimonides, bi-alkali antimonides, etc. … and diamond!
Semiconductor Physics – An Introduction, K. Seeger, 4th Ed., Springer-Verlag

## Slide 15
Prior work: H-terminated diamond(001)
J.D. Rameau, J. Smedley, E.M. Muller, T.E. Kidd, and P.D. Johnson, Phys. Rev. Lett. 106, 137602 (2011)
Emitted electrons from NEA CBM
eff = Evac – (ECBM  għ)  0.96 eV
… għ is real part of the electron-
polaron self energy and the
dimensionless Fröhlich coupling
constant for diamond g = 1.1
Emission ‘bands’ are replicas of electron distribution in CB separated by ħ = 165 meV optical phonon energy
I(n) = e-ggn/n! Poisson statistics govern emission strength for nth phonon band
(n = 0, 1, 2, …)
 ARPES measurement; ħω = 6.01 eV (208 nm)  α  4000 cm-1 (absorption depth  2.5 m)
n = 0
n = 1
n = 2
n = 3
.
.

## Slide 16
Franck-Condon mechanism in photoemission
Energy and momentum resonant emission:
… intermediate scattering optical phonon
of energy ħΩ and momentum q
Effective internal () and emitted vacuum () electron momenta matched; so that
q
p0
p

x,y
z
Photocathode
Vacuum
n = 1
 Phonon scattering based electron emission from semiconductor photocathodes

## Slide 17
Franck-Condon emission theory
W.A. Schroeder, L.A. Angeloni, I-J. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
 Analytical evaluation in parabolic band approximation with thermalized electron distribution at Te; ħΩ → 0
PEA
( > 0)
NEA
( < 0)
p0
E
p
E

vacuum
bulk
p0
E
p
E

vacuum
bulk
p0 = p + nq
p0 = p + nq

## Slide 18
Cesiated p-GaAs photocathode
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
 Measurements performed using TESS (Daresbury Laboratory, U.K.);  = 808 nm, T = 300 K
Absorption depth ~1 μm at 808 nm
 Long transport limit with low excess photo-
excitation energy in CB (ECB < 100 meV)
 Expect kBTe  25 meV due to rapid carrier
cooling during drift to emission face
Surface depletion region wd  10 nm traversed in less than ~200 fs optical phonon emission time by 25 meV electrons (m* = 0.067m0)
Controlled oxygen ‘poisoning’ of cesiation used to vary electron affinity  from 0.1 eV to +0.2 eV
BOTH QE and MTE measured as a function of 
VB
CB
[Zn] = 1019 cm-3
Evac.

ħω
wd

## Slide 19
Cesiated p-GaAs: MTE
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
Fit to experimental data employs one parameter: kBTe = 27 meV
 Consistent with expected drift of
electron distribution to emission
face in GaAs under E  3 kV/cm
acceleration field
MTE  kBTe for large PEA
 Expected for Boltzmann tail emission
NOTE:
 = * + 60 meV shift due to error in
assumption of instrument resolution
PEA
NEA
 = * + 60meV

## Slide 20
Cesiated p-GaAs: QE
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
Fit to experimental  dependence again employs kBTe = 27 meV
 Consistent with MTE data !!
Boltzmann tail emission drives exponential decay in QE with  for
large PEA
PEA
NEA
Emission band’s electron affinity
 and determine QE and
MTE of FC emission process

## Slide 21
Mg-doped p-GaN(0001) photocathode
W.A. Schroeder, L.A. Angeloni, I-J. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
 Spectral measurements performed at UIC;  = 230-410 nm, T = 300 K
Absorption depth 50-100 nm (ħω > Eg) and wd  40 nm
 Short transport limit in strong depletion field
with excess photo-excitation energy in CB
equipartitioned with l = 6 optical phonon modes:
… Electrons emitted in less than ~1 ps
optical phonon decay time
Electron affinity   +2.4 eV for lower CB
 Emission from population in upper CB
with DFT calculated =  0.1(0.2) eV
BOTH QE and MTE measured as a function of ħω
VB
CB
[Mg] = 5x1017 cm-3
Evac.

ħω
wd
Upper CB
2.5 eV

## Slide 22
GaN(0001): MTE
W.A. Schroeder, L.A. Angeloni, I-R. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
MTE consistent with
… kBTD = 75 meV ( the
‘average’ polaron formation energy)
MTE  230 meV at ħω = Eg (ECB  0) implies eff  0.3 eV in ~100 kV/cm surface depletion field
 Optical phonon mediated Franck-
Condon emission is from within
~10 nm of photocathode surface
Eg = 3.4eV

## Slide 23
GaN(0001): QE
W.A. Schroeder, L.A. Angeloni, I-R. Shan, and L.B. Jones, Phys. Rev. Applied 23, 054065 (2023)
Eg = 3.4eV
Same kBTe(ħω) dependence using
 = 0.3 eV also consistent with
measured spectral QE dependence
Overall QE significantly lower than for Cs:GaAs photocathode as CB = +2.4 eV
Signal below Eg due to photoexcitation from Mg dopants (EA = 0.1-0.2 eV)
NOTE:
Untreated epi-polished GaN wafer (Ra < 1 nm)
 Surface roughness effects negligible

## Slide 24
Fe-doped Ga2O3(010): Band structure
Thin-slab calculations give Evac. = 6.0(0.2) eV above valence band  point
 Lower CB   +1.2 eV
AND first ‘closed’ upper CB   1.1 eV
Photoexcitation into lower CB primarily from
(i) Two Fe dopant states (ħω < Eg)
([Fe]  1018 cm-3 for semi-insulating behavior)
(ii) Valance band (ħω > Eg)
 Amsterdam Suite with rSCAN functionals
LCB
UCB

## Slide 25
Fe-doped Ga2O3(010): Absorption α(ħω)
BOTH electron transport regimes expected in one photocathode:
‘Long’ transport for ħω < 4.5 eV
 Absorption depth > 400 μm;
Fe dopant state to CB transitions
‘Short’ transport for ħω > 4.5 eV
 Absorption depth < 100 nm;
band-to-band transitions
NOTE:
Strong Eg(T) variation, Urbach absorption
tail, and anisotropic valence band
contribute to Eg,eff.  4.5 eV at 300 K
L.A. Angeloni, I-J. Shan, J.H. Leach, and W.A. Schroeder, Appl. Phys. Lett. 124, 252104 (2024)
 Sample thickness: 450(50) m
‘short’ transport
‘long’ transport
αl

## Slide 26
Fe-doped Ga2O3(010): Two emission signals
Inner signal from direct LCB emission: = 6-7 meV … m* = 0.24m0 at = 0
Dominant outer signal from multi-phonon (g > 1) Franck-Condon emission from NEA UCB (  1.1 eV)
 Two Gaussian decomposition reveals sub-thermal emission signal !!
ħω = 4.33 eV
pT
Inner signal
MTE  6 meV
Outer signal
MTE  280 meV
300 K
Long transport regime
(ħω < Eg  4.5 eV)
 Te → Tlattice
Transport analysis in
internal drift field gives
kBTe  27 meV
L.A. Angeloni, I-J. Shan, J.H. Leach, and W.A. Schroeder, J. Appl. Phys. 139, 095706 (2026)

## Slide 27
Fe-doped Ga2O3(010): MTE
Two emission signals evident throughout
 Inner low MTE signal from lower CB ( > 0)
 Outer high MTE signal from upper CB ( < 0)
MTE is constant in ‘long’ transport regime
 kBTe  27 meV is constant
MTE increases with ħω in ‘short’ transport regime
 Equipartition of with l = 6 dominant
optical phonon modes (c.f. Mg:GaN(0001))
Observe step increase in MTE at ħω  Eg
 Evidence for Te increase due to polaron
formation energy;
AND inner signal converts to FC emission
from lower CB
Outer signal
Inner signal
25meV
‘Long’ transport
‘Short’ transport

## Slide 28
PEA:
NEA:
… N less than ||/(ħΩ)  g
NOTE:
… important when
Modified FC analysis: Multi-phonon emission
 Large Fröhlich coupling constant g and finite ħΩ  Significant polaron energy għΩ
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, Phys. Rev. Accel. & Beams 28, 123401 (2025)
:
Emission
CB
Polaron
ħω
n = 0
n = 1
n = 2
ħΩ
ħΩ
għΩ

## Slide 29
Beam brightness: FC emission
Chart:  (eV)
| -0.5 | -0.45 | -0.4 | -0.35 | -0.3 | -0.25 | -0.2 | -0.17499999999999999 | -0.15 | -0.125 | -0.1 | -7.4999999999999997E-2 | -0.05 | -2.5000000000000001E-2 | -0.01 | 0 | 0.01 | 2.5000000000000001E-2 | 0.05 | 7.4999999999999997E-2 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5
B 300K | 0 | 0.99588 | 0.99502 | 0.99387 | 0.99225 | 0.9899 | 0.9863 | 0.98039 | 0.9759 | 0.9697 | 0.96078 | 0.94737 | 0.92593 | 0.88889 | 0.81818 | 0.74227 | 0.66667 | 0.5678 | 0.41386 | 0.21654 | 0.10372 | 0.047097 | 0.0088133 | 0.0015248 | 0.00025145 | 4.0142e-05 | 6.2609e-06 | 9.5951e-07 | 1.4505e-07 | 2.1687e-08
B 100K | 0.11554 | 0.11552 | 0.1155 | 0.11548 | 0.11543 | 0.11537 | 0.11525 | 0.11515 | 0.115 | 0.11478 | 0.11439 | 0.11366 | 0.11199 | 0.10685 | 0.096477 | 0.077067 | 0.04306 | 0.012542 | 0.0011273 | 8.4316e-05 | 5.7662e-06 | 2.3423e-08 | 8.582e-11 | 2.9651e-13 | 9.8636e-16 | 3.1953e-18 | 1.0151e-20 | 3.1764e-23 | 9.8216e-26
B 500K | 2.7935 | 2.7879 | 2.7805 | 2.7705 | 2.7564 | 2.7359 | 2.7041 | 2.6814 | 2.6516 | 2.6115 | 2.556 | 2.4768 | 2.3589 | 2.1762 | 2.017 | 1.8816 | 1.7205 | 1.4578 | 1.0424 | 0.70862 | 0.46541 | 0.18742 | 0.071071 | 0.025915 | 0.0091937 | 0.0031959 | 0.0010937 | 0.0003697 | 0.00012371
B 400K | 1.8364 | 1.8338 | 1.8303 | 1.8254 | 1.8186 | 1.8083 | 1.7919 | 1.7799 | 1.7638 | 1.7415 | 1.7096 | 1.6617 | 1.5862 | 1.4595 | 1.3403 | 1.2331 | 1.101 | 0.88797 | 0.57256 | 0.34615 | 0.20068 | 0.062241 | 0.018037 | 0.0050066 | 0.0013491 | 0.00035572 | 9.2259e-05 | 2.362e-05 | 5.9839e-06
50 meV | 0.0095173 | 0.036258 | 0.13163 | 0.26847 | 0.43119 | 0.6055 | 0.77784 | 0.93512 | 1.0041 | 1.0644 | 1.1144 | 1.1524 | 1.1767 | 1.1852 | 1.1793 | 1.1469 | 1.084 | 0.9897 | 0.86576 | 0.71747 | 0.55433 | 0.39008 | 0.24131 | 0.12407 | 0.048255 | 0.010045
B 200K | 0.46146 | 0.46126 | 0.46099 | 0.46059 | 0.46002 | 0.45911 | 0.45757 | 0.45636 | 0.45464 | 0.45206 | 0.44798 | 0.44095 | 0.42739 | 0.39655 | 0.35609 | 0.30827 | 0.23969 | 0.14314 | 0.050169 | 0.01556 | 0.0045092 | 0.00033726 | 2.3065e-05 | 1.496e-06 | 9.3692e-08 | 5.724e-09 | 3.4328e-10 | 2.0294e-11 | 1.186e-12
25 meV | 0.0090645 | 0.032908 | 0.067117 | 0.1078 | 0.15137 | 0.19446 | 0.23378 | 0.2661 | 0.28811 | 0.2963 | 0.29483 | 0.271 | 0.21644 | 0.13858 | 0.060327 | 0.012064 | 0.00033515 | 2.9615e-09
100 meV | 0.0097545 | 0.083588 | 0.22118 | 0.78351 | 1.5555 | 2.422 | 3.2763 | 4.0163 | 4.2575 | 4.4576 | 4.6097 | 4.7066 | 4.7407 | 4.7393 | 4.7172 | 4.6672 | 4.5877 | 4.336 | 3.7248 | 2.8699 | 1.8854 | 0.96523 | 0.32313 | 0.047863 | 0.00012081 | 1.4293e-18
Chart:  (eV)
| -0.5 | -0.45 | -0.4 | -0.35 | -0.3 | -0.25 | -0.2 | -0.17499999999999999 | -0.15 | -0.125 | -0.1 | -7.4999999999999997E-2 | -0.05 | -2.5000000000000001E-2 | -0.01 | 0 | 0.01 | 2.5000000000000001E-2 | 0.05 | 7.4999999999999997E-2 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5
B 300K | 0 | 0.99588 | 0.99502 | 0.99387 | 0.99225 | 0.9899 | 0.9863 | 0.98039 | 0.9759 | 0.9697 | 0.96078 | 0.94737 | 0.92593 | 0.88889 | 0.81818 | 0.74227 | 0.66667 | 0.5678 | 0.41386 | 0.21654 | 0.10372 | 0.047097 | 0.0088133 | 0.0015248 | 0.00025145 | 4.0142e-05 | 6.2609e-06 | 9.5951e-07 | 1.4505e-07 | 2.1687e-08
B 100K | 0.11554 | 0.11552 | 0.1155 | 0.11548 | 0.11543 | 0.11537 | 0.11525 | 0.11515 | 0.115 | 0.11478 | 0.11439 | 0.11366 | 0.11199 | 0.10685 | 0.096477 | 0.077067 | 0.04306 | 0.012542 | 0.0011273 | 8.4316e-05 | 5.7662e-06 | 2.3423e-08 | 8.582e-11 | 2.9651e-13 | 9.8636e-16 | 3.1953e-18 | 1.0151e-20 | 3.1764e-23 | 9.8216e-26
B 500K | 2.7935 | 2.7879 | 2.7805 | 2.7705 | 2.7564 | 2.7359 | 2.7041 | 2.6814 | 2.6516 | 2.6115 | 2.556 | 2.4768 | 2.3589 | 2.1762 | 2.017 | 1.8816 | 1.7205 | 1.4578 | 1.0424 | 0.70862 | 0.46541 | 0.18742 | 0.071071 | 0.025915 | 0.0091937 | 0.0031959 | 0.0010937 | 0.0003697 | 0.00012371
B 400K | 1.8364 | 1.8338 | 1.8303 | 1.8254 | 1.8186 | 1.8083 | 1.7919 | 1.7799 | 1.7638 | 1.7415 | 1.7096 | 1.6617 | 1.5862 | 1.4595 | 1.3403 | 1.2331 | 1.101 | 0.88797 | 0.57256 | 0.34615 | 0.20068 | 0.062241 | 0.018037 | 0.0050066 | 0.0013491 | 0.00035572 | 9.2259e-05 | 2.362e-05 | 5.9839e-06
50 meV | 0.0095173 | 0.036258 | 0.13163 | 0.26847 | 0.43119 | 0.6055 | 0.77784 | 0.93512 | 1.0041 | 1.0644 | 1.1144 | 1.1524 | 1.1767 | 1.1852 | 1.1793 | 1.1469 | 1.084 | 0.9897 | 0.86576 | 0.71747 | 0.55433 | 0.39008 | 0.24131 | 0.12407 | 0.048255 | 0.010045
B 200K | 0.46146 | 0.46126 | 0.46099 | 0.46059 | 0.46002 | 0.45911 | 0.45757 | 0.45636 | 0.45464 | 0.45206 | 0.44798 | 0.44095 | 0.42739 | 0.39655 | 0.35609 | 0.30827 | 0.23969 | 0.14314 | 0.050169 | 0.01556 | 0.0045092 | 0.00033726 | 2.3065e-05 | 1.496e-06 | 9.3692e-08 | 5.724e-09 | 3.4328e-10 | 2.0294e-11 | 1.186e-12
25 meV | 0.0090645 | 0.032908 | 0.067117 | 0.1078 | 0.15137 | 0.19446 | 0.23378 | 0.2661 | 0.28811 | 0.2963 | 0.29483 | 0.271 | 0.21644 | 0.13858 | 0.060327 | 0.012064 | 0.00033515 | 2.9615e-09
100 meV | 0.0097545 | 0.083588 | 0.22118 | 0.78351 | 1.5555 | 2.422 | 3.2763 | 4.0163 | 4.2575 | 4.4576 | 4.6097 | 4.7066 | 4.7407 | 4.7393 | 4.7172 | 4.6672 | 4.5877 | 4.336 | 3.7248 | 2.8699 | 1.8854 | 0.96523 | 0.32313 | 0.047863 | 0.00012081 | 1.4293e-18
Brightness (a.u.)
 (eV)
= 500 K
400 K
300 K
200 K
100 K
MTE = 100 meV
MTE = 50 meV
MTE = 25 meV
 Optimum  for maximum beam brightness: Analytical evaluation in ħΩ  0 limit
For any polar semiconductor
photocathode maximum beam
brightness achieved for   0
at any desired MTE
Plotting transverse beam brightness
as a function of  reveals:
Higher for higher
 Cooling may not help unless one wants low MTE
(ii) MTE = 25 meV cannot be attained for 300 K
BUT: MTE 50 meV is readily achievable for
room temperature photocathodes
(e.g., in long transport limit)

## Slide 30
Metal photocathodes: Cu(001) and W(111)
 Single emitting band for both Cu(001) and W(111) and no upper conduction band emission

## Slide 31
Metal photocathodes: Cu(001) and W(111)
 Single emitting band for both Cu(001) and W(111) and no upper conduction band emission
W(111) photoemission NOT in agreement
with direct ‘one-step’ band emission theory
near and below threshold
 Additional emission mechanism (?)

## Slide 32
Umklapp electron scattering (UES) emission
Electron-electron Umklapp (G) scattering
… for small since E  0
Scattering strength
 Thermal electron mass obtained from ratio of
electron specific heats  (as T  0):
Measured with
 Number of Fermi surfaces from statistics:
to scatter into in the bulk
BUT only one final vacuum state
 Near threshold emission; Spherical Fermi surface approximation
/
p2
p
G

Brillouin zones
Fermi surface

## Slide 33
Umklapp electron scattering (UES) emission (contd.)
UES emissive electron energy distribution derived using Fermi-Dirac distribution f(E):
… Fermi energy set to zero
Electron inelastic mean free path (IMFP) (E  ) and (ħ) determine emission fractions:
and
Expect UES emission energy resonance at E  0 due to low :
UES-FC emission not independent of direct band emission (same initial state):
Excited distribution
Unoccupied states
Scattered distribution (UES physics)
R. F. Willis and N. E. Christensen, Phys. Rev. B 18, 5140 (1978)

## Slide 34
W(111) QE: Theory vs. experiment
fit used to obtain
… consistent with literature and
thin-slab calculations
Direct band plus UES emission fit (red line) employs
… all DFT-derived or literature values

## Slide 35
W(111) MTE: Theory vs. experiment
Direct band plus UES emission theory also consistent with MTE measurements
(with same parameters!)
For , the sub-threshold MTE for metal photocathodes is given by
Band structure calculations:
Direct one-step emission band parameters E(p)
(using DFT-determined and from )
Thin-slab evaluations of

## Slide 36
Summary
Direct ‘one-step’ photoemission simulation
 Emitting band(s) physical properties: E(p), local DOS
 Photoemission barrier quantum physics ( conservation) and recipient vacuum DOS
 with n > 2 and for good metals
(not ) for upper CB emission
BUT sub-thermal emission observed;
Momentum-resonant Franck-Condon (FC) electron emission
 Mediated by (optical)phonon scattering in polar semiconductors (q)
 emission dependence and for NEA
 Umklapp electron scattering emission in metals (G)
… Preliminary analysis: and 
Predicted QE and MTE consistent with experimental data
− Good agreement for Cu(001), Cu(111), W(111), Cs:GaAs, GaN, and Fe:Ga2O3(010)

## Slide 37
Thank You !

## Slide 38
Cs:GaAs transverse energy distribution
L.B. Jones, H.E. Scheibler, et al., J. Phys. D: Appl. Phys. 54, 205301 (2021)
NOTE
Other reports:
G. Vergara et al., J. Appl. Phys. 80, 1809 (1996)
V. Bakin et al., JETP Lett. 77, 167 (2003)
Z. Liu et al., J. Vac Sci. & Tech. B 23, 2758 (2005)
Evidence for direct band contribution?
Less than 5% of total emission
BUT MTE < 25 meV
(m*  0.067m0 for GaAs)

## Slide 39
Metallized diamond(001): A hybrid photocathode
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, PRAB 28, 123401 (2025)
 0.5 mm-thick CVD diamond: Back surface metallized [annealed C-Ti (+Pt+Au)]
Back surface photo-injection from Ti into diamond CB for ħω > 3.2 eV
Electron drift transport to emission face due to applied DC gun field
 kBTe  30 meV
… E  3 kV/cm, ħΩ = 165 meV
Emission from upper (  0.8 eV) and lower (  0.8 eV) CBs
 Two emission signals

## Slide 40
Metallized diamond(001): MTE and QE
Upper CB
Lower CB
MTE
Total QE
 Multi-phonon emission: g = 1.1, ħΩ = 165 meV, plus polaron self energy
Back surface injection efficiency with Ti DOS
L.A. Angeloni, I-J. Shan, and W.A. Schroeder, PRAB 28, 123401 (2025)