## Slide 1: iSAS Task 3.2: Flux trapping Progress at UKRI/STFC
O.B. Malyshev, D. Seal and L. Smith
R. Valizadeh and C. Bejamin

## Slide 2: iSAS Task 3.2 objectives
completed

## Slide 3: Facilities for Superconducting Properties Evaluation at UKRI/STFC/CI
EXP700: Magnetic field penetration facility (in-vacua)
EXP900: RS measurements with 7.8 GHz cavity
HP1
HP2

## Slide 4: The Choke Cavity Facility (EXP-900)
Two-part test cavity in LHe-free cryostat:
  Bulk Nb choke cavity
  Sample:
    planar disk 90 - 130 mm,
    thickness w = 1 – 10 mm
RF-DC compensation  RS (T, B)
VNA measurements  Δf  Δλ
Parameters:
  f0 = 7.8 GHz
  TSample ≥ 4 K
  RF power up to 1 W
  Bsample, pk ≤ 2.5 mT
    To be Bsample, pk ≤ 20 mT after moving to a new CI Bunker
1 sample test Rs(T) in 2 days
Example of results:
effect of magnetron power
for depositing Nb3Sn

## Slide 5: The Choke Cavity Facility updates
Facility set into operation in a new CI Bunker
  Cryogenics is operating
  RF with VNA - OK
  No radiation limit on RF power
    after completing jobs for the gate closing (long delays due to outside contractor, but progress over last two weeks)
RF rack is being updated:
  ongoing
    f0 = 7.8 GHz
    TSample ≥ 4 K
    RF power up to 1 W
    Bsample, pk ≤ 20 mT in CW mode
    Expected to be larger in pulsed mode
New Magnetic shield
CI SRF bunker

## Slide 6: The Choke Cavity Facility testing plans
Testing facility with Nb coated samples for Rs and Tc-RF
Testing the same samples with MFPF for Bfp(T), residual magnetisation and Tc-dc
Continue similar studies on both facilities with Nb3Sn

## Slide 7: Magnetic Field Penetration Facility
Magnet Housing
Sample Holder
HP1
HP2
Sample
SC coil
Hall probe for applied field
Hall probe for penetrated field
Large Sample Plate
To accommodate
samples  = 30-100 mm
Split cavity
Parts of cavity up to 100 mm . 100 mm
DC magnetic field
  parallel to the surface
  B ≤ 600 mT
  Field local to the sample surface
    2mm  10 mm

## Slide 8: Magnetic Field Penetration Facility update - 1
New poles for a c-shaped magnet produced
New ability to test curved surfaces:
  Cuts from 1.3 GHz cavity
  Half of 6 GHz cavity
Ability to relate performance of RF tested cavity to AC/DC characterisation such as
  Bfp(T),
  residual magnetisation
  Tc-dc
Ability of AC/DC characterisation of cavity prototypes
1.3 GHz mock cavity deposited Nb after cutting
1.3 GHz cavity cut
from an equator zone
Cavity cut from a tubular zone

## Slide 9: Magnetic Field Penetration Facility update - 2
New poles for a c-shaped magnet produced
New ability to test curved surfaces:
  Half of 6 GHz split cavity
  Half of a cut of 6 GHz cavity from INFN
No damage to 6 GHz split cavity
  Non-destructive test, cavity can be used for future coatings and testings
Ability to relate performance of RF tested cavity to AC/DC characterisation such as
  Bfp(T),
  residual magnetisation
  Tc-dc
Half of 6 GHz cavity deposited Nb
Half of 6 GHz cavity installed for MFP measurements

## Slide 10: Residual magnetisation
Residual sample magnetisation can be measured as a function of
operation temperature, T
applied magnetic field, B1app
Typical magnet residual magnetisation B1res
  stays in the range of B1res = 4 mT and
  does not change with T
Residual sample magnetisation B2res :
  varies from sample to sample and
  depends on T
Examples of residual magnetisation

## Slide 11: New low power RF testing facility (as a part of Task 3.4)
In CI RF bunker
Vacuum <10-7 mbar
Cryogenics: 3.0 K  Tcav  20 K
Magnetic shield is produced and delivered
Next steps – focus on RF:
  RF testing with VNA of uncoated cavity
    flanges and RF cables will be added next week
  RF testing with VNA of Nb coated cavity from IFAST (laser polished at RTU)
  RF testing with VNA of bulk Nb cavity
    After receiving after processing at CEA
  RF testing with VNA of Nb3Sn coated bulk Nb cavity
    As a part of Task 3.4
  Testing new RF system
    Software is still underdevelopment