## Slide 1
Cristian Pira
Nb3Sn on Cu films for 4.2K cavity operation
WP3 Meeting 08
20 March 2026
innovate for Sustainable Accelerating Systems
WP3
LNL Status

## Slide 2: Task 3.2 Flux Trapping
Nb3Sn Coating for large Cu slab for trapped flux measurements at HZB
Strong flux trapping, low Tc  poor dense film
Reasons?

## Slide 3: Task 3.3 RF Tunability
Developed a new fully seamless design for 1.3 GHz elliptical cavities
Cavity sent to HZB for testing the new Tuning System (Milestone 3.1)
Leak of 10-10 mbar*L/s on one of the two flanges.  Heat treatment necessary to release cold working
Further analysis required
Master Student thesis project will start on April

## Slide 4: Task 3.4 Adaptive Layer
Test CEA Adaptive Layer between Nb buffer layer and Cu substrate
Nb (30 μm)
Cu
ALD
Nb3Sn (1 μm)
Buffer Layer | Tc | ΔTc
No buffer layer | 13.8 K | 0.3 K
16 μm Nb | 16.5 K | 0.6 K
30 μm Nb | 16.7 K | 0.5 K
30 μm Nb + 18 nm Al2O3 | 16.3 K | 0.5 K
30 μm Nb + 25 nm AlZrOx | 16.9 K | 0.2 K
30 μm Nb + 5 nm Al2O3 + 22 nm ZrO2 | 16.8 K | 0.2 K
Slightly enhancement of Tc
Further analysis required
Master Student thesis project will start on April

## Slide 5
Objectives
Improve I.FAST 1.3-GHz superconducting coating recipe based on Tasks 3.2-3.4 results.
Prepare 1.3-GHz thin film cavities with an optimized coating recipe.
Perform full cavity characterization @4.2 K (Q vs E, Q vs F, and flux trapping in the VTS@SupraLab vertical test stand).
Tasks 3.5 Working Cavity
Deliverable 3.4 4.5-K Cavity Report on 4.5-K Cavity performance & tunability tests - INFN - Report M46
Milestone 3.4 Characterization of Nb3Sn reference cavity - Test report M34

## Slide 6: Optimized coating parameters
  1. Low cathode Power ≤ 250 mW/cm2 +
  2. High deposition Pressure: 2 x 10-2 mbar +
  3. Deposition Temperature: 600 ºC – 650 ºC +
  4. No post Annealing +
  5. Nb buffer layer ≥ 30 µm
  Tc > 17 K
Nb3Sn on Cu
Cu dissolved
G. Rosaz, FCC week 2025
Barrier Layer against Sn and Cu diffusion
Accomodation layer (release thermal stress)
Substrate’s Thermal Expansion coefficient drives the residual stress  Tc
D. Fonnesu et al., Recipe optimization and SRF test of Cu-compatible Nb3Sn films by DC magnetron sputtering from a stoichiometric target. Sci Rep 16, 3539 (2026)

## Slide 7: QPR sample comparison
Nb3Sn/bulk Nb
Sample #1 (just seen)
Nb3Sn/bulk Nb
Sample #2
Surface preparation:
BCP
Surface preparation:
Metallographic polishing + EP
Rz > 6µm

## Slide 8: Surface resistance #1
Bulk Nb QPR sample coated with Nb3Sn film
10 cm
4 K, 400 MHz
Tc = 17.2 K
Quench > 70 mT extrapolated @ 0 K
Rs ~ 25 nΩ @ 4 K, 20 mT
Comparable to (slightly better) than VTD sample up to 40 mT
 Slow cool down data
suggest flux trapping
Steep rise > 40 mT likely due to thermal dissipation
slow cooldown #1
fast cooldown #1
full thermal cycle #1
Courtesy of O. Kugeler, S. Keckert
Cornell VTD sample Keckert, S. et al., Supercond. Sci. Technol. 32, 2019

## Slide 9: Surface resistance #2
slow cooldown #1
fast cooldown #1
full thermal cycle #1
full thermal cycle #2
PRELIMINARY
Bulk Nb QPR sample coated with Nb3Sn film
10 cm
4 K, 400 MHz
Tc = 17.45 K
Quench > 85 mT extrapolated @ 0 K
Rs < 9 nΩ @ 4 K, 20 mT
Better than VTD sample up to 50 mT
Courtesy of O. Kugeler, S. Keckert
Substrate matters!
Low field Rs improved by more than a factor 2
High field rise mitigated
Cornell VTD sample Keckert, S. et al., Supercond. Sci. Technol. 32, 2019

## Slide 10: Surface resistance #2
Bulk Nb QPR sample coated with Nb3Sn film
10 cm
Tc = 17.45 K
Quench > 85 mT extrapolated @ 0 K
Rs < 9 nΩ @ 4 K, 20 mT
Better than VTD sample up to 50 mT
Substrate matters!
Low field Rs improved by more than a factor 2
High field rise mitigated

## Slide 11: Surface resistance #2
Bulk Nb QPR sample coated with Nb3Sn film
10 cm
Tc = 17.45 K
Quench > 85 mT extrapolated @ 0 K
Rs < 9 nΩ @ 4 K, 20 mT
Better than VTD sample up to 50 mT
Substrate matters!
Low field Rs improved by more than a factor 2
High field rise mitigated

## Slide 12: Surface resistance #3
Full Cu QPR sample / NbBL30/ Nb3Sn film
Cu
Nb-BL30
Nb3Sn

## Slide 13: Surface resistance #3
Full Cu QPR sample / NbBL30/ Nb3Sn film
VERY PRELIMINARY

## Slide 14: Surface resistance #3
Full Cu QPR sample / NbBL30/ Nb3Sn film
Cu
Nb-BL30
Nb3Sn
“Pinkles” on the surface

## Slide 15: 1.3 GHz coating system
Custom fixed rectangular planar magnetron with rotating cavity system
Current Status:
vacuum system assembled and tested
heating system completed and tested
magnetron test with first Nb target ignition completed
first Nb cavity coating planned for 2026
Coating on Cu cavity planned for 2027
ignited plasma
fixed rectangular magnetron
1.3 GHz rotating cavity

## Slide 16: 1.3 GHz coating system
Status and ongoing activity
Vacuum System
All metal system
New Turbo Pump
Ultimate Vacuum: 5*10-9 mbar, leak rate <10-12 mbar*L/s
Mock up cavity designed and commisioned
7 window (3 samples each for a total of 21 samples for each run) to monitor morphology, deposition rate, Tc, composition

## Slide 17: 1.3 GHz coating system
Status and ongoing activity
Rectangular Magnetron
3 sets of magnets to be tested (0.68 T, 0.92 T, 1.02 T)
Tested 0,92T configuration up to 1 A  classical power law obtained;
The race track seems open at the bottom
Shortcut at T>200 °C due to expansion of ground screen (solved)
Deposition rate Cut-off = 10 x Deposition rate at Equator/Iris position

## Slide 18: 1.3 GHz coating system
Activity Plan:
Optimize magnetron magnetic configuration (~ 2 weeks)
Optimize coating parameters in static position (~ 1 month)
Optimize coating parameters with rotating cavity (~ 2 months)
Coat the first Nb cavity (second half of 2026)

## Slide 19
Thank You!