## Slide 1: Radiation resistance of gallium oxide
Joanna Matulewicz
PHENIICS Fest
8 June 2026
Supervision: prof. Frederico Garrido, Université Paris-Saclay, France
dr hab. Renata Ratajczak, National Centre for Nuclear Research, Poland

## Slide 2: Outline
Motivation
What is β-Ga2O3?
Potential applications
Why is it implanted with rare earth ions?
Methodology
Ion implantation
RBS/c
XRD
TEM
Results
What happens after implantation with rare earth ions
Conclusion
Next steps

## Slide 3: β-Ga2O3
Wide bandgap semiconductor: 4.8 eV
It can handle high voltage
It can withstand high temperature
Resistant to high radiation
Low cost of production
Potential use: power electronics, optoelectronics, photodetectors, gas sensors…

## Slide 4: Why β-Ga2O3?
Ga2O3 is a crystal
β-Ga2O3 is the most stable form of Ga2O3
β-Ga2O3
monoclinic
γ-Ga2O3
cubic
500°C

## Slide 5: Rare earth doping
Doping with rare earth (RE) ions modifies the optical response
Doping with Yb extends the photoluminescence range into infrared
Can we obtain efficient and durable light emitters based on RE-doped β-Ga2O3?

## Slide 6: Methodology
Ion implantation
RBS/c
TEM
XRD
β-Ga2O3
Yb ions
Energy: 150 keV
Fluence range:
5×1012 - 1×1016 ions/cm2
β-Ga2O3
β-Ga2O3:Yb

## Slide 7: Methodology
Ion implantation
RBS/c
TEM
XRD
He ions
β-Ga2O3
β-Ga2O3:Yb
Rutherford Backscattering Spectroscopy in channeling mode
Quality of the crystal
Defects analysis
energy
counts

## Slide 8: Methodology
Ion implantation
RBS/c
TEM
XRD
X-ray
Quality of the crystal
Strain
Crystal phases
X-Ray Diffraction
β-Ga2O3
β-Ga2O3:Yb
angle
counts

## Slide 9: Methodology
Ion implantation
RBS/c
TEM
XRD
e-
Imaging
Identification of crystal phases
Destructive method
Transmission Electron Microscopy
β-Ga2O3
β-Ga2O3:Yb

## Slide 10: Results
5e12
2e13
3e13
6e13
1e14
2e14
3e14
6e14
1e15
2e15
6e15
1e16
fluence [ions/cm2]

## Slide 11: Damage accumulation
5e12
2e13
3e13
6e13
1e14
2e14
3e14
6e14
1e15
2e15
6e15
1e16
RBS/c
I
II
III
IV
III
IV

## Slide 12: Implantation with low fluences
surface
5e12
HRTEM
FFT
(Fast Fourier Transform)
[010] β-Ga2O3
[010] β-Ga2O3

## Slide 13: Implantation with low fluences
5e12
2e13
3e13
6e13
HRXRD
compressive strain
sample stage
β-Ga2O3
(020)

## Slide 14: Phase transition
HRXRD
γ-Ga2O3
(440)
β-Ga2O3
(020)
5e12
2e13
3e13
6e13
2e14

## Slide 15: Phase transition
1e14
HRTEM
FFT
[010] β-Ga2O3
[110] γ-Ga2O3

## Slide 16: Radiation resistance
Different response to irradiation: transformation from β to γ phase instead of amorphization
β/γ bilayers exhibit high radiation resistance: no amorphization observed even after irradiation with very high fluences
Amorphization - structural phase transformation from a crystalline solid to a solid that lacks any long-range order
doi:10.1016/B978-0-08-056033-5.00005-7

## Slide 17: Further implantation
3e14
HRTEM
FFT
[010] β-Ga2O3
[110] γ-Ga2O3
[110] γ-Ga2O3
stacking faults
I
II
III
IV

## Slide 18: Further implantation
HRXRD
5e12
2e13
3e13
6e13
2e14
3e14
6e14
2e15
6e15
1e16
β-Ga2O3
(020)
γ-Ga2O3
(440)

## Slide 19: Amorphization
1e15
1e16
[010] β-Ga2O3
[010] β-Ga2O3
[110] γ-Ga2O3
[110] γ-Ga2O3
amorphous
amorphous
I
II
III
IV

## Slide 20: Conclusion
Formation of γ phase
Increasing compressive strain
Strain relaxation
Stacking faults
Progressive amorphization

## Slide 21: Conclusion
The results challenge the concept of extreme radiation resistance of the γ phase or suggest that its stability may depend on irradiation conditions
A chemical effect of RE ions may play a significant role
Next step: implantation with a noble gas Xe

## Slide 22: Acknowledgements
The research was carried out within the NCN project UMO-2022/45/B/ST5/02810.
This research was supported by a French government scholarship France Excellence.