## Slide 1: Diamond Detector Development and Tests
V. Kubytskyi, S. Liu, P. Bambade, F. Bogard, J. Cayla, N. Fuster Martinez, I. Khvastunov, H. Monard, C. Sylvia, T. Tauchi,
N. Terunuma, T. Vinatier
French-Ukrainian workshop, 1 October, 2014

## Slide 2: Our Goals
Mastering the diamond detectors: physics, instrumentation, electronics
Development of application oriented diamond detectors
Using this devices at accelerator facilities

## Slide 3: Outline
Diamond as particle detector
Tests with diamond detector
Modeling of signal collection

## Slide 4: Diamond as particle detector
Depending on the applications in addition: fast low noise electronics charge amplifier,
current amplifier, attenuators, power supply, oscilloscope etc.
SPICE simulation for optimal parameters of the electrical circuit for given application

## Slide 5: Physical properties of CVD diamond
• Large band-gap⇒ low leakage current
• High breakdown field
• High mobility⇒ fast charge collection
• Large thermal conductivity
• High binding energy⇒ Radiation hardness
Fast pulse ⇒ several ns
High dynamic range
ADVANTAGES
Property Diamond Silicon |  | 
Density (g m-3) Band gap (eV) Resistivity (Ω cm) Breakdown voltage (V cm -1) Electron mobility (cm3 V-1 s-1) Hole mobility (cm3 V-1 s-1) Saturation velocity (μm ns-1) Dielectric constant Neutron transmutation cross-section(mb) Energy per e-h pair (eV) Atomic number Av.min.ionizing signal per 100 μm (e) | 3.5 5.5 >1012 107 1900 2300 141 (e-) 96(hole) 5.6 3.2 13 6 3600 | 2.32 1.1 105 103 1500 500 100 11.7 80 3.6 14 8000
Charge generated by 1 MIP for 500 µm diamond (with 100% CCE): 2.88 fC

## Slide 6
Calibration: Tests with well known
Radioactive Sources
241Am alpha source: Eα = 5.4 MeV
Allows to obtain diamond characteristics by Transient Current Technique.
+ current amplifier
Signal: Shockley-Ramo theorem

## Slide 7
2.27 MeV
0.55 MeV
+charge amplifier(4mV/fC)
Geant4 diamond simulation.
Sr90 spectrum

## Slide 8: Applications: PHIL beam monitor
In Vacuum Diamond Detector
CH1
CH3
HV
CH4
CH2
The same setup will be used at ATF2 for investigation of beam halo

## Slide 9
PHIL Facility
PHIL Electron Beam Parameters
Charge: 1pC-500 pC/bunch (1 bunch per RF pulse) ;
Duration of Charge: 7 ps FWHM;
Charge Stablility: < 2%;
Beam Energy: 3 to 5MeV;
Minimum Dispersion: < 1%;
Increase of incident charge slow down charge collection
Normalized on collected charge
Different characteristic times

## Slide 10: Modeling of charge collection in 1D
Drift-diffusion equations.
Poisson equation in this case can be solved analytically:
where
Numerical solution of drift-diffusion eqns. -> time evolution of charge densities inside the diamond
Generation, recombination terms can be added here

## Slide 11
Modeling Charge collection 1 MIP( created~18000e-h pairs)
High Voltage
electrons
holes
Collected charge as a function of time

## Slide 12
Collected charge as a function of time
Nmip ~10^5
Typical for beam halo

## Slide 13
Nmip ~10^8
Looks similar
Nmip 1
PHIL tests
Peak when charge densities
are separated in space
Slowing down due to space charge

## Slide 14: Future plans
We need:
-Fast, low noise charge amplifier (in case of Belle2 application 4 ns);
-understand ways of optimization of the detector; modeling
-characterize multistrip diamond detector in UHV