## Slide 1: Modeling of diamond sensor signal formation in extreme conditions
V. Kubytskyi, S. Liu, P. Bambade, F. Bogard, D. Jehanno,
C. Sylvia, P. Cornebise, T. Tauchi, N. Terunuma

## Slide 2: Outline
Introduction to DS
Modeling of charge collection
Results for 1-109 Mips
Conclusions

## Slide 3: 1.1 What is diamond sensor?
d=500μm
1 MIP≈36 in 1 μm
High Voltage
400 V
Reading side
0 V
1 MIP≈36 in 1 μm
1 MIP≈36 in 1 μm
Diamond
E = V/d
Introduction to DS
How many particle we detected???

## Slide 4: 1.2 Calibration of the sensor
Introduction to DS
241Am alpha source: Eα = 5.4 MeV
Allows to obtain diamond characteristics
by Transient Current Technique.
+ current amplifier (40dB)
Velocity saturation
241Am alpha source: Eα = 5.4 MeV

## Slide 5: 1.2 Calibration of the sensor
Introduction to DS
2.27 MeV
0.55 MeV
+ charge amplifier(4mV/fC)
Noise
Signal from 1 MIP
Sr90 spectrum
Geant4 diamond simulation.

## Slide 6: 1.3 Signals measured at ATF2
Introduction to DS
BEAM
Ch1
Ch2
Ch3
Ch4
Total charge in the diamond
50 V
200 V
400 V
10 waveforms at each position
ch1
ch2
ch3
ch4

## Slide 7: 1.4 Motivation for modeling
Correct calibration of our detector for maximum dynamic range
Understanding of processes during charge collection
Optimization of our DS for given application
Introduction to DS

## Slide 8: 2. Modeling of charge collection in 1D
Parameters:
-number of incident particles
-biased voltage
-diamond thickness
Time = 0
Time = 1
Time = K
Variables:
Motion of electrons and holes in external electric field create current on electrode.
Material parameters
Mobilities
μe = 1300..3100 [cm2/Vs]
μh = 2300 [cm2/Vs]
Saturation velosities
v_sat_e = 1.9*107 [cm/s]
v_sat_h = 1.4*107 [cm/s]
Lifetimes
τe = 300 ns
τh = 300 ns
(Pomorski et al.)

## Slide 9: 2.1 Current induced on the electrode
D
x0
q
q1
q2
If charge is moving:
More generally: Shockley-Ramo theorem,
works for many electrodes configuration
Same result
D
ν
Vb

## Slide 10: 2.2 Modeling of charge collection in 1D
Standard approach in semiconductor device modeling is solution of
Drift-diffusion equations.
Variables:
+ initial conditions (concentrations proportional to Nmip)
+ appropriate boundary conditions
We use Scharfetter-Gummel Discretization:
Solving for each time moment (by Runge-Kutta method) gives the evolution
of charge densities

## Slide 11: 2.3 Examples
Nmip=1
Nmip=1e6

## Slide 12: More particles
Nmip=1e8
Wrong!
Real waveforms
50 V
200 V
400 V

## Slide 13: 2.4 Taking into account the voltage drop
For Nmip 1-1e5 Vread << V0
Which is not the case when signal is large, and system behaves self-consistently:
-large I -> large Vread->small V->slow collection (small I ) and inverse
-small I -> small Vread->large V->fast collection (large I )
D
Vread
50 Ohm
V0
400V
We solve this equation at each time step to find settled regime
This significantly slows down the modeling speed
For Nmip=1e6 and V0=400V Vread =25 V

## Slide 14: 3. Results
Nmip=1e8
Nmip=5e8

## Slide 15: 3. Results
Nmip=1e9

## Slide 16: Role of material parameters

## Slide 17: Conclusions
We developed a 1D model of diamond sensor which takes to account: space-charge effects, voltage drop,….
Up to 1e6 Mips the charge collection is in linear regime; for larger intensities charge collection is non-linear.
Allows to determine the proper calibration of our DS.
Can be easily extended for taking to account energy distribution of incident particles; extension to 2D case is complicated
…

## Slide 18: Backup

## Slide 19: Physical properties of CVD diamond
• Large band-gap⇒ low leakage current
• High breakdown field
• High mobility⇒ fast charge collection
• Large thermal conductivity
• High binding energy⇒ Radiation hardness
Fast pulse ⇒ several ns
High dynamic range
ADVANTAGES
Property Diamond Silicon |  | 
Density (g m-3) Band gap (eV) Resistivity (Ω cm) Breakdown voltage (V cm -1) Electron mobility (cm3 V-1 s-1) Hole mobility (cm3 V-1 s-1) Saturation velocity (μm ns-1) Dielectric constant Neutron transmutation cross-section(mb) Energy per e-h pair (eV) Atomic number Av.min.ionizing signal per 100 μm (e) | 3.5 5.5 >1012 107 1900 2300 141 (e-) 96(hole) 5.6 3.2 13 6 3600 | 2.32 1.1 105 103 1500 500 100 11.7 80 3.6 14 8000
Charge generated by 1 MIP for 500 µm diamond (with 100% CCE): 2.88 fC

## Slide 20
Weighting Field for a Strip in a Parallel Plate Geometry
D
w
Weighting Field:

## Slide 21
D
w
v
I(t,x) = -e0*Ez[x,D-v*t]*v
When all charges have arrived at the electrodes the induced charge is equal to the total charge that has arrived at the electrode.
If the electronics ‘integration time’ ~ ‘peaking time’ ~ ‘shaping time’ is larger than the time it takes the electron to pass the induction gap, the readout strips that don’t receive any charge show zero signal.
If the electronics ‘integration time’ ~ ‘peaking time’ ~ ‘shaping time’ is smaller than than the time it takes the electron to pass the induction gap, the readout strips that don’t receive any charge show a signal different from zero that is strictly bipolar.
Weighting Field for a Strip in a Parallel Plate Geometry

## Slide 22
GEM Signals, Induced Currents
D = 1mm
w
v
W >> D
W=D
W=D/2
Central Strip
First Neighbour

## Slide 23
GEM Signals
D = 1mm
w
v
W=D/2
Central Strip
First Neighbour
W=D/2 (D=1mm, w=0.5mm)
Connecting an amplifier with Peaking Time = 10ns
 10% crosstalk !
In case the electronics peaking time is
smaller or of similar size as the time the electron takes to pass the induction gap, there is a sizable signal on the neighboring strips that do not even receive charges.
W=D/2
Central Strip
First Neighbor