## Slide 1: TYL-FJPPL: A_RD_07 Suppression of magnetic flux trapping to achieve high-Q of SRF cavities
Juliette Plouin, Enrico Cenni, Olivier Napoly (CEA)
Kensei Umemori, Mika Masuzawa, Kiyosumi Tsuchiya, Takayuki Kubo (KEK)
2017 Joint Workshop of the FKPPL and FJPPL
11 mai 2017
Strasbourg, France

## Slide 2
Superconducting transition
Magnetic probe signal
DB1
DB
B applied
B applied x 1.8
Bapplied
Magnetic probe
Total expulsion
Partial expulsion
Total expulsion
Partial expulsion
During supraconducting transition of a niobium cavity, some of the ambient magnetic field is trapped
 Surface resistance is improved 
 degradation of the Q0
Objective : limit flux trapping
Reduce ambient field
Improve flux expulsion during transition
ZOOM
T> Tc
T
T< Tc
Flux trapping

## Slide 3: Residual resistance history of single-cell cavity vertical tests
・R_res gradually increase?
・Q-values of large grain (LG) cavity were gradually decrease.
LG-1 cavity (<1.5 K)

## Slide 4: First stage of flux expulsion experiments at KEK-STF (2016/March ～ June)
Flux gate(FG)
Si temp. sensor
Heater
Some strange behaviors were observed during flux expulsion experiments.
  Asymmetric magnetic field
  Negative expulsion(?)
  Significant horizontal magnetic field
Temperature [K]
Magnetic flux [mG]
Example
E. Cenni & J. Plouin (CEA) participated to those tests in March 2017, in the frame of FJPPL

## Slide 5
Degradation of R_res?
Strange magnetic flux behavior?
Check magnetization for most of all the components of vertical test

## Slide 6
No. | name | Magnetic field [mG]
14 | Φ034 metal valve ① | 430
15 | Φ034 metal valve (which observed vacuum leak) | 80
19 | Φ034 metal valve ② | 59
25 | Volts and washers for support of input coupler shaft | 140
28 | Nuts and washers for hanging cavity | 110
29 | Stat-volts, nuts and washers for hanging cavity | 300
Study on magnetized components (example)
⑭
㉙
㉕
Measure inside magnetic shield by using 3-axis flux gate sensor.

## Slide 7: Effects of SUS shafts
SUS shafts for variable coupler were highly magnetized.
More than 1 G!!
Angle | Bx [mG] | By[mG] | Bz[mG] | B[mG]
0 | -7 | -11 | -6 | 15
90 | -6 | 2 | -9 | 11
180 | 6 | -11 | -7 | 15
270 | 8 | 130 | -49 | 139
If both shafts were removed B ≦ 2mG for any positions.
Magnetic field with shafts inside vertical test dewar

## Slide 8
Then…
Exchange SUS shafts to Ti
Exchange or remove SUS components as much as possible
Exchange metal valve to less magnetized one
And vertical tests were carried out.

## Slide 9: Vertical test setup
Flux gate sensor, Si temperature sensor, heater and solenoid coil were used.
Solenoid coil
Flux gate sensor
Si temperature sensor
(Equator and beamtube)
Heater

## Slide 10: Vertical test results
FG single-cell cavity (Tokyo-Denkai)
Nominal recipe (Not N-doping)
With cancelling coil
With thermal gradient by heater
Very high-Q was observed after the effort for demagnetization
Rres = 3.0nΩ

## Slide 11: Flux expulsion during cool-down(add 16mG with coil)
Equator temperature
Lower beampipe iris
Upper beampipe temperature
Clear flux expulsion(~90%) can be observed.
Temperature gradient of more than 1 degree between equator and lower beampipe iris.
FG single-cell cavity (ULVAC)
Nominal recipe (Not N-doping)
900 degree heat treatment applied
Add +16mG with coil (Total 9 + 16 = 25mG)
With thermal gradient by heater

## Slide 12
ESS magnetic shield
Cryophy, 2 mm
Diam 0,5 m, L = 1 m
Binside < 0,5 mT
(meas. at room temperature, meas. in LHe are foreseen)
Magnetic shields characterization : ESS

## Slide 13
IFMIF samples
mumetal, 2 mm
Diam 0,15 m, L = 0,6 m
Binside < 0,05 mT
IFMIFmagnetic shield
mumetal, 2 mm
l~2 m, L = 6 m
Binside < 0,5 mT
(meas. at room temperature)
Magnetic shields characterization : IFMIF

## Slide 14
Improvement of the magnetic shield of Vertical Cryostat CV2
cryostat
Existing magnetic shield (mumetal)
coil
cavity
B up to 10 mT
Measurement of B field inside the cryostat
Extra magnetic shield (Cryophy)
B ≈1 mT
LHe

## Slide 15
Design of the extra magnetic shield
Fabrication of this new magnetic shield is planned during 2017
w top plate
w/o top plate
w/o extra shield
B up to 10 mT
B ≈1 mT

## Slide 16
We have received a 6 GHz cavity (bulk Nb)
Cryocooler : better control of gradient and cooldown rate
Flux expulsion tests planned at Saclay
Monitoring of magnetic field and temperature
Cryostat :cavity in a vacuum vessel placed in a cryostat
Flux expulsion during cool-down on 6 GHz cavity
cernox
fluxgate
Applied field :
45°to cavity axis
// cavity axis
Flux expulsion calculation

## Slide 17: Summary
Effort has been achieved to eliminate magnetized elements in the vertical test cryostat
  High Q could be measured on a cavity
  Clear flux expulsion signal could be observed
New magnetic shields have been designed, fabricated and tested
   field around cavities < 0.5 mT
Improvement of the magnetic shield of the vertical test cryostat is planned
Flux expulsion on 6 GHz cavity is foreseen
At KEK
At CEA
KEK and CEA collaborate together within the international effort to high Q superconducting cavities