## Slide 1
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
1
Development of new fragmentation targets for the SPIRAL1 upgrade
and proposed release time measurement at LISE
Olivier BAJEAT

## Slide 2
The current targets in Carbon for projectile fragmentation
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
Several version of targets made in POCO graphite ZXF-5Q1 (grain size 1 µm)
Current Febiad TISS with C Target
Kr, Ni, Ca… primary beams
Ar, Ne, O… primary beams
2

## Slide 3
New beams from the SPIRAL 1 upgrade
Operation of new targets with other material than 12C is allowed since 2018 for Z ≤ 41 (up to Niobium)
Expected yields for targets such as SiC, CaO, NiO and Nb, with 12C, 95 AMeV 2∙1013 pps as primary beam were investigated on the basis of approximate release efficiencies or parametrizations [1]
SPIRAL 1 Upgrade
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
 | In target production Nb target (C Beam 3600W) [1] | Estimation 1+ beam intensities [1] | Yield at Isolde ion/µC [2]
60Zn | 1.4E7 | 7.9E5 | 2.1E5
63Ga | 9.7E7 | 3.5E6 | 1,2E6
66Ge | 4.6E8 | 2.9E7 | 3,6E5
67As | 4.5E7 | 1.5E5 | 
68Se | 2.0E6 | 7.4E3 | 
71Br | 2,1E7 | 1.2E6 | 7,5E4
74Kr | 1.3E8 | 8.4E6 | 6.3E6
[1]: P. Delahaye. List of RIB intensities. GANIL Internal report.
[2]: http://isoyields-classic.web.cern.ch/
3
explorated
Measured, X2 possible

## Slide 4
RIBs discussed during a workshop held in Feb. 2016 with Nb (A=93) target
rp process studies with 60-64Zn using ACTAR TPC (G.F. Grinyer et al.)
Shape coexistence with 72Kr and 74Rb using lifetime measurements and Coulomb excitation (N. Singh et al.)
Deformation studies with 67As and 63Ga using transfer reaction with MUGAST and AGATA (D. Mengoni et al.)
Cluster formation from fusion reaction with 74Kr using AGATA and SPIDER (E. Bonnet et al.)
LoIs for MUGAST from 2016 to 2019
71Br, 74Kr, 66Ge, 74-76Ge, 78Sr, 79Se for nuclear structure and astrophysics from transfer reactions (Beaumel et al., Assié et al., Mengoni et al., de Angelis et al. …)
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
4
Beam requests
Many experiments with reaccelerated beams would benefit from the development of a A~90 target

## Slide 5
Numerous targets could be considered for the Spiral1 upgrade:
  Metallic foils: Nb, Zr
  Porous ceramics : Al2O3, ZrO2, ZrC, Y2O3…
  Coating or infiltration deposited onto a reticulated-vitreous-carbon-foam (RVCF)
  Woven fibers…
SiC, Nb and Zr are under study at GANIL.
Investigation on SiC and Nb targets
Off-line heating test in a dedicate oven up to 2000°C
Porous SiC sample (POCO/SUPERSiC®)
Niobium foils
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
5

## Slide 6
Comparison of in target yields for Z > 29 in C, Nb, and Zr
60Zn, 64Ge, 63Ga, 67As, 72,74,76Kr, 68Se…
12C @95 MeV/u 3600W on Zirconium target
25
24
12C @95 MeV/u 3600W on Niobium target
6
68Se (78Kr 70,4 MeV/A 1000W)  X 6
Best production in C target with existing or possible primary beams and in Nb and Zr targets with C beam
ISOL-France meeting. 17-19 march 2021 – O. Bajeat

## Slide 7
Spiral 1 Nb or Zr targets under study
7
Diffusion inside the foil
Effusion from the surface of the foil to the ion source
Before the construction a qualification test is in preparation:
 data on diffusion (Arrhenus coefficients)
 data on sticking times
  Optimization of target design
Cooled part to be designed (beam stopper)
ANSYS simulation
ISOL-France meeting. 17-19 march 2021 – O. Bajeat

## Slide 8
Diffusion coefficients
Some data is available in littérature (with disparities).
But nothing for Ge, Ga, As, Kr, Se in Niobium and Zirconium.
8
Zn in Zirconium
Zn in Niobium
 | Melting T
Niobium | 2458°C
Zirconium | 1852°C
Diffusion efficiency
Fick’s law  diffusion efficiency can be calculated from D:
(d=thickness)
60Zn (143s) | D From [3] | Thickness mm | τD (s) | Diffusion efficiency
Zn in Niobium 2000°C | 2,1.10-9 | 0,01 | 12 | 0,84
 |  | 0,1 | 1200 | 0,13
Zn in Zirconium 1700°C | 1,1.10-5 | 0,01 | 2,3.10-3 | 1
 |  | 0,1 | 0,23 | 0,99
[3] G.J. Beyer et al., Nucl. Instr. and Meth. B 204 (2003) 225.
ISOL-France meeting. 17-19 march 2021 – O. Bajeat

## Slide 9
Total efficiency of a Nb and Zr Spiral1 target
Yield
Zn isotopes yield in niobium and zirconium targets 0.1 mm thick (41 disks) and 0.05 mm (82 disks).
Approximative calculation
9
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
: time of fligth between 2 collisions
+)
Sticking time:
Experimental data from [4]  τ0 = 2,4.10-15 s for Tantalum.
[4] R. Kirchner, NIM B70 (1992) 186-199
~ 10-13 s (Frenkel theory)
 | Mean sticking time in s Niobium 2000°C | Mean sticking time in s Zirconium 1800°C
Zn | 1,4.10-10 | 9,3.10-10
Ga | 6,3.10-7 | 0,13
Ge | 0,13 | 81
As | 0,22 | 250
Sticking times calculated with τ0 = 2.4 10-15 s and Ha values extracted from [4]
Effusion

## Slide 10
Skim of the reaction chamber
The chamber
Cooled connection for heating the foils.
Power: up to 2400 W (145 to 225 A / 5,4 to 10 V)
Samples
Niobium and Zirconium  1 foil 70 µm and stack of several thinner foils.
Carbon  0.5 mm (standard thickness for Spiral1)
The qualification test
Implantation of radioactive isotopes from LISE and online measurements of the implanted sample activity at low and high temperature without handling the active sample  release time and D
Sticking time will be refined from additional delay time when comparing several foils and one (knowing the number of collision by Molflow calculation)
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
10

## Slide 11
11
59Cu
63,64Ga
61Zn
65,64Ge
67As
60Cu
62Zn
Radioactive isotope production and selection with LISE (78Kr @ 70 MeV/u + 500 µm Be)
Example of LISE setting -> As to Cu
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
Geant4 simulations at 5 cm for 100 enA, i.e. ~104 implantations/s
Temperature dependent release time measurements (beam on/off)
JC Thomas
-> Extraction of diffusion coefficients
=
Measurement at different temperatures  D0 and Ea
Φ0
N0
Φ0=λN0
NT
Φrel
ΦT
ΦT–Φrel = λNT
Low T
High T
 µ0 
For Nb and Zr (pure diffusion):
R. Kirchner, NIM B70 (1992) 186-199.

## Slide 12
Condensation on cold surfaces
Cooled chamber
After release atoms can be deposited on cold surfaces (chamber walls, aluminium sockets in front of detectors…).
 The contribution of stuck atoms on the g detection will be deducted from simulations.
12

## Slide 13
Budget
13
Qualification test : ~ 6 k€ (under construction)
New Febiad/Niobium TISS : ~ 35 k€ included ~ 12 k€ for the target and the new T-box with cooled beam catcher
ISOL-France meeting. 17-19 march 2021 – O. Bajeat

## Slide 14
Conclusion
14
ISOL-France meeting. 17-19 march 2021 – O. Bajeat
Thank you for your attention.
Targets in Niobium or Zirconium are easy to manufacture and production rates should be interesting for 29<Z<40 isotopes.
The qualification test will give us quite precise data on diffusion and indication on sticking times for the elements of interest.
Then, the TISS will be optimized in term of material (Niobium or Zirconium), foil thickness and geometry.
Refined rate estimates for each element of interest will be possible knowing that only online tests of the TISS will give the effective production.