## Slide 1
Tuning the electronic properties of Quantum Materials
Accorder les propriétés électroniques des matériaux quantiques
Matthieu Le Tacon
Institute for Quantum Materials and Technologies (IQMT)
Vxx
Vxy

## Slide 2
Heinrich Hertz (1857-1894)
Otto Lehmann
(1855-1922)
(Liquid Crystals)

## Slide 3
the Research University
in the Helmholtz Association
Exzellenzuniversität (2019)

## Slide 4: Institute for Quantum Materials & Technologies (IQMT)
Quantum
Devices
Materials &
Molecules
Theory
Transport &
Spectroscopy
New
Quantum materials
(C. Meingast)
Quantum
Molecular
Systems
(M. Ruben)
Spectroscopy of
Quantum Materials
(M. Le Tacon)
Quantum
Transport (W. Wulfhekel)
Quantum
Optical
Devices
(R. Krupke)
Mesoscopic Quantum Systems
(A. Mirlin)
Theory of Quantum Materials
(J. Schmalian)
Quantum
Circuits
(W. Wernsdorfer)
8 9 Departments
ca. 120 staff (2022)
Close Theory-Experiment Interactions
Synthesis of new
Quantum Materials
Functionalisation
Devices for Quantum technologies
Building blocs for Quantum computer

## Slide 5: What are quantum materials?
Materials which electronic properties cannot be described as an assembly or essentially independent charge carriers (~ “electrons”)
  Semiconductors, band insulators or ‘simple metals’ on which most of our technology relies do generally not fall into the ‘quantum materials’ category
Copper
(Cu)
Quartz
(SiO2)
Silicium
(Si)
  Superconductors in which the electrons condense into a macroscopic wavefunction, are.

## Slide 6: Quantum Materials
Emergence: ‚more is different‘
new properties or structures of a system as a result of the interaction of its elements
Topology: ‚not that different‘
Properties of mathematical structures that are preserved under continuous deformations.
Notes: wir können den Becher kontinuierlich in den Donut verformen.

## Slide 7: Quantum Materials: a matter of energy scales
exchange interactions (J)
Coulomb Repulsion (U)
hopping (t)
e-
Spin-orbit
coupling
(l)

## Slide 8: Quantum Materials
(unconventional)
Superconductivity
(charge/spin)
density waves
Quantum Spin
Liquids
Topological Insulators
Weyl, Dirac Semimetals
quantum
Magnetism
Wide variety of ‘emergent’ physical phenomena
Highly tunable materials: chemical composition, external stimuli (Pressure, Field etc..)
Goal: understand the interplay between electronic orders

## Slide 9: From quantum materials to quantum devices
Need for functional quantum devices
A wealth of macroscopic quantum states
in quantum materials
Magnetism
Spin liquids
Topological states
Superconductivity
Single/entangled photon sources as quantum emitters
‘Artificial atoms’: superconducting circuits
?
He et al. Nature Materials 2018
Winkel et al.
PRX 2020
Quantum materials are generally relevant for (quantum) technology
Quantum technology can accelerate the research on quantum materials
Notes: Reply to the strategic recommendation ‘Sharpen the focus’

## Slide 10
‘A deeply original behavior always results – at some point – on an economically viable application’
(H. Alloul & H. J. Schulz – Physique des électrons dans les solides)
‘Was kann man damit bauen?’
Stuart Parkin
MPI Halle
Fert, Grünberg (1987)

## Slide 11
vulgarisation.fr
‘A deeply original behavior always results – at some point – on an economically viable application’
(H. Alloul & H. J. Schulz – Physique des électrons dans les solides)
‘Was kann man damit bauen?’

## Slide 12
● Synthesis Growth of new quantum materials
● Model predict new electronic properties
● Design materials with tailored electronic properties & functionalities
● Mapping electronic phase diagram
Coexisting, competing & intertwined orders
T
g
● Develop new tuning knobs to induce novel electronic states of matter
Strain tuning, symmetry breaking
single crystals, thin films, interfaces, monolayers
● Understand electronic structure and dynamics
Control of the competing electronic phases
Design of new electronic phases
functionalisation of
Quantum materials
A Quantum Materials optimization loop
Curiosity driven
research at every
step!

## Slide 13
High-Tc Cuprates
e-
YBa2Cu3O6+x
CuOx
chains
CuO2
planes
B. Keimer et al. Nature 518, 179 (2015)

## Slide 14
Elastic tuning of the electronic state of high-Tc cuprates
Pressure/stress is a good tool to investigate the interplay between SC and CDW orders
B. Keimer et al. Nature 518, 179 (2015)
Cuprates
Bosak, G. Garbarino, M. Krisch
N. Brookes, K. Kummer
S. M. Souliou, I. Vinograd, R. Heid
A. Haghighirad, M. Merz, T. Lacmann
H.-H. Kim, E. Lefrançois, H. Gretarsson, M. Minola, S. Nakata, B. Keimer
C.W. Hicks, M. E. Barber,
H. Noad, K. Ishida, A.P. Mackenzie

## Slide 15
Charge Density Wave?
M. Leroux
PhD thesis 2012
Metal
CDW
Instability of a metallic system towards the formation of a
periodic modulation of the charge density
Original prediction: R. Peierls in the 50s on 1D chains

## Slide 16
Charge density waves and superconductivity….
Chu and Knapp Phys. Lett. 46A, 33 (1973)
B. Keimer et al. Nature 518, 179 (2015)
Cuprates
Lee et al. Phys. Rev. Lett. 122, 147601 (2019)
BaNi2As2
a-Uranium
Feng et al. PNAS 109 7224 (2012)
dichalcogenides
Ortiz et al. Phys. Rev. Lett. 125, 247002 (2020)
Yu et al. Nat. Comm. 12, 3645 (2021)
Kagome
CDWs appear close to superconductivity
in the phase diagrams of many quantum materials.
Key question: nature of the interplay between these two orders?

## Slide 17: Scattering as a probe
System
Conservation Laws
Incident particle
Scattered particle
Initial
Final
Energy transferred to the system
Static correlations (Structure)
dynamics - Excitations
Momentum transferred to the system
0 (mod. Ghkl) homogeneous correlations
inhomogeneous correlations, dispersion
Neutrons
Photons
Electrons

## Slide 18
Tuning parameters for superconductivity in the cuprates
Chemical doping
LNCMI Grenoble
Magnetic field
Very large fields needed
to suppress SC
~25 T < H < ~150 T
Pressure
Small quantities of materials to study
Novel synthesis for each doping - disorder

## Slide 19
Charge Density Wave in the Cuprates
Reciprocal space
Real space

## Slide 20
Charge Density Wave in the Cuprates
Brighter x-ray sources (synchrotron radiation facilities)
Latest generation detectors
Huge dynamical range
No background
No cross-talk

## Slide 21
(0 K L) plane at Room Temperature
(0 K 0)
(0 0 L)
(0 K L) plane at 90 K
(0 K 0)
(0 0 L)
Charge Density Wave in the Cuprates
Ghiringhelli, MLT et al. Science 337, 821 (2012)
MLT et al. Nat. Phys. 10, 52 (2014)
Short-range CDW: 60-80
Weak correlations along c: 2D order

## Slide 22
H.-H. Kim et al. Phys. Rev. Lett. 126 037002 (2021)
Anisotropic, unidirectional CDW domains (cf. Comin et al. Science 347, 1335(2015))
CDW ‚morphology‘ (RIXS - ID32/ESRF)

## Slide 23
Short-range CDW: 60-80
Weak correlations along c: 2D order
Increase of CDW with H-field:
Evident competition with SC
CDW in the Cuprates: effect of magnetic field
Chang et al., Nat. Phys. 8, 871 (2012)
Blanco-Canosa et al., PRB 90, 054513 (2014)
Using very large pulsed fields:
long-range CDW: 00 at 26T
0 at 26T: 3D Order
Gerber et al. Science 350, 949 (2015)
Chang et al. Nat. Com. 7, 11494 (2016)
Jang et al. PNAS 113, 14465 (2016)
Nature of the interplay between CDWs and Superconductivity?
Insights on the microscopic mechanism behind the CDW?
Relationship between the 2D CDW and the field-induced 3D CDW?

## Slide 24
Magnetic Field
Hydrostatic pressure
Suppresses CDW
Enhances CDW
Yet what if we could suppress
superconductivity with pressure?
Chang et al., Nat. Phys. 8, 871 (2012)
S. M. Souliou et al., PRB 97, 020503(R) (2018)
Cyr-Choinière et al. Phys. Rev. B 98, 064513 (2018)
Pressure vs Magnetic Field

## Slide 25
Piezoelectric-based apparatus for uniaxial stress application
continuous, well-controlled uniaxial compression
C.W. Hicks et al., Rev. Sci. Instr. 85, 065003 (2014)
C. W. Hicks et al., Science 344, 283 (2014)
A. Steppke et al., Science 355, 1 (2017)
More information: Uniaxial Stress Technique and Investigations of Correlated Electron Systems,
Springer Thesis, M.E. Barber (2018)
modified version:
transmission geometry
adapted for HP cryostat
+
a-axis UD YBa2Cu3O6.67 needles
plasma-FIB thinned in the center
Uniaxial stress device

## Slide 26
Tc data under uniaxial stress
1.5 GPa ~
1% compression
Barber, M. E. et al. Phys. Rev. B 106, 184516 (2022).
Homogeneous and efficient suppression of
superconductivity with uniaxial pressure //a

## Slide 27
Uniaxial pressure dependence of the CDW
H.-H. Kim et al. Phys. Rev. Lett. 126 037002 (2021)

## Slide 28: Uniaxial stress and 3D-order
Γ
Q2D
H.-H. Kim, S. M. Souliou et al. Science 362, 1040 (2018)
0
1
0.5
Q2D
Q3D

## Slide 29: Uniaxial stress and 3D-order
Γ
Q3D
Q2D
H = 26T
long-range: 00
3D: 0 at 26T
Chang et al. Nat. Com. 7, 11494 (2016)
1% strain
long-range: 0
3D:
Q2D
Q3D
0
1
0.5
H.-H. Kim, S. M. Souliou et al. Science 362, 1040 (2018)

## Slide 30: Temperature dependence of the 3D-CDW
Q2D
Q3D
Complete suppression at low T: very strong competition with superconductivity
3D order present even above the uncompressed Tc
H = 26T
Gerber et al. Science 350, 949 (2015)
H.-H. Kim, S. M. Souliou et al. Science 362, 1040 (2018)

## Slide 31: CDW signature in Phonon spectra
GIANT superconductivity-induced Kohn anomaly at Q2D
2D-CDW is not a soft-mode driven CDW
MLT et al. Nat. Phys. 10, 52 (2014)
Elastic line
Phonon
T = 50K < Tc
H.-H. Kim, S. M. Souliou et al. Science 362, 1040 (2018)
Inelastic x-ray Scattering

## Slide 32: Inelastic x-ray scattering: Phonon anomalies
Q3D
SC-induced softening of the acoustic mode: extends along L
(0 0 6)
Y
*
*
Q2D
(0 0 7)
T
Z
Complete Softening of an optical phonon associated with the formation of the 3CDW
(0 0 6)
Y
*
*
Q3D
Q2D
(0 0 7)
T
Z
DFT calculation
H.-H. Kim, S. M. Souliou et al. Science 362, 1040 (2018)

## Slide 33
Response of CDW to uniaxial stress is symmetric
  b-CDW domains grow under a-stress
  a-CDW domains grow under b-stress
          The CDW is unidirectional and biaxial
The CDW is seen in all cuprates and seem to be the main competitor to high-Tc superconductivity and the thermodynamically stable state when SC is suppressed.
Suppressing CDW ordering tendencies should yield better superconductors!
A few things we learned
The formation of long-range CDW order is associated
with a lattice dynamics anomaly enhanced by stress as SC
is suppressed
The 3D CDW is soft-phonon-driven: lattice plays an active role

## Slide 34
What do we do exactly to the crystal structure when we apply strain?

## Slide 35
2D vs 3D CDW – an xrd study
Vinograd, Souliou et al. (2023)

## Slide 36
Detailed structural refinement
Refined Poisson ratio
Bond lengths
Buckling etc…

## Slide 37
XRD study of the 3D CDW
Vinograd, Souliou et al. (2023)
Quantitative determination of the strain and of its effects on the crystal structure
Strain-temperature phase diagram of the 3D CDW
Evidence for competition between 2D and 3D : the long-range 3D-CDW grows from the 2D correlations
TCDW

## Slide 38
the crystal lattice can be used as a ‘clean’ way to tune the electronic phase of quantum materials (statically but also dynamically)
It can be combined with structural and spectroscopic studies to gain fresh insights on the nature of the interplay between competing electronic phases
It can ultimately guide the design of functional quantum materials with tailored electronic properties
More generally…

## Slide 40
Dimensional crossover in CDW
CuO2
bilayer
chain layer
defect pins
CDW maxima
L=0.5
Short-range 2D CDW
Caplan et al., PRL 119, 107002 (2017)
Notes: If magnetic field or uniaxial strain is used to strengthen the CDW amplitude, at some point the Coulomb interaction will thus make that the inner layers between adjacent bilayers will be anti-aligned. The effective unit cell is a single unit cell, so long-range CDW peaks appear at integer L values. 30s

## Slide 41
CuO2
bilayer
chain layer
defect pins
CDW maxima
L=0.5
L=1
minimal
Coulomb repulsion
Short-range 2D CDW
Caplan et al., PRL 119, 107002 (2017)
Long-range 3D CDW
Dimensional crossover in CDW
Notes: If magnetic field or uniaxial strain is used to strengthen the CDW amplitude, at some point the Coulomb interaction will thus make that the inner layers between adjacent bilayers will be anti-aligned. The effective unit cell is a single unit cell, so long-range CDW peaks appear at integer L values. 30s

## Slide 42: Inelastic Photon Scattering
Raman Scattering: Inelastic scattering of ‘visible’ light
eV
3000 – 7000 Å >> a (~ 0 probe)
Energy resolution 0.1 meV
Selection rules:
- phonon symmetries
- k-space selectivity (electronic)
Devereaux and Hackl RMP 79, 175 (2007)
IXS: high resolution inelastic scattering x-ray scattering
0.5-0.7 Å < a ( 0 many BZ)
Energy resolution 1.5-3 meV
Mostly phonons
AQR Baron, arxiv: 1504.01098