## Slide 1
Jorge Vallejo Bustamante, Matthieu Bard, Victor Wu,
Rebeca Ribeiro-Palau, Taro Wakamura, Claude Fermon,
Myriam Pannetier-Lecoeur, Sophie Guéron, Meydi Ferrier,
Richard Deblock, Sandrine Autier Laurent, Vincent Bouchiat,
Gilles Montambaux Jean-Noël Fuchs, Frédéric Piechon, Hélène Bouchiat
LPS CNRS Université Paris-Saclay
C2N, CNRS Université Paris-Saclay
SPEC, CEA, CNRS
Orbital Diamagnetism and Paramagnetism of Graphene

## Slide 2
Why is orbital magnetism is interesting? Thermodynamic property Reveals properties of electronic wave functions not accessible through transport Meissner effect in superconductors 1933 …
Quantum oscillations in clean metals (de Haas van Alphen ) 1930…
Persistent currents in mesoscopic rings 1990…
2D materials 2020… -Berry phase of Bloch wavefunctions -van -Hove singularities in the presence of moiré potentials -Valley Hall effect Why no magnetisation measurements in graphene untill recently?
What is a good detector? GMR sensor ideal tool for experiments at the single flake level
Controlling chemical potential
Experimental results
Low field Singular Diamagnetism at the Dirac point : Mc Clure peak
Crossover with de Haas van Alphen oscillations
Physics of Moiré : Orbital paramagnetism at van Hove singularities
Preliminary results on bilayer graphene
F
= 2p F/F0
F0 = h/e

## Slide 3: Singular orbital diamagnetic susceptibility in graphene Mc Clure 1956
Low energy Dirac spectrum of Graphene
Massive 2DEG
DOS =0 at
Landau levels
Grand potential
Raoux A. Thèse, 2017

## Slide 4
B
Importance of the p Berry phase in graphene wave functions
Bloch waves in graphene 2 components on A and B atoms: pseudo spin
Geometrical phase acquired on trajectory C
in reciprocal space :
FB = p for Graphene
N
In magnetic field:
FB also enters in the quantization condition of Landau levels
Landau level at zero energy !
FB
Berry curvature

## Slide 5
2
2
2
1
0
DW(B)
M = - dW/dB - B 1/2
Landau levels in Graphene
300K at 1T
McClure 1956
Raoux, Fuchs,Piechon , Montambaux PRL 2014
Coalescence of the
B=0 spectrum into LL
small paramagnetic
contribution
of all these levels
Diamagnetic
contribution
En = _
increases with B !
c - B -1/2 diamagnetic diverges at B=0 !
(n +1/2 )
eB=

## Slide 6
Dice lattice
Paramagnetic divergence of the susceptibility at the Dirac point!
FB = 0 for the Dice lattice
N
B

## Slide 7
Diamagnetic McClure peak at m=0 broaden with temperature and disorder
t =2.7 eV ~ 3 10 4 K
Paramagnetic peak at the saddle point
Raoux, Fuchs,Piechon , Montambaux PRL 2014

## Slide 8
le=1 mm
Width of the McCure peak s0= 10mev ~ 100K
Screening of magnetic field on a few micron size detector
dB/B = 10 -6 very small effect!
Importance of the quality of Graphene!
D
-c0 =
m0 e2 vF2
D
1
p
Orders of magnitude:
s0= kB TD= ħ /te
Amplitude of disorder

## Slide 9
-High sensitivity and Compatible with gating
Detectors we tried:
-Hall bars (but sensitive to the gate voltage)
-MicroSQUIDs (limited to low fields ~0.1 T)
-Giant Magnetoresistance probes : Ideal!
Sensitivity
Requirements for magnetometry of a single graphene flake
ReW+W bridges
dB= 10-8 T /Hz ½
dB= 10-9 T /Hz ½
dB= 10-9 T /Hz ½

## Slide 10
1
2
1
2
Aligned
layers
Anti-parallel
layers
Giant Magnetoresistance Detector
Stack of hard and soft thin ferromagnetic layers:
only sensitive to in-plane component of the magnetic field
Sensitivity: 0.1 nT for an applied out of plane field of Bperp= 0.1 T, 1nT for Bperp =1T
Most applications :
Industry, speed control in cars
Biomagnetism , very sensitive NMR
Myriam Pannetier
Claude Fermon
CEA
soft
hard

## Slide 11: Measuring principle: GMRs and Gate modulation
Encapsulated graphene:
BN-G-BN stack
100nm Au top gate
1 Alumina
B: applied vertical magnetic field
Bh: compensation horizontal magnetic field
Measured field
Sensors: GMRs probes insensitive to perpendicular B. Collaboration: C Fermon et M Pannetier-Lecoeur, CEA
Gate modulation
,
Vallejo et al. Science 2021

## Slide 12
Measuring gate voltage dependent magnetisation in Graphene
B=0.2 T
Thesis J.Vallejo 2023
MC Clure Diamagnetic peak!
Only adjustable parameter amplitude of disorder

## Slide 13
Theoretical interpretation of the data: interplay of disorder and magnetic field
G. Montambaux,
s=0
s =0.1
Fresnel integral
Gaussian distribution of chemical potential
Standard deviation s

## Slide 14
Doping dependent orbital magnetisation in Graphene
Crossover between
Low field Diamagnetic
MC Clure peak
and dHvA oscillations
Diamagnetic
MC Clure peak
M(Vg)
M(Vg)
-----
G.Montambaux

## Slide 15: Orbital paramagnetism in 2D crystals
2D lattice: susceptibility is positive and diverges logarithmically near a saddle point in the band structure (vHs)
Near saddle point, hyperbolic open diamagnetic orbits
+ Tunneling
Vignale PRL 1991
Raoux, et al. PRB. 2015.
k space
Orbital paramagnetism:
Saddle points not accessible in pure graphene….
Notes: Eq.

## Slide 16
Moiré potentials in Graphene
aM ~ 10 nm >> ag
depends on the angle
between the 2 lattices
Super cell moiré lattice parameter

## Slide 17: Graphene/BN moiré
Moiré superpotential modifies graphene’s band structure: satellite Dirac peaks
Saddle points appear with van Hove singularities at low energy
Orbital paramagnetism ?
J.N. Fuchs, G.Montambaux, F.Piechon (Vallejo et al. 2023)
satellite
saddle points
Miniband spectrum

## Slide 18
Paramagnetic peaks!
van Hove log. singularities
at Saddle points
Diamagnetic and paramagnetic orbital magnetisation
Positions and intensity of singularities can be understood theoretically
J.N. Fuchs, G.Montambaux, F.Piechon (Vallejo et al. 2023)
Determined by
Raman spectroscopy
R.Ribeiro SPEC
sDP Diamagnetic Satellite Dirac peaks
McClure peak
aM= 9.5 ±0.5 nm
n0 Nb of carriers per moiré cell
Resistance
Magnetisation
BN / Graphene nearly aligned: gate voltage dependent magnetisation

## Slide 19
Very rich energy landscape!
- Satellite Dirac points seprated by
- Saddle points
Single parameter moiré potential tM
Electron hole symmetry breaking
depends on the sign of tM
Miniband spectrum of Graphene with a moiré potential
Mini Brillouin zone of the moiré band ~0.05 BZ graphene
J.N. Fuchs
F. Piechon
J. Vallejo
G. Montambaux
Inspired from Yankowitz Nature Physics 2011
Main Dirac Point

## Slide 20
Split Dirac points
Asymmettry of paramagnetic peaks
Related to different curvatures at saddle points
Can we understand the relative order of
magnitude of the peaks?
Determination of the moiré potential from the position of diamagnetic and paramagnetic peaks
Electron
bands
Hole bands
bands

## Slide 21
0.33
Anisotropic satellite Dirac and saddle points
Vsx aM tM/2h < Vsy ~ VF (graphene)
F. Piechon and J.N. Fuchs
KS
mS
x
Y
mS
KS

## Slide 22
0.015
Very anisotropic saddle points for E1 and H1 bands
F. Piechon and J.N. Fuchs
Analytical model (my second order in tM)
KS
mS
mS
KS

## Slide 23
Overlap between diamagnetic peaks at kS and ms (satellite Dirac points)
and paramagnetic peaks at saddle points between kS and ms
kS
mS
Para
Dia
Para
Dia
kS
Energy positions and relative amplitude between peaks depend on the moiré pot. tM
tM=-15meV disorder: s = 4.5 meV
tM=-23meV
Good agreement between theory and experiments

## Slide 24
0
0
0
0
0
0
Orbital magnetism in graphene bilayer
D=0
Gap opening with transverse electric field
Koshino PRB 2010
Susceptibility maximum in the gap
Paramagnetic peaks on the edge

## Slide 25
Orbital magnetism in zero field:
valley Hall effect
Effect of interactions: orbital ferromagnetism
Mesoscopic effects and
edge physics in large supercell moirés:
Analogy with Persistent currents in arrays of Aharonov Bohm rings
Topological insulators
Orbital magnetism in zero field:
valley Hall effect in bi-layers
(Vignale 2021)
Perspectives
Orbital ferromagnetism in twisted bilayers?
Interaction induced valley symmetry breaking
Quantum anomalous Hall effect
Sharpe et al Science 2019
Field hysteresis in transport
Direct investigation of magnetism ?

## Slide 26
Orbital magnetism in zero field:
valley Hall effect
Effect of interactions: orbital ferromagnetism
Mesoscopic effects and
edge physics in large supercell moirés:
Analogy with Persistent currents in arrays of Aharonov Bohm rings
Topological insulators
2D Topological insulators
Orbital ballistic currents along 1D phase coherent helical edge states
Expected:
Contribution of ballistic edge states current periodic in flux
amplitude evF/L
Small aperiodic contribution of diffusive surface states le/L( eVF/L)
Perspectives
Bi and BiBr flakes
Monolayers of WTe2
F0=h/e
Periodic in flux with:

## Slide 27
Mesoscopic effects and edge physics in large supercell graphene bilayer moirés:
Persistent currents in a network of (normal) ballistic Aharonov Bohm rings
Currents spatial distribution
In a square network
M.Pascaud
G.Montambaux PRL 1999
Magnetisation of an ensemble of AB rings
h/2e periodic
Saw tooth like paramagnetic currents
Role of interactions?
<I>
evF/L
disordered
F0=h/e
ballistic

## Slide 28
Jorge Vallejo Bustamante, Matthieu Bard, Victor Wu,
Rebeca Ribeiro-Palau, Taro Wakamura, Claude Fermon,
Myriam Pannetier-Lecoeur, Sophie Guéron, Meydi Ferrier,
Richard Deblock, Sandrine Autier Laurent, Vincent Bouchiat,
Gilles Montambaux Jean-Noël Fuchs, Frédéric Piechon, Hélène Bouchiat
LPS CNRS Université Paris-Saclay
C2N, CNRS Université Paris-Saclay
SPEC, CEA, CNRS
Orbital Diamagnetism and Paramagnetism of Graphene

## Slide 29
Other possible detectors:
Nano SQUIDs: can operate at larger applied magnetic field can measure a single mB
Less sensitive in magnetic field mT range dB= dF /S loop
NV centers magnetometers: sensitivity
But difficult to operate in the T range dB= 10-9 T /Hz ½

## Slide 30
Moiré potential
aM= 12.5 ±0.5 nm
Paramagnetic peaks!
Diamagnetic and paramagnetic orbital magnetisation
BN / Graphene nearly aligned: gate voltage dependent magnetisation
1T data out of the linear
response regime

## Slide 31: Singular orbital diamagnetic susceptibility in graphene Mc Clure 1956
Low energy Dirac spectrum of Graphene
Massive 2DEG
DOS =0 at
Landau levels
Grand potential
Raoux A. Thèse, 2017
Diverges!
but rounded with disorder
at m=0 M = - dW/dB - B 1/2
= - dM/dB - B -1/2
Diverges at B=0!