## Slide 1: Mesoscopic Klein-Schwinger effect in graphene
SFP 2023
Aurélien Schmitt, P. Vallet, D. Mele, M. Rosticher, T. Taniguchi, K. Watanabe, E. Bocquillon, G. Fève, J.M. Berroir, C. Voisin, J. Cayssol, M.O. Goerbig, J. Troost, E. Baudin and B. Plaçais

## Slide 2
Instability of vacuum in presence of an intense electric field
Electron-positron pair creation rate from non-perturbative theory
Schwinger field :
(for electron-positron : )
… on the roadmap of Zeta/Exawatt Lasers
Schwinger effect: breaking vacuum in a high electric-field
F. Sauter, Z. Phys. 1931
J. S. Schwinger, PRB 1951
Prefactors in C. Itzykson et J. B. Zuber, Quantum Field Theory, McGraw-Hill (2006)
d : spatial dimension
E : electric field

## Slide 3
2d-Schwinger in gapless neutral 2d-graphene
and electron-hole symmetry
Dora-Moessner, PRB (2010), Katsnelson-Volovik, ZhETF (2012),...
Berdyugin, Science (2022)
+ sign reversal of the Hall resistance

## Slide 4
2d-Schwinger in gapless neutral 2d-graphene
and electron-hole symmetry
Dora-Moessner, PRB (2010), Katsnelson-Volovik, ZhETF (2012),...
BUT
law is similar to Zener tunneling Vandecasteele et al., PRB (2010)
Electric-field induces doping-gradient, p-n junction, and 1d-collimation ….

## Slide 5
Klein-Schwinger effect

## Slide 6
Collimating p-n junction massive Dirac fermions
Long junction
Klein collimation mimics massive 1d-Dirac fermions
V. V. Cheianov, V. I. Falko, PRB-2006
J. Cayssol, B. Huard, D. Goldhaber-Gordon, PRB-2009
E.B. Sonin, PRB-2009
P.E. Allain, J.N. Fuchs, EPJB-2011
F. Sauter, Z-Phys 1931

## Slide 7
a universal 1d-Schwinger pair-creation rate
Schwinger effect with massive 1d Dirac fermions in graphene

## Slide 8
Universal quantized 1d-Schwinger conductance
Schwinger current over a length (

## Slide 9
Current saturation in hBN-encapsulated graphene FET

## Slide 10
Current saturation in hBN-encapsulated graphene FET
Meric et al. Nature Nanotechnology 3, 654–659 (2008)
Diffusive graphene

## Slide 11
Current saturation in hBN-encapsulated graphene FET
reminiscent of MOSFET pinchoff (carrier depletion at the drain side), albeit semimetallic
Si MOSFET (Sze, 2006)

## Slide 12
From current to differential conductance

## Slide 13
Vanishing Klein-tunneling conductance
Giant Klein collimation model :

## Slide 14
Semi-metallic Pinchoff Long-junction model
Toy-model of the Klein-collimation junction
L

## Slide 15
noise signatures of Klein collimation

## Slide 16
White GHz noise
Klein tunneling junction : shot-noise

## Slide 17
White GHz noise
Sweet noise dip
,
Shot-noise limited
Klein tunneling junction : shot-noise

## Slide 18
White GHz noise
Sweet noise dip
,
Shot-noise limited
Mesoscopic junction with a Fano factor
Klein tunneling junction : shot-noise

## Slide 19
Universal 1d Schwinger effect

## Slide 20
Evidence of mesoscopic Klein-Schwinger effect

## Slide 21
Evidence of mesoscopic Klein-Schwinger effect

## Slide 22
Evidence of mesoscopic Klein-Schwinger effect

## Slide 23
Evidence of mesoscopic Klein-Schwinger effect

## Slide 24
Universal 1d-Schwinger scaling:
Universal extrapolate
One parameter : Schwinger voltage

## Slide 25
The N-loop Schwinger prediction verified in detail
truncated rate
Full 1d-Schwinger
an important result for field theory
A device with a thin hBN dielectric (32nm) :
early onset of Schwinger pair creation

## Slide 26
Schwinger gap and length

## Slide 27
Klein-collimation origin of the Schwinger gap
Why finite- Schwinger pairs ?

## Slide 28
Pauli-blocking of low- by collimated transmitted carriers
A: Schwinger-pairs created at a finite with
Collimated saturation current

## Slide 29
Klein-tunneling
Schwinger-pair current
doping
vacuum
Schwinger as the intrinsic breakdown of Klein collimation

## Slide 30
Experimental observation of 1d-Schwinger effect
Schwinger is the breakdown of Klein collimation
Outlook: lifting spin/valley degeneracy ?
Outlook: Full counting statistics ? Vacuum polarization ?
A. Schmitt et al., Nat. Phys. 19, 830–835 (2023)
N&V R.K. Kumar 19, 768–769 (2023)
Dirac matter
accelerator
vacuum
« QED in a pencil trace » « QED in a graphene mosfet »

## Slide 31
A. Schmitt et al., Nat. Phys. 19, 830–835 (2023)
N&V R.K. Kumar 19, 768–769 (2023)
« QED in a pencil trace » « QED in a graphene mosfet »
Thank you !

## Slide 32
Current saturation in hBN-encapsulated graphene FET
Long devices
High-mobility >
Low edge contact resistance
Room temperature

## Slide 33
Saturation controlled by a « Klein collimation junction »
bulk OP saturation
exponential Klein tunneling saturation
bulk OP + Zener
Exponential saturation is extrinsically limited by a Zener instability

## Slide 34
Saturation controlled by a « Klein collimation junction »
Pinch-off free regime
Bulk current saturation controlled by optical phonons:

## Slide 35
Saturation controlled by a « Klein collimation junction »
Pinch-off regime
Exponential current saturation :

## Slide 36
Pinchoff regime : RF measurements
Small-signal equivalent circuit
(cf Sze, 2006)
SOURCE
GATE
DRAIN

## Slide 37
Pinchoff regime : RF measurements
Small-signal equivalent circuit
(cf Sze, 2006)
SOURCE
GATE
DRAIN
Pinchoff region

## Slide 38
w
Toy-model of the Klein-collimation junction
Pinchoff-free case : velocity saturation (OPs) + electronic compressibility + doping gradients in the presence of a local gate
Current density :
where
(electrochemical potential)
For monolayer graphene on a local gate :
+ electrostatics :
: Fermi velocity
: areal gate capacitance
: carrier density
: electrochemical potential of the gate
: low-bias mobility
: saturation field

## Slide 39
Toy-model of the Klein-collimation junction
Pinchoff-free case : velocity saturation (OPs) + electronic compressibility + doping gradients in the presence of a local gate
Pinchoff case : constant density in the channel  constant and uniform

## Slide 40
Toy-model of the semi-metallic pinchoff
Estimate of the voltage drop in the channel / in the pinchoff junction
Local drift-diffusion model : velocity saturation + electronic compressibility + doping gradients with a local gate

## Slide 41
Zener instability : flicker-noise
Klein collimation field
Bulk Zener field
A huge noise signals the destruction of the collimation junction
Zener instability is pushed to large
in long () devices

## Slide 42
Evidence of mesoscopic Klein-Schwinger effect
and
,

## Slide 43
Evidence of mesoscopic Klein-Schwinger effect
and
,
but obscured by Klein tunneling at low doping :

## Slide 44
Varied I-V according to hBN thickness / geometry ….
GrS1-25nm (L/W=0.75) GrS2-35nm (L/W=0.7) GrS3-42nm (L/W=1.5)
AuS1-34nm (L/W=0.75) AuS2-33nm (L/W=1.5) AuS3-90nm (L/W=1)

## Slide 45
Same 1d-Schwinger scaling in various geometry !
GrS1-25nm (L/W=0.75) GrS2-35nm (L/W=0.7) GrS3-42nm (L/W=1.5)
AuS1-34nm (L/W=0.75) AuS2-33nm (L/W=1.5) AuS3-90nm (L/W=1)

## Slide 46
The non-perturbative Schwinger prediction verified in detail
A device with a thin hBN dielectric (32nm)
Early onset of Schwinger pair creation

## Slide 47
The non-perturbative Schwinger prediction verified in detail
an important result for field theory

## Slide 48
Measured dependence
GrS1-25nm (L/W=0.75) GrS2-35nm (L/W=0.7) GrS3-42nm (L/W=1.5)
AuS1-34nm (L/W=0.75) AuS2-33nm (L/W=1.5) AuS3-90nm (L/W=1)

## Slide 49
Length of the Klein collimation junction
electrostatics
interactions

## Slide 50
NB: with
Length of the Klein collimation junction
electrostatics
interactions

## Slide 51
Length of the Klein collimation junction
electrostatics
interactions
The ansatz gives consistent Klein-junction lengths