## Slide 1: Perles liquides dans une matrice solide : rhéologie des émulsions solides
Elina Gilbert, Anniina Salonen, Christophe Poulard
elina.gilbert@universite-paris-saclay.fr
Laboratoire de Physique des Solides, CNRS, Université Paris-Saclay, France
Congrès de la Société Française de Physique - 2023

## Slide 2: Motivation
logG’, logG’’
log
Elastomer: crosslinked polymer chains

## Slide 3: Motivation
logG’, logG’’
log
Elastomer: crosslinked polymer chains
+ crosslinks = less flow, more stiffness
“coupling” of G’ and G’’ wrt physical chemistry
Elastomer-like material with separate control over G’ and G’’ ?

## Slide 4: Inclusion systems
DISPERSED PHASE
CONTINUOUS PHASE
Gas
Liquid
Solid
Liquid
Solid
Liquid foam
Solid foam
Solid emulsion
Liquid emulsion
Solid dispersion / granular media
Solid toughener
Notes: Need to take a step back  broader point of view
Phases with different degrees of condensation

## Slide 5: First approach for solid emulsions with liquid inclusions
Elastocapillary number accounts for all liquid inclusions, and yield stress foamy liquids
Style et al., 2014, Nature Physics, 11, 2
Gorlier et al., 2017, Journal of Colloid and Interface Science, 501
Experimental data for monodisperse inclusion corresponds to the literature for elasticity:
Influence of volume fraction modulated by elasto-capillary number
0
0.01
1
3
10
100
0.1
1/3
Notes: Confrontation experiments (emulsion + bubbly mat)
Correspond ok
Monodisperse
G’
=> What about G’ AND G’’

## Slide 6: Controlling the rheology of a solid emulsion with liquid droplets
PEG 600 (n=15) :
melting temperature:
Sylgard 184 / Sylgard 527 mixture :
Sylgard 184: purely elastic MPa
Sylgard 527: mainly elastic kPa
Curing at ambient temperature for 2 days
Solid
Silicone-based resin
Liquid
PEG 600
Control parameters:
Notes: My: peg in silicone
Peg 600 small, Tcryst=18°C
Mix sylgard: lower moduluseCainfluence droplets
Parameters studied: Phi, R

## Slide 7: Dispersed and continuous phases
Moduli of the dispersed phase increase above the continuous phase at colder temperature
Sylgard 527
Sylgard 184

## Slide 8: Generation of solid emulsions by breakup under shear
Rotation: aspiration between rotating rod and stator
Shearing between wall and rotor: breaking into droplets
Dimethylsiloxane-ethylene glycol 70:30
block copolymer
1cm
9mN.m-1

## Slide 9: Typical linear viscoelastic response of solid emulsions
Storage modulus:
very similar to elastomeric plateau
Loss modulus:
2 apparent slopes
Low frequencies: almost flat
High frequency: same slope as continuous phase

## Slide 10: Evolution of linear viscoelasticity with volume fraction
Almost no change in the slopes of either moduli
In G’:
No tendency in plateau evolution at low volume fraction
Decrease at higher volume fraction

## Slide 11: Evolution of linear viscoelasticity with volume fraction
Almost no change in the slopes of either moduli
In G’:
No tendency in plateau evolution at low volume fraction
Decrease at higher volume fraction
In G’’:
Slope at high frequency PDMS slope
Slope is lower than 1, close to 0.4 (usual for elastomers)  fractional rheology ?

## Slide 12: Evolution of linear viscoelasticity with volume fraction
Almost no change in the slopes of either moduli
In G’:
No tendency in plateau evolution at low volume fraction
Decrease at higher volume fraction
In G’’:
Slope at high frequency PDMS slope
Slope is lower than 1, close to 0.4 (usual for elastomers)  fractional rheology ?
Crossing frequency between plateau and power-law increase increases with volume fraction

## Slide 13: Evolution with volume fraction for liquid inclusions
Unexpected non-monotonous moduli  polydispersity ?
:
  Almost constant G’
  Increasing G’’
decorrelation of G’ and G’’ with regards to

## Slide 14: Evolution with temperature
Recovery of monotonous behavior
Comparison with rigid inclusions (glass beads):
  Similar evolution in G’’
  Discrepancy in G’
   First hypothesis: polydispersity

## Slide 15: Conclusions
Viscoelastic influence of liquid droplets in a soft matrix
  Modelling work in progress with fractional rheology
Decorrelations of storage and loss moduli with regards to volume fraction
  Influence of polydispersity on elastocapillary number
Interesting unexplained behavior with the temperature transition
Discrepancy with existing models already with liquid droplets
Non-trivial mechanical reponse from a mix of model materials
Interesting for tunable materials
Encapsulation of a phase-transition dispersed phase: thermal energy storage

## Slide 16
Thank you for your attention !

## Slide 17: Rheology of liquid emulsions
Rheology of liquid emulsions (Palierne, 1990):
Cael influences the way changes the rheological parameters
Viscosity for emulsions based on Newtonian liquids (Frankel & Acrivos, 1970):
Influence of the volume fraction on viscosity
Notes: Extension to oscillatory + viscoelastic : Palierne
! ECA ! Elastic modulus vs capillary pressure
 Determine influence inclusions

## Slide 18: Rheological characterization
Temperature [°C]
1
2
3
Sample
Plate-plate configuration
Peltier plate
Insulating box
Frequency sweep between 0.01Hz and 100Hz
Deformation 0.1%
Constant normal force 2N during temperature change
4
4h 70°C: crosslinking sample to rheometer
2h 25°C equilibrating frequency sweep
2d -10°C crystallization frequency sweep

## Slide 19: Master curve ?

## Slide 20: Adhesion first results with JKR experiment
Linearization of the force-contact relation:
Compression
Traction
~
Compression work
Energy release rate
G = W + dissipations
Compression
Traction
Jonhson, Kendall, Roberts, 1971, RSPA, 324, pp301-313
G

## Slide 21: Preliminary JKR results
G = W + dissipations
G W
 adhesion
Adhesion in all the samples
Preliminary data shows apparent influence of volume fraction
G
G

## Slide 22: Typical rheometry for solidified inclusions (T=-10°C)
G’ almost constant for , increasing with above
G’’ increases strongly with

## Slide 23: Sylgard 184 continuous phase
Little variation compared to the continuous phase: dominated by elasticity
Modulus decreases as thin films are formed
Same variation for G’ and G’’

## Slide 24: Microfluidics-generated samples
R≈150µm
PDMS cooled down and pushed through a peristaltic pump, allowing for reuse on the excess oil
PEG600 pushed through 10 syringes in the flow of PDMS
Sedimentation of the droplets leading to and curing at room temperature

## Slide 25: Influence of the elastocapillary number
1000µm
50µm
40%
Sylgard mix
Coherent : much larger droplets lead to a larger elastocapillary number, thus softening the sample

## Slide 26: Temperature transition for the larger droplets
Much clearer transition
Sample with smaller droplets shows a flatter curve
Multiple behaviors in frequency sweep depending on the temperature showing the influence of the progressive solidification of the dispersed phase

## Slide 27: Fractional rheology model
G
V,
« spring-pot » with intermediate behavior:
Another way to view it:
Infinite amount of relaxation times from small statistical events
How can we model a solid emulsion ?
Elastomeric continuous phase: already a power-law material
Droplets: modelized as an ensemble
Solid emulsion: simple mixing model

## Slide 28: Preliminary fit results
constant across all
Change from linear behavior around van also be lack of high frequency information
Similar frequency behavior across volume fraction
let’s compare the samples at a given frequency